Supporting Information

Self-Catalyzed Growth of Co-N Codoped Carbon Nanotubes for Advanced Multi-Heterointerface Engineering in Hierarchical Carbonaceous Microwave Absorbers

Yan Guo,1,2* Hongsen Long,2 Ziqi Wang,2 Shijun Luo,1 Lei Xu,1 Chuntai Liu,2 Changyu Shen2, Hu Liu2*

1School of Electronic Engineering, North China University of Water Resources and Electric Power, Zhengzhou 450046, China

2State Key Laboratory of Structural Analysis, Optimization and CAE Software for Industrial Equipment; National Engineering Research Center for Advanced Polymer Processing Technology, Zhengzhou University, Zhengzhou, Henan 450002, China

*: Correspondence authors

E-mail addresses: guoyan@ncwu.edu.cn (Y. G.); liuhu@zzu.edu.cn (H. L.)

Fig. S1. FTIR spectra of original MF and NaOH-treated MF.

Fig. S2. XRD patterns of MF and ZIF-67@MF.

Fig. S3. SEM images of (a&b) Co-NC@CF-600.

Fig. S4. A magnification of magnetic hysteresis loops of Co-NC@CF-600, Co-NC@CF-700, Co-NC@CF-800 and Co-NC@CF-900.

Fig. S5. N2 adsorption-desorption isotherms of (a) Co-NC@CF-600, (b) Co-NC@CF-700, (c) Co-NC@CF-800 and (d) Co-NC@CF-900.

Fig.e S6. 3D and 2D reflection loss plots with different thickness of Co-NC@CF-600 at 5 wt.% filler loading.

Fig. S7. 3D and 2D reflection loss plots with different thickness of Co-NC@CF-800 (a&c) at 10 wt.% filler loading and (b&d) 15 wt.% filler loading.

Fig. S8. (a) The complex permittivity and (b) complex permeability of Co-NC@CF-600.

Fig. S9. (a, b&c) The complex permittivity and (d, e&f) complex permeability of Co-NC@CF-800 at different filler loading.

Table S1. Comparison of EMW properties of various CNTs-based composite absorbers.

| Sample | Matching thickness (mm) | Filler loading (wt.%) | RLmin (dB) | EABmax (GHz) | SRLl | SRLlt | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ni3ZnC0.7/CNT/NPC | 2.58 | 30 | −66.6 | 7.04 | 2.22 | 0.86 | [1] |
| CoO@Co€PGN/CNTs | 3.4 | 15 | −63.39 | 6.5 | 4.23 | 1.24 | [2] |
| TiO2@C-Ni/CNTs | 1.8 | 15 | −32.3 | 5.5 | 2.15 | 1.20 | [3] |
| Co/CNTs-MXene@CF | 2.52 | 10 | −61.41 | 5.04 | 6.14 | 2.44 | [4] |
| CoFe@N-CNT/rGO | 2.0 | 20 | −33.2 | 3.8 | 1.66 | 0.83 | [5] |
| Co-N-C/CNTsHS | 2.5 | 8 | −60.2 | 5.1 | 7.53 | 3.01 | [6] |
| CNTs/Ni | 2 | 30 | −56.3 | 4.3 | 1.88 | 0.94 | [7] |
| Co/MnO/CNTs | 2.65 | 35 | −58.0 | 5.36 | 1.66 | 0.63 | [8] |
| Mo2N@CoFe@C/CNT | 2 | 20 | −53.5 | 5.0 | 2.68 | 1.34 | [9] |
| CNT/Ni@N-C | 2.5 | 30 | −55.1 | 11.2 | 1.84 | 0.73 | [10] |
| MXene-CNTs/Ni | 2.4 | 30 | −56.4 | 3.95 | 1.88 | 0.78 | [11] |
| MXene/C-CNTs | 2.7 | 30 | −45 | 4.9 | 1.50 | 0.56 | [12] |
| WS2-NS/CNTs | 1.95 | 40 | −51.6 | 5.4 | 1.29 | 0.66 | [13] |
| Fe3O4/CNTs | 1.68 | 50 | −59.2 | ∕ | 1.18 | 0.70 | [14] |
| HCF@CZ-CNTs | 2.9 | 10 | −53.5 | 8.02 | 5.35 | 1.84 | [15] |
| RBC@CNTs | 2.4 | 20 | −49.8 | 5.5 | 2.49 | 1.04 | [16] |
| Co-NC@CF-800 | 2.25 | 5 | −51.56 | 6.88 | 10.31 | 4.58 | This work |
| Co-NC@CF-900 | 3.15 | 5 | −50.65 | 5.28 | 10.13 | 3.22 | This work |

References

[1] Zhang F, Yin S, Chen Y, Zheng Q, Wang L, Jiang W (2022) Ligand-directed construction of CNTs-decorated metal carbide/carbon composites for ultra-strong and broad electromagnetic wave absorption. Chem Eng J 433:133586. https://doi.org/10.1016/j.cej.2021.133586

[2] Xu D, Ren Y, Guo X, Feng D, Yang R, Zhao B, Zhang R (2022) Multiscale core-shell CoO@Co€PGN/CNTs composites aerogels for ultra-wide microwave absorption. Compos Sci Technol 225:109524. https://doi.org/10.1016/j.compscitech.2022.109524

[3] Wu L, Liu X, Wan G, Peng X, He Z, Shi S, Wang G (2022) Ni/CNTs and carbon coating engineering to synergistically optimize the interfacial behaviors of TiO2 for thermal conductive microwave absorbers. Chem Eng J 448:137600. https://doi.org/10.1016/j.cej.2022.137600

[4] Wang B, Li S, Huang F, Wang S, Zhang H, Liu F, Liu Q (2022) Construction of multiple electron transfer paths in 1D core-shell hetetrostructures with MXene as interlayer enabling efficient microwave absorption. Carbon 187:56-66. https://doi.org/10.1016/j.carbon.2021.10.080

[5] Zhang X, Zhao Z, Xu J, Ouyang Q, Zhu C, Zhang X, Zhang X, Chen Y (2021) N-doped carbon nanotube arrays on reduced graphene oxide as multifunctional materials for energy devices and absorption of electromagnetic wave. Carbon 177:216-225. https://doi.org/10.1016/j.carbon.2021.02.085

[6] Zhang C, Chen G, Zhang R, Wu Z, Xu C, Man H, Che R (2021) Charge modulation of CNTs-based conductive network for oxygen reduction reaction and microwave absorption. Carbon 178:310-319. https://doi.org/10.1016/j.carbon.2021.03.030

[7] Yu R, Wen X, Liu J, Wang Y, Chen X, Wenelska K, Mijowska E, Tang T (2021) A green and high-yield route to recycle waste masks into CNTs/Ni hybrids via catalytic carbonization and their application for superior microwave absorption. Appl Catal B: Environ 298:120544. https://doi.org/10.1016/j.apcatb.2021.120544

[8] Xue W, Yang G, Bi S, Zhang J, Hou ZL (2021) Construction of caterpillar-like hierarchically structured Co/MnO/CNTs derived from MnO2/ZIF-8@ZIF-67 for electromagnetic wave absorption. Carbon 173:521-527. https://doi.org/10.1016/j.carbon.2020.11.016

[9] Xu C, Wang L, Li X, Qian X, Wu Z, You W, Pei K, Qin G, Zeng Q, Yang Z, Jin C, Che R (2021) Hierarchical Magnetic Network Constructed by CoFe Nanoparticles Suspended Within “Tubes on Rods” Matrix Toward Enhanced Microwave Absorption. Nanomicro Lett 13(1):47. https://doi.org/10.1007/s40820-020-00572-5

[10] Qiu Y, Yang H, Ma L, Lin Y, Zong H, Wen B, Bai X, Wang M (2021) In situ-derived carbon nanotube-decorated nitrogen-doped carbon-coated nickel hybrids from MOF/melamine for efficient electromagnetic wave absorption. J Colloid Interf Sci 581(Pt B):783-793. https://doi.org/10.1016/j.jcis.2020.07.151

[11] Li X, You W, Xu C, Wang L, Yang L, Li Y, Che R (2021) 3D Seed-Germination-Like MXene with In Situ Growing CNTs/Ni Heterojunction for Enhanced Microwave Absorption via Polarization and Magnetization. Nanomicro Lett 13(1):157. https://doi.org/10.1007/s40820-021-00680-w

[12] Cui Y, Wu F, Wang J, Wang Y, Shah T, Liu P, Zhang Q, Zhang B (2021) Three dimensional porous MXene/CNTs microspheres: Preparation, characterization and microwave absorbing properties. Compos Part A: Appl S 145:106378. https://doi.org/10.1016/j.compositesa.2021.106378

[13] Zhang D, Wang H, Cheng J, Han C, Yang X, Xu J, Shan G, Zheng G, Cao M (2020) Conductive WS2-NS/CNTs hybrids based 3D ultra-thin mesh electromagnetic wave absorbers with excellent absorption performance. Appl Surf Sci 528:147052. https://doi.org/10.1016/j.apsusc.2020.147052

[14] Zeng X, Zhu L, Yang B, Yu R (2020) Necklace-like Fe3O4 nanoparticle beads on carbon nanotube threads for microwave absorption and supercapacitors. Mater Design 189:108517. https://doi.org/10.1016/j.matdes.2020.108517

[15] Yang M, Yuan Y, Li Y, Sun X, Wang S, Liang L, Ning Y, Li J, Yin W, Che R, Li Y (2020) Dramatically enhanced electromagnetic wave absorption of hierarchical CNT/Co/C fiber derived from cotton and metal-organic-framework. Carbon 161:517-527. https://doi.org/10.1016/j.carbon.2020.01.073

[16] Yang H, Wen B, Wang L (2020) Carbon nanotubes modified CoZn/C composites with rambutan-like applied to electromagnetic wave absorption. Appl Surf Sci 509:145336. https://doi.org/10.1016/j.apsusc.2020.145336