Ionic Liquid-Assisted Polarized Alignment of Boron Nitride under Electric Fields: A New Paradigm for Constructing Thermal Conductive Pathways in Polymer Composites

Jianwen Wanga, Xueqing Liub, Beizhi Chua, Yumin Xiac, Yuwei Chena*, Yue Lia* and Jianming Zhanga*

- Key Laboratory of Advanced Rubber Material, Ministry of Education, Qingdao University of Science and Technology, Qingdao 266042

b. Key Laboratory of Optoelectronic Chemical Materials and Devices, Ministry of Education and Flexible Display Materials and Technology Co-innovation Centre of Hubei Province, Jianghan University, Wuhan 430056, China

c. State Key Laboratory for Modification of Chemical Fibers and Polymer Materials, College of Materials Science and Engineering, Donghua University, Shanghai 201600, China

Corresponding author:

Yuwei Chen, Email: YuweiChen@qust.edu.cn

Yue Li, Email: 03096@qust.edu.cn

Jianming Zhang, Email: zjm@qust.edu.cn

Figure S1. (a) and (a’) are RDF graphs of the BN-IL41 system; (b~g) and (b’~g’) are RDF graphs of the P110-BN-IL2 system.

Figure S2. (a) Probability of hydrogen bond length distribution, (b) Probability of hydrogen bond angle distribution.

Table S3. Zate potential of BN reagent

| Sample ID | Zeta Potential | Mobility | Conductance | Sample Count | Ref. Count | Electric Field |
| --- | --- | --- | --- | --- | --- | --- |
|  | (mV) | (μ/s)/(V/cm) | (μS) | Rate (kcps) | Rate (kcps) | (V/cm) |
| BN-1 | -13.52 | -1.06 | 103 | 1,275 | 3,590 | 11.08 |
| BN-2 | -13.98 | -1.09 | 103 | 1,275 | 3,590 | 11.08 |
| BN-3 | -14.22 | -1.11 | 103 | 1,275 | 3,590 | 11.08 |
| Mean: | -13.91 | -1.09 | 103 | 1,275 | 3,590 | 11.08 |
| Std Err: | 0.21 | 0.02 | 0 | 0 | 0 | 0.00 |
| Std Dev: | 0.36 | 0.03 | 0 | 0 | 0 | 0.00 |

Figure S4. (a–d) are SEM images of non-aligned IL/BN/PDMS composite films with IL:BN:PDMS ratios of 1:2:10, 1:3:10, 1:4:10, and 1:5:10, respectively. (a'–d') are the corresponding SEM images of the IL/BN/PDMS composite films after electric field-induced alignment.

Figure S5. (a–e) show SEM images of non-aligned IL/BN/PDMS composite films with IL:BN:PDMS ratios of 0.25:2:10, 0.5:2:10, 0.75:2:10, 1:2:10, and 1.5:2:10, respectively. (a'–e') are the corresponding SEM images of the IL/BN/PDMS composite films after electric field-induced alignment.

Figure S6. (a–d) show SEM images of non-aligned IL/BN/PDMS composite films with a fixed IL:BN ratio of 1:4 and varying IL/BN mass fractions of 20 wt%, 27 wt%, 33 wt%, and 38 wt%, respectively. (a'–d') are the corresponding SEM images of the IL/BN/PDMS composite films after electric field-induced alignment.

Figure S7. (a, b) are the thermal conductivity of the composites with varying IL and BN ratios.

Figure S8. (a, b) The difference in thermal conductivity between aligned and non-aligned composite materials with varying IL and BN ratios.