Recent Progress in Two-Dimensional van der Waals Heterojunctions for Flexible Energy Storage Applications

Ting Ding,1 Xupu Jiang,1 Jiaxin Quan,1 Rui Wang,1 Min Li,1, * Chuntao Lan,1, * Wujun Ma,1, 2, * and Meifang Zhu2

1College of Textile and Garment, Nantong University, Nantong 226019, China

2State Key Laboratory for Modification of Chemical Fibers and Polymer Materials, Donghua University, Shanghai 201620, China

*Corresponding authors:

E-mail addresses: mawj@ntu.edu.cn (W.J. Ma);

chuntaolan@outlook.com (C.T. Lan);

minmin0421@163.com (M. Li)

Supplementary Figures

Fig. S1. Cycling stability of MoS2/m-C hybrid nanosheet superstructures at a current density of 800 mA g-1 under low (3 °C) and high (50 °C) temperature conditions. Reproduced with permission [1]. Copyright 2015, WILEY.

Fig. S2. Raman spectra of the synthesized samples: 1 LNiO, 1 LMnO2, 2 L, 3 L, and 4 L. Reproduced with permission [2]. Copyright 2023, Elsevier.

Fig. S3. Schematic depiction of the band structure of the CoP-C/CN composite. Reproduced with permission [3]. Copyright 2023, Elsevier.

Fig. S4. Digital image of rGO samples woven into knitted gloves. Reproduced with permission [4]. Copyright 2019, Elsevier.

Fig. S5. Digital image of rGO/Ti3C2Tx heterojunction (95% rGO, 5% Ti3C2Tx). Reproduced with permission [4]. Copyright 2019, Elsevier.

Table S1. Comparison of different preparation methods.

|  | Advantages |  | Disadvantages |
| --- | --- | --- | --- |
| Direct stacking | (1) Simple operation. (2) No complex equipment required. (3) Suitable for preliminary studies. |  | (1) Prone to interface contamination. (2) Low precision in layer alignment. (3) Limited to exfoliable 2D materials. |
| CVD | (1) High crystallinity and uniformity. (2) Controllable layer thickness. (3) Suitable for large-area synthesis. |  | (1) Requires high-temperature equipment. (2) Complex process. (3) Potential substrate compatibility issues. |
| In situ growth | (1) Atomically clean interfaces. (2) Precise control over heterostructure design. (3) Strong interlayer bonding. |  | (1) Expensive equipment (e.g., MBE chamber). (2) Low throughput for large areas. (3) Strict process optimization needed. |
| Solution-based methods | (1) Low-cost and scalable for large-area production. (2) Compatible with low-temperature processes. (3) Suitable for organic/inorganic hybrid systems. |  | (1) Lower crystallinity and purity. (2) Difficulty in controlling layer thickness and uniformity. (3) Solvent residue risks. |

Table S2. Performance Comparison of Representative 2D vdWHs.

| Electrode material | Methods | Performance | Ref. |
| --- | --- | --- | --- |
| MoS2/m-C | Direct stacking | higher specific capacity of 1113 mAh g−1 at 400 mA g−1 excellent rate capability (943 mAh g−1 at 6400 mA g−1) | [1] |
| NiO/MnO2 | Direct stacking | specific capacitance: 2L: 3.6 × 103 F g−1; 4L: 5.8 × 103 F g−1 capacitance retention: 2L: 14.8%; 4L: 12.9%. | [2] |
| NiFe-LDH/MXene | Direct stacking | highest microwave absorption of −58.2 dB at a thickness of only 2 mm | [5] |
| CoP-C/g-C3N4 | Direct stacking | H2 production rate :1503 μmol∙g−1∙h−1 (AQY: 3.03 % at 400 nm) | [3] |
| FTO-WO3/Fe2O3 | CVD | photocurrent density: 1.25 times compared with FTO-WO3 | [6] |
| g-C3N4/WS2 | CVD | degradation of TC (84%) and SMX (96%), under visible light | [7] |
| Co9S8/MoS2 | CVD | reversibility: 424.5 mAh g–1 at 2 A g–1 at the 1600th cycle, 401.1 mAh g–1 at 5 A g–1 at the 800th cycle rate capacity: 210.1 mAh g–1 at 20 A g–1 | [8] |
| CoS/MoS2 | CVD | cycling stability: 510.9 mAh g−1 at 1 A g−1 at the 1000th cycle rate performance: 341 mAh g−1 at 10 A g−1 | [9] |
| α-MnO2/MXene | In situ growth | specific capacitance: 334.3 F g−1 at 0.5 A g−1 capacitance: 90.9% retained after 5000 cycles | [10] |
| Co(OH)2/MXene | In situ growth | total pseudo-capacitance: 153.0 F g−1 with a Ti3C2Tx loading of 25 wt%, twice of that of the bare Co(OH)2 | [11] |
| Bi2S3/Ti3C2Tx | In situ growth | capacity: 615 C g−1 at 3 A g−1 capacitance retention: 91% | [12] |
| ZnIn2S4/nitrogen-doped graphene | In situ growth | detection limit: 0.33 pmol L−1 within the linear scope of 1 pmol L−1 to 5 μmol L−1 | [13] |
| rGO/MnO | In situ growth | capacity: 860 mAh g−1 at 0.1 A g−1 rate capability: 211 mAh g−1 at 10 A g−1 | [14] |
| Ni3S2/d-Ti3C2 | In situ growth | specific capacity of 2204 F g−1 at 1 A g−1 | [15] |
| g-C3N4/SnS2 | Solution-based methods | degradation of Cr(VI): 85% degradation of 2,4-DCP: 94% | [16] |
| CCN/BOI | Solution-based methods | photo-degradation of tetracycline (TC, 20 mg/L) after 120 min visible light irradiation: 80% | [17] |
| 1T-MoS2/Ti3C2Tz | Solution-based methods | specific capacitance: 250 F g−1 at 1 A g−1 capacitance retention: 82.3% (at 10 A g−1) after 5000 cycles | [18] |
| NiCoAl-LDH/V4C3Tx | Solution-based methods | specific capacity: 627 C g−1 at 1 A g−1\ | [19] |

References:

1. Jiang H, Ren D, Wang H et al (2015) 2D monolayer MoS2–carbon interoverlapped superstructure: Engineering ideal atomic interface for lithium ion storage. Adv Mater 27: 3687-3695.

2. Alanazi M, Ghrib T, Ercan F et al (2023) Structural, optical, and electrical investigation of multilayered MnO2(n)/ NiO(p) heterojunctions for supercapacitors applications. Surf Interfaces 42: 103321..

3. Huang Z, Long X, Liu M et al (2024) Constructing CoP-C/g-C3N4 nanocomposites with P-C bond bridged interface and van der Waals heterojunctions for enhanced photocatalytic H2 evolution. J Colloid Interface Sci 653: 1293-1303.

4. Wang Z, Chen Y, Yao M et al (2020) Facile fabrication of flexible rGO/MXene hybrid fiber-like electrode with high volumetric capacitance. J Power Sources 448: 227398.

5. Li Q, Li Y, Fulari A V et al (2020) Performance of chemically synthesized Mn3O4/rGO nanocomposite for electrochemical supercapacitor: A cost-effective high-performance electrode. Nanotechnology 31: 415403.

6. Zhang Y-F, Zhu Y-K, Lv C-X et al (2020) Enhanced visible-light photoelectrochemical performance via chemical vapor deposition of Fe2O3 on a WO3 film to form a heterojunction. Rare Met 39: 841-849.

7. Gnanaguru M V L, Naushad M, Tatarchuk T et al (2023) One-step calcination synthesis of 2D/2D g-C3N4/WS2 van der Waals heterojunction for visible light-induced photocatalytic degradation of pharmaceutical pollutants. Environ Sci Pollut Res 30: 78537-78553.

8. He Y, Liu C, Peng S et al (2023) Micro-flower-like MoS2-modified Co9S8 heterostructure as anode material for sodium-ion batteries with superior reversibility and rate capacity. J Mater Sci Technol 145: 210-220.

9. He Y, Liu C, Xie Z et al (2023) Construction of cobalt sulfide/molybdenum disulfide heterostructure as the anode material for sodium ion batteries. Adv Compos Hybrid Mater 6: 85.

10. Meng W, Zhou J, Wang G et al (2022) Constructing 2D/2D heterojunction of MnO2 nanolamellas grown on MXene nanosheets for boosted supercapacitor performance. J Energy Storage 56: 106105.

11. Jiang H, Wang Z, Dong L et al (2020) Co(OH)2/MXene composites for tunable pseudo-capacitance energy storage. Electrochim Acta 353: 136607.

12. Li Y, Deng Y, Zhang X et al (2021) Facile fabrication of novel Ti3C2Tx-supported fallen leaf-like Bi2S3 nanopieces by a combined local-repulsion and macroscopic attraction strategy with enhanced symmetrical supercapacitor performance. Electrochim Acta 366: 137406.

13. Ding L, Zhang Z, Wen Z et al (2022) 2D/2D heterojunction of ZnIn2S4/N-doped graphene nanosheets for off-type high-performance photoelectrochemical aptasensor. Sensor Actuat B-Chem 367: 132033.

14. Liu W, Zhang X, Xu Y et al (2022) 2D Graphene/MnO heterostructure with strongly stable interface enabling high-performance flexible solid-state lithium-ion capacitors. Adv Funct Mater 32: 2202342.

15. Zhao Y, Guo J, Liu A et al (2020) 2D heterostructure comprised of Ni3S2/d-Ti3C2 supported on Ni foam as binder-free electrode for hybrid supercapacitor. J Alloys Compd 814: 152271.

16. Song T, Zhang X, Che Q et al (2022) Heterojunction nanoarchitectonics with SnS2/g-C3N4 S-scheme toward enhanced photooxidation and photoreduction. J Ind Eng Chem 113: 389-400.

17. Kong X, Cao L, Shi Y et al (2023) Construction of S-scheme 2D/2D crystalline carbon nitride/BiOIO3 van der Waals heterojunction for boosted photocatalytic degradation of antibiotics. Molecules 28: 5098.

18. Yin X, Zheng W, Tang H et al (2023) Novel 2D/2D 1T-MoS2/Ti3C2Tz heterostructures for high-voltage symmetric supercapacitors. Nanoscale 15: 10437-10446.

19. Wang X, Li H, Li H et al (2019) Heterostructures of Ni–Co–Al layered double hydroxide assembled on V4C3 MXene for high-energy hybrid supercapacitors. J Mater Chem A 7: 2291-2300.