Supporting Information

Modulation of magnetodielectric equilibrium in porous biochar embedded with MOF-derived Fe3O4/CeO2 for excellent electromagnetic absorption and anti-microbial properties

Youyan Zhanga, Di Lanb, Zihan Wangc, Guodi Xud, Zhihua Gaoa, Guixian Bue, Xiaozhong Zhonge,*, Pengfei Yina,*

- College of Science, Sichuan Agricultural University, Ya’an 625014, P.R. China

- School of Materials Science and Engineering, Hubei University of Automotive Technology, Shiyan 442002, P.R. China

- College of Food Science, Sichuan Agricultural University, Ya’an 625014, P.R. China

- College of Mechanical and Electrical Engineering, Sichuan Agricultural University, Ya’an 625014, P.R. China

- College of Life Science, Sichuan Agricultural University, Ya’an 625014, P.R. China

*Corresponding authors: xiaozhong@sicau.edu.cn (Xiaozhong Zhong); yinpengfei@sicau.edu.cn (Pengfei Yin)

Fig.S1 SEM images of sugarcane-derived porous biochar (a) and polyhedral morphology of Ce-UIO-66.

Fig.S2 Survey spectrum of XPS in CMF-3 (a), high-resolution spectrum of Fe 2p in CMF-2 (b) and CMF-4 (c), high-resolution XPS spectrum of O 1s in CMF-1 (d), CMF-2 (e), and CMF-4 (f).

Fig.S3 Hysteresis loops (a) and BET surface area (b) of CMF-1, CMF-2, CMF-3, and CMF-4.

Fig.S4 Conduction part (a) and polarization part (b) of imaginary permittivity in the CMF-1, CMF-2, CMF-3, and CMF-4.

Fig.S5 RCS simulations of CMF-1 (a), CMF-2 (b), and CMF-4 (c).

Fig.S6 Graphical contrasting of comprehensive properties between the CMF-3 and other related composites.

Tab.S1 Microwave absorbing performance and antibacterial activity of the CMF-3 and other composites reported in recent years.

| Composites | RL/dB | dRL/mm | EAB/GHz | dEAB/mm | Anti-bacteria | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| GO/MWCNTs/Fe3O4 | -43.00 | 2.80 | 8.72 | 2.80 | / | [77] |
| CeO2-x/CNTS | -52.40 | 4.00 | 5.21 | 2.00 | / | [78] |
| RGO/MXene/Fe3O4 | -51.20 | 2.90 | 4.70 | 2.90 | / | [79] |
| Fe3O4/Fe3S4 | -45.33 | 3.30 | 5.03 | 2.00 | / | [80] |
| PAQR/Fe3O4 | -47.79 | 2.48 | 4.80 | 1.51 | / | [81] |
| CeO2/C-700 | -50.10 | 2.30 | 6.00 | 2.30 | / | [82] |
| CeO2/C/Co | -56.20 | 2.30 | 7.30 | 2.70 | / | [83] |
| Fe3O4@Fe@C | -59.09 | 1.85 | 4.72 | 1.65 | / | [84] |
| ABS@CF/CeO2/rGO | -40.90 | 2.20 | 6.60 | 2.20 | / | [85] |
| CMF-3 | -60.60 | 2.00 | 6.40 | 2.19 | Yes | This work |