Supporting Information

Efficient visible light-driven photocatalytic CO2 reduction by self-assembled CsPbBr3 perovskite quantum dots on two-dimensional Bi2O2CO3 petals

Won Seok Cho, Jin Hyuk Cho, Jae Yong Park, Wan Jae Dong*, Soo Yong Kim*, Jong-Lam Lee*

Fig. S1 (a) Transmission electron microscope (TEM) image and electron energy loss spectroscopy (EELS) elemental map of CPB QD. (b, c) High-resolution TEM images and (d, e) electron diffraction patterns of CPB QD.

Fig. S2 (a) Transmission electron microscope (TEM) image and electron energy loss spectroscopy (EELS) elemental map of CPB QD/BOC. (b, c) High-resolution TEM images and (d, e) electron diffraction patterns of CPB QD/BOC.

Fig. S3 FTIR spectra of CPB QDs.

Fig. S4 Mechanism for the enhanced excitonic peak in CPB QD/BOC hybrids compared to isolated CPB QDs.

Fig. S5 Photoluminescence mapping images of BOC, CPB QD, and CPB QD/BOC at an excitation wavelength of 375 nm.

Fig. S6 Photograph images of PC CO2 RR reactor and its components.

Fig. S7 Proposed mechanism for C2H4 formation in the CPB QD/BOC hybrid photocatalyst.

Fig. S8 500 MHz 1H 1D liquid nuclear magnetic resonance spectra of CPB/QD BOC.

Fig. S9 XRD patterns of CPB QD, CPB QD/BOC, and CPB QD/BOC after PC CO2 RR.

Fig. S10 Electrostatic attraction, S-scheme charge separation, and 2D structural support in CPB QD/BOC hybrid for enhanced cycling stability.

Table S1 Calculated time constants of CPB QD and CPB QD/BOC photocatalyst based on time-resolved photoluminescence spectra.

| Photocatalyst | τamp (ns) | τ1 (ns) | τ2 (ns) |
| --- | --- | --- | --- |
| CPB QD | 1.7 | 1.06 | 4.9 |
| CPB QD/BOC | 0.09 | 0.28 | 0.04 |

Table S2 Performance comparison of PC CO2 RR based on CPB QD material from recent literature.

| Photocatalyst | Conditions | Light source | Products (μmol g–1 h–1) | Ref |
| --- | --- | --- | --- | --- |
| CsPbBr3 QD/BOC | Ethyl acetate/DI | 150W Xe lamp 200 mW cm-2 | CO 80.5 CH4 12.2 C2H4 10.7 | This work |
| CsPbBr3 | Ethyl acetate | 100W Xe lamp | CO 4.3 CH4 1.5 H2 0.1 | R1 |
| CsPbBr3/GO | Ethyl acetate | 100W Xe lamp 150 mW cm-2 | CO 4.9 CH4 2.5 H2 0.13 | R2 |
| CsPbBr3/ZIF-8 | Gas (CO2 + H2O) | 100W Xe lamp 150 mW cm-2 | CO 0.5 CH4 1.8 | R3 |
| CsPbBr3 QDs/PCN | Acetonitrile/water | 300W Xe lamp | CO 148.9 | R4 |
| CsPbBr3 NC/a-TiO2 | Ethyl acetate/IPA | 150W Xe lamp 150 mW cm-2 | CO 3.9 CH4 6.7 H2 1.5 | R5 |
| CsPbBr3/USGO /α-Fe2O3 | Acetonitrile/water | 300W Xe lamp 100 mW cm-2 | CO 73.8 | R6 |
| CsPbBr3/P3HT | Acetonitrile/DI | 300W Xe lamp | CO 145.45 CH4 23.05 | R7 |

References

[R1]	J. Hou, S. Cao, Y. Wu, Z. Gao, F. Liang, Y. Sun, Z. Lin, L. Sun, Chem. Eur. J. 23 (2017), 9481-9485.

[R2]	Y.-F. Xu, M.-Z. Yang, B.-X. Chen, X.-D. Wang, H.-Y. Chen, D.-B. Kuang, C.-Y. Su, J. Am. Chem. Soc. 139 (2017), 5660-5663.

[R3]	Z.-C. Kong, J.-F. Liao, Y.-J. Dong, Y.-F. Xu, H.-Y. Chen, D.-B. Kuang, C.-Y. Su, ACS Energy Lett. 3 (2018), 2656-2662.

[R4]	M. Ou, W. Tu, S. Yin, W. Xing, S. Wu, H. Wang, S. Wan, Q. Zhong, R. Xu, Angew. Chem. 130 (2018), 13758-13762.

[R5]	Y. F. Xu, X. D. Wang, J. F. Liao, B. X. Chen, H. Y. Chen, D. B. Kuang, Adv. Mater. interfaces 5 (2018), 1801015.

[R6]	Y. F. Mu, W. Zhang, G. X. Dong, K. Su, M. Zhang, T. B. Lu, Small 16 (2020), 2002140.

[R7]	L. Li, Z. Zhang, C. Ding, J. Xu, Chem. Eng. J. 419 (2021), 129543.