Supplementary Data

Microstructural reorganisation and mechanical property enhancement in PHAs and their wood biocomposites through post-fabrication heat treatment.

Vincent Mathel1,2*, Pauline Le Quellec2, Shazed Aziz1,2, Darren Martin1,2, Peter Halley1,2, Michael Tobias Heitzmann2,3, Luigi-Jules Vandi2,3*

1School of Chemical Engineering, The University of Queensland, Brisbane, QLD 4072, Australia

2Centre for Advanced Materials Processing and Manufacturing (AMPAM), The University of Queensland, Brisbane QLD 4072, Australia

3School of Mechanical and Mining Engineering, The University of Queensland, Brisbane QLD 4072, Australia

*Corresponding authors: Vincent Mathel (E-mail: v.mathel@uq.edu.au); Luigi-Jules Vandi (E-mail: l.vandi@uq.edu.au)

Table S1: Evolution of Molecular weight of materials in function of post-fabrication heat treatment condition

| Post-fabrication heat treatment temperature (℃) | Molecular Weight (10-3g.mol-1) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | PHBV |  | PHBV/P34HB |  | PHBV-Wood |  | PHBV/P34HB-Wood |  |
| ↓ |  |  |  |  |  |  |  |  |
| Duration (min) → |  |  |  |  |  |  |  |  |
|  | 5 | 30 | 5 | 30 | 5 | 30 | 5 | 30 |
| Non-treated | 282.9 |  | 277.2 |  | 233.1 |  | 199.9 |  |
| 70 |  | 278.3 |  | 271.5 |  | 240.2 |  | 214.8 |
| 100 |  | 283.5 |  | 271.3 |  | 238.0 |  | 205.2 |
| 125 |  | 280.1 |  | 267.4 |  | 222.2 |  | 198.6 |
| 150 | 283.8 | 260.9 | 257.4 | 256.8 | 213.1 | 199.5 | 195.7 | 185.3 |
| 160 |  | 252.9 |  | 249.5 |  | 179.1 |  | 170.7 |
| 170 |  | 230.1 |  | 225.1 |  | 159.9 |  | 152.1 |
| 175 | 283.3 | 196.0 | 286.0 | 199.3 | 222.9 | 151.6 | 189.5 | 134.7 |
| 180 |  | 175.6 |  | 175.3 |  | 144.7 |  | 125.6 |
| 185 | 270.8 |  | 210.8 |  | 218.8 |  | 195.4 |  |

Fig.S1: heating DSC curves obtained after heat post-treatment during 5 min for a) PHBV, b) PHBV/P34HB, c) PHBV-Wood, d) PHBV/P34HB-wood and heat post-treatment during 30 min for e) PHBV, f) PHBV/P34HB, g) PHBV-Wood, h) PHBV/P34HB-wood

Fig.S2: DMA curves obtained after heat post-treatment during 5 min for a) PHBV, b) PHBV/P34HB, c) PHBV-Wood, d) PHBV/P34HB-wood and heat post-treatment during 30 min for e) PHBV, f) PHBV/P34HB, g) PHBV-Wood, h) PHBV/P34HB-wood

Table S2: Evolution of melting temperature and degree of crystallinity of materials as a function of post-fabrication heat treatment condition

| Post-fabrication heat treatment temperature (℃) | Melting temperature - Tm (℃) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | PHBV |  | PHBV/P34HB |  | PHBV-Wood |  | PHBV/P34HB-Wood |  |
| ↓ |  |  |  |  |  |  |  |  |
| Duration (min) → |  |  |  |  |  |  |  |  |
|  | 5 | 30 | 5 | 30 | 5 | 30 | 5 | 30 |
| Non-treated | 173.1±0.4 |  | 172.2±0.5 |  | 171.9±0.3 |  | 171.1±0.1 |  |
| 70 | - | - | - | 171.9±0.5 | - | 171.8±0.5 | - | - |
| 100 | 173.8±0.4 | 173.5±0.3 | 172.2±0.1 | 172.0±0.1 | 172.2±0.2 | 171.6±0.1 | 171.4±0.1 | 171.0±0.2 |
| 125 | 172.9±0.1 | 173.0±0.5 | 172.0±0.5 | 172.0±0.5 | 171.3±0.1 | 171.4±0.2 | 171.1±0.2 | 171.4±0.2 |
| 150 | 173.2±0.1 | 174.5±0.2 | 172.1±0.1 | 173.2±0.2 | 171.7±0.2 | 173.1±0.2 | 171.4±0.1 | 171.2±0.2 |
| 160 | 173.4±0.1 | 175.2±0.1 | 172.4±0.1 | 172.6±0.2 | 172.0±0.1 | 174.3±0.2 | 171.7±0.1 | 172.0±0.1 |
| 170 | 173.5±0.3 | 178.7±0.2 | 173.4±0.5 | 176.6±0.5 | 171.6±0.1 | 179.1±0.4 | 171.1±0.1 | 177.9±0.4 |
| 175 | 173.9±0.1 | 182.7±0.5 | 172.2±0.8 | 182.1±0.4 | 172.4±0.1 | 183.7±0.5 | 171.6±0.3 | 183.3±0.5 |
| 180 | 174.3±0.1 | 185.4±0.5 | 173.0±0.1 | 184.7±0.5 | 172.57±0.3 | 183.9±0.3 | 171.5±0.3 | 184.9±0.5 |
| 185 | 175.4±1.0 | - | 172.2±0.1 | - | 174.4±1.0 | - | 171.7±0.7 | - |

|  | Crystallinity degree - Xc (%) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Non-treated | 64±1 |  | 45±1 |  | 56±3 |  | 36±5 |  |
| 70 | - | - | - | 48±1 | - | 62±2 | - | - |
| 100 | 64±1 | 64±3 | 46±1 | 49±2 | 59±1 | 63±1 | 39±3 | 45±4 |
| 125 | 65±3 | 68±3 | 46±2 | 55±1 | 60±1 | 64±2 | 42±1 | 49±3 |
| 150 | 66±1 | 71±1 | 46±3 | 56±1 | 55±1 | 70±3 | 47±2 | 52±2 |
| 160 | 71±5 | 74±1 | 53±1 | 59±5 | 61±3 | 71±2 | 45±1 | 54±1 |
| 170 | 70±2 | 76±2 | 54±2 | 61±1 | 65±3 | 79±3 | 46±3 | 55±1 |
| 175 | 72±1 | 74±2 | 55±1 | 53±1 | 72±4 | 80±2 | 49±3 | 52±2 |
| 180 | 74±1 | 78±5 | 53±3 | 52±5 | 66±1 | 83±3 | 46±1 | 48±2 |
| 185 | 76±1 | - | 51±1 | - | 68±6 | - | 39±1 | - |

Table S3: Evolution of %MAF and %RAF of materials in function of heat post-treatment condition

| Post-treatment temperature (℃) | % MAF |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | PHBV |  | PHBV/P34HB |  | PHBV-Wood |  | PHBV/P34HB-Wood |  |
| ↓ |  |  |  |  |  |  |  |  |
| Duration (min) → |  |  |  |  |  |  |  |  |
|  | 5 | 30 | 5 | 30 | 5 | 30 | 5 | 30 |
| Non-treated | 0.37 |  | 0.73 |  | 0.45 |  | 0.63 |  |
| 70 | - | 0.40 | - | 0.69 | - | 0.39 | - | 0.57 |
| 100 | 0.42 | 0.45 | 0.72 | 0.71 | 0.38 | 0.41 | 0.70 | 0.59 |
| 125 | 0.48 | 0.54 | 0.72 | 0.73 | 0.45 | 0.47 | 0.64 | 0.64 |
| 150 | 0.55 | 0.55 | 0.78 | 0.75 | 0.43 | 0.47 | 0.65 | 0.65 |
| 160 | 0.52 | 0.53 | 0.76 | 0.76 | 0.44 | 0.51 | 0.67 | 0.65 |
| 170 | 0.49 | 0.52 | 0.73 | 0.73 | 0.46 | 0.44 | 0.62 | 0.65 |
| 175 | 0.52 | 0.47 | 0.71 | 0.73 | 0.40 | 0.37 | 0.64 | 0.57 |
| 180 | 0.56 | 0.48 | 0.78 | 0.72 | 0.45 | 0.43 | 0.68 | 0.62 |
| 185 | 0.55 | - | 0.76 | - | 0.50 | - | 0.72 | - |
|  | % RAF |  |  |  |  |  |  |  |
| Non-treated | 35.4±1.5 |  | 25.9±0.2 |  | 37.2±1.0 |  | 22.2±0.5 |  |
| 70 | - | 0.46 | - | 0.23 | - | 0.41 | - | 0.30 |
| 100 | 0.43 | 0.40 | 0.19 | 0.20 | 0.41 | 0.39 | 0.20 | 0.27 |
| 125 | 0.37 | 0.31 | 0.20 | 0.17 | 0.35 | 0.30 | 0.22 | 0.22 |
| 150 | 0.30 | 0.29 | 0.15 | 0.16 | 0.36 | 0.30 | 0.23 | 0.21 |
| 160 | 0.34 | 0.30 | 0.16 | 0.16 | 0.33 | 0.27 | 0.21 | 0.22 |
| 170 | 0.35 | 0.30 | 0.16 | 0.18 | 0.31 | 0.31 | 0.22 | 0.23 |
| 175 | 0.32 | 0.35 | 0.17 | 0.19 | 0.36 | 0.36 | 0.23 | 0.29 |
| 180 | 0.29 | 0.33 | 0.14 | 0.19 | 0.31 | 0.31 | 0.19 | 0.23 |
| 185 | 0.30 | - | 0.19 | - | 0.28 | - | 0.17 | - |

Fig. S3: Evolution of Tg evaluated by DMA for heat post-treated materials for 5 min (left) and 30 min (right)

Table S4: Evolution of Tg evaluated by DMA for all materials in function of heat post-treatment condition

| Post-treatment temperature (℃) | Tg (℃) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | PHBV |  | PHBV/P34HB |  | PHBV-Wood |  | PHBV/P34HB-Wood |  |
| ↓ |  |  |  |  |  |  |  |  |
| Duration (min) → |  |  |  |  |  |  |  |  |
|  | 5 | 30 | 5 | 30 | 5 | 30 | 5 | 30 |
| Non-treated | 19.1 |  | 17.2 |  | 21.7 |  | 15.8 |  |
| 70 | - | 19.3 | - | 14.7 | - | 19.4 | - | 16.5 |
| 100 | 21.0 | 19.8 | 14.6 | 14.2 | 19.7 | 19.2 | 17.5 | 14.2 |
| 125 | 19.0 | 18.2 | 12.1 | 14.6 | 18.9 | 19.4 | 17.6 | 13.7 |
| 150 | 18.5 | 17.1 | 13.8 | 15.6 | 17.1 | 16.1 | 13.9 | 13.7 |
| 160 | 18.4 | 14.8 | 14.3 | 13.8 | 16.6 | 19.4 | 15.3 | 16.6 |
| 170 | 18.4 | 16.6 | 14.2 | 14.8 | 17.6 | 19.0 | 14.7 | 17.5 |
| 175 | 16.1 | 18.1 | 14.7 | 17.5 | 16.2 | 18.8 | 15.6 | 18.5 |
| 180 | 16.9 | 17.5 | 13.8 | 17.5 | 15.7 | 18.8 | 17.6 | 17.0 |
| 185 | 15.4 | - | 10.2 | - | 15.7 | - | 16.6 | - |

Table S5: Evolution of tensile modulus and stress and strain at break of materials in function of post-fabrication heat treatment condition.

| Post-fabrication heat treatment temperature (℃) | Tensile modulus (GPa) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | PHBV |  | PHBV/P34HB |  | PHBV-Wood |  | PHBV/P34HB-Wood |  |
| ↓ |  |  |  |  |  |  |  |  |
| Duration (min) → |  |  |  |  |  |  |  |  |
|  | 5 | 30 | 5 | 30 | 5 | 30 | 5 | 30 |
| Non-treated | 3.3±0.1 |  | 1.7±0.1 |  | 4.8±0.6 |  | 2.3±0.2 |  |
| 70 | - | 3.2±0.1 | - | 1.7±0.1 | - | 4.7±0.5 | - | 2.5±0.2 |
| 100 | 3.1±0.1 | 3.1±0.1 | 1.6±0.1 | 1.6±0.1 | 4.2±0.2 | 4.3±0.2 | 2.3±0.3 | 2.5±0.3 |
| 125 | 3.0±0.2 | 2.8±0.2 | 1.5±0.1 | 1.4±0.1 | 4.0±0.1 | 3.8±0.2 | 2.2±0.1 | 2.1±0.1 |
| 150 | 2.9±0.2 | 2.5±0.2 | 1.4±0.1 | 1.2±0.1 | 3.9±0.1 | 3.7±0.3 | 2.1±0.1 | 1.8±0.1 |
| 160 | 2.5±0.1 | 2.7±0.2 | 1.2±0.1 | 1.2±0.1 | 4.0±0.2 | 3.7±0.3 | 2.1±0.2 | 1.8±0.1 |
| 170 | 2.5±0.2 | 2.7±0.08 | 1.2±0.1 | 1.2±0.1 | 3.8±0.4 | 4.3±0.1 | 2.0±0.1 | 1.9±0.1 |
| 175 | 2.5±0.2 | 3.2±0.2 | 1.3±0.1 | 1.2±0.1 | 3.9±0.2 | 4.4±0.1 | 2.0±0.1 | 1.9±0.2 |
| 180 | 2.4±0.2 | 3.0±0.4 | 1.1±0.1 | 1.3±0.2 | 3.8±0.3 | 4.8±0.3 | 1.9±0.1 | 2.2±0.2 |
| 185 | 2.3±0.2 | - | 1.0±0.1 | - | 3.6±0.3 | - | 1.9±0.1 | - |
|  | Tensile stress (at maximum load) (MPa) |  |  |  |  |  |  |  |
| Non-treated | 35.4±1.5 |  | 25.9±0.2 |  | 37.2±1.0 |  | 22.2±0.5 |  |
| 70 | - | 35.3±0.9 | - | 25.9±0.7 | - | 35.9±1.5 | - | 22.1±0.7 |
| 100 | 35.9±0.8 | 34.7±0.7 | 26.0±0.4 | 24.6±0.4 | 34.7±1.2 | 35.6±1.3 | 21.4±0.7 | 22.1±0.6 |
| 125 | 34.1±1.1 | 33.4±0.8 | 24.8±0.4 | 23.7±0.8 | 35.5±0.9 | 33.8±1.3 | 20.8±0.4 | 20.2±0.3 |
| 150 | 33±1.0 | 30.6±0.7 | 23.4±0.6 | 21.7±0.6 | 34.9±0.8 | 33.8±0.2 | 20.3±0.2 | 19.1±0.3 |
| 160 | 33.8±0.8 | 30.5±0.5 | 22.7±0.8 | 21.1±0.3 | 34.1±0.3 | 33.2±0.8 | 20.3±0.3 | 18.4±0.2 |
| 170 | 32.5±1.0 | 30.5±0.5 | 22.5±0.6 | 20.6±0.5 | 34.2±1.1 | 33.7±0.9 | 19.5±0.5 | 17.7±0.5 |
| 175 | 32.6±1.2 | 32.4±1.5 | 22.8±0.7 | 20.6±0.6 | 33.8±0.6 | 35.6±0.6 | 19.8±0.5 | 17.4±0.8 |
| 180 | 31.7±0.4 | 33.1±0.5 | 22.2±0.5 | 20.4±0.8 | 33.9±0.4 | 35.7±0.9 | 19.2±0.8 | 17.5±0.5 |
| 185 | 30.2±0.6 | - | 21.2±0.4 | - | 33.7±1.4 | - | 18.6±0.5 | - |
|  | Tensile strain at break (%) |  |  |  |  |  |  |  |
| Non-treated | 3.3±0.4 |  | 33.9±17.4 |  | 1.3±0.1 |  | 8.5±0.8 |  |
| 70 | - | 3.6±0.4 | - | 57.8±19.4 | - | 1.3±0.2 | - | 9.0±0.6 |
| 100 | 4.9±1.8 | 7.9±2.0 | 61.5±23.1 | 113.7±39.8 | 1.1±0.1 | 1.8±0.2 | 8.4±2.3 | 12.4±2.3 |
| 125 | 12.4±8.0 | 18.9±6.9 | 107.6±32.9 | 165.4±65.6 | 2.2±0.5 | 2.6±0.4 | 15.1±2.0 | 24.8±2.5 |
| 150 | 14.0±9.7 | 25.0±7.0 | 135.1±35.7 | 268.4±51.4 | 2.2±0.4 | 3.4±0.9 | 16.9±3.6 | 31.4±5.8 |
| 160 | 16.4±5.3 | 37.5±10.3 | 151.6±56.7 | 205.0±51.4 | 3.3±0.3 | 3.5±0.4 | 20.5±2.2 | 30.6±7.5 |
| 170 | 21.8±5.4 | 36.6±10.7 | 188.5±60.6 | 124.7±46.5 | 3.1±0.3 | 3.5±0.5 | 30.0±9.3 | 23.4±3.7 |
| 175 | 18.0±9.1 | 34.7±14.2 | 182.1±58.7 | 104.5±29.4 | 4.1±0.7 | 2.8±0.3 | 25.7±3.9 | 13.1±2.9 |
| 180 | 46.5±30.6 | 27.2±24.6 | 233.3±76.0 | 49.7±21.0 | 4.1±0.6 | 2.0±0.5 | 25.7±6.8 | 6.4±1.4 |
| 185 | 30.4±8.4 | - | 198.7±77.7 | - | 3.7±0.2 | - | 32.9±4.6 | - |

Fig. S3: Evolution of tan ẟ  for PHBV, P3HB, PHBV/P34HB (top),PHBV-wood, P34HB-wood, PHBV/P34HB-wood (bottom) and their post-fabrication thermal treatment at 150, 170 and 180 ℃ for 30 min

Table S6: Evolution of shrinkage in materials as a function of post-fabrication heat treatment conditions

| Post-fabrication heat treatment temperature (℃) | Shrinkage (%) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | PHBV |  | PHBV/P34HB |  | PHBV-Wood |  | PHBV/P34HB-Wood |  |
| ↓ |  |  |  |  |  |  |  |  |
| Duration (min) → |  |  |  |  |  |  |  |  |
|  | 5 | 30 | 5 | 30 | 5 | 30 | 5 | 30 |
| Non-treated | -1.26% |  | -1.26% |  | -0.16% |  | -0.16% |  |
| 70 | - | -1.42% | - | -1.26% | - | -0.16% | - | -0.16% |
| 100 | -1.26% | -1.73% | -1.10% | -1.42% | -0.16% | -0.31% | 0.00% | -0.31% |
| 125 | -1.26% | -1.73% | -1.26% | -1.26% | -0.16% | -0.47% | 0.00% | -0.16% |
| 150 | -1.42% | -1.73% | -1.26% | -1.42% | 0.00% | -0.31% | -0.16% | -0.16% |
| 160 | -1.57% | -2.05% | -1.26% | -1.57% | -0.16% | -0.31% | 0.00% | -0.16% |
| 170 | -1.57% | -2.36% | -1.26% | -2.05% | -0.16% | -0.47% | -0.16% | -0.47% |
| 175 | -1.73% | -2.83% | -1.26% | -2.83% | -0.16% | -0.79% | 0.00% | -0.79% |
| 180 | -1.89% | -5.35% | -1.42% | -5.83% | -0.31% | -1.89% | -0.16% | -2.36% |
| 185 | -1.89% | - | -1.42% | - | -0.31% | - | -0.31% | - |