# ENHANCING REPROCESSABILITY OF DYNAMIC POLYMER COMPOSITES WITH THERMALLY SENSITIVE PARTICLES AND CONTROLLED PARTICLE-MATRIX INTERFACES

Hoogmartens Anthony1, Schlögl Sandra2, Leterrier Yves1, Michaud Véronique1

1Laboratory for Processing of Advanced Composites (LPAC), Ecole Polytechnique Fédérale de Lausanne (EPFL), Station 12, Lausanne, 1015, Vaud, Switzerland.

2Chemistry of Functional Polymers, Polymer Competence Center

Leoben GmbH (PCCL), Sauraugasse, Leoben, 8700, Styria, Austria.

Advanced Composites and Hybrid Materials

Corresponding author: Véronique Michaud (veronique.michaud@epfl.ch)

Contributing authors: anthony.hoogmartens@epfl.ch; sandra.schloegl@pccl.at; yves.leterrier@epfl.ch; veronique.michaud@epfl.ch;

# Structural characterization of cystamine

Fig. S1 1H NMR cystamine: 1H NMR (400 MHz, d-methanol, δ ppm): 3.20 (t, 4H), 3.03 (t, 4H)

# Characterization of the polyester particles

Fig.S2 DSC measurement of the polyester particles

Table 1: Additional information for the polyester particles

|  | PLA | PET |
| --- | --- | --- |
| Tg [°C] | 55.68 | 80 |
| Melting point Tm [°C] | 150-160 | 240-250 |
| Enthalpy of melting [J/g] | 38.49 | 55.1 |
| Degree of crystallinity Xc [%] | 41.4 [1] | 39.3 [2] |

# TGA, amplitude sweep, glass transition temperature and viscosity measurements – main and control formulations

Fig.S3 TGA measurements for the main formulation and the control formulations

Fig.S4 Amplitude sweep of the main formulation and the control formulations

Fig. S5 Glass transition temperature measurements of the main formulation and the control formulations

Fig.S6 Flow curves of the matrix and composites

# Stress relaxation measurements of the matrix

Fig.S7 Normalised relaxation modulus versus time for different temperatures of the main formulation. The relaxation time for the test at 100°C is 32194 seconds which is extrapolated from the given data

# Topology freezing temperature measurements

The topology freezing temperature (TV) is the temperature at which a vitrimer network stops flowing on practical timescales. It is defined as the temperature where the stress relaxation time 𝜏* becomes very long (typically 107 seconds), meaning the network behaves like a solid.

The Tv can be extrapolated from the Arrhenius fitted line (blue curve in Fig. 8) to a relaxation time of 107 s (τ(Tv) = 107).

τT= τ0eEaRT orlnτ=lnτ0+ EaR . 1T ≈lnτ=m1000T+b

where Ea is the activation energy of the bond-exchange process, R is the gas constant, τ0 is the pre-exponential factor, m the slope and b the intercept.

In this case, Ea = 105.1 kJ/mol-1 and τ0 = eb = e-23.8 = 4x10-11s

Tv= EaR(lnτv-lnτ0)=315.6 K or 42.5°C

This value is comparable to that of other systems having dynamic ester bonds and exhibiting a rather low Tg (for example Tg = 8°C and Tv = 48.7°C [1]).

Fig.S8 Stress relaxation times (Arrhenius diagram) of the main and control formulations

# The influence of the PLA particles on the curing behaviour

Fig.S9 Total heat of reaction and conversion in function of volume percentage of PLA particles

# References

1. 	Zhang C, Lan Q, Zhai T, et al (2018) Melt Crystallization Behavior and Crystalline Morphology of Polylactide/Poly(ε-caprolactone) Blends Compatibilized by Lactide-Caprolactone Copolymer. Polymers 10:1181. https://doi.org/10.3390/polym10111181

2. 	Ronkay F, Molnár B, Nagy D, et al (2020) Melting temperature versus crystallinity: new way for identification and analysis of multiple endotherms of poly(ethylene terephthalate). J Polym Res 27:372. https://doi.org/10.1007/s10965-020-02327-7