Supporting Information for

Ion-Driven Exfoliation of Two-Dimensional ZIF-L sheets via Phosphate Intercalation for Advanced Epoxy Anti-Corrosion Coatings

Mohammad Ghaderi, Kim Dam-Johansen, Huichao Bi*

CoaST, Department of Chemical and Biochemical Engineering, Technical University of Denmark (DTU), Building 229, 2800 Kgs. Lyngby, Denmark

* Corresponding Authors. Huichao Bi (E-mail: bihuichao@hotmail.com)

2. Results and discussion

Figure S1. C1s (a), N1s (b), O1s (c), and Zn 2p (d) high-resolution XPS spectra of ZIF-L.

Table S1. The extracted parameters obtained by fitting EIS data of steel samples immersed in 3.5 wt. % NaCl solution.

| Sample | Time (h) | Electrical equivalent circuit | Rs (Ω cm2) | Y0,f1 (× 10-4)(Ω-1 cm-2 sn) | nf1 | Rf1 (Ω cm2) | Y0,dl (× 10-4)(Ω-1 cm-2 sn) | ndl | Rct | Warburg, Y0,w (Ω-1 cm-2 s0.5) | RT |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Blank | 2 | R(QR) | 5.0 | - | - | - | 5.0 | 0.81 | 870.8 | - | 875.8 |
|  | 4 | R(QR)(Q(WR) | 5.6 | 4.49 | 0.85 | 6.13 | 5.03 | 0.82 | 1353 | 0.0052 | 1364.7 |
|  | 6 | R(QR)(Q(WR) | 4.5 | 4.80 | 0.84 | 5.79 | 6.68 | 0.80 | 1180 | 0.0079 | 1190.2 |
|  | 24 | R(QR)(Q(WR) | 4.8 | 9.69 | 0.80 | 1104 | 1.71 | 0.93 | 4.21 | 0.013 | 1113 |

Table S2. The extracted parameters obtained by fitting EIS data of steel samples immersed in 3.5 wt. % NaCl solution containing ZIF-L extract.

| Sample | Time (h) | Electrical equivalent circuit | Rs (Ω cm2) | Y0,f1 (× 10-4)(Ω-1 cm-2 sn) | nf1 | Rf1 (Ω cm2) | Y0,dl (× 10-4)(Ω-1 cm-2 sn) | ndl | Rct | L (Henri) | Rt |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ZIF-L | 2 | R(Q(R(QR(LR)))) | 7.0 | 1.8 | 0.85 | 1452 | 4.1 | 0.79 | 697.9 | 13130 | 2138.9 |
|  | 4 | R(Q(R(QR(LR)))) | 7.0 | 1.2 | 0.87 | 1134 | 2.2 | 0.64 | 1662 | 67880 | 2803 |
|  | 6 | R(Q(R(QR(LR)))) | 7.0 | 1.22 | 0.87 | 1132 | 2.6 | 0.64 | 1251 | 60010 | 2390 |
|  | 24 | R(Q(R(QR(LR)))) | 7.0 | 1.1 | 0.88 | 1332 | 3.58 | 0.76 | 586.2 | 13860 | 1925 |

Table S3. The extracted parameters obtained by fitting EIS data of steel samples immersed in 3.5 wt. % NaCl solution containing PZIF extract.

| Sample | Time (h) | Electrical equivalent circuit | Rs (Ω cm2) | Y0,f1 (× 10-4)(Ω-1 cm-2 sn) | nf1 | Rf1 (Ω cm2) | Y0,f2 (× 10-4)(Ω-1 cm-2 sn) | nf2 | Rf2 (Ω cm2) | Y0,dl (× 10-6)(Ω-1 cm-2 sn) | ndl | Rct | Rt |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PZIF | 2 | R(QR)(QR)(QR) | 7.2 | 0.47 | 0.73 | 45.7 | 2.65 | 1 | 8003 | 1.98 | 0.64 | 2984 | 11039.9 |
|  | 4 | R(QR)(QR)(QR) | 6.9 | 2.42 | 0.59 | 4724 | 3.24 | 1 | 13230 | 0.19 | 0.8 | 60.23 | 18021 |
|  | 6 | R(QR)(QR)(QR) | 7 | 0.19 | 0.78 | 79.3 | 2.27 | 0.86 | 23170 | 3.04 | 0.58 | 1392 | 24648 |
|  | 24 | R(QR)(QR)(QR) | 5.7 | 6.45 | 0.47 | 684.2 | 3.05 | 0.78 | 16190 | 0.31 | 0.86 | 62.5 | 16942 |