Supporting Material

Regulating water states in organic–inorganic hybrid gel coatings to suppress icing/frosting and improve thermal efficiency in heat exchangers

Eunji Lee1, Jong Woo Kang2, and Ji-Hun Seo1*

seojh79@korea.ac.kr

1 Department of Materials Science and Engineering, Korea University, 145 Anam-ro, Seongbuk-gu, Seoul 02840, Republic of Korea

2 Department of Orthopedic Surgery, College of Medicine, Korea University, Ansan, Republic of Korea

Fig. S1 The coating surface morphology of gels. a Digital images and b SEM images of coating surfaces.

Fig. S2 Characterization of silica nanoparticles and gels. a SEM images of silica nanoparticles and gels. b EDS atomic graph and images of each gel

Fig. S3 Analysis of ice-propagation on Al substrates and silica–MPC hybrid gels. a Ice-delay times (td) of bare Al substrates, silica, MPC, and silica–MPC hybrid gels measured at different Ts (-10, -15, -20, -25 and -30 ˚C) within 60 min. b Arrhenius plots used to extract activation energy (Ea) required for ice propagation on each surface

Fig. S4 Frost thickness measured at a –10 °C, b -15 °C, c -20 °C, and d -30 °C (Tair = 15 °C, and RH = 80%)

Fig. S5 Frost mass and frost density measured for each surface (Tair = 15 °C, RH = 80%, Ts = -15 ˚C)

Fig. S6 Digital images of gel-coated surfaces before and after the 3-cycle test.

Fig. S7 Cross-cut test on surface of silica-MPC hybrid gel. Digital images of a before and b after the test. Threshold images of cross-cut c before and d after the test.

For adhesion test, a specialized cross-cut tester with 2 mm-spaced blades was used to create a lattice pattern, and a tape with an adhesion strength of 3.5 N cm⁻¹ was applied and removed. To ensure accurate analysis, the detached area was calculated using ImageJ software with a threshold image analysis. The results showed that the detached area was approximately 2.9%, which corresponds to a grade of 4B, according to ASTM D3359.

Fig. S8 The mechanical properties under impact loads. Digital images of silica–MPC hybrid gel coated surfaces. a before and b after the wear resistance test.

Wear resistance was evaluated using a sandpaper-abrasion test based on the principles of ASTM G133. A #1000-grit sandpaper was fixed on a flat substrate, and the gel-coated sample was slid in a reciprocating manner under a normal load of 100 g at 40 cycles/min for 1000 cycles. Digital images were obtained to assess surface damage and changes in surface roughness.

Fig. S9 Digital images of coated gel surfaces on the stainless steel substrates before and after the anti-icing test.

Fig. S10 Anti-icing performance of superhydrophobic coated surfaces (Ta = 15 °C, RH = 80%, and Ts = -10 °C). The superhydrophobic coating was prepared using the same formulation reported in our previous study [1]. Digital images a top-view images of surfaces and b cross-sectional images before and after the icing test.

Fig. S11 FTIR spectrum of acrylated silica nanoparticles confirming the absence of silanol-related OH vibrational features.

Reference

1. Bitgaram K,Joonbum L, Eunji L, Kihun J, Ji-Hun S. (2024) One-pot coatable fluorinated polyurethane resin solution for robust superhydrophobic anti-fouling surface. Prog Org Coat 187:108097. https://doi.org/10.1016/j.porgcoat.2023.108097