Platinum Nanozymes Loaded Contact Lenses: Screening of Oxidoreductase Activities and Efficient Degradation of Organic Dye

Said El Turk*, 1, Mohammed Ayaz Uddin1, Aswathi Ram P.1, Afra AlMeraikhi3, Aisha T. Khaleel3, Valentyn S. Volkov4, Andreas Schiffer1, Wael Zaki1, and Haider Butt*, 1,2

1Department of Mechanical & Nuclear Engineering, Khalifa University of Science and Technology, Abu Dhabi, P.O. Box 127788, United Arab Emirates

2Advanced Digital & Additive Manufacturing (ADAM) Research Group, Khalifa University of Science and Technology, Abu Dhabi 127788, United Arab Emirates.

3Borouge Pte. Ltd., Abu Dhabi, United Arab Emirates

4Emerging Technologies Research Center, XPANCEO, Dubai Investment Park First, Dubai, United Arab Emirates

*Corresponding author: 100049722@ku.ac.ae, Haider.Butt@ku.ac.ae

Figure S1: Bulk specimens used for tensile, flexural, and tear tests.

Figure S2: TEM imaging of Pt NZs solution (0.5 mM) at low magnification (left) and high magnification (right).

Figure S3: The absorption spectra of: a) MB. b) A solution of MB and H2O2.

Figure S4: TEM imaging of lens storage water solution (Left) and EDS spectra (right).

Figure S5: Artificial Anterior Chamber leakage assessment: a) Representative image showing the setup used. b) Transmission spectra obtained.

Figure S6: Biocompatibility of transparent (T), Pt NZs (P)-, and Au NZs (G)- loaded hydrogel extracts in human dermal fibroblasts after 24 h exposure. (a)Cytotoxicity assessed by lactate dehydrogenase (LDH) release into the supernatant, normalised to media (0%) and lysis (100%) controls. (b) Cell viability quantified by Calcein-AM/propidium iodide (Live/Dead) staining and expressed as the percentage of live cells relative to total fluorescence. (c) Representative fluorescence micrographs of fibroblasts co-stained with Calcein-AM (green, live cells) and propidium iodide (red, dead cells) following 24 h incubation with media (Control), T extract, P, extract, or G extract; scale bar = 750 µm. Data are presented as mean ± SD (n = 3 per group). Statistical analysis was performed by one-way ANOVA followed by Dunnett's multiple comparisons test (each extract vs. Control). ns, not significant.

Figure S7: Transmission spectra of a lens before and after three cycles of exposure to H2O2.

Figure S8: The 3D printing of multi-material discs using two different resins and incorporating Au NZs only in Resin 2.

Figure S9: Antibacterial assay: The agar plate after approximately 24 hours of incubating the lenses with bacteria.