Self-powered Rehabilitation Monitoring via Cation-Regulated Interfacial Polarization in Fluoride-filled P(VDF-TrFE) sensors

Yingjuan Yan,a Weimin Xia,a,* Yinghui Wang,a Haixuan Ren,b Wei Xia,b Jing Li,b Xusheng Wang,b Zhicheng Zhang,c, *

- School of Materials Science and Engineering, Xi’an University of Technology, Xi’an 710048, China.

- College of Printing, Packaging and Digital Media, Xi’an University of Technology, Xi’an 710054, China.

- School of Chemistry, Xi’an Jiaotong University, Xi’an 710049, China.

*Authors to whom correspondence should be addressed:

Dr. Weimin Xia, Email: xiaweimin@xaut.edu.cn (W. Xia).

1. Piezoelectric properties of composites

Figure S1 (a-d) show the quasi-static |d33| curves of the composite film as a function of the AlF3, BaF2, CaF2, and MgF2 content, respectively

2. Crystal structure of composite films

Figure S2 (a-d) show the XRD patterns of a series of P(VDF-TrFE) samples doped with different concentrations of AlF3, BaF2, CaF2, and MgF2

Table 1 β phase diffraction peak related to P(VDF-TrFE) was subjected to FWHM quantitative analysis

| Sample | 2θ (°) | FWHM (°) | θ | β (rad) | D (nm) |
| --- | --- | --- | --- | --- | --- |
| P(VDF-TrFE) | 19.3 | 0.77 | 9.650 | 0.01344 | 10.47 |
| PA | 19.69 | 0.90 | 9.845 | 0.01571 | 8.96 |
| PB | 19.52 | 0.84 | 9.760 | 0.01466 | 9.60 |
| PC | 19.62 | 0.85 | 9.810 | 0.01484 | 9.48 |
| PM | 19.67 | 0.88 | 9.835 | 0.01536 | 9.16 |

3. Phase transition kinetics of composite films

Figure S3 (a-d) show the FTIR spectra of a series of P(VDF-TrFE) samples doped with different concentrations of AlF3, BaF2, CaF2, and MgF2

Figure S4 (a-d) show the curves depicting the variation of the β-phase content in P(VDF-TrFE) doped with different concentrations of AlF3, BaF2, CaF2, and MgF2 as a function of doping concentration

Figure S5 (a-d) show a series of DSC curves for P(VDF-TrFE) doped with different concentrations of AlF3, BaF2, CaF2, and MgF2, respectively

Figure S6 (a-d) Plot of crystallinity versus doping concentration for P(VDF-TrFE) doped with different amounts of AlF3, BaF2, CaF2, and MgF2

4. XPS Spectroscopy of samples

Figure S7 (a) High-resolution XPS total spectra of AlF3, BaF2, CaF2, and MgF2 powders (b) High-resolution F 1s XPS spectra of P(VDF-TrFE), AlF3, BaF2, CaF2, and MgF2 powders, respectively

Figure S8 High-resolution C1s XPS fitting of AlF3 powders

Figure S9 (a-c) show the high-resolution XPS spectra of the C1s peak in the PB, PC, and PM composite films, respectively (d-f) show the high-resolution XPS spectra of the C1s peak in BaF2, CaF2, and MgF2 powders, respectively

Figure S10 (a-d) show the high-resolution XPS spectra of the cations Al 2p, Ba 3d, Ca 2p, and Mg 1s in AlF3, BaF2, CaF2, and MgF2 powders, respectively (e-h) show the high-resolution XPS spectra of the cations Al 2p, Ba 3d, Ca 2p, and Mg 1s in the PA, PB, PC, and PM composite films, respectively

5. Dielectric properties of composites

Figure S11 (a-c) show the frequency-dependent dielectric properties of P(VDF-TrFE) doped with different concentrations of BaF2, CaF2, and MgF2, respectively (d-f) show the corresponding plots of the dielectric constant as a function of doping concentration

Figure S12 (a-c) show the dielectric temperature spectra of P(VDF-TrFE) doped with 7% BaF2, CaF2, and MgF2, respectively, in the frequency range of 100 Hz to 1 MHz

6. Electrical Properties of composites

Figure S13 Electrical test devices

Figure S14 (a-d) show the electrical output characteristics of P(VDF-TrFE) doped with different concentrations of AlF3, BaF2, CaF2, and MgF2, respectively

Figure S15 (a-d) show the frequency dependence of the output voltages of the P(VDF-TrFE), PB, PC, and PM piezoelectric sensors, respectively

Figure S16 Circuit Diagram for an External Load