In vitro investigations on the effects of graphene and graphene oxide on polycaprolactone bone tissue engineering scaffolds

Yanhao Hou 1, Weiguang Wang 1,*, Paulo Bartolo 1, 2,*

1 School of Engineering, Faculty of Science and Engineering, The University of Manchester, Manchester, UK

2 Singapore Centre for 3D Printing, School of Mechanical and Aerospace Engineering, Nanyang Technological University, Singapore

* Corresponding authors: weiguang.wang@manchester.ac.uk; paulojorge.dasilvabartolo@manchester.ac.uk; pbartolo@ntu.edu.sg

- Supplementary material

Table S1. DSC data of PCL scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -39.083±2.387 | 66.843±0.237 | 79.387±2.484 | - | - | 56.908±1.781 |
| 24 H | -42.240±0.934 | 65.853±0.280 | 83.210±2.583 | - | - | 59.649±1.851 |
| 48 H | -43.693±1.737 | 65.820±0.269 | 82.943±1.040 | - | - | 59.458±0.745 |
| 72 H | -43.257±1.582 | 66.717±0.099 | 83.597±2.203 | - | - | 59.926±1.579 |
| 96 H | -40.407±2.194 | 66.380±0.286 | 81.997±0.864 | - | - | 58.779±0.619 |
| 120 H | -43.383±1.368 | 66.270±0.642 | 80.447±2.543 | - | - | 57.668±1.823 |
| 144 H | -43.240±1.426 | 66.077±0.530 | 82.737±1.538 | - | - | 59.309±1.103 |
| 168 H | -43.617±1.873 | 66.563±0.332 | 66.563±0.332 | - | - | 58.769±1.816 |
| 192 H | -41.333±1.064 | 65.360±0.279 | 86.783±3.558 | - | - | 62.210±2.550 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 25.437±0.222 | 56.713±1.824 | 40.655±1.307 |
| 24 H | - | - | - | 26.637±0.327 | 59.147±2.256 | 42.399±1.618 |
| 48 H | - | - | - | 26.143±0.438 | 59.133±0.361 | 42.389±0.259 |
| 72 H | - | - | - | 25.490±0.482 | 59.243±1.548 | 42.468±1.110 |
| 96 H | - | - | - | 25.670±0.630 | 58.847±0.981 | 42.184±0.703 |
| 120 H | - | - | - | 26.387±0.375 | 57.273±1.746 | 41.056±1.252 |
| 144 H | - | - | - | 27.010±0.473 | 58.537±0.716 | 41.962±0.513 |
| 168 H | - | - | - | 25.580±0.200 | 58.027±1.852 | 41.596±1.327 |
| 192 H | - | - | - | 26.077±0.748 | 60.753±2.587 | 43.551±1.854 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -64.133±0.180 | 58.027±0.490 | 51.330±1.866 | - | - | 36.796±1.337 |
| 24 H | -43.570±1.994 | 58.120±0.470 | 54.183±1.883 | - | - | 38.841±1.350 |
| 48 H | -42.470±1.286 | 58.800±1.650 | 53.460±0.927 | - | - | 38.323±0.664 |
| 72 H | -42.603±0.515 | 59.550±1.704 | 53.523±1.599 | - | - | 38.368±1.146 |
| 96 H | -41.403±1.390 | 59.460±1.221 | 53.443±1.363 | - | - | 38.311±0.977 |
| 120 H | -42.153±0.373 | 58.800±1.532 | 52.250±1.273 | - | - | 37.455±0.913 |
| 144 H | -43.677±1.652 | 57.817±1.080 | 54.047±0.993 | - | - | 38.743±0.712 |
| 168 H | -43.610±1.739 | 58.340±0.806 | 53.303±1.873 | - | - | 38.210±1.342 |
| 192 H | -42.217±0.917 | 57.217±0.709 | 56.360±2.691 | - | - | 40.401±1.929 |

Table S2. DSC data of G1 scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -40.407±1.223 | 68.550±0.272 | 82.883±0.910 | - | - | 60.015±0.659 |
| 24 H | -41.810±1.429 | 68.453±0.067 | 88.073±2.560 | - | - | 63.772±1.854 |
| 48 H | -41.287±0.540 | 67.680±1.101 | 83.503±1.228 | - | - | 60.464±0.889 |
| 72 H | -41.737±1.638 | 67.430±0.535 | 87.570±3.145 | - | - | 63.408±2.277 |
| 96 H | -41.250±0.305 | 67.367±0.739 | 87.217±1.779 | - | - | 63.152±1.288 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 35.717±0.370 | 55.430±0.564 | 40.136±0.408 |
| 24 H | - | - | - | 37.003±0.194 | 58.157±1.755 | 42.110±1.271 |
| 48 H | - | - | - | 36.070±0.279 | 55.073±0.940 | 39.878±0.681 |
| 72 H | - | - | - | 36.620±0.382 | 58.057±2.060 | 42.038±1.492 |
| 96 H | - | - | - | 36.303±0.489 | 57.693±1.187 | 41.775±0.860 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -41.14±1.546 | 58.440±0.225 | 55.803±0.479 | - | - | 40.406±0.347 |
| 24 H | -41.847±1.402 | 57.530±0.199 | 59.650±1.484 | - | - | 43.192±1.074 |
| 48 H | -41.790±0.295 | 57.813±0.303 | 56.160±0.895 | - | - | 40.665±0.648 |
| 72 H | -41.747±1.609 | 58.237±0.674 | 59.317±2.083 | - | - | 42.950±1.508 |
| 96 H | -41.597±0.583 | 57.590±0.416 | 59.243±0.931 | - | - | 42.897±0.674 |

Table S3. DSC data of G3 scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -41.367±0.833 | 67.893±0.505 | 83.223±1.001 | - | - | 61.503±0.740 |
| 12 H | -42.623±1.503 | 66.020±0.580 | 87.317±3.337 | - | - | 64.528±2.466 |
| 24 H | -42.420±0.973 | 66.313±0.393 | 86.843±3.378 | - | - | 64.179±2.497 |
| 36 H | -43.423±2.972 | 66.703±0.714 | 85.390±1.699 | - | - | 63.105±1.255 |
| 48 H | -41.807±1.684 | 66.327±0.110 | 85.900±2.188 | - | - | 63.482±1.617 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 36.660±0.491 | 54.767±0.587 | 40.473±0.434 |
| 12 H | - | - | - | 37.240±0.324 | 56.163±0.859 | 41.506±0.635 |
| 24 H | - | - | - | 37.390±0.295 | 56.870±2.097 | 42.028±1.550 |
| 36 H | - | - | - | 37.733±0.266 | 56.713±2.668 | 41.912±1.972 |
| 48 H | - | - | - | 37.617±0.459 | 56.427±2.355 | 41.700±1.741 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -41.283±0.641 | 58.117±0.414 | 56.480±0.339 | - | - | 41.740±0.250 |
| 12 H | -42.640±1.192 | 58.173±0.136 | 58.567±0.643 | - | - | 43.282±0.475 |
| 24 H | -41.933±1.404 | 57.603±0.095 | 59.253±2.295 | - | - | 43.789±1.696 |
| 36 H | -43.050±2.511 | 57.990±0.149 | 59.323±2.359 | - | - | 43.841±1.743 |
| 48 H | -41.980±1.776 | 57.533±0.673 | 59.127±1.736 | - | - | 43.696±1.283 |

Table S4. DSC data of G5 scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -42.817±1.003 | 65.647±0.441 | 85.130±1.853 | - | - | 63.072±1.324 |
| 12 H | -41.753±1.410 | 66.643±0.504 | 87.663±3.753 | - | - | 66.149±2.832 |
| 18 H | -42.507±2.481 | 65.313±0.151 | 85.460±1.946 | - | - | 64.486±1.468 |
| 24 H | -41.717±1.405 | 66.797±0.354 | 86.070±3.644 | - | - | 64.946±2.749 |
| 36 H | -42.003±0.965 | 65.363±0.549 | 65.363±0.549 | - | - | 65.363±0.549 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 38.093±0.580 | 56.843±1.183 | 42.893±0.893 |
| 12 H | - | - | - | 38.377±0.570 | 56.937±2.370 | 42.963±1.788 |
| 18 H | - | - | - | 37.167±0.206 | 55.980±0.893 | 42.241±0.673 |
| 24 H | - | - | - | 38.257±0.172 | 56.207±1.969 | 42.412±1.486 |
| 36 H | - | - | - | 38.200±0.141 | 53.480±1.692 | 40.355±1.277 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -41.340±0.659 | 58.303±0.457 | 58.663±1.468 | - | - | 43.416±1.284 |
| 12 H | -41.780±1.282 | 58.713±0.283 | 59.760±2.713 | - | - | 45.093±2.047 |
| 18 H | -41.780±0.985 | 58.237±0.045 | 58.963±1.021 | - | - | 44.492±0.770 |
| 24 H | -41.513±1.467 | 58.590±0.131 | 58.520±3.025 | - | - | 44.158±2.282 |
| 36 H | -42.157±2.637 | 58.327±0.172 | 56.203±1.722 | - | - | 42.410±1.300 |

Table S5. DSC data of G7 scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -41.907±2.258 | 66.090±0.338 | 79.947±2.445 | - | - | 64.069±2.612 |
| 6 H | -42.107±1.185 | 65.697±0.613 | 86.220±1.654 | - | - | 66.459±1.275 |
| 12 H | -41.437±1.236 | 65.190±0.889 | 81.897±2.705 | - | - | 63.126±2.085 |
| 18 H | -41.783±0.821 | 65.297±0.211 | 80.693±2.484 | - | - | 62.199±1.914 |
| 24 H | -41.517±1.311 | 65.047±0.110 | 81.360±0.255 | - | - | 62.712±0.197 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 39.333±0.556 | 51.273±1.367 | 39.522±1.054 |
| 6 H | - | - | - | 39.190±0.632 | 56.813±1.159 | 43.792±0.893 |
| 12 H | - | - | - | 38.300±0.377 | 53.837±1.790 | 41.497±1.380 |
| 18 H | - | - | - | 38.430±0.419 | 52.960±1.421 | 40.822±1.095 |
| 24 H | - | - | - | 38.500±0.556 | 54.777±1.601 | 42.222±1.234 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -42.073±1.427 | 57.987±0.335 | 56.763±1.504 | - | - | 44.796±1.278 |
| 6 H | -42.097±1.284 | 58.467±0.599 | 59.493±1.306 | - | - | 45.858±1.007 |
| 12 H | -41.420±1.127 | 58.383±0.784 | 57.043±1.836 | - | - | 43.969±1.415 |
| 18 H | -41.890±1.022 | 58.897±0.083 | 56.417±1.538 | - | - | 43.486±1.185 |
| 24 H | -41.740±0.674 | 58.117±1.042 | 57.883±2.205 | - | - | 44.617±1.700 |

Table S6. DSC data of GO1 scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -38.797±0.492 | 66.200±0.495 | 81.000±1.961 | - | - | 58.651±1.420 |
| 24 H | -42.380±1.396 | 66.337±0.639 | 80.777±2.241 | - | - | 58.489±1.623 |
| 48 H | -42.793±0.897 | 66.923±0.517 | 82.607±0.800 | - | - | 59.814±0.580 |
| 72 H | -42.760±0.615 | 66.553±0.214 | 83.703±1.936 | - | - | 60.608±1.402 |
| 96 H | -42.390±0.963 | 66.323±0.458 | 83.643±3.662 | - | - | 60.565±2.651 |
| 120 H | -42.747±0.240 | 66.243±0.602 | 82.280±2.212 | - | - | 59.578±1.601 |
| 144 H | -42.910±0.223 | 66.017±0.794 | 83.770±2.232 | - | - | 60.657±1.616 |
| 168 H | -42.163±1.121 | 65.807±0.118 | 87.427±2.614 | - | - | 63.304±1.893 |
| 192 H | -40.763±1.999 | 65.783±0.320 | 88.143±2.696 | - | - | 63.823±1.952 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 35.777±0.143 | 54.100±1.232 | 39.173±0.893 |
| 24 H | - | - | - | 36.063±0.577 | 53.220±0.763 | 38.536±0.552 |
| 48 H | - | - | - | 35.890±0.254 | 54.677±0.310 | 39.591±0.225 |
| 72 H | - | - | - | 36.360±0.502 | 55.007±0.516 | 39.830±0.374 |
| 96 H | - | - | - | 36.050±0.679 | 54.893±2.310 | 39.748±1.673 |
| 120 H | - | - | - | 36.800±1.742 | 54.203±0.686 | 39.248±0.497 |
| 144 H | - | - | - | 37.010±0.390 | 55.597±1.544 | 40.257±1.118 |
| 168 H | - | - | - | 36.983±0.200 | 57.367±1.752 | 41.538±1.269 |
| 192 H | - | - | - | 36.767±0.242 | 58.127±1.805 | 42.089±1.307 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -38.957±0.152 | 58.133±0.263 | 56.043±1.084 | - | - | 40.580±0.785 |
| 24 H | -42.863±1.114 | 58.210±0.653 | 55.343±1.255 | - | - | 40.073±0.909 |
| 48 H | -42.660±0.919 | 58.600±0.036 | 56.550±0.187 | - | - | 40.947±0.135 |
| 72 H | -42.530±0.859 | 58.067±0.378 | 57.187±1.488 | - | - | 41.408±1.078 |
| 96 H | -42.200±0.313 | 58.343±1.005 | 57.250±1.916 | - | - | 41.454±1.387 |
| 120 H | -42.797±0.078 | 58.367±1.175 | 56.993±2.771 | - | - | 41.268±2.006 |
| 144 H | -42.950±0.313 | 57.970±0.318 | 57.830±1.958 | - | - | 41.874±1.418 |
| 168 H | -42.750±0.219 | 57.420±0.511 | 60.473±2.049 | - | - | 43.788±1.483 |
| 192 H | -41.413±2.428 | 57.417±0.415 | 60.830±2.030 | - | - | 44.046±1.470 |

Table S7. DSC data of GO3 scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -41.153±1.907 | 66.533±0.512 | 81.517±1.479 | - | - | 60.242±1.093 |
| 24 H | -43.893±1.383 | 65.607±0.380 | 87.297±1.652 | - | - | 64.514±1.221 |
| 48 H | -43.937±1.319 | 66.123±0.511 | 86.147±0.987 | - | - | 63.664±0.729 |
| 72 H | -42.890±1.591 | 65.887±0.275 | 83.727±2.605 | - | - | 61.875±1.925 |
| 96 H | -42.927±0.424 | 65.623±0.316 | 83.377±1.420 | - | - | 61.617±1.050 |
| 120 H | -41.887±0.726 | 64.760±0.418 | 84.840±2.865 | - | - | 62.698±2.117 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 37.893±0.124 | 53.070±0.952 | 39.220±0.704 |
| 24 H | - | - | - | 38.173±0.769 | 56.170±1.278 | 41.511±0.945 |
| 48 H | - | - | - | 38.420±0.147 | 55.337±0.431 | 40.895±0.318 |
| 72 H | - | - | - | 38.887±0.291 | 53.697±2.169 | 39.683±1.603 |
| 96 H | - | - | - | 38.827±0.340 | 53.293±1.097 | 39.385±0.811 |
| 120 H | - | - | - | 39.230±0.775 | 54.747±1.740 | 40.459±1.286 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -41.793±1.656 | 57.720±0.462 | 57.143±0.832 | - | - | 42.230±0.615 |
| 24 H | -43.640±0.922 | 57.567±0.376 | 60.763±0.871 | - | - | 44.905±0.644 |
| 48 H | -43.750±1.164 | 57.837±0.352 | 60.130±0.767 | - | - | 44.437±0.567 |
| 72 H | -42.377±1.251 | 57.903±0.239 | 58.537±1.991 | - | - | 43.260±1.471 |
| 96 H | -44.117±1.209 | 57.403±0.170 | 58.407±0.637 |  |  | 43.163±0.471 |
| 120 H | -43.043±0.451 | 57.493±0.287 | 59.673±2.287 | - | - | 44.100±1.690 |

Table S8. DSC data of GO5 scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -40.443±2.249 | 66.013±0.090 | 81.800±1.302 | - | - | 61.724±0.983 |
| 12 H | -44.600±1.020 | 65.793±0.133 | 86.183±2.040 | - | - | 65.032±1.539 |
| 24 H | -42.073±0.809 | 65.393±0.210 | 85.460±2.792 | - | - | 64.486±2.106 |
| 48 H | -43.933±1.264 | 65.727±0.240 | 78.007±5.997 | - | - | 58.862±4.525 |
| 72 H | -43.330±1.640 | 65.560±0.370 | 83.313±1.650 | - | - | 62.866±1.245 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 38.893±0.384 | 52.470±1.055 | 39.593±0.796 |
| 12 H | - | - | - | 39.843±0.305 | 54.717±1.400 | 41.288±1.056 |
| 24 H | - | - | - | 40.047±0.204 | 54.317±1.847 | 40.986±1.394 |
| 48 H | - | - | - | 39.567±0.558 | 49.350±4.033 | 37.238±3.043 |
| 72 H | - | - | - | 40.227±0.172 | 52.893±0.881 | 39.912±0.665 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -42.193±1.136 | 57.797±0.159 | 57.547±0.790 | - | - | 43.423±0.596 |
| 12 H | -42.577±1.404 | 57.850±0.418 | 60.497±1.718 | - | - | 45.649±1.296 |
| 24 H | -41.763±1.108 | 57.700±0.248 | 60.220±2.096 | - | - | 45.440±1.582 |
| 48 H | -44.033±1.357 | 59.523±0.647 | 54.467±3.807 | - | - | 41.099±2.873 |
| 72 H | -43.187±1.655 | 57.103±0.356 | 58.860±1.290 | - | - | 44.414±0.974 |

Table S9. DSC data of GO7 scaffolds.

| Degradation time | Tg (℃) | Tm (℃) | ∆Hm (j/g) | Tc (℃) | ∆Hc (j/g) | χc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| First heating cycle |  |  |  |  |  |  |
| 0 H | -42.397±1.490 | 65.307±0.777 | 82.850±1.705 | - | - | 63.861±1.314 |
| 12 H | -42.197±1.312 | 66.423±0.407 | 82.387±1.707 | - | - | 63.504±1.316 |
| 24 H | -41.847±0.811 | 64.807±0.111 | 80.950±2.111 | - | - | 62.396±1.627 |
| 48 H | -43.787±1.487 | 65.077±0.265 | 77.037±6.026 | - | - | 59.380±4.645 |
| 72 H | -42.843±0.538 | 64.813±0.323 | 78.840±5.079 | - | - | 60.770±3.915 |
| Cooling cycle |  |  |  |  |  |  |
| 0 H | - | - | - | 39.467±0.221 | 51.873±1.432 | 39.984±1.104 |
| 12 H | - | - | - | 40.153±0.316 | 52.187±0.889 | 40.226±0.685 |
| 24 H | - | - | - | 39.847±0.162 | 50.960±1.650 | 39.280±1.272 |
| 48 H | - | - | - | 40.267±0.161 | 49.070±3.898 | 37.823±3.004 |
| 72 H | - | - | - | 40.390±0.596 | 50.230±3.668 | 38.717±2.827 |
| Second heating cycle |  |  |  |  |  |  |
| 0 H | -41.287±2.640 | 58.207±0.731 | 58.763±1.356 | - | - | 45.295±1.045 |
| 12 H | -42.383±1.267 | 57.853±0.104 | 58.010±1.097 | - | - | 44.714±0.845 |
| 24 H | -42.747±2.040 | 57.800±0.089 | 56.807±1.574 | - | - | 43.787±1.213 |
| 48 H | -42.187±1.582 | 57.700±0.193 | 54.787±4.162 | - | - | 42.230±3.208 |
| 72 H | -42.877±0.647 | 57.673±0.287 | 55.930±3.885 | - | - | 43.111±2.995 |