Appendix

Table A1 ePCMs prepared from suspension polymerization

| Core material |  | Shell | Latent heat (J/ | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Butyl stearate, Paraffin wax | Organic | Acrylate-based polymer | 63.98-93.97 | 29.08-32.12 | - | 500 | 210 | 10-80 | [134] |
| n-Octadecane | Organic | n-butyl methacrylate | 116.4-144.3 | 20.8-21.6 | - | 1000 | 249 | 1-46 | [48] |
| n-Octadecane | Organic | Styrene-divinylbenzene | 91-125 | 29 | - | - | 230 | 71-207 | [135] |
| Paraffin wax | Organic | Polystyrene, nonadecane, tetradecane | 41.6, 119.8, 48.9 | - | - | - | 120 | 38.01,10.48, 11.24 | [136] |
| n-Octadecane | Organic | Polybutyl methacrylate, Poly butyl acrylate | 96-112 | 29.1-33.1 | - | 1000 | 248 | 2-74 | [137] |
| n-Octadecane | Organic | n-octadecyl methacrylate-methacrylic acid | 46-93 | 21.0-22.1 | - | - | 236 | 0.5-4 | [138] |
| n-Octadecane | Organic | Butylene glycol diacrylate, divinyl benzene, trimethylolpropanetriacrylate, pentaerythritol tetraacrylate | 83.6-182.6 | 29.3-35.2 | - | - | 239 | 0.72-0.75 | [139] |
| Paraffin wax | Organic | Polystyrene | 102.42 | - | - | - | - | 4.80 | [140] |
| Paraffin wax | Organic | Polystyrene | 21.2-41.7 | 98-113 | - | - | - | 200 | [141] |
| n-Octadecane | Organic | Styrene-divinylbenzene | 126 | 29 | - | - | 230 | 80 | [142] |
| Paraffin wax | Organic | Styrene-methylmethacrylate | 87.50 | - | - | - | 325 | 380 | [143] |
| Rubitherm RT31 | Organic | Polystyrene | 75.7-135.3 | 31.56 | - | - | - | 4-53.2 | [45] |
| n-Octadecane | Organic | Polystyrene, styrene butylene glycol diacrylate, styrene divinylbenzene, styrene poly divinylbenzene | 22.0-156.9 | 24.34-30.84 | - | - | ≈200 | 50 | [144] |
| Rubitherm RT27 | Organic | Polystyrene | - | - | - | - | - | 500 | [49] |
| n-Octadecane | Organic | Poly divinylbenzene | 192 | 22.6 | - | - | - | 1.5 | [145] |
| n-Octadecane | Organic | Tripropylene glycol diacrylate | 104 | - | - | - | - | 0.3-0.6 | [146] |
| Na2HPO4.7H2O | Salt hydrate | Polymethylmethacrylate | 150 | 51 | - | - | - | 6.8 | [147] |

Table A2 ePCMs prepared from interfacial polymerization

| Core material | Core type | Shell | Latent heat (J/g) | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Paraffin wax | Organic Organic Organic Organic Organic Organic Organic Organic Organic Organic Organic Organic | Polyamide | 121.7 | 29-44 | - | - | - | 6.4 | [148] |
| n-Octadecane |  | Polyurea Polyurea Polyurea Polyurea Polyurea Polyurea Polyurea Polyurea | 110-117.5 | - | - | - | 167 | 5-10 | [149] |
| Butachlor |  |  | - | - | - | - | - | 1-20 | [150] |
| n-Eicosane |  |  | 29.34-63.55 | 35.7-36.5 | - | - | - | - | [151] |
| Insecticide |  |  | - | - | - | - | - | 30-40 | [152] |
| Octadecane |  |  | 62.6-112 | 29.5-30.8 | - | - | - | 1 | [153] |
| Migrin oil |  |  | - | - | - | - | - | 7.6-12.4 | [154] |
| n-Octadecane |  |  | - | - | - | - | - | 7.3 | [155] |
| n-Octadecane |  |  | 113.4-117.5 | 29.8-31.0 | - | - | - | 5-10 | [156] |
| Ovalbumin |  | Polyurea | - | - | - | - | - | 0.05-8.0 | [157] |
| Xylitol |  | Polyurethane-urea | 95.5-196.3 | - | - | - | 220 | 11.2-21.6 | [40] |
| Paraffin |  | Poly methyl methacrylate | - | 64.93 | - | - | - | 0.2-0.4 | [158] |
| Sodium phosphate dodecahydrate | Salt hydrate | Silica | 177 | 57.4 | 0.45-0.50 | 30 | 83.6 | - | [159] |

Table A3 ePCMs prepared from emulsion polymerization

| Core material | Core type | Shell | Latent heat (J/g) | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Capric/stearic acid | Organic | Poly methyl methacrylate (PMMA) | 51.98-116.25 | 20.20-21.03 | - | - | - | 1.3 | [160] |
| n-Hexadecane | Organic | PMMA | 68.89-145.61 | - | - | - | - | 0.22-1.05 | [161] |
| Paraffin wax | Organic | PMMA | 101 | 24-33 |  |  | 140-160 | 0.25 | [162] |
| Docosane | Organic | PMMA | 54.6 | 41 |  | 5000 | 120 | 0.14-0.446 | [163] |
| n-Nonadecane | Organic | PMMA | 139.20 | 31.23 | 0.18 | 5000 | 140 | 0.01-35 | [164] |
| n-Nonadecane | Organic | PMMA | 148.05 | 17.23 | - | - | - | 0.140-0.466 | [165] |
| n-Octacosane | Organic | PMMA | 86.4 | 50.6 | - | 5000 | 160 | 0.15-0.33 | [166] |
| n-Heptadecane, n-eicosane, n-nonadecane, n-octadecane, n-tetracosane | Organic | PMMA | 171.14-265.6 | 19.24-35.80 | 0.19-0.20 | 5000 | 120-180 | 0.01-100 | [167] |
| n-Heptadecane | Organic | PMMA | 81.5 | 18.4 | - | 5000 | 150 | 0.14-0.40 | [53] |
| n-Eicosane | Organic | PMMA | 84.2 | 35.2 | - | 5000 | - | 0.70 | [168] |
| Myristic acid+Palmitic acid | Organic | PMMA | 100.46 | 37.98 | - | 5000 | 250 | 0.1-300 | [169] |
| Stearic acid | Organic | PMMA | 50-73.5 | 60-89 | - | - | 290-347 | ≈0.117-0.420 | [170] |
| Paraffin wax, Palmitic acid | Organic | Polystyrene co-ethylacrylate | 49.03, 97.93 | 36.71, 59.12 |  |  |  | 0.166, 0.265 | [171] |
| n-Octadecane | Organic | Polystyrene | 6.48-49.76 | - | - | - | - | 0.08 | [172] |
| n-Tetracosane/n-Octadecane | Organic | Polystyrene | 156.39 | 25.96 | - | 5000 | 170 | 0.01-115 | [173] |

Table A4 ePCMs prepared from mini emulsion polymerization

| Core material | Core type | Shell | Latent heat (J/g) | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Paraffin wax | Organic | Polystyrene | 107.1 | 21-29.5 | - | 5000 |  | 0.1 | [174] |
| Paraffin wax | Organic | Polystyrene | - | - | - | - | - | 0.1 | [175] |
| n-Tetradecane | Organic | Polystyrene | 98.71 | 4.04 | - | 40 | - | 0.132 | [176] |
| n-Dotriacontane | Organic | Polystyrene | 174.8 | 70.9 | - | - | - | 0.1682 | [177] |
| n-Dodecanol | Organic | Styrene butyl acrylate | 90.5-109.2 | 25-27 | - | - | 151 | 0.1 | [178] |
| n-Hexadecane | Organic | Urea-formaldehyde | 114.6-143.7 | 16.15-16.36 | - | 1000 | - | 0.27 | [55] |
| n-Dodecanol | Organic | Poly methyl methacrylate | 98.8 | 18.2 | - | - | 161 | 0.150 | [56] |
| RT80 | Organic | Styrene butyl acrylate | 4.9-23.9 | 77.7-84.1 | - | 220 | - | 0.052-0.112 | [46] |
| Na2HPO4·10H2O | Salt hydrate | SiO2 | 58 | 32 | - | - | - | 0.29-1.050 | [179] |

Table A5 ePCMs prepared from In-situ polymerization

| Core material | Core type | Shell | Latent heat (J/g) | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| n-Docosane | Organic | Melamine formaldehyde (MFA) | 150 | - | - | - | - | 10 | [180] |
| Dodecanol | Organic | Polyethylene glycol-modified melamine formaldehyde | 118.9 | 25.8 | - | - | - | 0.83-14.4 | [181] |
| n-nonadecane, n-octadecane, n-eicosane | Organic | MFA | 161, 167, 172 | 219.3, 36.5, 45.3 |  |  |  | 0.3-6.4 | [182] |
| Decanoic acid | Organic | Polymelamine-urea-formaldehyde | 88 | 33 | - | - | 100-120 | 0.28 | [183] |
| n-Eicosane | Organic | MFA | 134.3 | 36.9 | - | - | 20 | 0.1-10 | [184] |
| n-Octadecane | Organic | MFA | 144 | 40.6 | - | - | 102-180 | 2.2 | [185] |
| n-Octadecane | Organic | MFA | 169-172 | 30.4-30.5 | - | - | 195 | 0.9 | [186] |
| n-Dodecanol | Organic | MFA | 187.5 | 21.5 | - | - | - | 23.2-30.6 | [187] |
| n-Octadecane | Organic | MFA | 160-170 | - | - | - | - | 1.0 | [188] |
| n-Hexadecane, n-Eicosane | Organic | MFA | 163-170 | - | - | - | - | 10 | [189] |
| Paraffin wax | Organic | Carboxymethyl cellulose modified melamine formaldehyde | 83.46 | - | - | - | - | 0.05 | [190] |
| Polythiol | Organic | Poly melamine formaldehyde | - | - | - | 100 |  | 1-10 | [191] |
| Paraffin wax | Organic | Aniline | 30-32 | 53.4 | - | 1000 |  | 0.3-0.5 | [192] |
| n-Octadecane | Organic | MFA | 102-166 | - | - | - |  | 1-2 | [193] |
| Paraffin wax | Organic | SiO2/Graphene oxide | 87.1-89.7 | 49.2-49.7 | - | 50 |  | 20 | [194] |
| n-hexadecane, n-Octadecane | Organic | MFA | 150-210 | - | - | - |  | 5-20 | [195] |
| n-Octadecane | Organic | MFA | 44-166 | 24.4 | - | - |  | 0.2-1.8 | [196] |
| n-Tetradecane | Organic | Urea/formaldehyde | 66.01-134.16 | 5.57-9.01 | - | - |  | 0.1 | [69] |
| n-Docosane | Organic | MFA | 17.74-57.81 | 55.69-56.72 | 0.081-0.116 | - |  | 5-20 | [197] |
| n-Docosane | Organic | MFA | - | - | - | - |  | 3.6 | [198] |
| Paraffin wax | Organic | MFA | 157 | 129.4 | - | - |  | 15 | [199] |
| n-Octadecane | Organic | MFA | 146.25 | 26.91 | - | - |  | 20 | [200] |
| Oleic acid | Organic | Ag2O+urea formaldehyde | 71.7 | 5.21 | 0.6347 | 1000 |  | 0.122 | [201] |
| Na2HPO4·12H2O | Salt hydrate | Methyl methacrylate and urea formaldehyde | 121.2 | 51.5 | 0.405 | - |  | 0.5 | [202] |
| MgNO3·6H2O | Salt hydrate | Ethyl-2-cyanoacrylate | 83.2 | 91 | - | 100 |  | 0.1-0.2 | [203] |
| Polyethylene glycol/Na2CO3·10H2O/n-hexadecane | Organic/inorganic | Polyurea-formaldehyde | 44.6 | 17.7 | - | - | - | 1-500 | [204] |

Table A6 ePCMs prepared from the sol-gel method

| Core material | Core type | Shell | Latent heat (J/g) | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| n-Octadecane | Organic | SiO2 | 22.03-87.46 | 23.34-23.84 | 0.874-0.904 |  | 202.5 | 2-4 | [38] |
| n-Eicosane | Organic | Fe3O4/SiO2 | 125.6-237.1 | 39.15-41.73 | - | - | 197 | 4-6 | [205] |
| Palmitic acid | Organic | SiO2 | 168.2-180.9 | 60.92-61.6 | 0.49-0.77 | 2500 | - | 0.155-0.949 | [206] |
| Palmitic acid | Organic | TiO2 | 63.3 | 61.7 | - | - | 203 | 0.2-0.4 | [78] |
| Lauric acid | Organic | SiO2 | 62.28-154.05 | 41.18-44.22 | - | 30 | - | - | [85] |
| n-Octadecane | Organic | Polymethyl methacrylate/SiO2 | 178.9 | - | - | - | - | 10 | [207] |
| Tris methyl aminomethane | Organic | SiO2 | 146 | 110-155 | 0.478 | - | - | 0.1-0.2 | [208] |
| n-Octadecane | Organic | SiO2 | 123-214.6 | 26.6-27.2 | 0.151-0.621 | - | - | 7-16 | [33] |
| Paraffin RT 28 | Organic | SiO2/Expended graphite | 112.8, 104.4 | 27.53, 27.72 | 0.162,0.246 | - | - | 5-20,1-5 | [209] |
| Paraffin | Organic | SiO2 | 156.86 | 57.96 | - | - | - | 40-60 | [59] |
| Paraffin | Organic | SiO2 | 115.07 | 55.66 | - | 100 | - | 0.265 | [41] |
| n-Eicosane | Organic | TiO2 | 97.60-195.60 | 41.47-43.88 | 0.749-0.865 | - | - | 1.5-2 | [210] |
| Paraffin | Organic | SiO2 | 130.8-165.7 | 57.84-58.37 | - | - | 200 | 8-15 | [34] |
| Stearic acid | Organic | SiO2 | 162.0-171.0 | 52.6-53.5 | - | - | 150 | 20-30 | [211] |
| Paraffin | Organic | TiO2 | 161.1 | 58.8 | - | - | 200 | - | [35] |
| Paraffin | Organic | TiO2 | 73.47 | 56.5 | - | 100 | 190 | 0.238 | [79] |
| Stearic acid | Organic | TiO2 | 123.96 | 54.35-55.04 | 0.42-0.52 | 2500 | - | 0.58-0.94 | [80] |
| n-Pentadecane | Organic | SiO2 | 46.4-55.8 | - | - | - | - | 4-8 | [212] |
| Paraffin | Organic | SiO2 -TiO2 | 93.7 | 29 | - | 1000 | - | 11 | [213] |
| Tin | Metallic | SiO2 | 48 | 228.3 | - | 20 | - | 0.055-0.105 | [214] |
| Indium | Metallic | SiO2 | 19.6 | 155.3 | - | 100 | - | 0.2 | [215] |
| Na2SO4·10H2O | Salt hydrate | SiO2 | 180.7 | - | - | - | - | 0.120 | [216] |
| Na2SO4 | Salt hydrate | SiO2 | 170.6 | 887.91 | 0.59-0.87 | 50 | - | ≈0.280 | [217] |
| Lauric acid | Organic | SiO2 | 160.0 | 38.8 | - | 3000 | 170 | 0.357 | [218] |
| Paraffin | Organic | SiO2 | 115.07 | 55.66 | - | 100 | - | 0.265 | [219] |
| Lauric acid | Organic | SiO2 | 165.6 | 36.7 | - | 1200 | 170 | 0.340 | [43] |
| Palmitic acid | Organic | SiO2 | 109.9 | 62.9 | - | 100 | 220 | 0.474 | [81] |
| Paraffin | Organic | SiO2 | 72.88 | 38.73 | - | - | 200 | - | [220] |
| Stearic acid | Organic | SiO2 | 182.53 | 70.37 | - | 30 | 190 | 10-20 | [84] |
| Paraffin | Organic | SiO2 | 80.8 | 57.4 | - | - | - | 5.386 | [221] |
| Paraffin | Organic | TiO2 | 107.54 | 60.41 | - | - | 250.2 | 2-5 | [222] |
| Myristic acid | Organic | TiO2 | 96.64 | 56.95 | - | - | 240 | 0.5 | [223] |
| n-Octadecane | Organic | TiO2 | 31.52-42.57 | 25.61-26.09 | - | 100 | 150 | 2-5 | [74] |
| Stearic acid | Organic | TiO2 | 131.5 | 68.61 | - | 3 | 200 | >5 | [224] |
| Stearic acid | Organic | SiO2 | 66.4 | 67.25 | - | - | - | 0.35 | [225] |
| Palmitic acid | Organic | SiO2 | 34.5 | 64.8 | - | - | 210 | 1.2 | [75] |
| Capric acid | Organic | TiO2 | 88.8 | 31.1 | - | 50 | 160 | - | [76] |
| Myristic acid | Organic | SiO2 | 114.46 | 54.81 | - | 50 | 150 | 0.597 | [77] |

Table A7 ePCMs prepared from the coacervation method

| Core material | Core type | Shell | Latent heat (J/g) | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Coco-fatty acid | Organic | Gelatin and gum arabic | - | 29-31 | - | - | - | 1000 | [226] |
| Paraffin wax | Organic | Gelatin and gum arabic | 20-90 | - | - | - | - | 50-100 | [227] |
| Rubitherm RT 27 | Organic | Sterilized gelatine/arabic gum, agar agar/arabic gum | 79, 78 | 298.3-301.3, 299.5-302.5 | - | - | - | 9,12 | [228] |
| Paraffin wax | Organic | Gelatin and gum arabic | 193.4-239.7 | - | - | - | - | - | [15] |
| Octanic acid | Organic | Urea-formaldehyde, MFA, urea+ MFA | 16.48-93.95 | 6.23-13.91 | - | - | - | 0.2-1.5 | [229] |
| n-Tetradecane | Organic | Gelatin | 192 | 5.30 | - | - | - | 90-125 | [230] |
| Eicosane | Organic | MFA | 134.3 | 36.9 | - | - | - | 1.89 0.1-10 | [184] |
| Paraffin wax | Organic | Gelatin and gum arabic | 20-90 | - | - | 1000 | - | 50-100 | [63] |
| n-octadecane,n-Hexadecane | Organic | Gelatin-gum arabic mixture | 19.70-165.80 | 11-38 | - | - | - | - | [231] |

Table A8 ePCMs prepared from spray drying method

| Core material | Core type | Shell | Latent heat (J/g) | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Poppyseed oil | Organic | Gelatin and gum arabic | - | 185 | - | - | - | ≈5 | [232] |
| Rubitherm RT 27 | Organic | Low-density polyethylene, ethyl vinyl acetate | 98.1 | 28.40 | - | 3000 | - | 3.9 | [233] |
| n-octadecane | Organic | TiO2 | 92-97 | 28.7 | - | - | - | 0.1-5.0 | [64] |
| Flaxseed oil | Organic | Gum arabic | - | - | - | - | - | ≈23 | [234] |

Table A9 ePCMs prepared from some other less common methods

| Core material | Core type | Shell | Latent heat (J/g) | Melting Temperature (°C) | Thermal conductivity | Thermal Cycles | Thermal Stability (°C) | Size (µm) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al | Metallic Metallic Metallic Metallic Metallic Metallic Metallic Metallic Metallic Metallic Metallic | Al2O3–C | 266 | 660.3 | 8 | 20 | - | ≈20-50 | [235] |
| Al-Si |  | Al2O3 | 271.9-303.2 | ≈570-580 | - | 20 | - | ≈100 | [236] |
| Al |  | Al2O3 | 273-301 | 661-660 | - | 100 | - | ≈36 | [237] |
| Al |  | Al2O3 | 237-298 | 578-579 | - | 100 | - | ≈29-44 | [238] |
| Al |  | Al2O3 | 233 | 579 | - | 300 | - | 37.3 | [239] |
| Sn-Pb |  | SnO2 | 27.48–44.62 | 184.1-284.5 | - | - | - | - | [240] |
| Sn |  | Al2O3 | 54.49 | 229.1 | 35 | 100 | - | 0.06-2 | [241] |
| Sn |  | SnO2 | 53 | 232 | 4.2 | 100 | - | - | [242] |
| Al-Si |  | Al2O3 | 108-122 | 577 | 2.16–3.20 | 300 | - | 10-40 | [243] |
| Zn-Al |  | ZnO/Al2O3 | 117 | 437–512 | - | 100 | - | - | [244] |
| Al |  | Al2O3 | 180 | 660 | - | - | - | - | [245] |
| n-octadecane | Organic | SiO2/Polydopamine/Ag | 26.13-71.95 | 27.73 | 1.346 | 100 | 15-230 | - | [97] |
| Na2SO4·10H2O | Salt hydrate Salt hydrate Salt hydrate Salt hydrate Salt hydrate | SiO2 | 38.6 | 27.3 | - | - |  | 2-3 | [246] |
| Na2HPO4·12H2O |  | SiO2 | 69.3 | 36.6 | - | - |  | 2-3 | [246] |
| Sodium phosphate dodecahydrate |  | Cellulose acetate butyrate/Methylene diisocyanate | 140 | 133 | - | - | - | 3 | [247, 248] |
| Mg(NO3)2·6H2O |  | SiO2 | 112.8 | - | 1.4 | 500 | 200 | 0.3-1.0 | [249] |
| MgCl2.6H2O |  | Acrylic | 118.3 | 95.3 | - | - | - | - | [250] |