Interfacial robustness of commercial amine-based inhibitors mitigates under-deposit corrosion of carbon steel in simulated sour conditions: A merged electrochemical and machine learning study

Eman M. Fayyad1, Adewale K. Ipadeola1*, Mostafa H. Sliem1, Dana Abdeen2, Noora Al-Qahtani1, Ashwin RajKumar3, Joel Jeffrey3, Phaneendra K. Yalavarthy3, Aboubakr M. Abdullah1*

1 Center for Advanced Materials, Qatar University, Doha 2713, Qatar

2 Qatar Shell Research and Technology Centre, P.O. Box 3747, Doha, Qatar

3 Department of Computational and Data Sciences (CDS), Indian Institute of Science (IISc),

Bangalore, India.

*Corresponding author: ak.ipadeola@qu.edu.qa; bakr@qu.edu.qa

Fig. S1 (a) Plots of Rct vs. concentration of corrosion inhibitors and (b) Corrosion rates vs. concentration of corrosion inhibitors in sour conditions, 60oC and 1000 rpm

Table S1 EIS parameters obtained for pristine CS, CS/CR1 and CS/CR2 in sour electrolyte (3.5 wt. % NaCl + 1000 ppm Na2S + CO2 purging) at 1000 rpm, 60oC and different inhibitors’ concentrations (Cinh)

| Samples’ name | Cinh (ppm) | Rf (Ω.cm2) |  | CPEf |  | Rct (Ω.cm2) | CPEdl |  | Cdl (µF.cm-2) | Corrosion rate (mmpy) | θ | I.E. (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Yf (µS.sn cm-2) | nf |  | Ydl x 10-6 (µS.sn cm-2) | ndl |  |  |  |  |
| CS (blank) | --- | --- |  | --- | --- | 915 | 194 | 0.57 | 52.6 | 0.3306 | --- | --- |
| CS/CR1 | 5 | 1477 |  | 15.7 | 0.50 | 4980 | 337.0 | 0.66 | 440 | 0.0608 | 0.816 | 81.6 |
|  | 25 | 4633 |  | 15.5 | 0.90 | 9915 | 163.0 | 0.80 | 183 | 0.0305 | 0.908 | 90.8 |
|  | 50 |  | 6500 | 15.0 | 0.93 | 33500 | 82.2 | 0.90 | 91.9 | 0.0090 | 0.973 | 97.3 |
|  | 100 | 1980 |  | 31.9 | 0.97 | 27280 | 118.6 | 0.70 | 196 | 0.0111 | 0.966 | 96.6 |
|  | 200 | 1499 |  | 43.0 | 0.92 | 18000 | 164.5 | 0.69 | 267 | 0.0168 | 0.949 | 94.9 |
|  | 300 | 1055 |  | 64.3 | 0.81 | 13660 | 155.5 | 0.63 | 242 | 0.0221 | 0.933 | 93.3 |
|  | 400 | 980 |  | 100.0 | 0.70 | 9650 | 245.0 | 0.55 | 495 | 0.0314 | 0.905 | 90.5 |
| CS/CR2 | 5 | 940 |  | 22.6 | 1.00 | 3900 | 128.0 | 0.90 | 118 | 0.0776 | 0.765 | 76.5 |
|  | 25 | 1179 |  | 17.8 | 0.80 | 5660 | 33.0 | 0.92 | 28.5 | 0.0535 | 0.838 | 83.8 |
|  | 50 | 2460 |  | 10.4 | 1.00 | 8400 | 9.0 | 0.88 | 6.32 | 0.0360 | 0.891 | 89.1 |
|  | 100 | 3170 |  | 25.5 | 0.73 | 14000 | 23.0 | 0.88 | 19.7 | 0.0216 | 0.935 | 93.5 |
|  | 200 | 4460 |  | 3.8 | 0.58 | 18700 | 4.1 | 0.99 | 3.99 | 0.0162 | 0.951 | 95.1 |
|  | 300 | 1050 |  | 52.7 | 1.00 | 13500 | 27.9 | 0.95 | 26.5 | 0.0224 | 0.932 | 93.2 |
|  | 400 | 750 |  | 66.0 | 0.72 | 11800 | 29.7 | 0.89 | 26.1 | 0.0256 | 0.922 | 92.2 |

Table S2 PDP parameters of pristine CS, CS/CR1 and CS/CR2 in sour electrolyte (3.5 wt. % NaCl + 1000 ppm Na2S + CO2 purging) at 1000 rpm, 60oC and different inhibitors’ concentrations (0 – 400 ppm)

| Samples | Conc. (ppm) | Ecorr (mV) | icorr (µAcm−2) |  | ba (V/decade) | bc (V/decade) | I.E. (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CS (blank) | 0 | -677 | 147 | 0.065 |  | 0.414 | --- |
| CS/CR1 | 5 | -654 | 24.5 | 0.056 |  | 0.168 | 83.3 |
|  | 25 | -635 | 12.0 | 0.056 |  | 0.120 | 91.8 |
|  | 50 | -604 | 2.60 | 0.032 |  | 0.116 | 98.2 |
|  | 100 | -612 | 5.00 | 0.042 |  | 0.113 | 96.6 |
|  | 200 | -610 | 8.80 | 0.059 |  | 0.148 | 94.0 |
|  | 300 | -621 | 11.0 | 0.051 |  | 0.144 | 92.5 |
|  | 400 | -633 | 15.0 | 0.058 |  | 0.146 | 89.8 |
| CS/CR2 | 5 | -671 | 35.0 | 0.090 |  | 0.180 | 76.2 |
|  | 25 | -659 | 25.0 | 0.040 |  | 0.170 | 82.9 |
|  | 50 | -647 | 12.0 | 0.058 |  | 0.142 | 91.8 |
|  | 100 | -619 | 9.60 | 0.026 |  | 0.154 | 93.5 |
|  | 200 | -610 | 6.20 | 0.013 |  | 0.131 | 95.8 |
|  | 300 | -634 | 10.7 | 0.059 |  | 0.150 | 92.7 |
|  | 400 | -637 | 12.2 | 0.069 |  | 0.110 | 91.7 |

Table S3 PDP parameters of CS/SiO2(partial)/CR1, CS/SiO2(partial)/CR2, CS/SiO2(full)/CR1 and CS/SiO2(full)/CR2 in the electrolyte (3.5 wt. % NaCl + 1000 ppm Na2S + CO2 purging) at 1000 rpm, 60oC and optimized inhibitors’ concentrations (i.e., CR1 (50 ppm) and CR2 (200 ppm))

| Samples | Time (h) | Ecorr (V) | icorr (µA.cm−2) | ba (V/decade) | bc (V/decade) | IE (%) |
| --- | --- | --- | --- | --- | --- | --- |
| CS/SiO2(partial)/CR1 | 0 | -0.715 | 37.0 | 0.055 | 0.276 | 74.8 |
|  | 6 | -0.669 | 22.5 | 0.037 | 0.095 | 84.7 |
|  | 12 | -0.617 | 9.80 | 0.033 | 0.079 | 93.3 |
|  | 24 | -0.627 | 13.5 | 0.031 | 0.056 | 90.8 |
| CS/SiO2(partial)/CR2 | 0 | -0.737 | 42.5 | 0.130 | 0.524 | 71.1 |
|  | 6 | -0.713 | 32.5 | 0.027 | 0.045 | 77.9 |
|  | 12 | -0.682 | 16.0 | 0.043 | 0.048 | 89.1 |
|  | 24 | -0.638 | 7.90 | 0.010 | 0.025 | 94.6 |
| CS/SiO2(full)/CR1 | 0 | -0.735 | 65.0 | 0.052 | 0. 307 | 55.8 |
|  | 6 | -0.723 | 46.3 | 0.033 | 0.021 | 68.5 |
|  | 12 | -0.695 | 24.3 | 0.016 | 0.048 | 83.5 |
|  | 24 | -0.666 | 33.0 | 0.089 | 0.114 | 77.6 |
| CS/SiO2(full)/CR2 | 0 | -0.718 | 52.5 | 0.089 | 0.211 | 64.4 |
|  | 6 | -0.681 | 35.8 | 0.078 | 0.131 | 75.6 |
|  | 12 | -0.668 | 18.7 | 0.038 | 0.147 | 87.3 |
|  | 24 | -0.643 | 12.0 | 0.106 | 0.062 | 91.8 |

Fig. S2 EDX spectra of (a) CS/CR1, (b) CS/CR2, (c) CS/SiO2/CR1 and (d) CS/SiO2/CR2 after electrochemical corrosion tests for 24 h in sour electrolyte

Table S4 EDX compositions of inhibited CS with and without SiO2 deposit after 24 h electrochemical corrosion tests

| Elements | CS/CR1 | CS/CR2 | CS/SiO2/CR1 | CS/SiO2/CR2 |
| --- | --- | --- | --- | --- |
| C (wt.%) | 15.20 ± 0.98 | 15.90 ± 1.12 | 18.90 ± 2.10 | 17.20 ± 2.62 |
| O (wt.%) | 22.50 ± 0.07 | 23.20 ± 0.14 | 23.10 ± 0.42 | 24.50 ± 0.80 |
| Na (wt.%) | 3.90 ± 1.70 | 4.90 ± 2.35 | 14.50 ± 2.96 | 11.40 ± 1.15 |
| S (wt.%) | 5.80 ± 0.08 | 5.70 ± 0.08 | 2.07 ± 0.03 | 2.00 ± 0.03 |
| N (wt.%) | 25.40 ± 0.05 | 23.20 ± 0.05 | 8.37 ± 0.04 | 12.30 ± 0.04 |
| P (wt.%) | 14.50 ± 0.07 | 12.60 ± 0.04 | 3.36 ± 0.05 | 5.30 ± 0.04 |
| Fe (wt.%) | 12.70 ± 1.57 | 14.50 ± 1.32 | 18.80 ± 0.17 | 16.70 ± 0.05 |
| Si (wt.%) | - | - | 2.07 ± 0.03 | 10.60 ± 0.51 |

Fig. S3 (a) XPS wide scan and deconvoluted S 2p spectra of (b) CS, and CS/SiO2, and (c) CS/CR1, CS/CR2, CS/SiO2/CR1, and CS/SiO2/CR2 after electrochemical corrosion tests for 24 h in sour electrolyte

Table S5: The Feature importance based on Linear Regression analysis

| Features | Coefficient | p-value |  | Significant (p < 0.05) |
| --- | --- | --- | --- | --- |
| const | 42.956842 | 0.00 |  | True |
| EIS | 18.568218 | 0.00 | True |  |
| PDP | 24.388625 | 0.00 |  | True |
| Time | 1.190687 | 0.00 |  | True |
| SiO2 deposit | -32.765892 | 0.00 |  | True |
| CR1 | 23.096244 | 0.00 |  | True |
| CR2 | 19.860598 | 0.00 |  | True |
| Concentration | 0.026079 | 0.09 |  | False |

Table S6: Re-fitted performance metrics for the models using Pinh as the target output variable

| Models | Train R2 | Test R2 | Train RMSE | Test RMSE | Train MAE | Test MAE |
| --- | --- | --- | --- | --- | --- | --- |
| XGBoost | 1.00 | 0.94 | 0.0 | 0.6 | 0.0 | 0.6 |
| Gradient Boosting | 0.97 | 0.92 | 0.7 | 0.7 | 0.5 | 0.7 |
| Random Forest | 0.97 | 0.90 | 0.6 | 0.8 | 0.5 | 0.6 |
| Decision Tree | 1.00 | 0.77 | 0.0 | 1.3 | 0.0 | 1.1 |
| Linear Regression | 0.58 | 0.44 | 2.3 | 2.0 | 1.9 | 1.6 |
| KNN | 0.48 | 0.23 | 2.6 | 2.3 | 2.0 | 1.7 |

Fig. S4 (a) Linear Regression Coefficients and their statistical significance, (b) Random Forest Feature Importance, (c) XGBoost Feature Importance, (d) SHAP Feature Importance for Random Forest; and (e) SHAP Feature Importance for XGBoost