# Development of magnetic solid phase micro-extraction (MSPE) method for the extraction and preconcentration of the selected β-blockers

Online Resource 1 List of runs obtained using fractional factorial design (FFD) and the corresponding percentage extraction recoveries (%ER)

| Runs | MA (mg) | pH | ET (min) | DT (min) | EV (µL) | ACE (%ER) | MET (%ER) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 10 | 3 | 5 | 15 | 1000 | 5.5 | 5.2 |
| 2 | 60 | 3 | 5 | 5 | 100 | 20.6 | 14.8 |
| 3 | 10 | 9 | 5 | 5 | 1000 | 37.5 | 36.1 |
| 4 | 60 | 9 | 5 | 15 | 100 | 82.1 | 76.2 |
| 5 | 10 | 3 | 20 | 15 | 100 | 2.6 | 2.3 |
| 6 | 60 | 3 | 20 | 5 | 1000 | 26.1 | 20.9 |
| 7 | 10 | 9 | 20 | 5 | 100 | 67.9 | 64.1 |
| 8 | 60 | 9 | 20 | 15 | 1000 | 82.8 | 81.8 |
| 9 (C) | 35 | 6 | 12.5 | 10 | 550 | 90.8 | 62.6 |
| 10 (C) | 35 | 6 | 12.5 | 10 | 550 | 90.4 | 68.2 |
| 11 (C) | 35 | 6 | 12.5 | 10 | 550 | 87.8 | 69.3 |

Online Resource 2 Factors and their corresponding levels used in CCD for optimization

| Variables | -α | Low level (-1) | Central point (0) | High level (+1) | +α |
| --- | --- | --- | --- | --- | --- |
| Mass of adsorbent (mg) | 0.31 | 10 | 35 | 60 | 70.26 |
| pH | 1.76 | 3 | 6 | 9 | 10.24 |

Online Resource 3 List of runs obtained using central composite design (CCD) and the corresponding percentage extraction recoveries (%ER)

| Standard Run | pH | MA | ACE (%R) | MET (%R) |
| --- | --- | --- | --- | --- |
| 1 | 3.0 | 10.0 | 22.8 | 33.4 |
| 2 | 3.0 | 60.0 | 32.9 | 36.7 |
| 3 | 9.0 | 10.0 | 71.5 | 73.1 |
| 4 | 9.0 | 60.0 | 99.4 | 98.7 |
| 5 | 2.6 | 35.0 | 13.3 | 17.1 |
| 6 | 9.4 | 35.0 | 98.9 | 97.7 |
| 7 | 6.0 | 6.3 | 41.6 | 45.1 |
| 8 | 6.0 | 63.7 | 77.3 | 75.8 |
| 9 (C) | 6.0 | 35.0 | 69.3 | 71.2 |
| 10 (C) | 6.0 | 35.0 | 69.0 | 70.9 |
| 11 (C) | 6.0 | 35.0 | 69.4 | 71.3 |

Online Resource 4 Equations of adsorption isotherm models

| Models | Equations |
| --- | --- |
| Langmuir isotherm | CeQe= 1Qm KL+1QmCe RL= 11+ KLCo |
| Freundlich isotherm | lnQe= lnKF + 1nlnCe |
| Dubunin-Radushkevich isotherm | lnQe= lnQD-R -βƐ2 Ɛ = RTln(1+ 1Ce) E=1√2β |
| Sips isotherm | ln(QeQmax-Qe)= 1nlnCe+lnKs |

Where Qe (mg g­1) denotes maximum adsorption capacity of β blockers per unit mass of the adsorbent; KL (L mg­1) represents Langmuir constant related to the rate of adsorption; RL represents dimensionless Langmuir constant; n and KF ((mg g­1) (L mg­1)1/n are Freundlich constants which provide information about the adsorption intensity and adsorption capacity, respectively; β (mol2 J−2), Ɛ and QD-R(mg g­1) represent adsorption energy constant, Polanyi potential and theoretical monolayer adsorption capacity, respectively; T (K) and R (8.314 J mol−1 K−1) and T (K) are temperature and gas constant, respectively; E (kJ mol­1) represents adsorption mean free energy; Ks (1/mg) is Sips equilibrium constant, βR-P denotes exponent that lies between 0 and 1 and A is R-P isotherm constant.

Online Resource 5 Nitrogen adsorption-desorption isotherms of (a) Fe3O4, (b) NH2-MIL-101(Cr) and (c) Fe3O4@NH2-MIL-101(Cr)

Online Resource 6 Point of zero charge of the Fe3O4@NH2-MIL-101(Cr)

Online Resource 7 Desirability profile of MET confirming the optimum conditions

Online Resource 8 Adsorption isotherm data fitted to Langmuir model, (a) ACE and (b) MET

Online Resource 9 Adsorption isotherm data fitted to Freundlich model, (a) ACE and (b) MET

Online Resource 10 Adsorption isotherm data fitted to Dubinin-Radushkevich model, (a) ACE and (b) MET

Online Resource 11 Adsorption isotherm data fitted to Sips model (a) ACE and (b) MET