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[bookmark: _GoBack]Fig. S1 SEM images showing (a & b) the side and top views of scaffold 1, and (c & d) the side and top views of scaffold 3 prepared using the 3DP/TIPS method 
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Scaffold 1:
3DP/TIPS
PLGA: 12%
nHA: 40%

Scaffold 3:
3DP/TIPS
PLGA: 8%
nHA: 40%





