Practical Analysis of Nanosecond Water-Jet Guided Laser Wood Machining

Doumbia Bakary S.1, 2, 3,* Yang Chunmei1, 2,*, Ma Yan2, Liu Qingwei1, 2, and Qu Wen1, 2 , Liu Jiuqing1, 2

1Northeast Forestry University, College of Mechanical and Electrical Engineering, Harbin, 150040, China; 2Forestry and Woodworking Machinery Engineering Technology Center, Northeast Forestry University, Harbin 150040, China; 3University of Science Technical and Technology of Bamako (USTTB), Faculty of Sciences and Technology (FAST), Bamako 423, Mali; * Corresponding authors: doumbak_01@yahoo.fr.

- Abstract

Water jet assisted laser machining is an advanced and eco-friendly technique suitable for efficient and precise processing of wood and wooden part. In the paper entitled “Experimental and Theoretical Modeling of Nanosecond Water Jet Guided Laser Machining for Different Wood Specimens, ”the investigation takes into account the process analysis and practical application of laminated object manufacturing (LOM) nanosecond water-jet guided laser (NWJGL) for machining different wood types. The workpiece includes Korean pine and Northeast China ash wood of 3 mm thickness with a water content of 7.21 % and 7.13 % each, machined under different laser power and cutting speeds. These process parameters and influences on woodcut surface geometry were experimentally analyzed using scanning electron microscopy (SEM) and Analysis Of Variance (NOVA) with the Origin software, the experiment and parameters interaction and influence on the workpiece are reported.

- Introduction

In nanosecond water-jet-guided (NWJG) laser wood machining, the water-jet guides the laser beam during the process. Therefore, a pulsed Nd: YAG laser can be water-jet assisted to machine a wide range of materials, namely, ceramics, plastics, wood, and composites, with outstanding results[1]. However, NWJG Nd: YAG laser system for thin wood laser cutting is a novel development prospect for wood machining in the industry. The process is illustrated in Figure 1. The water jet flows co-axially with a laser beam through an annular nozzle. The water cooling affects the cut kerf, cleaning the excess heat and the debris [1]. When applied for wood laser-cutting, it has been reported that water reduces the surface roughness, decreases the kerf width, and increases the cutting speed [2][3][4]. Besides its numerous advantages, the selected NWJGL technology can process objects at 45° to the standard object orientation.

Figure 1. Nanosecond water-jet-guided laser woodworking setup.

  - Parametrical Characterizations

NWJGL wood machining is a complex process that considers mechanical and thermal actions. Therefore, numerous factors from different equipment and workpiece may be influencing the process. An illustration of these sources and factors is shown in Figure 2.

Figure 2. Parametrical characterization of NWJGL wood machining.

The mechanism of the water-jet equipment is an auxiliary processing phase of the NWJGL system in influencing consideration factors. Water is continuously sprayed on the cut area during the process, so the moisture content in the proceeded wood is ignored. Besides, the other thermophysical properties of the selected wood workpiece, namely, Korean pine and Northeast China ash wood, were constant. The beam’s wavelength and pulse width were also fixed for a nanosecond laser beam source. The considered parameters include laser power and cutting speed, jet feed speed, water pressure, Nozzle size, and wood thickness. Therefore, as shown in Table 1, the two wood types were machined under different machining conditions. The influence of laser power, cutting speed, and their interaction on kerf width was investigated herein via experiment analysis. The control variable method was used based on the numerical relationship between laser power, cutting speed, and kerf width. Five direct measurements of the cut kerf width were carried out for each selected value of laser power and cutting speed.

Table 1. Nanosecond water-jet guided wood machining conditions.

| Test conditions | Laser power (W) | Cutting speed (mm/s) | Pulse frequency (Hz) |  |
| --- | --- | --- | --- | --- |
| M1 | Constant (fixed at 8 W) | 1.57 mm/s, 2.35 mm/s, 3.62 mm/s, 4.68 mm/s, 5.34 mm/s and 6.26 mm/s | 15 Hz |
| M2 | 2 W, 4 W, 6 W, 8 W, 10 W and 10 W | Constant (fixed at 2.36 mm/s) | 15 Hz |

M1: Korean pine and Northeast China ash specimen of 3 mm machined under experimental conditions of different laser cutting speeds of 1.57 mm/s, 3.62 mm/s, 4.68 mm/s and 6.26mm/s, pulse frequency of 15Hz, at a fixed laser power of the nanosecond water-guided laser system of 8 W.

M2: Korean pine and Northeast China ash specimen of 3 mm machined under experimental conditions of different laser power of 2 W, 4 W, 6 W, 8 W, 10 W and 12 W, pulse frequency of 15Hz, at a fixed laser cutting speed of the nanosecond water-guided laser system of 2.36 mm/s.

- Result of Experiment Analysis

Considering the experimental conditions in Table 1, a practical test was carried out using the NWJGL equipment to machine Korean pine and the Northeast China ash wood specimens of 3 mm thickness. The experimental data of the kerf width of these workpieces and the difference between them are reported and analyzed.

  - Appendix A

Using the experimental data (Table 2) of the kerf width of the Korean pine and the Northeast China ash at a constant material’s properties and fixed laser cutting speed of 2.36 mm/s under different values of laser powers (condition M2), a One-Way ANOVA was carried out with NWJG laser power as the single independent variable.

The means comparison test using the Tukey test for Korean pine and Northeast China ash kerf width is reported in Table 3 and Figure 3.

Table 2. The kerf width data of the Korean pine and the Northeast China ash under M2.

| Kerf width of the Korean pine (Pinus Koraiensis) (mm) |  |  |  |  |  | Kerf width data of Northeast China ash (Fraxinus mandshurica) (mm) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P2 | P4 | P6 | P8 | P10 | P12 | A2 | A4 | A6 | A8 | A10 | A12 |
| 0.64 | 0.71 | 0.78 | 0.83 | 0.89 | 0.93 | 0.53 | 0.56 | 0.62 | 0.71 | 0.79 | 0.83 |
| 0.63 | 0.70 | 0.79 | 0.85 | 0.91 | 0.97 | 0.52 | 0.59 | 0.61 | 0.69 | 0.81 | 0.86 |
| 0.66 | 0.73 | 0.77 | 0.88 | 0.93 | 0.95 | 0.54 | 0.58 | 0.64 | 0.72 | 0.78 | 0.85 |
| 0.69 | 0.71 | 0.81 | 0.84 | 0.96 | 0.98 | 0.52 | 0.60 | 0.61 | 0.68 | 0.82 | 0.89 |
| 0.67 | 0.74 | 0.80 | 0.86 | 0.89 | 1.12 | 0.56 | 0.57 | 0.63 | 0.73 | 0.76 | 0.91 |

Pk and Ak are the kerf width data of Korean pine and Northeast China ash at different laser power, where k takes the values of 2 W, 4 W, 6 W, 8 W, 10 W, and 12 W.

Figure 3. Kerf width box charts of Korean pine and Northeast China ash under M2.

Table 3. Means comparison (Tukey Test) under M2.

|  | MeanDiff | SEM | q Value | Prob | Alpha | Sig | LCL | UCL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P4 P2 | 0.06 | 0.01889 | 4.49089 | 0.09426 | 0.05 | 0 | -0.00488 | 0.12488 |
| P6 P2 | 0.132 | 0.01889 | 9.87995 | 5.70591E-7 | 0.05 | 1 | 0.06712 | 0.19688 |
| P6 P4 | 0.072 | 0.01889 | 5.38906 | 0.01812 | 0.05 | 1 | 0.00712 | 0.13688 |
| P8 P2 | 0.194 | 0.01889 | 14.52054 | 0 | 0.05 | 1 | 0.12912 | 0.25888 |
| P8 P4 | 0.134 | 0.01889 | 10.02965 | 4.18674E-7 | 0.05 | 1 | 0.06912 | 0.19888 |
| P8 P6 | 0.062 | 0.01889 | 4.64058 | 0.07317 | 0.05 | 0 | -0.00288 | 0.12688 |
| P10 P2 | 0.258 | 0.01889 | 19.31081 | 1.74159E-8 | 0.05 | 1 | 0.19312 | 0.32288 |
| P10 P4 | 0.198 | 0.01889 | 14.81993 | 0 | 0.05 | 1 | 0.13312 | 0.26288 |
| P10 P6 | 0.126 | 0.01889 | 9.43086 | 1.55959E-6 | 0.05 | 1 | 0.06112 | 0.19088 |
| P10 P8 | 0.064 | 0.01889 | 4.79028 | 0.05627 | 0.05 | 0 | -8.7916E-4 | 0.12888 |
| P12 P2 | 0.332 | 0.01889 | 24.84958 | 2.28907E-8 | 0.05 | 1 | 0.26712 | 0.39688 |
| P12 P4 | 0.272 | 0.01889 | 20.35869 | 1.24762E-7 | 0.05 | 1 | 0.20712 | 0.33688 |
| P12 P6 | 0.2 | 0.01889 | 14.96962 | 0 | 0.05 | 1 | 0.13512 | 0.26488 |
| P12 P8 | 0.138 | 0.01889 | 10.32904 | 2.39862E-7 | 0.05 | 1 | 0.07312 | 0.20288 |
| P12 P10 | 0.074 | 0.01889 | 5.53876 | 0.01341 | 0.05 | 1 | 0.00912 | 0.13888 |
| A2 P2 | -0.124 | 0.01889 | 9.28117 | 2.21838E-6 | 0.05 | 1 | -0.18888 | -0.05912 |
| A2 P4 | -0.184 | 0.01889 | 13.77205 | 0 | 0.05 | 1 | -0.24888 | -0.11912 |
| A2 P6 | -0.256 | 0.01889 | 19.16112 | 1.72013E-8 | 0.05 | 1 | -0.32088 | -0.19112 |
| A2 P8 | -0.318 | 0.01889 | 23.8017 | 2.22024E-8 | 0.05 | 1 | -0.38288 | -0.25312 |
| A2 P10 | -0.382 | 0.01889 | 28.59198 | 0 | 0.05 | 1 | -0.44688 | -0.31712 |
| A2 P12 | -0.456 | 0.01889 | 34.13074 | 0 | 0.05 | 1 | -0.52088 | -0.39112 |
| A4 P2 | -0.078 | 0.01889 | 5.83815 | 0.0072 | 0.05 | 1 | -0.14288 | -0.01312 |
| A4 P4 | -0.138 | 0.01889 | 10.32904 | 2.39862E-7 | 0.05 | 1 | -0.20288 | -0.07312 |
| A4 P6 | -0.21 | 0.01889 | 15.7181 | 0 | 0.05 | 1 | -0.27488 | -0.14512 |
| A4 P8 | -0.272 | 0.01889 | 20.35869 | 1.24762E-7 | 0.05 | 1 | -0.33688 | -0.20712 |
| A4 P10 | -0.336 | 0.01889 | 25.14897 | 2.30602E-8 | 0.05 | 1 | -0.40088 | -0.27112 |
| A4 P12 | -0.41 | 0.01889 | 30.68773 | 0 | 0.05 | 1 | -0.47488 | -0.34512 |
| A4 A2 | 0.046 | 0.01889 | 3.44301 | 0.40402 | 0.05 | 0 | -0.01888 | 0.11088 |
| A6 P2 | -0.036 | 0.01889 | 2.69453 | 0.75012 | 0.05 | 0 | -0.10088 | 0.02888 |
| A6 P4 | -0.096 | 0.01889 | 7.18542 | 3.50125E-4 | 0.05 | 1 | -0.16088 | -0.03112 |
| A6 P6 | -0.168 | 0.01889 | 12.57448 | 5.80852E-8 | 0.05 | 1 | -0.23288 | -0.10312 |
| A6 P8 | -0.23 | 0.01889 | 17.21507 | 0 | 0.05 | 1 | -0.29488 | -0.16512 |
| A6 P10 | -0.294 | 0.01889 | 22.00535 | 1.50841E-6 | 0.05 | 1 | -0.35888 | -0.22912 |
| A6 P12 | -0.368 | 0.01889 | 27.54411 | 0 | 0.05 | 1 | -0.43288 | -0.30312 |
| A6 A2 | 0.088 | 0.01889 | 6.58663 | 0.0014 | 0.05 | 1 | 0.02312 | 0.15288 |
| A6 A4 | 0.042 | 0.01889 | 3.14362 | 0.54215 | 0.05 | 0 | -0.02288 | 0.10688 |
| A8 P2 | 0.048 | 0.01889 | 3.59271 | 0.34112 | 0.05 | 0 | -0.01688 | 0.11288 |
| A8 P4 | -0.012 | 0.01889 | 0.89818 | 0.99996 | 0.05 | 0 | -0.07688 | 0.05288 |
| A8 P6 | -0.084 | 0.01889 | 6.28724 | 0.00273 | 0.05 | 1 | -0.14888 | -0.01912 |
| A8 P8 | -0.146 | 0.01889 | 10.92783 | 1.09782E-7 | 0.05 | 1 | -0.21088 | -0.08112 |
| A8 P10 | -0.21 | 0.01889 | 15.7181 | 0 | 0.05 | 1 | -0.27488 | -0.14512 |
| A8 P12 | -0.284 | 0.01889 | 21.25687 | 4.68583E-7 | 0.05 | 1 | -0.34888 | -0.21912 |
| A8 A2 | 0.172 | 0.01889 | 12.87388 | 8.00847E-8 | 0.05 | 1 | 0.10712 | 0.23688 |
| A8 A4 | 0.126 | 0.01889 | 9.43086 | 1.55959E-6 | 0.05 | 1 | 0.06112 | 0.19088 |
| A8 A6 | 0.084 | 0.01889 | 6.28724 | 0.00273 | 0.05 | 1 | 0.01912 | 0.14888 |
| A10 P2 | 0.134 | 0.01889 | 10.02965 | 4.18674E-7 | 0.05 | 1 | 0.06912 | 0.19888 |
| A10 P4 | 0.074 | 0.01889 | 5.53876 | 0.01341 | 0.05 | 1 | 0.00912 | 0.13888 |
| A10 P6 | 0.002 | 0.01889 | 0.1497 | 1 | 0.05 | 0 | -0.06288 | 0.06688 |
| A10 P8 | -0.06 | 0.01889 | 4.49089 | 0.09426 | 0.05 | 0 | -0.12488 | 0.00488 |
| A10 P10 | -0.124 | 0.01889 | 9.28117 | 2.21838E-6 | 0.05 | 1 | -0.18888 | -0.05912 |
| A10 P12 | -0.198 | 0.01889 | 14.81993 | 0 | 0.05 | 1 | -0.26288 | -0.13312 |
| A10 A2 | 0.258 | 0.01889 | 19.31081 | 1.74159E-8 | 0.05 | 1 | 0.19312 | 0.32288 |
| A10 A4 | 0.212 | 0.01889 | 15.8678 | 0 | 0.05 | 1 | 0.14712 | 0.27688 |
| A10 A6 | 0.17 | 0.01889 | 12.72418 | 5.67933E-8 | 0.05 | 1 | 0.10512 | 0.23488 |
| A10 A8 | 0.086 | 0.01889 | 6.43694 | 0.00195 | 0.05 | 1 | 0.02112 | 0.15088 |
| A12 P2 | 0.21 | 0.01889 | 15.7181 | 0 | 0.05 | 1 | 0.14512 | 0.27488 |
| A12 P4 | 0.15 | 0.01889 | 11.22722 | 8.76393E-8 | 0.05 | 1 | 0.08512 | 0.21488 |
| A12 P6 | 0.078 | 0.01889 | 5.83815 | 0.0072 | 0.05 | 1 | 0.01312 | 0.14288 |
| A12 P8 | 0.016 | 0.01889 | 1.19757 | 0.99933 | 0.05 | 0 | -0.04888 | 0.08088 |
| A12 P10 | -0.048 | 0.01889 | 3.59271 | 0.34112 | 0.05 | 0 | -0.11288 | 0.01688 |
| A12 P12 | -0.122 | 0.01889 | 9.13147 | 3.17237E-6 | 0.05 | 1 | -0.18688 | -0.05712 |
| A12 A2 | 0.334 | 0.01889 | 24.99927 | 2.2977E-8 | 0.05 | 1 | 0.26912 | 0.39888 |
| A12 A4 | 0.288 | 0.01889 | 21.55626 | 4.81252E-7 | 0.05 | 1 | 0.22312 | 0.35288 |
| A12 A6 | 0.246 | 0.01889 | 18.41264 | 1.60743E-8 | 0.05 | 1 | 0.18112 | 0.31088 |
| A12 A8 | 0.162 | 0.01889 | 12.1254 | 6.29047E-8 | 0.05 | 1 | 0.09712 | 0.22688 |
| A12 A10 | 0.076 | 0.01889 | 5.68846 | 0.00986 | 0.05 | 1 | 0.01112 | 0.14088 |

Sig equals one (σ=1) indicates that at 0.05 level, the difference of the means is significant, whereas Sig equals zero (σ=0) shows that the difference of the means is not significant.

Under different cutting speeds at a fixed laser power of 8 W (conditions M1), using the kerf width data of the Korean pine and Northeast China ash as reported in Table 4, a One-Way ANOVA with NWJGL cutting speed as a single independent variable was carried out.

The means comparison of the kerf width of the two wood workpieces using the Tukey Test is reported in Table 5. Figure 4 depicts Korean pine and Northeast China ash wood workpiece's kerf width repartition.

Table 4. The kerf width data of the Korean pine and the Northeast China ash under M1.

| Kerf width of the Korean pine (Pinus Koraiensis) (mm) |  |  |  |  |  | Kerf width data of Northeast China ash (Fraxinus mandshurica) (mm) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P1.57 | P2.35 | P3.62 | P4.68 | P5.34 | P6.26 | A1.57 | A2.35 | A3.62 | A4.68 | A5.34 | A6.26 |
| 0.94 | 0.90 | 0.85 | 0.79 | 0.73 | 0.66 | 0.81 | 0.78 | 0.69 | 0.63 | 0.57 | 0.52 |
| 0.95 | 0.89 | 0.89 | 0.81 | 0.76 | 0.68 | 0.79 | 0.79 | 0.71 | 0.66 | 0.59 | 0.54 |
| 0.93 | 0.92 | 0.88 | 0.80 | 0.74 | 0.67 | 0.82 | 0.74 | 0.73 | 0.64 | 0.56 | 0.55 |
| 0.97 | 0.90 | 0.86 | 0.83 | 0.73 | 0.65 | 0.81 | 0.76 | 0.69 | 0.62 | 0.57 | 0.53 |
| 1.12 | 0.88 | 0.84 | 0.81 | 0.75 | 0.63 | 0.83 | 0.77 | 0.72 | 0.65 | 0.58 | 1.52 |

Pi and Ai are the kerf width data of Korean pine and Northeast China ash at different laser-cutting speeds, where i, takes different values of 1.57 mm/s. 2.35 mm/s, 3.62 mm/s, 4.68 mm/s, 5.34 mm/s, and 6.26 mm/s.

Figure 4. Kerf width box charts of Korean pine and Northeast China ash under M2.

Table 5. Means comparison of kerf width data (Tukey Test) under M1.

|  | MeanDiff | SEM | q Value | Prob | Alpha | Sig | LCL | UCL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P2.35 P1.57 | -0.084 | 0.08227 | 1.44399 | 0.99641 | 0.05 | 0 | -0.36649 | 0.19849 |
| P3.62 P1.57 | -0.118 | 0.08227 | 2.02846 | 0.95037 | 0.05 | 0 | -0.40049 | 0.16449 |
| P3.62 P2.35 | -0.034 | 0.08227 | 0.58447 | 1 | 0.05 | 0 | -0.31649 | 0.24849 |
| P4.68 P1.57 | -0.174 | 0.08227 | 2.99112 | 0.61504 | 0.05 | 0 | -0.45649 | 0.10849 |
| P4.68 P2.35 | -0.09 | 0.08227 | 1.54713 | 0.99357 | 0.05 | 0 | -0.37249 | 0.19249 |
| P4.68 P3.62 | -0.056 | 0.08227 | 0.96266 | 0.99992 | 0.05 | 0 | -0.33849 | 0.22649 |
| P5.34 P1.57 | -0.24 | 0.08227 | 4.12568 | 0.16744 | 0.05 | 0 | -0.52249 | 0.04249 |
| P5.34 P2.35 | -0.156 | 0.08227 | 2.6817 | 0.75554 | 0.05 | 0 | -0.43849 | 0.12649 |
| P5.34 P3.62 | -0.122 | 0.08227 | 2.09722 | 0.93812 | 0.05 | 0 | -0.40449 | 0.16049 |
| P5.34 P4.68 | -0.066 | 0.08227 | 1.13456 | 0.99959 | 0.05 | 0 | -0.34849 | 0.21649 |
| P6.26 P1.57 | -0.324 | 0.08227 | 5.56967 | 0.01259 | 0.05 | 1 | -0.60649 | -0.04151 |
| P6.26 P2.35 | -0.24 | 0.08227 | 4.12568 | 0.16744 | 0.05 | 0 | -0.52249 | 0.04249 |
| P6.26 P3.62 | -0.206 | 0.08227 | 3.54121 | 0.36215 | 0.05 | 0 | -0.48849 | 0.07649 |
| P6.26 P4.68 | -0.15 | 0.08227 | 2.57855 | 0.79731 | 0.05 | 0 | -0.43249 | 0.13249 |
| P6.26 P5.34 | -0.084 | 0.08227 | 1.44399 | 0.99641 | 0.05 | 0 | -0.36649 | 0.19849 |
| A1.57 P1.57 | -0.17 | 0.08227 | 2.92236 | 0.64756 | 0.05 | 0 | -0.45249 | 0.11249 |
| A1.57 P2.35 | -0.086 | 0.08227 | 1.47837 | 0.99561 | 0.05 | 0 | -0.36849 | 0.19649 |
| A1.57 P3.62 | -0.052 | 0.08227 | 0.8939 | 0.99996 | 0.05 | 0 | -0.33449 | 0.23049 |
| A1.57 P4.68 | 0.004 | 0.08227 | 0.06876 | 1 | 0.05 | 0 | -0.27849 | 0.28649 |
| A1.57 P5.34 | 0.07 | 0.08227 | 1.20332 | 0.99929 | 0.05 | 0 | -0.21249 | 0.35249 |
| A1.57 P6.26 | 0.154 | 0.08227 | 2.64731 | 0.76984 | 0.05 | 0 | -0.12849 | 0.43649 |
| A2.35 P1.57 | -0.214 | 0.08227 | 3.67874 | 0.30754 | 0.05 | 0 | -0.49649 | 0.06849 |
| A2.35 P2.35 | -0.13 | 0.08227 | 2.23475 | 0.9078 | 0.05 | 0 | -0.41249 | 0.15249 |
| A2.35 P3.62 | -0.096 | 0.08227 | 1.65027 | 0.98915 | 0.05 | 0 | -0.37849 | 0.18649 |
| A2.35 P4.68 | -0.04 | 0.08227 | 0.68761 | 1 | 0.05 | 0 | -0.32249 | 0.24249 |
| A2.35 P5.34 | 0.026 | 0.08227 | 0.44695 | 1 | 0.05 | 0 | -0.25649 | 0.30849 |
| A2.35 P6.26 | 0.11 | 0.08227 | 1.89094 | 0.96955 | 0.05 | 0 | -0.17249 | 0.39249 |
| A2.35 A1.57 | -0.044 | 0.08227 | 0.75638 | 0.99999 | 0.05 | 0 | -0.32649 | 0.23849 |
| A3.62 P1.57 | -0.274 | 0.08227 | 4.71016 | 0.06484 | 0.05 | 0 | -0.55649 | 0.00849 |
| A3.62 P2.35 | -0.19 | 0.08227 | 3.26617 | 0.4842 | 0.05 | 0 | -0.47249 | 0.09249 |
| A3.62 P3.62 | -0.156 | 0.08227 | 2.6817 | 0.75554 | 0.05 | 0 | -0.43849 | 0.12649 |
| A3.62 P4.68 | -0.1 | 0.08227 | 1.71904 | 0.98505 | 0.05 | 0 | -0.38249 | 0.18249 |
| A3.62 P5.34 | -0.034 | 0.08227 | 0.58447 | 1 | 0.05 | 0 | -0.31649 | 0.24849 |
| A3.62 P6.26 | 0.05 | 0.08227 | 0.85952 | 0.99997 | 0.05 | 0 | -0.23249 | 0.33249 |
| A3.62 A1.57 | -0.104 | 0.08227 | 1.7878 | 0.97984 | 0.05 | 0 | -0.38649 | 0.17849 |
| A3.62 A2.35 | -0.06 | 0.08227 | 1.03142 | 0.99984 | 0.05 | 0 | -0.34249 | 0.22249 |
| A4.68 P1.57 | -0.342 | 0.08227 | 5.8791 | 0.00661 | 0.05 | 1 | -0.62449 | -0.05951 |
| A4.68 P2.35 | -0.258 | 0.08227 | 4.43511 | 0.10333 | 0.05 | 0 | -0.54049 | 0.02449 |
| A4.68 P3.62 | -0.224 | 0.08227 | 3.85064 | 0.2467 | 0.05 | 0 | -0.50649 | 0.05849 |
| A4.68 P4.68 | -0.168 | 0.08227 | 2.88798 | 0.66364 | 0.05 | 0 | -0.45049 | 0.11449 |
| A4.68 P5.34 | -0.102 | 0.08227 | 1.75342 | 0.98259 | 0.05 | 0 | -0.38449 | 0.18049 |
| A4.68 P6.26 | -0.018 | 0.08227 | 0.30943 | 1 | 0.05 | 0 | -0.30049 | 0.26449 |
| A4.68 A1.57 | -0.172 | 0.08227 | 2.95674 | 0.63135 | 0.05 | 0 | -0.45449 | 0.11049 |
| A4.68 A2.35 | -0.128 | 0.08227 | 2.20037 | 0.91613 | 0.05 | 0 | -0.41049 | 0.15449 |
| A4.68 A3.62 | -0.068 | 0.08227 | 1.16894 | 0.99946 | 0.05 | 0 | -0.35049 | 0.21449 |
| A5.34 P1.57 | -0.408 | 0.08227 | 7.01366 | 5.23211E-4 | 0.05 | 1 | -0.69049 | -0.12551 |
| A5.34 P2.35 | -0.324 | 0.08227 | 5.56967 | 0.01259 | 0.05 | 1 | -0.60649 | -0.04151 |
| A5.34 P3.62 | -0.29 | 0.08227 | 4.9852 | 0.03945 | 0.05 | 1 | -0.57249 | -0.00751 |
| A5.34 P4.68 | -0.234 | 0.08227 | 4.02254 | 0.19457 | 0.05 | 0 | -0.51649 | 0.04849 |
| A5.34 P5.34 | -0.168 | 0.08227 | 2.88798 | 0.66364 | 0.05 | 0 | -0.45049 | 0.11449 |
| A5.34 P6.26 | -0.084 | 0.08227 | 1.44399 | 0.99641 | 0.05 | 0 | -0.36649 | 0.19849 |
| A5.34 A1.57 | -0.238 | 0.08227 | 4.0913 | 0.17614 | 0.05 | 0 | -0.52049 | 0.04449 |
| A5.34 A2.35 | -0.194 | 0.08227 | 3.33493 | 0.45241 | 0.05 | 0 | -0.47649 | 0.08849 |
| A5.34 A3.62 | -0.134 | 0.08227 | 2.30351 | 0.88962 | 0.05 | 0 | -0.41649 | 0.14849 |
| A5.34 A4.68 | -0.066 | 0.08227 | 1.13456 | 0.99959 | 0.05 | 0 | -0.34849 | 0.21649 |
| A6.26 P1.57 | -0.25 | 0.08227 | 4.29759 | 0.12879 | 0.05 | 0 | -0.53249 | 0.03249 |
| A6.26 P2.35 | -0.166 | 0.08227 | 2.8536 | 0.67954 | 0.05 | 0 | -0.44849 | 0.11649 |
| A6.26 P3.62 | -0.132 | 0.08227 | 2.26913 | 0.89896 | 0.05 | 0 | -0.41449 | 0.15049 |
| A6.26 P4.68 | -0.076 | 0.08227 | 1.30647 | 0.99851 | 0.05 | 0 | -0.35849 | 0.20649 |
| A6.26 P5.34 | -0.01 | 0.08227 | 0.1719 | 1 | 0.05 | 0 | -0.29249 | 0.27249 |
| A6.26 P6.26 | 0.074 | 0.08227 | 1.27209 | 0.99883 | 0.05 | 0 | -0.20849 | 0.35649 |
| A6.26 A1.57 | -0.08 | 0.08227 | 1.37523 | 0.99765 | 0.05 | 0 | -0.36249 | 0.20249 |
| A6.26 A2.35 | -0.036 | 0.08227 | 0.61885 | 1 | 0.05 | 0 | -0.31849 | 0.24649 |
| A6.26 A3.62 | 0.024 | 0.08227 | 0.41257 | 1 | 0.05 | 0 | -0.25849 | 0.30649 |
| A6.26 A4.68 | 0.092 | 0.08227 | 1.58151 | 0.9923 | 0.05 | 0 | -0.19049 | 0.37449 |
| A6.26 A5.34 | 0.158 | 0.08227 | 2.71608 | 0.74091 | 0.05 | 0 | -0.12449 | 0.44049 |

Sig equals one (σ=1) indicates that the difference of the means is significant at the 0.05 level, whereas Sig equals zero (σ=0) proves that the difference of the means is not significant.

  - Appendix B

Considering the machining conditions M1 and M2 ( see Table 1),  a two-way ANOVA with replication was conducted with laser power and cutting speed as independent variables influencing the Korean pine’s kerf width (Table 6). The parameters interaction and their effects on the kerf width were evaluated using Bonferroni Test. Table 7, Table 8 and Table 9 report the means comparison results for cutting speed, laser power, and interaction. The value of Sigma (σ) is used to define the comparison of the means. Thus, Sig equals one (σ=1) indicates that at 0.05 level of variance, the difference of the means is significant, whereas Sig equals zero (σ=0) indicates that the difference of the means is not significant.

Table 6. Kerf width data of Korean pine under conditions M1 and M2.

| Kerf width (Pi, Pk) of the Korean pine (Pinus Koraiensis) (mm) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P1.57 | P2.35 | P3.62 | P4.68 | P5.34 | P6.26 | P2 | P4 | P6 | P8 | P10 | P12 |
| 0.94 | 0.90 | 0.85 | 0.79 | 0.73 | 0.66 | 0.64 | 0.71 | 0.78 | 0.83 | 0.89 | 0.93 |
| 0.95 | 0.89 | 0.89 | 0.81 | 0.76 | 0.68 | 0.63 | 0.70 | 0.79 | 0.85 | 0.91 | 0.97 |
| 0.93 | 0.92 | 0.88 | 0.80 | 0.74 | 0.67 | 0.66 | 0.73 | 0.77 | 0.88 | 0.93 | 0.95 |
| 0.97 | 0.90 | 0.86 | 0.83 | 0.73 | 0.65 | 0.69 | 0.71 | 0.81 | 0.84 | 0.96 | 0.98 |
| 1.12 | 0.88 | 0.84 | 0.81 | 0.75 | 0.63 | 0.67 | 0.74 | 0.80 | 0.86 | 0.89 | 1.12 |

Pi and Pk are the Korean pine (Pinus Koraiensis) kerf width data at different NWJGL cutting speeds and powers; i takes different values of 1.57 mm/s. 2.35 mm/s, 3.62 mm/s, 4.68 mm/s, 5.34 mm/s, and 6.26 mm/s; k takes the values of 2 W, 4 W, 6 W, 8 W, 10 W, and 12 W.

Table 7. Means comparisons of laser cutting speed.

|  | Mean Diff | SEM | t Value | Prob | Alpha | Sig | LCL | UCL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S2.35 S 1.57 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 3.62 S 1.57 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 3.62 S2.35 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 4.68 S 1.57 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 4.68 S2.35 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 4.68 S 3.62 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 5.34 S 1.57 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 5.34 S2.35 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 5.34 S 3.62 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S 5.34 S 4.68 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S6.26 S 1.57 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S6.26 S2.35 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S6.26 S 3.62 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S6.26 S 4.68 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |
| S6.26 S 5.34 | 0 | 0.00942 | 0 | 1 | 0.05 | 0 | -0.02812 | 0.02812 |

Sig equals one (σ=1) indicates that at 0.05 level, the difference of the means is significant, whereas Sig equals zero (σ=0) shows that the difference of the means is not significant.

Table 8. Means comparisons of laser power.

|  | Mean Diff | SEM | t Value | Prob | Alpha | Sig | LCL | UCL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P4 P2 | 0.06 | 0.00942 | 6.36794 | 3.62186E-8 | 0.05 | 1 | 0.03188 | 0.08812 |
| P6 P2 | 0.132 | 0.00942 | 14.00947 | 1.6852E-27 | 0.05 | 1 | 0.10388 | 0.16012 |
| P6 P4 | 0.072 | 0.00942 | 7.64153 | 4.13986E-11 | 0.05 | 1 | 0.04388 | 0.10012 |
| P8 P2 | 0.194 | 0.00942 | 20.58968 | 1.42296E-43 | 0.05 | 1 | 0.16588 | 0.22212 |
| P8 P4 | 0.134 | 0.00942 | 14.22174 | 4.76518E-28 | 0.05 | 1 | 0.10588 | 0.16212 |
| P8 P6 | 0.062 | 0.00942 | 6.58021 | 1.21972E-8 | 0.05 | 1 | 0.03388 | 0.09012 |
| P10 P2 | 0.258 | 0.00942 | 27.38215 | 8.89383E-58 | 0.05 | 1 | 0.22988 | 0.28612 |
| P10 P4 | 0.198 | 0.00942 | 21.01421 | 1.56099E-44 | 0.05 | 1 | 0.16988 | 0.22612 |
| P10 P6 | 0.126 | 0.00942 | 13.37268 | 7.5879E-26 | 0.05 | 1 | 0.09788 | 0.15412 |
| P10 P8 | 0.064 | 0.00942 | 6.79247 | 4.03602E-9 | 0.05 | 1 | 0.03588 | 0.09212 |
| P12 P2 | 0.332 | 0.00942 | 35.23595 | 1.68414E-71 | 0.05 | 1 | 0.30388 | 0.36012 |
| P12 P4 | 0.272 | 0.00942 | 28.868 | 1.41354E-60 | 0.05 | 1 | 0.24388 | 0.30012 |
| P12 P6 | 0.2 | 0.00942 | 21.22647 | 5.2145E-45 | 0.05 | 1 | 0.17188 | 0.22812 |
| P12 P8 | 0.138 | 0.00942 | 14.64627 | 3.84929E-29 | 0.05 | 1 | 0.10988 | 0.16612 |
| P12 P10 | 0.074 | 0.00942 | 7.8538 | 1.27314E-11 | 0.05 | 1 | 0.04588 | 0.10212 |

Sig equals one (σ=1) indicates that at 0.05 level, the difference of the means is significant, whereas Sig equals zero (σ=0) shows that the difference of the means is not significant.

Table 9. Interaction.

| Cutting speed | Laser power | Cutting speed | Laser power | MeanDiff | SEM | t Value | Prob | Alpha | Sig | LCL | UCL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S 1.57 | P 4 | S 1.57 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 1.57 | P6 | S 1.57 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 1.57 | P6 | S 1.57 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 1.57 | P 8 | S 1.57 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 1.57 | P 8 | S 1.57 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 1.57 | P 8 | S 1.57 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 1.57 | P 10 | S 1.57 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 1.57 | P 10 | S 1.57 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 1.57 | P 10 | S 1.57 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 1.57 | P 10 | S 1.57 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 1.57 | P 12 | S 1.57 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 1.57 | P 12 | S 1.57 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 1.57 | P 12 | S 1.57 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 1.57 | P 12 | S 1.57 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 1.57 | P 12 | S 1.57 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S2.35 | P2 | S 1.57 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S2.35 | P2 | S 1.57 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S2.35 | P2 | S 1.57 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S2.35 | P2 | S 1.57 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S2.35 | P2 | S 1.57 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S2.35 | P2 | S 1.57 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S2.35 | P 4 | S 1.57 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S2.35 | P 4 | S 1.57 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S2.35 | P 4 | S 1.57 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S2.35 | P 4 | S 1.57 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S2.35 | P 4 | S 1.57 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S2.35 | P 4 | S 1.57 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S2.35 | P 4 | S2.35 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S2.35 | P6 | S 1.57 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S2.35 | P6 | S 1.57 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S2.35 | P6 | S 1.57 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S2.35 | P6 | S 1.57 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S2.35 | P6 | S 1.57 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S2.35 | P6 | S 1.57 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S2.35 | P6 | S2.35 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S2.35 | P6 | S2.35 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S2.35 | P 8 | S 1.57 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S2.35 | P 8 | S 1.57 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S2.35 | P 8 | S 1.57 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S2.35 | P 8 | S 1.57 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S2.35 | P 8 | S 1.57 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S2.35 | P 8 | S 1.57 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S2.35 | P 8 | S2.35 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S2.35 | P 8 | S2.35 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S2.35 | P 8 | S2.35 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S2.35 | P 10 | S 1.57 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S2.35 | P 10 | S 1.57 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S2.35 | P 10 | S 1.57 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S2.35 | P 10 | S 1.57 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S2.35 | P 10 | S 1.57 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S2.35 | P 10 | S 1.57 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S2.35 | P 10 | S2.35 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S2.35 | P 10 | S2.35 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S2.35 | P 10 | S2.35 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S2.35 | P 10 | S2.35 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S2.35 | P 12 | S 1.57 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S2.35 | P 12 | S 1.57 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S2.35 | P 12 | S 1.57 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S2.35 | P 12 | S 1.57 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S2.35 | P 12 | S 1.57 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S2.35 | P 12 | S 1.57 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S2.35 | P 12 | S2.35 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S2.35 | P 12 | S2.35 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S2.35 | P 12 | S2.35 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S2.35 | P 12 | S2.35 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S2.35 | P 12 | S2.35 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 3.62 | P2 | S 1.57 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P2 | S 1.57 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 3.62 | P2 | S 1.57 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 3.62 | P2 | S 1.57 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 3.62 | P2 | S 1.57 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 3.62 | P2 | S 1.57 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 3.62 | P2 | S2.35 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P2 | S2.35 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 3.62 | P2 | S2.35 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 3.62 | P2 | S2.35 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 3.62 | P2 | S2.35 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 3.62 | P2 | S2.35 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 3.62 | P 4 | S 1.57 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 3.62 | P 4 | S 1.57 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P 4 | S 1.57 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 3.62 | P 4 | S 1.57 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 3.62 | P 4 | S 1.57 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 3.62 | P 4 | S 1.57 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 3.62 | P 4 | S2.35 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 3.62 | P 4 | S2.35 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P 4 | S2.35 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 3.62 | P 4 | S2.35 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 3.62 | P 4 | S2.35 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 3.62 | P 4 | S2.35 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 3.62 | P 4 | S 3.62 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 3.62 | P6 | S 1.57 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 3.62 | P6 | S 1.57 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 3.62 | P6 | S 1.57 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P6 | S 1.57 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 3.62 | P6 | S 1.57 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 3.62 | P6 | S 1.57 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 3.62 | P6 | S2.35 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 3.62 | P6 | S2.35 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 3.62 | P6 | S2.35 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P6 | S2.35 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 3.62 | P6 | S2.35 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 3.62 | P6 | S2.35 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 3.62 | P6 | S 3.62 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 3.62 | P6 | S 3.62 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 3.62 | P 8 | S 1.57 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 3.62 | P 8 | S 1.57 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 3.62 | P 8 | S 1.57 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 3.62 | P 8 | S 1.57 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P 8 | S 1.57 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 3.62 | P 8 | S 1.57 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 3.62 | P 8 | S2.35 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 3.62 | P 8 | S2.35 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 3.62 | P 8 | S2.35 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 3.62 | P 8 | S2.35 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P 8 | S2.35 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 3.62 | P 8 | S2.35 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 3.62 | P 8 | S 3.62 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 3.62 | P 8 | S 3.62 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 3.62 | P 8 | S 3.62 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 3.62 | P 10 | S 1.57 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 3.62 | P 10 | S 1.57 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 3.62 | P 10 | S 1.57 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 3.62 | P 10 | S 1.57 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 3.62 | P 10 | S 1.57 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P 10 | S 1.57 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 3.62 | P 10 | S2.35 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 3.62 | P 10 | S2.35 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 3.62 | P 10 | S2.35 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 3.62 | P 10 | S2.35 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 3.62 | P 10 | S2.35 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P 10 | S2.35 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 3.62 | P 10 | S 3.62 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 3.62 | P 10 | S 3.62 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 3.62 | P 10 | S 3.62 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 3.62 | P 10 | S 3.62 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 3.62 | P 12 | S 1.57 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 3.62 | P 12 | S 1.57 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 3.62 | P 12 | S 1.57 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 3.62 | P 12 | S 1.57 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 3.62 | P 12 | S 1.57 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 3.62 | P 12 | S 1.57 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P 12 | S2.35 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 3.62 | P 12 | S2.35 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 3.62 | P 12 | S2.35 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 3.62 | P 12 | S2.35 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 3.62 | P 12 | S2.35 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 3.62 | P 12 | S2.35 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 3.62 | P 12 | S 3.62 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 3.62 | P 12 | S 3.62 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 3.62 | P 12 | S 3.62 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 3.62 | P 12 | S 3.62 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 3.62 | P 12 | S 3.62 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 4.68 | P2 | S 1.57 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P2 | S 1.57 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 4.68 | P2 | S 1.57 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 4.68 | P2 | S 1.57 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 4.68 | P2 | S 1.57 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 4.68 | P2 | S 1.57 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 4.68 | P2 | S2.35 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P2 | S2.35 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 4.68 | P2 | S2.35 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 4.68 | P2 | S2.35 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 4.68 | P2 | S2.35 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 4.68 | P2 | S2.35 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 4.68 | P2 | S 3.62 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P2 | S 3.62 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 4.68 | P2 | S 3.62 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 4.68 | P2 | S 3.62 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 4.68 | P2 | S 3.62 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 4.68 | P2 | S 3.62 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 4.68 | P 4 | S 1.57 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 4.68 | P 4 | S 1.57 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 4 | S 1.57 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 4.68 | P 4 | S 1.57 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 4.68 | P 4 | S 1.57 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 4.68 | P 4 | S 1.57 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 4.68 | P 4 | S2.35 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 4.68 | P 4 | S2.35 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 4 | S2.35 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 4.68 | P 4 | S2.35 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 4.68 | P 4 | S2.35 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 4.68 | P 4 | S2.35 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 4.68 | P 4 | S 3.62 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 4.68 | P 4 | S 3.62 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 4 | S 3.62 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 4.68 | P 4 | S 3.62 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 4.68 | P 4 | S 3.62 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 4.68 | P 4 | S 3.62 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 4.68 | P 4 | S 4.68 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 4.68 | P6 | S 1.57 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 4.68 | P6 | S 1.57 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 4.68 | P6 | S 1.57 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P6 | S 1.57 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 4.68 | P6 | S 1.57 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 4.68 | P6 | S 1.57 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 4.68 | P6 | S2.35 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 4.68 | P6 | S2.35 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 4.68 | P6 | S2.35 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P6 | S2.35 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 4.68 | P6 | S2.35 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 4.68 | P6 | S2.35 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 4.68 | P6 | S 3.62 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 4.68 | P6 | S 3.62 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 4.68 | P6 | S 3.62 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P6 | S 3.62 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 4.68 | P6 | S 3.62 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 4.68 | P6 | S 3.62 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 4.68 | P6 | S 4.68 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 4.68 | P6 | S 4.68 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 4.68 | P 8 | S 1.57 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 4.68 | P 8 | S 1.57 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 4.68 | P 8 | S 1.57 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 4.68 | P 8 | S 1.57 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 8 | S 1.57 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 4.68 | P 8 | S 1.57 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 4.68 | P 8 | S2.35 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 4.68 | P 8 | S2.35 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 4.68 | P 8 | S2.35 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 4.68 | P 8 | S2.35 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 8 | S2.35 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 4.68 | P 8 | S2.35 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 4.68 | P 8 | S 3.62 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 4.68 | P 8 | S 3.62 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 4.68 | P 8 | S 3.62 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 4.68 | P 8 | S 3.62 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 8 | S 3.62 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 4.68 | P 8 | S 3.62 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 4.68 | P 8 | S 4.68 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 4.68 | P 8 | S 4.68 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 4.68 | P 8 | S 4.68 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 4.68 | P 10 | S 1.57 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 4.68 | P 10 | S 1.57 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 4.68 | P 10 | S 1.57 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 4.68 | P 10 | S 1.57 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 4.68 | P 10 | S 1.57 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 10 | S 1.57 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 4.68 | P 10 | S2.35 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 4.68 | P 10 | S2.35 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 4.68 | P 10 | S2.35 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 4.68 | P 10 | S2.35 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 4.68 | P 10 | S2.35 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 10 | S2.35 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 4.68 | P 10 | S 3.62 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 4.68 | P 10 | S 3.62 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 4.68 | P 10 | S 3.62 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 4.68 | P 10 | S 3.62 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 4.68 | P 10 | S 3.62 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 10 | S 3.62 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 4.68 | P 10 | S 4.68 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 4.68 | P 10 | S 4.68 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 4.68 | P 10 | S 4.68 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 4.68 | P 10 | S 4.68 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 4.68 | P 12 | S 1.57 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 4.68 | P 12 | S 1.57 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 4.68 | P 12 | S 1.57 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 4.68 | P 12 | S 1.57 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 4.68 | P 12 | S 1.57 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 4.68 | P 12 | S 1.57 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 12 | S2.35 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 4.68 | P 12 | S2.35 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 4.68 | P 12 | S2.35 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 4.68 | P 12 | S2.35 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 4.68 | P 12 | S2.35 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 4.68 | P 12 | S2.35 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 12 | S 3.62 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 4.68 | P 12 | S 3.62 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 4.68 | P 12 | S 3.62 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 4.68 | P 12 | S 3.62 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 4.68 | P 12 | S 3.62 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 4.68 | P 12 | S 3.62 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 4.68 | P 12 | S 4.68 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 4.68 | P 12 | S 4.68 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 4.68 | P 12 | S 4.68 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 4.68 | P 12 | S 4.68 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 4.68 | P 12 | S 4.68 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 5.34 | P2 | S 1.57 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P2 | S 1.57 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 5.34 | P2 | S 1.57 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 5.34 | P2 | S 1.57 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 5.34 | P2 | S 1.57 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 5.34 | P2 | S 1.57 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 5.34 | P2 | S2.35 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P2 | S2.35 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 5.34 | P2 | S2.35 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 5.34 | P2 | S2.35 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 5.34 | P2 | S2.35 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 5.34 | P2 | S2.35 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 5.34 | P2 | S 3.62 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P2 | S 3.62 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 5.34 | P2 | S 3.62 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 5.34 | P2 | S 3.62 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 5.34 | P2 | S 3.62 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 5.34 | P2 | S 3.62 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 5.34 | P2 | S 4.68 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P2 | S 4.68 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S 5.34 | P2 | S 4.68 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S 5.34 | P2 | S 4.68 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S 5.34 | P2 | S 4.68 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S 5.34 | P2 | S 4.68 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S 5.34 | P 4 | S 1.57 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 5.34 | P 4 | S 1.57 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 4 | S 1.57 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 5.34 | P 4 | S 1.57 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 5.34 | P 4 | S 1.57 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 5.34 | P 4 | S 1.57 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 5.34 | P 4 | S2.35 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 5.34 | P 4 | S2.35 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 4 | S2.35 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 5.34 | P 4 | S2.35 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 5.34 | P 4 | S2.35 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 5.34 | P 4 | S2.35 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 5.34 | P 4 | S 3.62 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 5.34 | P 4 | S 3.62 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 4 | S 3.62 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 5.34 | P 4 | S 3.62 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 5.34 | P 4 | S 3.62 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 5.34 | P 4 | S 3.62 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 5.34 | P 4 | S 4.68 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 5.34 | P 4 | S 4.68 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 4 | S 4.68 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S 5.34 | P 4 | S 4.68 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S 5.34 | P 4 | S 4.68 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S 5.34 | P 4 | S 4.68 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S 5.34 | P 4 | S 5.34 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S 5.34 | P6 | S 1.57 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 5.34 | P6 | S 1.57 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 5.34 | P6 | S 1.57 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P6 | S 1.57 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 5.34 | P6 | S 1.57 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 5.34 | P6 | S 1.57 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 5.34 | P6 | S2.35 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 5.34 | P6 | S2.35 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 5.34 | P6 | S2.35 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P6 | S2.35 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 5.34 | P6 | S2.35 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 5.34 | P6 | S2.35 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 5.34 | P6 | S 3.62 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 5.34 | P6 | S 3.62 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 5.34 | P6 | S 3.62 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P6 | S 3.62 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 5.34 | P6 | S 3.62 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 5.34 | P6 | S 3.62 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 5.34 | P6 | S 4.68 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 5.34 | P6 | S 4.68 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 5.34 | P6 | S 4.68 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P6 | S 4.68 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S 5.34 | P6 | S 4.68 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S 5.34 | P6 | S 4.68 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S 5.34 | P6 | S 5.34 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S 5.34 | P6 | S 5.34 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S 5.34 | P 8 | S 1.57 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 5.34 | P 8 | S 1.57 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 5.34 | P 8 | S 1.57 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 5.34 | P 8 | S 1.57 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 8 | S 1.57 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 5.34 | P 8 | S 1.57 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 5.34 | P 8 | S2.35 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 5.34 | P 8 | S2.35 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 5.34 | P 8 | S2.35 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 5.34 | P 8 | S2.35 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 8 | S2.35 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 5.34 | P 8 | S2.35 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 5.34 | P 8 | S 3.62 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 5.34 | P 8 | S 3.62 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 5.34 | P 8 | S 3.62 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 5.34 | P 8 | S 3.62 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 8 | S 3.62 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 5.34 | P 8 | S 3.62 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 5.34 | P 8 | S 4.68 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 5.34 | P 8 | S 4.68 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 5.34 | P 8 | S 4.68 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 5.34 | P 8 | S 4.68 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 8 | S 4.68 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S 5.34 | P 8 | S 4.68 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S 5.34 | P 8 | S 5.34 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S 5.34 | P 8 | S 5.34 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S 5.34 | P 8 | S 5.34 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S 5.34 | P 10 | S 1.57 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 5.34 | P 10 | S 1.57 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 5.34 | P 10 | S 1.57 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 5.34 | P 10 | S 1.57 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 5.34 | P 10 | S 1.57 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 10 | S 1.57 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 5.34 | P 10 | S2.35 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 5.34 | P 10 | S2.35 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 5.34 | P 10 | S2.35 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 5.34 | P 10 | S2.35 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 5.34 | P 10 | S2.35 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 10 | S2.35 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 5.34 | P 10 | S 3.62 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 5.34 | P 10 | S 3.62 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 5.34 | P 10 | S 3.62 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 5.34 | P 10 | S 3.62 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 5.34 | P 10 | S 3.62 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 10 | S 3.62 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 5.34 | P 10 | S 4.68 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 5.34 | P 10 | S 4.68 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 5.34 | P 10 | S 4.68 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 5.34 | P 10 | S 4.68 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 5.34 | P 10 | S 4.68 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 10 | S 4.68 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S 5.34 | P 10 | S 5.34 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S 5.34 | P 10 | S 5.34 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S 5.34 | P 10 | S 5.34 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S 5.34 | P 10 | S 5.34 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S 5.34 | P 12 | S 1.57 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 5.34 | P 12 | S 1.57 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 5.34 | P 12 | S 1.57 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 5.34 | P 12 | S 1.57 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 5.34 | P 12 | S 1.57 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 5.34 | P 12 | S 1.57 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 12 | S2.35 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 5.34 | P 12 | S2.35 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 5.34 | P 12 | S2.35 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 5.34 | P 12 | S2.35 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 5.34 | P 12 | S2.35 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 5.34 | P 12 | S2.35 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 12 | S 3.62 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 5.34 | P 12 | S 3.62 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 5.34 | P 12 | S 3.62 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 5.34 | P 12 | S 3.62 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 5.34 | P 12 | S 3.62 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 5.34 | P 12 | S 3.62 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 12 | S 4.68 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 5.34 | P 12 | S 4.68 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 5.34 | P 12 | S 4.68 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 5.34 | P 12 | S 4.68 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 5.34 | P 12 | S 4.68 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S 5.34 | P 12 | S 4.68 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S 5.34 | P 12 | S 5.34 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S 5.34 | P 12 | S 5.34 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S 5.34 | P 12 | S 5.34 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S 5.34 | P 12 | S 5.34 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S 5.34 | P 12 | S 5.34 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S6.26 | P2 | S 1.57 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P2 | S 1.57 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S6.26 | P2 | S 1.57 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S6.26 | P2 | S 1.57 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S6.26 | P2 | S 1.57 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S6.26 | P2 | S 1.57 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S6.26 | P2 | S2.35 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P2 | S2.35 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S6.26 | P2 | S2.35 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S6.26 | P2 | S2.35 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S6.26 | P2 | S2.35 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S6.26 | P2 | S2.35 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S6.26 | P2 | S 3.62 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P2 | S 3.62 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S6.26 | P2 | S 3.62 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S6.26 | P2 | S 3.62 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S6.26 | P2 | S 3.62 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S6.26 | P2 | S 3.62 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S6.26 | P2 | S 4.68 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P2 | S 4.68 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S6.26 | P2 | S 4.68 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S6.26 | P2 | S 4.68 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S6.26 | P2 | S 4.68 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S6.26 | P2 | S 4.68 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S6.26 | P2 | S 5.34 | P2 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P2 | S 5.34 | P 4 | -0.06 | 0.02308 | -2.5997 | 1 | 0.05 | 0 | -0.15377 | 0.03377 |
| S6.26 | P2 | S 5.34 | P6 | -0.132 | 0.02308 | -5.71934 | 3.75432E-5 | 0.05 | 1 | -0.22577 | -0.03823 |
| S6.26 | P2 | S 5.34 | P 8 | -0.194 | 0.02308 | -8.4057 | 2.36267E-11 | 0.05 | 1 | -0.28777 | -0.10023 |
| S6.26 | P2 | S 5.34 | P 10 | -0.258 | 0.02308 | -11.17872 | 1.77252E-18 | 0.05 | 1 | -0.35177 | -0.16423 |
| S6.26 | P2 | S 5.34 | P 12 | -0.332 | 0.02308 | -14.38502 | 7.59174E-27 | 0.05 | 1 | -0.42577 | -0.23823 |
| S6.26 | P 4 | S 1.57 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S6.26 | P 4 | S 1.57 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 4 | S 1.57 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S6.26 | P 4 | S 1.57 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S6.26 | P 4 | S 1.57 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S6.26 | P 4 | S 1.57 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S6.26 | P 4 | S2.35 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S6.26 | P 4 | S2.35 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 4 | S2.35 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S6.26 | P 4 | S2.35 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S6.26 | P 4 | S2.35 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S6.26 | P 4 | S2.35 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S6.26 | P 4 | S 3.62 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S6.26 | P 4 | S 3.62 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 4 | S 3.62 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S6.26 | P 4 | S 3.62 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S6.26 | P 4 | S 3.62 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S6.26 | P 4 | S 3.62 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S6.26 | P 4 | S 4.68 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S6.26 | P 4 | S 4.68 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 4 | S 4.68 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S6.26 | P 4 | S 4.68 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S6.26 | P 4 | S 4.68 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S6.26 | P 4 | S 4.68 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S6.26 | P 4 | S 5.34 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S6.26 | P 4 | S 5.34 | P 4 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 4 | S 5.34 | P6 | -0.072 | 0.02308 | -3.11964 | 1 | 0.05 | 0 | -0.16577 | 0.02177 |
| S6.26 | P 4 | S 5.34 | P 8 | -0.134 | 0.02308 | -5.806 | 2.47362E-5 | 0.05 | 1 | -0.22777 | -0.04023 |
| S6.26 | P 4 | S 5.34 | P 10 | -0.198 | 0.02308 | -8.57902 | 8.74639E-12 | 0.05 | 1 | -0.29177 | -0.10423 |
| S6.26 | P 4 | S 5.34 | P 12 | -0.272 | 0.02308 | -11.78531 | 4.55006E-20 | 0.05 | 1 | -0.36577 | -0.17823 |
| S6.26 | P 4 | S6.26 | P2 | 0.06 | 0.02308 | 2.5997 | 1 | 0.05 | 0 | -0.03377 | 0.15377 |
| S6.26 | P6 | S 1.57 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S6.26 | P6 | S 1.57 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S6.26 | P6 | S 1.57 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P6 | S 1.57 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S6.26 | P6 | S 1.57 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S6.26 | P6 | S 1.57 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S6.26 | P6 | S2.35 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S6.26 | P6 | S2.35 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S6.26 | P6 | S2.35 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P6 | S2.35 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S6.26 | P6 | S2.35 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S6.26 | P6 | S2.35 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S6.26 | P6 | S 3.62 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S6.26 | P6 | S 3.62 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S6.26 | P6 | S 3.62 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P6 | S 3.62 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S6.26 | P6 | S 3.62 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S6.26 | P6 | S 3.62 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S6.26 | P6 | S 4.68 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S6.26 | P6 | S 4.68 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S6.26 | P6 | S 4.68 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P6 | S 4.68 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S6.26 | P6 | S 4.68 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S6.26 | P6 | S 4.68 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S6.26 | P6 | S 5.34 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S6.26 | P6 | S 5.34 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S6.26 | P6 | S 5.34 | P6 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P6 | S 5.34 | P 8 | -0.062 | 0.02308 | -2.68636 | 1 | 0.05 | 0 | -0.15577 | 0.03177 |
| S6.26 | P6 | S 5.34 | P 10 | -0.126 | 0.02308 | -5.45937 | 1.28392E-4 | 0.05 | 1 | -0.21977 | -0.03223 |
| S6.26 | P6 | S 5.34 | P 12 | -0.2 | 0.02308 | -8.66567 | 5.30947E-12 | 0.05 | 1 | -0.29377 | -0.10623 |
| S6.26 | P6 | S6.26 | P2 | 0.132 | 0.02308 | 5.71934 | 3.75432E-5 | 0.05 | 1 | 0.03823 | 0.22577 |
| S6.26 | P6 | S6.26 | P 4 | 0.072 | 0.02308 | 3.11964 | 1 | 0.05 | 0 | -0.02177 | 0.16577 |
| S6.26 | P 8 | S 1.57 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S6.26 | P 8 | S 1.57 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S6.26 | P 8 | S 1.57 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S6.26 | P 8 | S 1.57 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 8 | S 1.57 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S6.26 | P 8 | S 1.57 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S6.26 | P 8 | S2.35 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S6.26 | P 8 | S2.35 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S6.26 | P 8 | S2.35 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S6.26 | P 8 | S2.35 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 8 | S2.35 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S6.26 | P 8 | S2.35 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S6.26 | P 8 | S 3.62 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S6.26 | P 8 | S 3.62 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S6.26 | P 8 | S 3.62 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S6.26 | P 8 | S 3.62 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 8 | S 3.62 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S6.26 | P 8 | S 3.62 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S6.26 | P 8 | S 4.68 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S6.26 | P 8 | S 4.68 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S6.26 | P 8 | S 4.68 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S6.26 | P 8 | S 4.68 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 8 | S 4.68 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S6.26 | P 8 | S 4.68 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S6.26 | P 8 | S 5.34 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S6.26 | P 8 | S 5.34 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S6.26 | P 8 | S 5.34 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S6.26 | P 8 | S 5.34 | P 8 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 8 | S 5.34 | P 10 | -0.064 | 0.02308 | -2.77301 | 1 | 0.05 | 0 | -0.15777 | 0.02977 |
| S6.26 | P 8 | S 5.34 | P 12 | -0.138 | 0.02308 | -5.97931 | 1.0625E-5 | 0.05 | 1 | -0.23177 | -0.04423 |
| S6.26 | P 8 | S6.26 | P2 | 0.194 | 0.02308 | 8.4057 | 2.36267E-11 | 0.05 | 1 | 0.10023 | 0.28777 |
| S6.26 | P 8 | S6.26 | P 4 | 0.134 | 0.02308 | 5.806 | 2.47362E-5 | 0.05 | 1 | 0.04023 | 0.22777 |
| S6.26 | P 8 | S6.26 | P6 | 0.062 | 0.02308 | 2.68636 | 1 | 0.05 | 0 | -0.03177 | 0.15577 |
| S6.26 | P 10 | S 1.57 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S6.26 | P 10 | S 1.57 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S6.26 | P 10 | S 1.57 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S6.26 | P 10 | S 1.57 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S6.26 | P 10 | S 1.57 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 10 | S 1.57 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S6.26 | P 10 | S2.35 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S6.26 | P 10 | S2.35 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S6.26 | P 10 | S2.35 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S6.26 | P 10 | S2.35 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S6.26 | P 10 | S2.35 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 10 | S2.35 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S6.26 | P 10 | S 3.62 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S6.26 | P 10 | S 3.62 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S6.26 | P 10 | S 3.62 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S6.26 | P 10 | S 3.62 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S6.26 | P 10 | S 3.62 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 10 | S 3.62 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S6.26 | P 10 | S 4.68 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S6.26 | P 10 | S 4.68 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S6.26 | P 10 | S 4.68 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S6.26 | P 10 | S 4.68 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S6.26 | P 10 | S 4.68 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 10 | S 4.68 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S6.26 | P 10 | S 5.34 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S6.26 | P 10 | S 5.34 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S6.26 | P 10 | S 5.34 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S6.26 | P 10 | S 5.34 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S6.26 | P 10 | S 5.34 | P 10 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 10 | S 5.34 | P 12 | -0.074 | 0.02308 | -3.2063 | 1 | 0.05 | 0 | -0.16777 | 0.01977 |
| S6.26 | P 10 | S6.26 | P2 | 0.258 | 0.02308 | 11.17872 | 1.77252E-18 | 0.05 | 1 | 0.16423 | 0.35177 |
| S6.26 | P 10 | S6.26 | P 4 | 0.198 | 0.02308 | 8.57902 | 8.74639E-12 | 0.05 | 1 | 0.10423 | 0.29177 |
| S6.26 | P 10 | S6.26 | P6 | 0.126 | 0.02308 | 5.45937 | 1.28392E-4 | 0.05 | 1 | 0.03223 | 0.21977 |
| S6.26 | P 10 | S6.26 | P 8 | 0.064 | 0.02308 | 2.77301 | 1 | 0.05 | 0 | -0.02977 | 0.15777 |
| S6.26 | P 12 | S 1.57 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S6.26 | P 12 | S 1.57 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S6.26 | P 12 | S 1.57 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S6.26 | P 12 | S 1.57 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S6.26 | P 12 | S 1.57 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S6.26 | P 12 | S 1.57 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 12 | S2.35 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S6.26 | P 12 | S2.35 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S6.26 | P 12 | S2.35 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S6.26 | P 12 | S2.35 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S6.26 | P 12 | S2.35 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S6.26 | P 12 | S2.35 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 12 | S 3.62 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S6.26 | P 12 | S 3.62 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S6.26 | P 12 | S 3.62 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S6.26 | P 12 | S 3.62 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S6.26 | P 12 | S 3.62 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S6.26 | P 12 | S 3.62 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 12 | S 4.68 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S6.26 | P 12 | S 4.68 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S6.26 | P 12 | S 4.68 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S6.26 | P 12 | S 4.68 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S6.26 | P 12 | S 4.68 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S6.26 | P 12 | S 4.68 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 12 | S 5.34 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S6.26 | P 12 | S 5.34 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S6.26 | P 12 | S 5.34 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S6.26 | P 12 | S 5.34 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S6.26 | P 12 | S 5.34 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |
| S6.26 | P 12 | S 5.34 | P 12 | 0 | 0.02308 | 0 | 1 | 0.05 | 0 | -0.09377 | 0.09377 |
| S6.26 | P 12 | S6.26 | P2 | 0.332 | 0.02308 | 14.38502 | 7.59174E-27 | 0.05 | 1 | 0.23823 | 0.42577 |
| S6.26 | P 12 | S6.26 | P 4 | 0.272 | 0.02308 | 11.78531 | 4.55006E-20 | 0.05 | 1 | 0.17823 | 0.36577 |
| S6.26 | P 12 | S6.26 | P6 | 0.2 | 0.02308 | 8.66567 | 5.30947E-12 | 0.05 | 1 | 0.10623 | 0.29377 |
| S6.26 | P 12 | S6.26 | P 8 | 0.138 | 0.02308 | 5.97931 | 1.0625E-5 | 0.05 | 1 | 0.04423 | 0.23177 |
| S6.26 | P 12 | S6.26 | P 10 | 0.074 | 0.02308 | 3.2063 | 1 | 0.05 | 0 | -0.01977 | 0.16777 |

Sig equals one (σ=1) indicates that at 0.05 level, the difference of the means is significant, whereas Sig equals zero (σ=0) shows that the difference of the means is not significant.

At α (0.05) level of variance, the Korean pine’s kerf width means comparison for the cutting speed, laser power and their interaction is illustrated in Figure 5.

a) Cutting speed.                                                          b) Laser power.

b) Interaction.

Figure 5. Illustration of the means comparison test.

  - Appendix C

Under conditions M1 and M2 (Table 1), a two-way ANOVA with laser power and cutting speed affecting Northeast China ash’s kerf width (Table 10) was carried out. Similarly, the interaction and influence of the parameters on the kerf width were evaluated using Bonferroni Test. The means comparison is reported in Table 11, Table 12, and Table 13, respectively, for the cutting speed,  laser power, and interaction.

Table 10. Kerf width data of Northeast China ash under conditions M1 and M2.

| Kerf width (Ai, Ak) data of Northeast China ash (Fraxinus mandshurica) (mm) |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A1.57 | A2.35 | A3.62 | A4.68 | A5.34 | A6.26 | A2 | A4 | A6 | A8 | A10 | A12 |
| 0.81 | 0.78 | 0.69 | 0.63 | 0.57 | 0.52 | 0.53 | 0.56 | 0.62 | 0.71 | 0.79 | 0.83 |
| 0.79 | 0.79 | 0.71 | 0.66 | 0.59 | 0.54 | 0.52 | 0.59 | 0.61 | 0.69 | 0.81 | 0.86 |
| 0.82 | 0.74 | 0.73 | 0.64 | 0.56 | 0.55 | 0.54 | 0.58 | 0.64 | 0.72 | 0.78 | 0.85 |
| 0.81 | 0.76 | 0.69 | 0.62 | 0.57 | 0.53 | 0.52 | 0.60 | 0.61 | 0.68 | 0.82 | 0.89 |
| 0.83 | 0.77 | 0.72 | 0.65 | 0.58 | 1.52 | 0.56 | 0.57 | 0.63 | 0.73 | 0.76 | 0.91 |

Ai and Ak denote the kerf width data of Northeast China ash (Fraxinus mandshurica) at different cutting speeds and laser power; where i takes the values of cutting speeds and k, the values of laser powers.

Table 11. Means comparisons of cutting speed.

|  | Mean Diff | SEM | t Value | Prob | Alpha | Sig | LCL | UCL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S2.35 S1.57 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S3.62 S1.57 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S3.62 S2.35 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S4.68 S1.57 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S4.68 S2.35 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S4.68 S3.62 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S5.34 S1.57 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S5.34 S2.35 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S5.34 S3.62 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S5.34 S4.68 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S6.26 S1.57 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S6.26 S2.35 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S6.26 S3.62 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S6.26 S4.68 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |
| S6.26 S5.34 | 0 | 0.0055 | 0 | 1 | 0.05 | 0 | -0.01641 | 0.01641 |

Sig equals one (σ=1) indicates that at 0.05 level, the difference of the means is significant, whereas Sig equals zero (σ=0) suggests that the difference of the means is not significant.

Table 12. Means comparisons of laser power.

|  | Mean Diff | SEM | t Value | Prob | Alpha | Sig | LCL | UCL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P4 P2 | 0.046 | 0.0055 | 8.36748 | 6.99783E-13 | 0.05 | 1 | 0.02959 | 0.06241 |
| P6 P2 | 0.088 | 0.0055 | 16.00735 | 1.34484E-32 | 0.05 | 1 | 0.07159 | 0.10441 |
| P6 P4 | 0.042 | 0.0055 | 7.63987 | 4.17798E-11 | 0.05 | 1 | 0.02559 | 0.05841 |
| P8 P2 | 0.172 | 0.0055 | 31.2871 | 6.38985E-65 | 0.05 | 1 | 0.15559 | 0.18841 |
| P8 P4 | 0.126 | 0.0055 | 22.91962 | 1.01596E-48 | 0.05 | 1 | 0.10959 | 0.14241 |
| P8 P6 | 0.084 | 0.0055 | 15.27974 | 9.27087E-31 | 0.05 | 1 | 0.06759 | 0.10041 |
| P10 P2 | 0.258 | 0.0055 | 46.93064 | 5.54168E-88 | 0.05 | 1 | 0.24159 | 0.27441 |
| P10 P4 | 0.212 | 0.0055 | 38.56316 | 1.32137E-76 | 0.05 | 1 | 0.19559 | 0.22841 |
| P10 P6 | 0.17 | 0.0055 | 30.92329 | 2.77221E-64 | 0.05 | 1 | 0.15359 | 0.18641 |
| P10 P8 | 0.086 | 0.0055 | 15.64355 | 1.10928E-31 | 0.05 | 1 | 0.06959 | 0.10241 |
| P12 P2 | 0.334 | 0.0055 | 60.75517 | 2.37491E-103 | 0.05 | 1 | 0.31759 | 0.35041 |
| P12 P4 | 0.288 | 0.0055 | 52.3877 | 1.74988E-94 | 0.05 | 1 | 0.27159 | 0.30441 |
| P12 P6 | 0.246 | 0.0055 | 44.74782 | 3.40677E-85 | 0.05 | 1 | 0.22959 | 0.26241 |
| P12 P8 | 0.162 | 0.0055 | 29.46808 | 1.11857E-61 | 0.05 | 1 | 0.14559 | 0.17841 |
| P12 10 | 0.076 | 0.0055 | 13.82453 | 5.07838E-27 | 0.05 | 1 | 0.05959 | 0.09241 |

Sig equals one (σ=1) indicates that at 0.05 level, the difference of the means is significant, whereas Sig equals zero (σ=0) suggests that the difference of the means is not significant.

Table 13. Interaction.

| Cutting Speed | Laser Power | Cutting Speed | Laser Power | MeanDiff | SEM | t Value | Prob | Alpha | Sig | LCL | UCL |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S1.57 | P4 | S1.57 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S1.57 | P6 | S1.57 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S1.57 | P6 | S1.57 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S1.57 | P8 | S1.57 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S1.57 | P8 | S1.57 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S1.57 | P8 | S1.57 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S1.57 | P10 | S1.57 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S1.57 | P10 | S1.57 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S1.57 | P10 | S1.57 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S1.57 | P10 | S1.57 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S1.57 | P12 | S1.57 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S1.57 | P12 | S1.57 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S1.57 | P12 | S1.57 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S1.57 | P12 | S1.57 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S1.57 | P12 | S1.57 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S2.35 | P2 | S1.57 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S2.35 | P2 | S1.57 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S2.35 | P2 | S1.57 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S2.35 | P2 | S1.57 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S2.35 | P2 | S1.57 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S2.35 | P2 | S1.57 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S2.35 | P4 | S1.57 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S2.35 | P4 | S1.57 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S2.35 | P4 | S1.57 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S2.35 | P4 | S1.57 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S2.35 | P4 | S1.57 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S2.35 | P4 | S1.57 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S2.35 | P4 | S2.35 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S2.35 | P6 | S1.57 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S2.35 | P6 | S1.57 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S2.35 | P6 | S1.57 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S2.35 | P6 | S1.57 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S2.35 | P6 | S1.57 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S2.35 | P6 | S1.57 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S2.35 | P6 | S2.35 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S2.35 | P6 | S2.35 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S2.35 | P8 | S1.57 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S2.35 | P8 | S1.57 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S2.35 | P8 | S1.57 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S2.35 | P8 | S1.57 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S2.35 | P8 | S1.57 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S2.35 | P8 | S1.57 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S2.35 | P8 | S2.35 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S2.35 | P8 | S2.35 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S2.35 | P8 | S2.35 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S2.35 | P10 | S1.57 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S2.35 | P10 | S1.57 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S2.35 | P10 | S1.57 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S2.35 | P10 | S1.57 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S2.35 | P10 | S1.57 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S2.35 | P10 | S1.57 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S2.35 | P10 | S2.35 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S2.35 | P10 | S2.35 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S2.35 | P10 | S2.35 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S2.35 | P10 | S2.35 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S2.35 | P12 | S1.57 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S2.35 | P12 | S1.57 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S2.35 | P12 | S1.57 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S2.35 | P12 | S1.57 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S2.35 | P12 | S1.57 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S2.35 | P12 | S1.57 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S2.35 | P12 | S2.35 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S2.35 | P12 | S2.35 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S2.35 | P12 | S2.35 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S2.35 | P12 | S2.35 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S2.35 | P12 | S2.35 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S3.62 | P2 | S1.57 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P2 | S1.57 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S3.62 | P2 | S1.57 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S3.62 | P2 | S1.57 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S3.62 | P2 | S1.57 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S3.62 | P2 | S1.57 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S3.62 | P2 | S2.35 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P2 | S2.35 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S3.62 | P2 | S2.35 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S3.62 | P2 | S2.35 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S3.62 | P2 | S2.35 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S3.62 | P2 | S2.35 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S3.62 | P4 | S1.57 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S3.62 | P4 | S1.57 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P4 | S1.57 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S3.62 | P4 | S1.57 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S3.62 | P4 | S1.57 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S3.62 | P4 | S1.57 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S3.62 | P4 | S2.35 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S3.62 | P4 | S2.35 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P4 | S2.35 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S3.62 | P4 | S2.35 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S3.62 | P4 | S2.35 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S3.62 | P4 | S2.35 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S3.62 | P4 | S3.62 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S3.62 | P6 | S1.57 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S3.62 | P6 | S1.57 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S3.62 | P6 | S1.57 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P6 | S1.57 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S3.62 | P6 | S1.57 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S3.62 | P6 | S1.57 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S3.62 | P6 | S2.35 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S3.62 | P6 | S2.35 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S3.62 | P6 | S2.35 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P6 | S2.35 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S3.62 | P6 | S2.35 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S3.62 | P6 | S2.35 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S3.62 | P6 | S3.62 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S3.62 | P6 | S3.62 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S3.62 | P8 | S1.57 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S3.62 | P8 | S1.57 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S3.62 | P8 | S1.57 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S3.62 | P8 | S1.57 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P8 | S1.57 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S3.62 | P8 | S1.57 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S3.62 | P8 | S2.35 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S3.62 | P8 | S2.35 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S3.62 | P8 | S2.35 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S3.62 | P8 | S2.35 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P8 | S2.35 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S3.62 | P8 | S2.35 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S3.62 | P8 | S3.62 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S3.62 | P8 | S3.62 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S3.62 | P8 | S3.62 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S3.62 | P10 | S1.57 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S3.62 | P10 | S1.57 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S3.62 | P10 | S1.57 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S3.62 | P10 | S1.57 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S3.62 | P10 | S1.57 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P10 | S1.57 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S3.62 | P10 | S2.35 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S3.62 | P10 | S2.35 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S3.62 | P10 | S2.35 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S3.62 | P10 | S2.35 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S3.62 | P10 | S2.35 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P10 | S2.35 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S3.62 | P10 | S3.62 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S3.62 | P10 | S3.62 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S3.62 | P10 | S3.62 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S3.62 | P10 | S3.62 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S3.62 | P12 | S1.57 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S3.62 | P12 | S1.57 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S3.62 | P12 | S1.57 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S3.62 | P12 | S1.57 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S3.62 | P12 | S1.57 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S3.62 | P12 | S1.57 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P12 | S2.35 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S3.62 | P12 | S2.35 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S3.62 | P12 | S2.35 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S3.62 | P12 | S2.35 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S3.62 | P12 | S2.35 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S3.62 | P12 | S2.35 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S3.62 | P12 | S3.62 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S3.62 | P12 | S3.62 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S3.62 | P12 | S3.62 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S3.62 | P12 | S3.62 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S3.62 | P12 | S3.62 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S4.68 | P2 | S1.57 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P2 | S1.57 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S4.68 | P2 | S1.57 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S4.68 | P2 | S1.57 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S4.68 | P2 | S1.57 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S4.68 | P2 | S1.57 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S4.68 | P2 | S2.35 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P2 | S2.35 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S4.68 | P2 | S2.35 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S4.68 | P2 | S2.35 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S4.68 | P2 | S2.35 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S4.68 | P2 | S2.35 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S4.68 | P2 | S3.62 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P2 | S3.62 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S4.68 | P2 | S3.62 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S4.68 | P2 | S3.62 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S4.68 | P2 | S3.62 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S4.68 | P2 | S3.62 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S4.68 | P4 | S1.57 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S4.68 | P4 | S1.57 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P4 | S1.57 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S4.68 | P4 | S1.57 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S4.68 | P4 | S1.57 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S4.68 | P4 | S1.57 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S4.68 | P4 | S2.35 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S4.68 | P4 | S2.35 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P4 | S2.35 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S4.68 | P4 | S2.35 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S4.68 | P4 | S2.35 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S4.68 | P4 | S2.35 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S4.68 | P4 | S3.62 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S4.68 | P4 | S3.62 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P4 | S3.62 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S4.68 | P4 | S3.62 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S4.68 | P4 | S3.62 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S4.68 | P4 | S3.62 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S4.68 | P4 | S4.68 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S4.68 | P6 | S1.57 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S4.68 | P6 | S1.57 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S4.68 | P6 | S1.57 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P6 | S1.57 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S4.68 | P6 | S1.57 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S4.68 | P6 | S1.57 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S4.68 | P6 | S2.35 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S4.68 | P6 | S2.35 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S4.68 | P6 | S2.35 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P6 | S2.35 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S4.68 | P6 | S2.35 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S4.68 | P6 | S2.35 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S4.68 | P6 | S3.62 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S4.68 | P6 | S3.62 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S4.68 | P6 | S3.62 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P6 | S3.62 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S4.68 | P6 | S3.62 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S4.68 | P6 | S3.62 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S4.68 | P6 | S4.68 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S4.68 | P6 | S4.68 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S4.68 | P8 | S1.57 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S4.68 | P8 | S1.57 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S4.68 | P8 | S1.57 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S4.68 | P8 | S1.57 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P8 | S1.57 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S4.68 | P8 | S1.57 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S4.68 | P8 | S2.35 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S4.68 | P8 | S2.35 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S4.68 | P8 | S2.35 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S4.68 | P8 | S2.35 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P8 | S2.35 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S4.68 | P8 | S2.35 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S4.68 | P8 | S3.62 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S4.68 | P8 | S3.62 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S4.68 | P8 | S3.62 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S4.68 | P8 | S3.62 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P8 | S3.62 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S4.68 | P8 | S3.62 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S4.68 | P8 | S4.68 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S4.68 | P8 | S4.68 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S4.68 | P8 | S4.68 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S4.68 | P10 | S1.57 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S4.68 | P10 | S1.57 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S4.68 | P10 | S1.57 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S4.68 | P10 | S1.57 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S4.68 | P10 | S1.57 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P10 | S1.57 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S4.68 | P10 | S2.35 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S4.68 | P10 | S2.35 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S4.68 | P10 | S2.35 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S4.68 | P10 | S2.35 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S4.68 | P10 | S2.35 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P10 | S2.35 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S4.68 | P10 | S3.62 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S4.68 | P10 | S3.62 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S4.68 | P10 | S3.62 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S4.68 | P10 | S3.62 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S4.68 | P10 | S3.62 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P10 | S3.62 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S4.68 | P10 | S4.68 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S4.68 | P10 | S4.68 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S4.68 | P10 | S4.68 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S4.68 | P10 | S4.68 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S4.68 | P12 | S1.57 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S4.68 | P12 | S1.57 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S4.68 | P12 | S1.57 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S4.68 | P12 | S1.57 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S4.68 | P12 | S1.57 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S4.68 | P12 | S1.57 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P12 | S2.35 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S4.68 | P12 | S2.35 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S4.68 | P12 | S2.35 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S4.68 | P12 | S2.35 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S4.68 | P12 | S2.35 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S4.68 | P12 | S2.35 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P12 | S3.62 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S4.68 | P12 | S3.62 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S4.68 | P12 | S3.62 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S4.68 | P12 | S3.62 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S4.68 | P12 | S3.62 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S4.68 | P12 | S3.62 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S4.68 | P12 | S4.68 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S4.68 | P12 | S4.68 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S4.68 | P12 | S4.68 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S4.68 | P12 | S4.68 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S4.68 | P12 | S4.68 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S5.34 | P2 | S1.57 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P2 | S1.57 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S5.34 | P2 | S1.57 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S5.34 | P2 | S1.57 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S5.34 | P2 | S1.57 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S5.34 | P2 | S1.57 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S5.34 | P2 | S2.35 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P2 | S2.35 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S5.34 | P2 | S2.35 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S5.34 | P2 | S2.35 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S5.34 | P2 | S2.35 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S5.34 | P2 | S2.35 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S5.34 | P2 | S3.62 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P2 | S3.62 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S5.34 | P2 | S3.62 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S5.34 | P2 | S3.62 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S5.34 | P2 | S3.62 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S5.34 | P2 | S3.62 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S5.34 | P2 | S4.68 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P2 | S4.68 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S5.34 | P2 | S4.68 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S5.34 | P2 | S4.68 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S5.34 | P2 | S4.68 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S5.34 | P2 | S4.68 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S5.34 | P4 | S1.57 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S5.34 | P4 | S1.57 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P4 | S1.57 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S5.34 | P4 | S1.57 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S5.34 | P4 | S1.57 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S5.34 | P4 | S1.57 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S5.34 | P4 | S2.35 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S5.34 | P4 | S2.35 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P4 | S2.35 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S5.34 | P4 | S2.35 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S5.34 | P4 | S2.35 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S5.34 | P4 | S2.35 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S5.34 | P4 | S3.62 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S5.34 | P4 | S3.62 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P4 | S3.62 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S5.34 | P4 | S3.62 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S5.34 | P4 | S3.62 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S5.34 | P4 | S3.62 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S5.34 | P4 | S4.68 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S5.34 | P4 | S4.68 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P4 | S4.68 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S5.34 | P4 | S4.68 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S5.34 | P4 | S4.68 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S5.34 | P4 | S4.68 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S5.34 | P4 | S5.34 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S5.34 | P6 | S1.57 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S5.34 | P6 | S1.57 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S5.34 | P6 | S1.57 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P6 | S1.57 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S5.34 | P6 | S1.57 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S5.34 | P6 | S1.57 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S5.34 | P6 | S2.35 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S5.34 | P6 | S2.35 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S5.34 | P6 | S2.35 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P6 | S2.35 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S5.34 | P6 | S2.35 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S5.34 | P6 | S2.35 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S5.34 | P6 | S3.62 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S5.34 | P6 | S3.62 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S5.34 | P6 | S3.62 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P6 | S3.62 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S5.34 | P6 | S3.62 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S5.34 | P6 | S3.62 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S5.34 | P6 | S4.68 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S5.34 | P6 | S4.68 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S5.34 | P6 | S4.68 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P6 | S4.68 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S5.34 | P6 | S4.68 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S5.34 | P6 | S4.68 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S5.34 | P6 | S5.34 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S5.34 | P6 | S5.34 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S5.34 | P8 | S1.57 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S5.34 | P8 | S1.57 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S5.34 | P8 | S1.57 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S5.34 | P8 | S1.57 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P8 | S1.57 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S5.34 | P8 | S1.57 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S5.34 | P8 | S2.35 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S5.34 | P8 | S2.35 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S5.34 | P8 | S2.35 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S5.34 | P8 | S2.35 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P8 | S2.35 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S5.34 | P8 | S2.35 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S5.34 | P8 | S3.62 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S5.34 | P8 | S3.62 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S5.34 | P8 | S3.62 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S5.34 | P8 | S3.62 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P8 | S3.62 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S5.34 | P8 | S3.62 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S5.34 | P8 | S4.68 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S5.34 | P8 | S4.68 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S5.34 | P8 | S4.68 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S5.34 | P8 | S4.68 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P8 | S4.68 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S5.34 | P8 | S4.68 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S5.34 | P8 | S5.34 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S5.34 | P8 | S5.34 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S5.34 | P8 | S5.34 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S5.34 | P10 | S1.57 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S5.34 | P10 | S1.57 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S5.34 | P10 | S1.57 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S5.34 | P10 | S1.57 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S5.34 | P10 | S1.57 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P10 | S1.57 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S5.34 | P10 | S2.35 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S5.34 | P10 | S2.35 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S5.34 | P10 | S2.35 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S5.34 | P10 | S2.35 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S5.34 | P10 | S2.35 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P10 | S2.35 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S5.34 | P10 | S3.62 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S5.34 | P10 | S3.62 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S5.34 | P10 | S3.62 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S5.34 | P10 | S3.62 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S5.34 | P10 | S3.62 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P10 | S3.62 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S5.34 | P10 | S4.68 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S5.34 | P10 | S4.68 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S5.34 | P10 | S4.68 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S5.34 | P10 | S4.68 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S5.34 | P10 | S4.68 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P10 | S4.68 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S5.34 | P10 | S5.34 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S5.34 | P10 | S5.34 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S5.34 | P10 | S5.34 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S5.34 | P10 | S5.34 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S5.34 | P12 | S1.57 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S5.34 | P12 | S1.57 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S5.34 | P12 | S1.57 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S5.34 | P12 | S1.57 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S5.34 | P12 | S1.57 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S5.34 | P12 | S1.57 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P12 | S2.35 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S5.34 | P12 | S2.35 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S5.34 | P12 | S2.35 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S5.34 | P12 | S2.35 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S5.34 | P12 | S2.35 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S5.34 | P12 | S2.35 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P12 | S3.62 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S5.34 | P12 | S3.62 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S5.34 | P12 | S3.62 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S5.34 | P12 | S3.62 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S5.34 | P12 | S3.62 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S5.34 | P12 | S3.62 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P12 | S4.68 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S5.34 | P12 | S4.68 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S5.34 | P12 | S4.68 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S5.34 | P12 | S4.68 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S5.34 | P12 | S4.68 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S5.34 | P12 | S4.68 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S5.34 | P12 | S5.34 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S5.34 | P12 | S5.34 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S5.34 | P12 | S5.34 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S5.34 | P12 | S5.34 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S5.34 | P12 | S5.34 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S6.26 | P2 | S1.57 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P2 | S1.57 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S6.26 | P2 | S1.57 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S6.26 | P2 | S1.57 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S6.26 | P2 | S1.57 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S6.26 | P2 | S1.57 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S6.26 | P2 | S2.35 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P2 | S2.35 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S6.26 | P2 | S2.35 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S6.26 | P2 | S2.35 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S6.26 | P2 | S2.35 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S6.26 | P2 | S2.35 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S6.26 | P2 | S3.62 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P2 | S3.62 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S6.26 | P2 | S3.62 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S6.26 | P2 | S3.62 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S6.26 | P2 | S3.62 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S6.26 | P2 | S3.62 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S6.26 | P2 | S4.68 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P2 | S4.68 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S6.26 | P2 | S4.68 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S6.26 | P2 | S4.68 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S6.26 | P2 | S4.68 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S6.26 | P2 | S4.68 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S6.26 | P2 | S5.34 | P2 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P2 | S5.34 | P4 | -0.046 | 0.01347 | -3.41601 | 0.52041 | 0.05 | 0 | -0.10071 | 0.00871 |
| S6.26 | P2 | S5.34 | P6 | -0.088 | 0.01347 | -6.53497 | 6.46977E-7 | 0.05 | 1 | -0.14271 | -0.03329 |
| S6.26 | P2 | S5.34 | P8 | -0.172 | 0.01347 | -12.7729 | 1.17301E-22 | 0.05 | 1 | -0.22671 | -0.11729 |
| S6.26 | P2 | S5.34 | P10 | -0.258 | 0.01347 | -19.15935 | 1.21031E-38 | 0.05 | 1 | -0.31271 | -0.20329 |
| S6.26 | P2 | S5.34 | P12 | -0.334 | 0.01347 | -24.8032 | 4.81764E-51 | 0.05 | 1 | -0.38871 | -0.27929 |
| S6.26 | P4 | S1.57 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S6.26 | P4 | S1.57 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P4 | S1.57 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S6.26 | P4 | S1.57 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S6.26 | P4 | S1.57 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S6.26 | P4 | S1.57 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S6.26 | P4 | S2.35 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S6.26 | P4 | S2.35 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P4 | S2.35 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S6.26 | P4 | S2.35 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S6.26 | P4 | S2.35 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S6.26 | P4 | S2.35 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S6.26 | P4 | S3.62 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S6.26 | P4 | S3.62 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P4 | S3.62 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S6.26 | P4 | S3.62 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S6.26 | P4 | S3.62 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S6.26 | P4 | S3.62 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S6.26 | P4 | S4.68 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S6.26 | P4 | S4.68 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P4 | S4.68 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S6.26 | P4 | S4.68 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S6.26 | P4 | S4.68 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S6.26 | P4 | S4.68 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S6.26 | P4 | S5.34 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S6.26 | P4 | S5.34 | P4 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P4 | S5.34 | P6 | -0.042 | 0.01347 | -3.11896 | 1 | 0.05 | 0 | -0.09671 | 0.01271 |
| S6.26 | P4 | S5.34 | P8 | -0.126 | 0.01347 | -9.35689 | 9.44604E-14 | 0.05 | 1 | -0.18071 | -0.07129 |
| S6.26 | P4 | S5.34 | P10 | -0.212 | 0.01347 | -15.74335 | 2.60816E-30 | 0.05 | 1 | -0.26671 | -0.15729 |
| S6.26 | P4 | S5.34 | P12 | -0.288 | 0.01347 | -21.38719 | 9.58445E-44 | 0.05 | 1 | -0.34271 | -0.23329 |
| S6.26 | P4 | S6.26 | P2 | 0.046 | 0.01347 | 3.41601 | 0.52041 | 0.05 | 0 | -0.00871 | 0.10071 |
| S6.26 | P6 | S1.57 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S6.26 | P6 | S1.57 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S6.26 | P6 | S1.57 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P6 | S1.57 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S6.26 | P6 | S1.57 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S6.26 | P6 | S1.57 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S6.26 | P6 | S2.35 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S6.26 | P6 | S2.35 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S6.26 | P6 | S2.35 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P6 | S2.35 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S6.26 | P6 | S2.35 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S6.26 | P6 | S2.35 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S6.26 | P6 | S3.62 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S6.26 | P6 | S3.62 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S6.26 | P6 | S3.62 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P6 | S3.62 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S6.26 | P6 | S3.62 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S6.26 | P6 | S3.62 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S6.26 | P6 | S4.68 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S6.26 | P6 | S4.68 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S6.26 | P6 | S4.68 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P6 | S4.68 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S6.26 | P6 | S4.68 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S6.26 | P6 | S4.68 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S6.26 | P6 | S5.34 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S6.26 | P6 | S5.34 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S6.26 | P6 | S5.34 | P6 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P6 | S5.34 | P8 | -0.084 | 0.01347 | -6.23793 | 2.93585E-6 | 0.05 | 1 | -0.13871 | -0.02929 |
| S6.26 | P6 | S5.34 | P10 | -0.17 | 0.01347 | -12.62438 | 2.87099E-22 | 0.05 | 1 | -0.22471 | -0.11529 |
| S6.26 | P6 | S5.34 | P12 | -0.246 | 0.01347 | -18.26822 | 1.58146E-36 | 0.05 | 1 | -0.30071 | -0.19129 |
| S6.26 | P6 | S6.26 | P2 | 0.088 | 0.01347 | 6.53497 | 6.46977E-7 | 0.05 | 1 | 0.03329 | 0.14271 |
| S6.26 | P6 | S6.26 | P4 | 0.042 | 0.01347 | 3.11896 | 1 | 0.05 | 0 | -0.01271 | 0.09671 |
| S6.26 | P8 | S1.57 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S6.26 | P8 | S1.57 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S6.26 | P8 | S1.57 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S6.26 | P8 | S1.57 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P8 | S1.57 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S6.26 | P8 | S1.57 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S6.26 | P8 | S2.35 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S6.26 | P8 | S2.35 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S6.26 | P8 | S2.35 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S6.26 | P8 | S2.35 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P8 | S2.35 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S6.26 | P8 | S2.35 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S6.26 | P8 | S3.62 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S6.26 | P8 | S3.62 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S6.26 | P8 | S3.62 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S6.26 | P8 | S3.62 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P8 | S3.62 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S6.26 | P8 | S3.62 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S6.26 | P8 | S4.68 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S6.26 | P8 | S4.68 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S6.26 | P8 | S4.68 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S6.26 | P8 | S4.68 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P8 | S4.68 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S6.26 | P8 | S4.68 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S6.26 | P8 | S5.34 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S6.26 | P8 | S5.34 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S6.26 | P8 | S5.34 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S6.26 | P8 | S5.34 | P8 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P8 | S5.34 | P10 | -0.086 | 0.01347 | -6.38645 | 1.38445E-6 | 0.05 | 1 | -0.14071 | -0.03129 |
| S6.26 | P8 | S5.34 | P12 | -0.162 | 0.01347 | -12.03029 | 1.03587E-20 | 0.05 | 1 | -0.21671 | -0.10729 |
| S6.26 | P8 | S6.26 | P2 | 0.172 | 0.01347 | 12.7729 | 1.17301E-22 | 0.05 | 1 | 0.11729 | 0.22671 |
| S6.26 | P8 | S6.26 | P4 | 0.126 | 0.01347 | 9.35689 | 9.44604E-14 | 0.05 | 1 | 0.07129 | 0.18071 |
| S6.26 | P8 | S6.26 | P6 | 0.084 | 0.01347 | 6.23793 | 2.93585E-6 | 0.05 | 1 | 0.02929 | 0.13871 |
| S6.26 | P10 | S1.57 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S6.26 | P10 | S1.57 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S6.26 | P10 | S1.57 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S6.26 | P10 | S1.57 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S6.26 | P10 | S1.57 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P10 | S1.57 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S6.26 | P10 | S2.35 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S6.26 | P10 | S2.35 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S6.26 | P10 | S2.35 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S6.26 | P10 | S2.35 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S6.26 | P10 | S2.35 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P10 | S2.35 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S6.26 | P10 | S3.62 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S6.26 | P10 | S3.62 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S6.26 | P10 | S3.62 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S6.26 | P10 | S3.62 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S6.26 | P10 | S3.62 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P10 | S3.62 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S6.26 | P10 | S4.68 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S6.26 | P10 | S4.68 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S6.26 | P10 | S4.68 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S6.26 | P10 | S4.68 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S6.26 | P10 | S4.68 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P10 | S4.68 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S6.26 | P10 | S5.34 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S6.26 | P10 | S5.34 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S6.26 | P10 | S5.34 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S6.26 | P10 | S5.34 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S6.26 | P10 | S5.34 | P10 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P10 | S5.34 | P12 | -0.076 | 0.01347 | -5.64384 | 5.3842E-5 | 0.05 | 1 | -0.13071 | -0.02129 |
| S6.26 | P10 | S6.26 | P2 | 0.258 | 0.01347 | 19.15935 | 1.21031E-38 | 0.05 | 1 | 0.20329 | 0.31271 |
| S6.26 | P10 | S6.26 | P4 | 0.212 | 0.01347 | 15.74335 | 2.60816E-30 | 0.05 | 1 | 0.15729 | 0.26671 |
| S6.26 | P10 | S6.26 | P6 | 0.17 | 0.01347 | 12.62438 | 2.87099E-22 | 0.05 | 1 | 0.11529 | 0.22471 |
| S6.26 | P10 | S6.26 | P8 | 0.086 | 0.01347 | 6.38645 | 1.38445E-6 | 0.05 | 1 | 0.03129 | 0.14071 |
| S6.26 | P12 | S1.57 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S6.26 | P12 | S1.57 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S6.26 | P12 | S1.57 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S6.26 | P12 | S1.57 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S6.26 | P12 | S1.57 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S6.26 | P12 | S1.57 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P12 | S2.35 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S6.26 | P12 | S2.35 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S6.26 | P12 | S2.35 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S6.26 | P12 | S2.35 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S6.26 | P12 | S2.35 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S6.26 | P12 | S2.35 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P12 | S3.62 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S6.26 | P12 | S3.62 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S6.26 | P12 | S3.62 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S6.26 | P12 | S3.62 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S6.26 | P12 | S3.62 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S6.26 | P12 | S3.62 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P12 | S4.68 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S6.26 | P12 | S4.68 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S6.26 | P12 | S4.68 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S6.26 | P12 | S4.68 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S6.26 | P12 | S4.68 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S6.26 | P12 | S4.68 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P12 | S5.34 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S6.26 | P12 | S5.34 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S6.26 | P12 | S5.34 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S6.26 | P12 | S5.34 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S6.26 | P12 | S5.34 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |
| S6.26 | P12 | S5.34 | P12 | 0 | 0.01347 | 0 | 1 | 0.05 | 0 | -0.05471 | 0.05471 |
| S6.26 | P12 | S6.26 | P2 | 0.334 | 0.01347 | 24.8032 | 4.81764E-51 | 0.05 | 1 | 0.27929 | 0.38871 |
| S6.26 | P12 | S6.26 | P4 | 0.288 | 0.01347 | 21.38719 | 9.58445E-44 | 0.05 | 1 | 0.23329 | 0.34271 |
| S6.26 | P12 | S6.26 | P6 | 0.246 | 0.01347 | 18.26822 | 1.58146E-36 | 0.05 | 1 | 0.19129 | 0.30071 |
| S6.26 | P12 | S6.26 | P8 | 0.162 | 0.01347 | 12.03029 | 1.03587E-20 | 0.05 | 1 | 0.10729 | 0.21671 |
| S6.26 | P12 | S6.26 | P10 | 0.076 | 0.01347 | 5.64384 | 5.3842E-5 | 0.05 | 1 | 0.02129 | 0.13071 |

Sig equals one (σ=1) indicates that at 0.05 level, the difference of the means is significant, whereas Sig equals zero (σ=0) suggests that the difference of the means is not significant.

Additionally, at α (0.05) level of variance, this means comparison graphically illustrated in Figure 6.

a) Cutting speed.                                                          b) Laser power.

b) Interaction.

Figure 6. Graphic of the means comparison test.

References

Gong Y. An On-line Learning and Training Tool for Laser Cutting. University of Manchester, 2014.

Yang C, Jiang T, Yu Y, Dun G, Ma Y, Liu J. Study on the surface quality of wood processed by water-jet assisted nanosecond laser. BioResources 2018;13:3125–34. https://doi.org/10.15376/biores.13.2.3125-3134.

Jiang T, Yang C, Yu Y, S. Doumbia B, Liu J, Ma Y. Prediction and Analysis of Surface Quality of Northeast China Ash Wood during Water-Jet Assisted CO2 Laser Cutting. J Renew Mater 2021;9:119–28. https://doi.org/10.32604/jrm.2021.011490.

GABZDVL JT. THE EFFECT OF LASER MODE AND COAXIAL GAS JET ON LASER CUTTING . JACEK TADEUSZ GABZDVL A thesis presented for the Degree of Doctor of Philosophy of the University of London . September 1989 John Percy Research Group Royal School of Mines Imperial College o. 1989.