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Table S1: Efficacy of Nanocomposite A at 20 mg/ml against biofilm developed for 24 hours at 37 °C
	Bacterial Strain
	Surface
	No. of surviving cells before treatment (CFU/ml)
	No. of surviving cells after treatment(CFU/ml)
	LR (log reduction)
	% SF
	% Killed

	E.coli 
	Glass
	6.23 x108
	5.15 x108
	0.08270
	82.66
	17.34

	Klebsiella spp. 
	Glass
	6.13 x108
	4.01 x108
	0.18428
	65.42
	34.58

	Pseudomonas spp.
	Glass
	6.39 x108

	6.01 x108

	0.02664
	94.05
	5.95

	Staphylococcus aureus 
	Glass
	6.88 x108
	3.69 x108
	0.27059
	53.63
	46.37



Table S2: Efficacy of Nanocomposite A at 30 mg/ml against biofilm developed for 24 hours at 37 °C.
	Bacterial Strain
	Surface
	No. of surviving cells before treatment (CFU/ml)
	No. of surviving cells after treatment (CFU/ml)
	LR (log reduction)
	% SF
	% Killed

	E.coli 
	Glass
	6.23 x108
	4.25 x108
	0.16608
	68.22
	31.78

	Klebsiella spp. 
	Glass
	6.13 x108
	3.00 x108
	0.31033
	48.94
	51.06

	Pseudomonas spp.
	Glass
	6.39 x108

	5.10 x108
	0.09794
	79.81
	20.19

	Staphylococcus aureus 
	Glass
	6.88 x108
	2.09 x108
	0.51741
	30.38
	69.62



Table S3: Efficacy of Nanocomposite B at 5 mg/ml against Biofilm developed for 24 hours at 37 °C. 
	Bacterial Strain
	Surface
	No. of surviving cells before treatment (CFU/ml)
	No. of surviving cells after treatment (CFU/ml)
	LR (log reduction)
	%SF
	%
Killed

	Pseudomonas spp.
	Glass
	6.39 x108

	5.79 x108
	0.0428238
	90.61
	9.39

	Staphylococcus aureus 
	Glass
	6.88 x108
	6.39 x108
	0.0320777
	92.88
	7.12



Table S4: Efficacy of Nanocomposite B at 20 mg/ml against Biofilm developed for 24 hours at 37 °C. 
	Bacterial Strain
	Surface
	No. of surviving cells before treatment (CFU/ml)
	No. of surviving cells after treatment
(CFU/ml)
	LR (log reduction)
	%SF
	%
Killed

	E.coli 
	Glass
	6.23 x108
	5.65 x108
	0.0424406
	90.69
	9.31

	Klebsiella spp. 
	Glass
	6.13 x108
	4.26 x108
	0.1580776
	69.49
	30.51

	Pseudomonas spp.
	Glass
	6.39 x108
	5.09 x108
	0.0987597
	79.66
	20.34

	Staphylococcus aureus 
	Glass
	6.88 x108
	2.39 x108
	0.4591701
	34.74
	65.26



Table S5: Efficacy of Nanocomposite B at 30 mg/ml against Biofilm developed for 24 hours at 37 °C. 
	Bacterial Strain
	Surface
	No. of surviving cells before treatment (CFU/ml)
	No. of surviving cells after treatment
(CFU/ml)
	LR
(log reduction)
	%SF
	%
Killed

	E.coli 
	Glass
	6.23 x108
	4.55 x108
	0.1364987
	73.03
	26.97

	Klebsiella spp. 
	Glass
	6.13 x108
	4.00 x108
	0.1854194
	65.25
	34.75

	Pseudomonas spp.
	Glass
	6.39 x108
	4.10 x108
	0.1927356
	64.16
	35.84

	Staphylococcus aureus 
	Glass
	6.88 x108
	1.20 x108
	0.7584535
	17.44
	82.56
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