Supplementary materials for Intrinsic electro-optical and thermodynamic properties of 4,4′-Bis(N-carbazolyl)-1,1′-biphenyl (CBP) as a potential candidate for nonlinear optical applications: A DFT investigation

Pierre Ferdinand Bissi Nyandoua, Ali Raza Ayubb, Patrick Noudema, Côme Damien Désiré Mvemec, David Fouejioa, Serge Sylvain Zekenga*

aMechanic, Materials and Complex Structures Laboratory, Department of Physics, Faculty of Science, University of Yaounde I, P.O. Box 812, Yaounde, Cameroon

bKey Laboratory of Clusters Science of Ministry of Education, School of Chemistry and Chemical Engineering, Beijing Institute of Technology, Beijing, 100081, P. R. China

cMaterials Science Laboratory, Department of Physics, Faculty of Science, University of Maroua, P.O. Box 814, Maroua, Cameroon

M06-2X

ωB97XD

Figure S1: Optimized structure of CBP using M06-2X, and ωB97XD functionals

Table S1: Bond lengths (Å) in the CBP molecule

|  | B3LYP | M06-2X | ωB97XD | Expa |
| --- | --- | --- | --- | --- |
| C1-C2 | 1.40 | 1.40 | 1.40 | 1.40 |
| C1-C6 | 1.38 | 1.38 | 1.38 | 1.37 |
| C1-H7 | 1.08 | 1.08 | 1.08 | 0.95 |
| C2-C3 | 1.39 | 1.38 | 1.38 | 1.38 |
| C2-H8 | 1.08 | 1.08 | 1.08 | 1.03 |
| C3-C4 | 1.39 | 1.39 | 1.39 | 1.39 |
| C3-H9 | 1.08 | 1.08 | 1.08 | 0.98 |
| C4-C5 | 1.41 | 1.41 | 1.40 | 1.41 |
| C4-N58 | 1.39 | 1.39 | 1.39 | 1.40 |
| C5-C6 | 1.39 | 1.39 | 1.39 | 1.38 |
| C5-C15 | 1.44 | 1.44 | 1.44 | 1.44 |
| C6-H10 | 1.08 | 1.08 | 1.08 | 0.97 |
| C11-C12 | 1.39 | 1.39 | 1.39 | 1.39 |
| C11-C15 | 1.41 | 1.41 | 1.40 | 1.41 |
| C11-N58 | 1.39 | 1.39 | 1.39 | 1.39 |
| C12-C13 | 1.39 | 1.38 | 1.38 | 139 |
| C12-H16 | 1.08 | 1.08 | 1.08 | 0.99 |
| C13-C14 | 1.40 | 1.40 | 1.40 | 1.40 |
| C13-H17 | 1.08 | 1.08 | 1.08 | 1.00 |
| C14-H18 | 1.08 | 1.08 | 1.08 | 0.98 |
| C14-C59 | 1.38 | 1.38 | 1.38 | 1.37 |
| C15-C59 | 1.39 | 1.39 | 1.39 | 1.39 |
| C19-C20 | 1.39 | 1.39 | 1.39 | 1.39 |
| C19-C23 | 1.39 | 1.39 | 1.39 | 1.38 |
| C19-N58 | 1.41 | 1.41 | 1.41 | 1.41 |
| C20-H31 | 1.08 | 1.08 | 1.08 | 0.96 |
| C20-C61 | 1.38 | 1.38 | 1.38 | 1.38 |
| C21-C22 | 1.40 | 1.39 | 1.39 | 1.39 |
| C21-C24 | 1.48 | 1.48 | 1.48 | 1.48 |
| C21-C61 | 1.40 | 1.39 | 1.39 | 1.39 |
| C22-C23 | 1.38 | 1.38 | 1.38 | 1.38 |
| C22-H32 | 1.08 | 1.08 | 1.08 | 0.99 |
| C23-H33 | 1.08 | 1.08 | 1.08 | 0.95 |
| C24-C25 | 1.40 | 1.39 | 1.39 | 1.39 |
| C24-C30 | 1.40 | 1.39 | 1.39 | 1.39 |
| C25-C26 | 1.38 | 1.38 | 1.38 | 1.38 |
| C25-H56 | 1.08 | 1.08 | 1.08 | 0.99 |
| C26-H27 | 1.08 | 1.08 | 1.08 | 0.95 |
| C26-C28 | 1.39 | 1.39 | 1.39 | 1.38 |
| C28-C29 | 1.39 | 1.39 | 1.39 | 1.39 |
| C28-N57 | 1.42 | 1.41 | 1.41 | 1.41 |
| C29-C30 | 1.38 | 1.38 | 1.38 | 1.38 |
| C29-H34 | 1.08 | 1.08 | 1.08 | 0.96 |
| C30-H35 | 1.08 | 1.08 | 1.08 | 0.98 |
| C36-C37 | 1.40 | 1.40 | 1.40 | 1.40 |
| C36-C41 | 1.38 | 1.38 | 1.38 | 1.37 |
| C36-H42 | 1.08 | 1.08 | 1.08 | 0.98 |
| C37-C38 | 1.39 | 1.38 | 1.38 | 1.39 |
| C37-H43 | 1.08 | 1.08 | 1.08 | 1.00 |
| C38-C39 | 1.39 | 1.39 | 1.39 | 1.39 |
| C38-H44 | 1.08 | 1.08 | 1.08 | 0.99 |
| C39-C40 | 1.41 | 1.41 | 1.40 | 1.41 |
| C39-N57 | 1.39 | 1.39 | 1.39 | 1.39 |
| C40-C41 | 1.39 | 1.39 | 1.39 | 1.39 |
| C40-C51 | 1.44 | 1.44 | 1.44 | 1.44 |
| C41-H45 | 1.08 | 1.08 | 1.08 | 0.98 |
| C46-C47 | 1.39 | 1.39 | 1.39 | 1.39 |
| C46-C51 | 1.41 | 1.41 | 1.40 | 1.41 |
| C46-N57 | 1.39 | 1.39 | 1.39 | 1.40 |
| C47-C48 | 1.39 | 1.38 | 1.38 | 1.38 |
| C47-H52 | 1.08 | 1.08 | 1.08 | 0.98 |
| C48-C49 | 1.40 | 1.40 | 1.40 | 1.40 |
| C48-H53 | 1.08 | 1.08 | 1.08 | 1.03 |
| C49-C50 | 1.38 | 1.38 | 1.38 | 1.37 |
| C49-H54 | 1.08 | 1.08 | 1.08 | 0.95 |
| C50-C51 | 1.39 | 1.39 | 1.39 | 1.38 |
| C50-H55 | 1.08 | 1.08 | 1.08 | 0.97 |
| C59-H60 | 1.08 | 1.08 | 1.08 | 0.98 |
| C61-H62 | 1.08 | 1.08 | 1.08 | 0.98 |

(a) Experimental data for bonds lengths [1]

Table S2: Angles (°) of valence in the CBP molecule

|  | B3LYP | M06-2X | ωB97XD | Exp(a) |
| --- | --- | --- | --- | --- |
| A(C2,C1,C6) | 120.56 | 120.58 | 120.57 | 120.77 |
| A(C2,C1,H7) | 119.54 | 119.49 | 119.52 | 117.4 |
| A(C6,C1,H7) | 119.88 | 119.91 | 119.90 | 121.8 |
| A(C1,C2,C3) | 121.43 | 121.56 | 121.49 | 121.47 |
| A(C1,C2,H8) | 119.44 | 119.35 | 119.38 | 118.5 |
| A(C3,C2,H8) | 119.11 | 119.07 | 119.11 | 120.0 |
| A(C2,C3,C4) | 117.76 | 117.50 | 117.58 | 117.42 |
| A(C2,C3,H9) | 120.88 | 121.18 | 121.12 | 121.0 |
| A(C4,C3,H9) | 121.34 | 121.30 | 121.29 | 121.6 |
| A(C3,C4,C5) | 121.53 | 121.66 | 121.64 | 121.58 |
| A(C3,C4,N58) | 129.51 | 129.36 | 129.33 | 129.55 |
| A(C5,C4,N58) | 108.92 | 108.94 | 109.00 | 108.76 |
| A(C4,C5,C6) | 119.50 | 119.65 | 119.66 | 119.32 |
| A(C4,C5,C15) | 106.87 | 106.77 | 106.74 | 106.89 |
| A(C6,C5,C15) | 133.62 | 133.56 | 133.58 | 133.75 |
| A(C1,C6,C5) | 119.18 | 119.01 | 119.03 | 119.42 |
| A(C1,C6,H10) | 120.42 | 120.65 | 120.60 | 120.6 |
| A(C5,C6,H10) | 120.39 | 120.33 | 120.36 | 120.0 |
| A(C12,C11,C15) | 121.53 | 121.66 | 121.64 | 121.43 |
| A(C12,C11,N58) | 129.51 | 129.36 | 129.33 | 129.46 |
| A(C15,C11,N58) | 108.92 | 108.94 | 109.00 | 109.11 |
| A(C11,C12,C13) | 117.76 | 117.50 | 117.58 | 117.41 |
| A(C11,C12,H16) | 121.34 | 121.30 | 121.29 | 119.8 |
| A(C13,C12,H16) | 120.88 | 121.18 | 121.12 | 122.7 |
| A(C12,C13,C14) | 121.43 | 121.56 | 121.49 | 121.76 |
| A(C12,C13,H17) | 119.11 | 119.07 | 119.11 | 118.5 |
| A(C14,C13,H17) | 119.44 | 119.35 | 119.38 | 119.7 |
| A(C13,C14,H18) | 119.54 | 119.49 | 119.52 | 121.7 |
| A(C13,C14,C59) | 120.56 | 120.58 | 120.57 | 120.20 |
| A(H18,C14,C59) | 119.88 | 119.91 | 119.90 | 118.0 |
| A(C5,C15,C11) | 106.87 | 106.77 | 106.74 | 107.14 |
| A(C5,C15,C59) | 133.62 | 133.56 | 133.58 | 133.29 |
| A(C11,C15,C59) | 119.50 | 119.65 | 119.66 | 119.51 |
| A(C20,C19,C23) | 119.20 | 119.68 | 119.61 | 118.81 |
| A(C20,C19,N58) | 120.40 | 120.15 | 120.18 | 120.30 |
| A(C23,C19,N58) | 120.39 | 120.15 | 120.19 | 120.88 |
| A(C19,C20,H31) | 119.46 | 119.28 | 119.38 | 118.3 |
| A(C19,C20,C61) | 120.22 | 119.95 | 120.01 | 119.93 |
| A(H31,C20,C61) | 120.30 | 120.74 | 120.59 | 121.8 |
| A(C22,C21,C24) | 121.08 | 120.82 | 120.85 | 121.56 |
| A(C22,C21,C61) | 117.81 | 118.34 | 118.29 | 116.71 |
| A(C24,C21,C61) | 121.10 | 120.83 | 120.85 | 121.73 |
| A(C21,C22,C23) | 121.26 | 121.02 | 121.02 | 121.80 |
| A(C21,C22,H32) | 119.57 | 119.48 | 119.57 | 119.8 |
| A(C23,C22,H32) | 119.11 | 119.44 | 119.36 | 118.2 |
| A(C19,C23,C22) | 120.22 | 119.95 | 120.01 | 120.54 |
| A(C19,C23,H33) | 119.46 | 119.28 | 119.38 | 118.5 |
| A(C22,C23,H33) | 120.30 | 120.74 | 120.58 | 121.0 |
| A(C21,C24,C25) | 121.09 | 120.82 | 120.85 | 121.56 |
| A(C21,C24,C30) | 121.08 | 120.81 | 120.85 | 121.73 |
| A(C25,C24,C30) | 117.81 | 118.35 | 118.29 | 116.71 |
| A(C24,C25,C26) | 121.26 | 121.01 | 121.02 | 121.80 |
| A(C24,C25,H56) | 119.59 | 119.50 | 119.59 | 119.8 |
| A(C26,C25,H56) | 119.13 | 119.47 | 119.38 | 118.2 |
| A(C25,C26,H27) | 120.30 | 120.76 | 120.59 | 121.0 |
| A(C25,C26,C28) | 120.21 | 119.94 | 120.00 | 120.54 |
| A(H27,C26,C28) | 119.47 | 119.29 | 119.39 | 118.5 |
| A(C26,C28,C29) | 119.22 | 119.71 | 119.62 | 118.81 |
| A(C26,C28,N57) | 120.38 | 120.14 | 120.18 | 120.88 |
| A(C29,C28,N57) | 120.38 | 120.14 | 120.19 | 120.30 |
| A(C28,C29,C30) | 120.21 | 119.94 | 120.00 | 119.93 |
| A(C28,C29,H34) | 119.47 | 119.29 | 119.39 | 118.3 |
| A(C30,C29,H34) | 120.31 | 120.76 | 120.59 | 121.8 |
| A(C24,C30,C29) | 121.26 | 121.01 | 121.02 | 122.18 |
| A(C24,C30,H35) | 119.59 | 119.50 | 119.59 | 119.6 |
| A(C29,C30,H35) | 119.14 | 119.47 | 119.38 | 118.2 |
| A(C37,C36,C41) | 120.57 | 120.59 | 120.57 | 120.20 |
| A(C37,C36,H42) | 119.54 | 119.48 | 119.51 | 121.7 |
| A(C41,C36,H42) | 119.88 | 119.91 | 119.90 | 118.0 |
| A(C36,C37,C38) | 121.43 | 121.56 | 121.49 | 121.76 |
| A(C36,C37,H43) | 119.44 | 119.35 | 119.38 | 119.7 |
| A(C38,C37,H43) | 119.11 | 119.07 | 119.11 | 118.5 |
| A(C37,C38,C39) | 117.75 | 117.49 | 117.57 | 117.41 |
| A(C37,C38,H44) | 120.89 | 121.19 | 121.12 | 122.7 |
| A(C39,C38,H44) | 121.35 | 121.31 | 121.30 | 119.8 |
| A(C38,C39,C40) | 121.54 | 121.67 | 121.65 | 121.43 |
| A(C38,C39,N57) | 129.50 | 129.35 | 129.32 | 129.46 |
| A(C40,C39,N57) | 108.92 | 108.93 | 108.99 | 109.11 |
| A(C39,C40,C41) | 119.49 | 119.64 | 119.65 | 119.51 |
| A(C39,C40,C51) | 106.86 | 106.77 | 106.741 | 107.14 |
| A(C41,C40,C51) | 133.63 | 133.57 | 133.59 | 133.29 |
| A(C36,C41,C40) | 119.18 | 119.01 | 119.03 | 199.66 |
| A(C36,C41,H45) | 120.42 | 120.65 | 120.60 | 120.5 |
| A(C40,C41,H45) | 120.39 | 120.33 | 120.36 | 119.8 |
| A(C47,C46,C51) | 121.54 | 121.67 | 121.65 | 121.58 |
| A(C47,C46,N57) | 129.50 | 129.35 | 129.32 | 129.55 |
| A(C51,C46,N57) | 108.92 | 108.93 | 108.99 | 108.76 |
| A(C46,C47,C48) | 117.75 | 117.49 | 117.56 | 117.42 |
| A(C46,C47,H52) | 121.35 | 121.31 | 121.30 | 121.6 |
| A(C48,C47,H52) | 120.89 | 121.18 | 121.12 | 121.0 |
| A(C47,C48,C49) | 121.43 | 121.56 | 121.49 | 121.47 |
| A(C47,C48,H53) | 119.11 | 119.07 | 119.11 | 120.0 |
| A(C49,C48,H53) | 119.44 | 119.35 | 119.38 | 118.5 |
| A(C48,C49,C50) | 120.57 | 120.59 | 120.57 | 120.77 |
| A(C48,C49,H54) | 119.54 | 119.48 | 119.51 | 117.4 |
| A(C50,C49,H54) | 119.88 | 119.91 | 119.90 | 121.8 |
| A(C49,C50,C51) | 119.18 | 119.01 | 119.03 | 119.42 |
| A(C49,C50,H55) | 120.42 | 120.65 | 120.60 | 120.6 |
| A(C51,C50,H55) | 120.39 | 120.33 | 120.36 | 120.0 |
| A(C40,C51,C46) | 106.86 | 106.77 | 106.74 | 106.89 |
| A(C40,C51,C50) | 133.63 | 133.57 | 133.60 | 133.75 |
| A(C46,C51,C50) | 119.49 | 119.64 | 119.65 | 119.32 |
| A(C28,N57,C39) | 125.78 | 125.70 | 125.74 | 126.39 |
| A(C28,N57,C46) | 125.79 | 125.70 | 125.73 | 125.13 |
| A(C39,N57,C46) | 108.42 | 108.59 | 108.52 | 108.11 |
| A(C4,N58,C11) | 108.40 | 108.57 | 108.50 | 108.11 |
| A(C4,N58,C19) | 125.79 | 125.71 | 125.75 | 125.13 |
| A(C11,N58,C19) | 125.80 | 125.71 | 125.74 | 126.39 |
| A(C14,C59,C15) | 119.18 | 119.01 | 119.03 | 119.66 |
| A(C14,C59,H60) | 120.42 | 120.65 | 120.60 | 120.5 |
| A(C15,C59,H60) | 120.39 | 120.33 | 120.36 | 119.8 |
| A(C20,C61,C21) | 121.26 | 121.02 | 121.02 | 122.18 |
| A(C20,C61,H62) | 119.11 | 119.43 | 119.36 | 118.2 |
| A(C21,C61,H62) | 119.57 | 119.49 | 119.57 | 119.6 |

(a) Experimental data for angles of valence [1]

Table S3: Atomic charges in the CBP molecule

| Atoms | B3LYP | M06-2X | ωB97XD |
| --- | --- | --- | --- |
| C1 | -0.22 | -0.22 | -0.22 |
| C2 | -0.18 | -0.18 | -0.18 |
| C3 | -0.24 | -0.25 | -0.25 |
| C4 | 0.19 | 0.20 | 0.20 |
| C5 | -0.08 | -0.08 | -0.08 |
| C6 | -0.17 | -0.17 | -0.17 |
| H7 | 0.20 | 0.20 | 0.20 |
| H8 | 0.20 | 0.20 | 0.20 |
| H9 | 0.21 | 0.22 | 0.21 |
| H10 | 0.20 | 0.21 | 0.20 |
| C11 | 0.19 | 0.20 | 0.20 |
| C12 | -0.24 | -0.25 | -0.25 |
| C13 | -0.18 | -0.18 | -0.18 |
| C14 | -0.22 | -0.22 | -0.22 |
| C15 | -0.08 | -0.08 | -0.08 |
| H16 | 0.21 | 0.22 | 0.21 |
| H17 | 0.20 | 0.20 | 0.20 |
| H18 | 0.20 | 0.20 | 0.20 |
| C19 | 0.15 | 0.16 | 0.16 |
| C20 | -0.20 | -0.20 | -0.20 |
| C21 | -0.04 | -0.05 | -0.04 |
| C22 | -0.17 | -0.18 | -0.18 |
| C23 | -0.20 | -0.20 | -0.20 |
| C24 | -0.04 | -0.05 | -0.04 |
| C25 | -0.17 | -0.18 | -0.18 |
| C26 | -0.19 | -0.20 | -0.20 |
| H27 | 0.21 | 0.22 | 0.22 |
| C28 | 0.15 | 0.16 | 0.16 |
| C29 | -0.19 | -0.20 | -0.20 |
| C30 | -0.17 | -0.18 | -0.18 |
| H31 | 0.21 | 0.22 | 0.22 |
| H32 | 0.20 | 0.21 | 0.21 |
| H33 | 0.21 | 0.22 | 0.22 |
| H34 | 0.21 | 0.22 | 0.22 |
| H35 | 0.20 | 0.21 | 0.21 |
| C36 | -0.22 | -0.22 | -0.22 |
| C37 | -0.18 | -0.18 | -0.18 |
| C38 | -0.24 | -0.25 | -0.25 |
| C39 | 0.19 | 0.20 | 0.20 |
| C40 | -0.08 | -0.08 | -0.08 |
| C41 | -0.17 | -0.17 | -0.17 |
| H42 | 0.20 | 0.20 | 0.20 |
| H43 | 0.20 | 0.20 | 0.20 |
| H44 | 0.21 | 0.22 | 0.21 |
| H45 | 0.20 | 0.20 | 0.20 |
| C46 | 0.19 | 0.20 | 0.20 |
| C47 | -0.24 | -0.25 | -0.25 |
| C48 | -0.18 | -0.18 | -0.18 |
| C49 | -0.22 | -0.22 | -0.22 |
| C50 | -0.17 | -0.17 | -0.17 |
| C51 | -0.08 | -0.08 | -0.08 |
| H52 | 0.21 | 0.22 | 0.21 |
| H53 | 0.20 | 0.20 | 0.20 |
| H54 | 0.20 | 0.20 | 0.20 |
| H55 | 0.20 | 0.20 | 0.20 |
| H56 | 0.20 | 0.21 | 0.21 |
| N57 | -0.42 | -0.43 | -0.43 |
| N58 | -0.42 | -0.43 | -0.43 |
| C59 | -0.17 | -0.17 | -0.17 |
| H60 | 0.20 | 0.21 | 0.20 |
| C61 | -0.17 | -0.18 | -0.18 |
| H62 | 0.20 | 0.21 | 0.21 |

Table S4: Second order perturbation theory for CBP using B3LYP/6-311G(d,p)

| Donnor | type | Acceptor | type | E(2) (kcal/mol) | εj-εi(a.u) | Fi,j (a.u) |
| --- | --- | --- | --- | --- | --- | --- |
| C1-C2 | σ | C1-C6 | σ* | 3.02 | 1.27 | 0.055 |
| C1-C2 | σ | C1-H7 | σ* | 1.09 | 1.14 | 0.031 |
| C1-C2 | σ | C2-C3 | σ* | 2.98 | 1.27 | 0.055 |
| C1-C2 | σ | C2-H8 | σ* | 1.07 | 1.14 | 0.031 |
| C1-C2 | σ | C3-H9 | σ* | 2.48 | 1.13 | 0.047 |
| C1-C2 | σ | C6-H10 | σ* | 2.51 | 1.13 | 0.048 |
| C1-C6 | σ | C1-C2 | σ* | 2.95 | 1.26 | 0.055 |
| C1-C6 | σ | C1-H7 | σ* | 1.17 | 1.14 | 0.033 |
| C1-C6 | σ | C2-H8 | σ* | 2.20 | 1.14 | 0.045 |
| C1-C6 | σ | C5-C6 | σ* | 3.76 | 1.27 | 0.062 |
| C1-C6 | σ | C5-C15 | σ* | 4.97 | 1.22 | 0.070 |
| C1-C6 | σ | C6-H10 | σ* | 1.20 | 1.14 | 0.033 |
| C1-C6 | π | C2-C3 | π* | 21.10 | 0.28 | 0.069 |
| C1-C6 | π | C4-C5 | π* | 18.10 | 0.28 | 0.067 |
| C1-H7 | σ | C1-C2 | σ* | 0.59 | 1.08 | 0.023 |
| C1-H7 | σ | C1-C6 | σ* | 0.68 | 1.10 | 0.024 |
| C1-H7 | σ | C2-C3 | σ* | 3.97 | 1.09 | 0.059 |
| C1-H7 | σ | C2-H8 | σ* | 0.66 | 0.96 | 0.022 |
| C1-H7 | σ | C5-C6 | σ* | 4.09 | 1.09 | 0.060 |
| C1-H7 | σ | C6-H10 | σ* | 0.66 | 0.95 | 0.022 |
| C2-C3 | σ | C1-C2 | σ* | 2.93 | 1.27 | 0.055 |
| C2-C3 | σ | C1-H7 | σ* | 2.11 | 1.15 | 0.044 |
| C2-C3 | σ | C2-H8 | σ* | 1.03 | 1.14 | 0.031 |
| C2-C3 | σ | C3-C4 | σ* | 4.02 | 1.27 | 0.064 |
| C2-C3 | σ | C3-H9 | σ* | 1.38 | 1.14 | 0.036 |
| C2-C3 | σ | C4-N58 | σ* | 6.32 | 1.13 | 0.075 |
| C2-C3 | π | C1-C6 | π* | 17.44 | 0.29 | 0.064 |
| C2-C3 | π | C4-C5 | π* | 20.65 | 0.28 | 0.072 |
| C2-H8 | σ | C1-C2 | σ* | 0.55 | 1.08 | 0.022 |
| C2-H8 | σ | C1-C6 | σ* | 3.87 | 1.10 | 0.058 |
| C2-H8 | σ | C1-H7 | σ* | 0.67 | 0.96 | 0.023 |
| C2-H8 | σ | C2-C3 | σ* | 0.61 | 1.10 | 0.023 |
| C2-H8 | σ | C3-C4 | σ* | 4.18 | 1.08 | 0.060 |
| C2-H8 | σ | C3-H9 | σ* | 0.65 | 0.96 | 0.022 |
| C3-C4 | σ | C2-C3 | σ* | 3.39 | 1.29 | 0.059 |
| C3-C4 | σ | C2-H8 | σ* | 2.22 | 1.16 | 0.045 |
| C3-C4 | σ | C3-H9 | σ* | 1.42 | 1.15 | 0.036 |
| C3-C4 | σ | C4-C5 | σ* | 5.07 | 1.25 | 0.071 |
| C3-C4 | σ | C4-N58 | σ* | 2.48 | 1.14 | 0.047 |
| C3-C4 | σ | C5-C15 | σ* | 1.69 | 1.23 | 0.041 |
| C3-C4 | σ | C11-N58 | σ* | 2.15 | 1.14 | 0.044 |
| C3-H9 | σ | C1-C2 | σ* | 3.76 | 1.09 | 0.057 |
| C3-H9 | σ | C2-C3 | σ* | 1.04 | 1.10 | 0.030 |
| C3-H9 | σ | C2-H8 | σ* | 0.65 | 0.97 | 0.022 |
| C3-H9 | σ | C3-C4 | σ* | 0.78 | 1.09 | 0.026 |
| C3-H9 | σ | C4-C5 | σ* | 4.55 | 1.06 | 0.062 |
| C4-C5 | σ | C3-C4 | σ* | 4.72 | 1.23 | 0.068 |
| C4-C5 | σ | C3-H9 | σ* | 2.55 | 1.10 | 0.048 |
| C4-C5 | σ | C4-N58 | σ* | 1.22 | 1.09 | 0.033 |
| C4-C5 | σ | C5-C6 | σ* | 3.89 | 1.24 | 0.062 |
| C4-C5 | σ | C5-C15 | σ* | 2.71 | 1.18 | 0.051 |
| C4-C5 | σ | C6-H10 | σ* | 2.53 | 1.10 | 0.047 |
| C4-C5 | σ | C15-C59 | σ* | 5.05 | 1.24 | 0.071 |
| C4-C5 | σ | C19-N58 | σ* | 4.89 | 1.06 | 0.064 |
| C4-C5 | π | C1-C6 | π* | 20.80 | 0.28 | 0.070 |
| C4-C5 | π | C2-C3 | π* | 18.64 | 0.28 | 0.065 |
| C4-C5 | π | C4-C5 | π* | 0.72 | 0.28 | 0.013 |
| C4-C5 | π | C11-C15 | π* | 18.56 | 0.28 | 0.065 |
| C4-N58 | σ | C2-C3 | σ* | 0.91 | 1.36 | 0.031 |
| C4-N58 | σ | C3-C4 | σ* | 2.16 | 1.35 | 0.048 |
| C4-N58 | σ | C4-C5 | σ* | 1.36 | 1.32 | 0.038 |
| C4-N58 | σ | C5-C6 | σ* | 2.40 | 1.36 | 0.051 |
| C4-N58 | σ | C11-C12 | σ* | 3.90 | 1.35 | 0.065 |
| C4-N58 | σ | C11-N58 | σ* | 2.30 | 1.21 | 0.047 |
| C4-N58 | σ | C19-C20 | σ* | 1.18 | 1.33 | 0.035 |
| C4-N58 | σ | C19-C20 | π* | 0.86 | 0.79 | 0.026 |
| C4-N58 | σ | C19-N58 | σ* | 2.64 | 1.18 | 0.050 |
| C5-C6 | σ | C1-C6 | σ* | 3.29 | 1.28 | 0.058 |
| C5-C6 | σ | C1-H7 | σ* | 2.30 | 1.14 | 0.046 |
| C5-C6 | σ | C4-C5 | σ* | 4.58 | 1.23 | 0.067 |
| C5-C6 | σ | C4-N58 | σ* | 2.08 | 1.12 | 0.043 |
| C5-C6 | σ | C5-C15 | σ* | 5.21 | 1.21 | 0.071 |
| C5-C6 | σ | C6-H10 | σ* | 1.20 | 1.13 | 0.033 |
| C5-C6 | σ | C11-C15 | σ* | 0.95 | 1.23 | 0.030 |
| C5-C15 | σ | C1-C6 | σ* | 1.46 | 1.23 | 0.038 |
| C5-C15 | σ | C3-C4 | σ* | 3.99 | 1.22 | 0.062 |
| C5-C15 | σ | C4-C5 | σ* | 2.61 | 1.19 | 0.050 |
| C5-C15 | σ | C4-N58 | σ* | 0.76 | 1.08 | 0.025 |
| C5-C15 | σ | C5-C6 | σ* | 4.61 | 1.22 | 0.067 |
| C5-C15 | σ | C11-C12 | σ* | 3.99 | 1.22 | 0.062 |
| C5-C15 | σ | C11-C15 | σ* | 2.61 | 1.19 | 0.050 |
| C5-C15 | σ | C11-N58 | σ* | 0.76 | 1.08 | 0.025 |
| C5-C15 | σ | C14-C59 | σ* | 1.46 | 1.23 | 0.038 |
| C5-C15 | σ | C15-C59 | σ* | 4.61 | 1.22 | 0.067 |
| C6-H10 | σ | C1-C2 | σ* | 3.82 | 1.08 | 0.057 |
| C6-H10 | σ | C1-C6 | σ* | 0.78 | 1.10 | 0.026 |
| C6-H10 | σ | C1-H7 | σ* | 0.66 | 0.97 | 0.023 |
| C6-H10 | σ | C4-C5 | σ* | 4.79 | 1.05 | 0.064 |
| C6-H10 | σ | C5-C6 | σ* | 0.81 | 1.09 | 0.027 |
| C11-C12 | σ | C4-N58 | σ* | 2.15 | 1.14 | 0.044 |
| C11-C12 | σ | C5-C15 | σ* | 1.69 | 1.23 | 0.041 |
| C11-C12 | σ | C11-C15 | σ* | 5.07 | 1.25 | 0.071 |
| C11-C12 | σ | C11-N58 | σ* | 2.48 | 1.14 | 0.047 |
| C11-C12 | σ | C12-C13 | σ* | 3.39 | 1.29 | 0.059 |
| C11-C12 | σ | C12-H16 | σ* | 1.42 | 1.15 | 0.036 |
| C11-C12 | σ | C13-H17 | σ* | 2.22 | 1.16 | 0.045 |
| C11-C15 | σ | C5-C6 | σ* | 5.05 | 1.24 | 0.071 |
| C11-C15 | σ | C5-C15 | σ* | 2.71 | 1.18 | 0.051 |
| C11-C15 | σ | C11-C12 | σ* | 4.72 | 1.23 | 0.068 |
| C11-C15 | σ | C11-N58 | σ* | 1.22 | 1.09 | 0.033 |
| C11-C15 | σ | C12-H16 | σ* | 2.55 | 1.10 | 0.048 |
| C11-C15 | σ | C15-C59 | σ* | 3.89 | 1.24 | 0.062 |
| C11-C15 | σ | C19-N58 | σ* | 4.90 | 1.06 | 0.064 |
| C11-C15 | σ | C59-H60 | σ* | 2.53 | 1.10 | 0.047 |
| C11-C15 | π | C4-C5 | π* | 18.56 | 0.28 | 0.065 |
| C11-C15 | π | C11-C15 | π* | 0.72 | 0.28 | 0.013 |
| C11-C15 | π | C12-C13 | π* | 18.65 | 0.28 | 0.065 |
| C11-C15 | π | C14-C59 | π* | 20.80 | 0.28 | 0.070 |
| C11-N58 | σ | C3-C4 | σ* | 3.90 | 1.35 | 0.065 |
| C11-N58 | σ | C4-N58 | σ* | 2.30 | 1.21 | 0.047 |
| C11-N58 | σ | C11-C12 | σ* | 2.16 | 1.35 | 0.048 |
| C11-N58 | σ | C11-C15 | σ* | 1.36 | 1.32 | 0.038 |
| C11-N58 | σ | C12-C13 | σ* | 0.91 | 1.36 | 0.031 |
| C11-N58 | σ | C15-C59 | σ* | 2.40 | 1.36 | 0.051 |
| C11-N58 | σ | C19-C20 | π* | 0.97 | 0.79 | 0.027 |
| C11-N58 | σ | C19-C23 | σ* | 1.15 | 1.33 | 0.035 |
| C11-N58 | σ | C19-N58 | σ* | 2.62 | 1.18 | 0.050 |
| C12-C13 | σ | C11-C12 | σ* | 4.02 | 1.27 | 0.064 |
| C12-C13 | σ | C11-N58 | σ* | 6.32 | 1.13 | 0.075 |
| C12-C13 | σ | C12-H16 | σ* | 1.38 | 1.14 | 0.036 |
| C12-C13 | σ | C13-C14 | σ* | 2.93 | 1.27 | 0.055 |
| C12-C13 | σ | C13-H17 | σ* | 1.03 | 1.14 | 0.031 |
| C12-C13 | σ | C14-H18 | σ* | 2.11 | 1.15 | 0.044 |
| C12-C13 | π | C11-C15 | π* | 20.65 | 0.28 | 0.072 |
| C12-C13 | π | C14-C59 | π* | 17.44 | 0.29 | 0.064 |
| C12-H16 | σ | C11-C12 | σ* | 0.78 | 1.09 | 0.026 |
| C12-H16 | σ | C11-C15 | σ* | 4.55 | 1.06 | 0.062 |
| C12-H16 | σ | C12-C13 | σ* | 1.04 | 1.10 | 0.030 |
| C12-H16 | σ | C13-C14 | σ* | 3.76 | 1.09 | 0.057 |
| C12-H16 | σ | C13-H17 | σ* | 0.65 | 0.97 | 0.022 |
| C13-C14 | σ | C12-C13 | σ* | 2.98 | 1.27 | 0.055 |
| C13-C14 | σ | C12-H16 | σ* | 2.48 | 1.13 | 0.047 |
| C13-C14 | σ | C13-H17 | σ* | 1.07 | 1.14 | 0.031 |
| C13-C14 | σ | C14-H18 | σ* | 1.09 | 1.14 | 0.031 |
| C13-C14 | σ | C14-C59 | σ* | 3.02 | 1.27 | 0.055 |
| C13-C14 | σ | C59-H60 | σ* | 2.51 | 1.13 | 0.048 |
| C13-H17 | σ | C11-C12 | σ* | 4.18 | 1.08 | 0.060 |
| C13-H17 | σ | C12-C13 | σ* | 0.61 | 1.10 | 0.023 |
| C13-H17 | σ | C12-H16 | σ* | 0.65 | 0.96 | 0.022 |
| C13-H17 | σ | C13-C14 | σ* | 0.55 | 1.08 | 0.022 |
| C13-H17 | σ | C14-H18 | σ* | 0.67 | 0.96 | 0.023 |
| C13-H17 | σ | C14-C59 | σ* | 3.87 | 1.10 | 0.058 |
| C14-H18 | σ | C12-C13 | σ* | 3.97 | 1.09 | 0.059 |
| C14-H18 | σ | C13-C14 | σ* | 0.59 | 1.08 | 0.023 |
| C14-H18 | σ | C13-H17 | σ* | 0.66 | 0.96 | 0.022 |
| C14-H18 | σ | C14-C59 | σ* | 0.68 | 1.10 | 0.024 |
| C14-H18 | σ | C15-C59 | σ* | 4.09 | 1.09 | 0.060 |
| C14-H18 | σ | C59-H60 | σ* | 0.66 | 0.95 | 0.022 |
| C14-C59 | σ | C5-C15 | σ* | 4.97 | 1.22 | 0.070 |
| C14-C59 | σ | C13-C14 | σ* | 2.95 | 1.26 | 0.055 |
| C14-C59 | σ | C13-H17 | σ* | 2.20 | 1.14 | 0.045 |
| C14-C59 | σ | C14-H18 | σ* | 1.17 | 1.14 | 0.033 |
| C14-C59 | σ | C15-C59 | σ* | 3.76 | 1.27 | 0.062 |
| C14-C59 | σ | C59-H60 | σ* | 1.20 | 1.14 | 0.033 |
| C14-C59 | π | C11-C15 | π* | 18.11 | 0.28 | 0.067 |
| C14-C59 | π | C12-C13 | π* | 21.11 | 0.28 | 0.069 |
| C15-C59 | σ | C4-C5 | σ* | 0.95 | 1.23 | 0.030 |
| C15-C59 | σ | C5-C15 | σ* | 5.21 | 1.21 | 0.071 |
| C15-C59 | σ | C11-C15 | σ* | 4.58 | 1.23 | 0.067 |
| C15-C59 | σ | C11-N58 | σ* | 2.08 | 1.12 | 0.043 |
| C15-C59 | σ | C14-H18 | σ* | 2.30 | 1.14 | 0.046 |
| C15-C59 | σ | C14-C59 | σ* | 3.29 | 1.28 | 0.058 |
| C15-C59 | σ | C59-H60 | σ* | 1.20 | 1.13 | 0.033 |
| C19-C20 | σ | C4-N58 | σ* | 2.37 | 1.14 | 0.047 |
| C19-C20 | σ | C11-N58 | σ* | 0.52 | 1.14 | 0.022 |
| C19-C20 | σ | C19-C23 | σ* | 4.54 | 1.26 | 0.068 |
| C19-C20 | σ | C19-N58 | σ* | 1.77 | 1.11 | 0.040 |
| C19-C20 | σ | C20-H31 | σ* | 1.21 | 1.15 | 0.033 |
| C19-C20 | σ | C20-C61 | σ* | 3.42 | 1.28 | 0.059 |
| C19-C20 | σ | C23-H33 | σ* | 2.22 | 1.15 | 0.045 |
| C19-C20 | σ | C61-H62 | σ* | 2.20 | 1.15 | 0.045 |
| C19-C20 | π | C4-N58 | σ* | 2.01 | 0.70 | 0.037 |
| C19-C20 | π | C11-N58 | σ* | 1.77 | 0.70 | 0.034 |
| C19-C20 | π | C21-C61 | π* | 20.03 | 0.29 | 0.069 |
| C19-C20 | π | C22-C23 | π* | 19.87 | 0.29 | 0.068 |
| C19-C23 | σ | C4-N58 | σ* | 0.55 | 1.14 | 0.022 |
| C19-C23 | σ | C11-N58 | σ* | 2.32 | 1.14 | 0.046 |
| C19-C23 | σ | C19-C20 | σ* | 4.51 | 1.26 | 0.067 |
| C19-C23 | σ | C19-N58 | σ* | 1.77 | 1.11 | 0.040 |
| C19-C23 | σ | C20-H31 | σ* | 2.22 | 1.15 | 0.045 |
| C19-C23 | σ | C22-C23 | σ* | 3.42 | 1.28 | 0.059 |
| C19-C23 | σ | C22-H32 | σ* | 2.21 | 1.15 | 0.045 |
| C19-C23 | σ | C23-H33 | σ* | 1.21 | 1.15 | 0.033 |
| C19-N58 | σ | C4-C5 | σ* | 1.18 | 1.33 | 0.035 |
| C19-N58 | σ | C4-N58 | σ* | 2.55 | 1.22 | 0.050 |
| C19-N58 | σ | C11-C15 | σ* | 1.18 | 1.33 | 0.035 |
| C19-N58 | σ | C11-N58 | σ* | 2.57 | 1.22 | 0.050 |
| C19-N58 | σ | C19-C20 | σ* | 1.59 | 1.34 | 0.041 |
| C19-N58 | σ | C19-C23 | σ* | 1.58 | 1.34 | 0.041 |
| C19-N58 | σ | C20-C61 | σ* | 1.41 | 1.36 | 0.039 |
| C19-N58 | σ | C22-C23 | σ* | 1.41 | 1.36 | 0.039 |
| C20-H31 | σ | C19-C20 | σ* | 0.74 | 1.08 | 0.025 |
| C20-H31 | σ | C19-C23 | σ* | 4.50 | 1.08 | 0.062 |
| C20-H31 | σ | C19-N58 | σ* | 0.84 | 0.93 | 0.025 |
| C20-H31 | σ | C20-C61 | σ* | 0.91 | 1.10 | 0.028 |
| C20-H31 | σ | C21-C61 | σ* | 4.14 | 1.08 | 0.060 |
| C20-H31 | σ | C61-H62 | σ* | 0.71 | 0.96 | 0.023 |
| C20-C61 | σ | C19-C20 | σ* | 3.61 | 1.27 | 0.060 |
| C20-C61 | σ | C19-N58 | σ* | 4.26 | 1.11 | 0.062 |
| C20-C61 | σ | C20-H31 | σ* | 1.25 | 1.15 | 0.034 |
| C20-C61 | σ | C21-C24 | σ* | 3.48 | 1.17 | 0.057 |
| C20-C61 | σ | C21-C61 | σ* | 3.82 | 1.26 | 0.062 |
| C20-C61 | σ | C61-H62 | σ* | 1.12 | 1.15 | 0.032 |
| C21-C22 | σ | C21-C24 | σ* | 3.29 | 1.16 | 0.055 |
| C21-C22 | σ | C21-C61 | σ* | 4.02 | 1.25 | 0.063 |
| C21-C22 | σ | C22-C23 | σ* | 3.44 | 1.27 | 0.059 |
| C21-C22 | σ | C22-H32 | σ* | 1.21 | 1.13 | 0.033 |
| C21-C22 | σ | C23-H33 | σ* | 2.21 | 1.14 | 0.045 |
| C21-C22 | σ | C24-C25 | σ* | 1.93 | 1.25 | 0.044 |
| C21-C22 | σ | C61-H62 | σ* | 2.52 | 1.13 | 0.048 |
| C21-C24 | σ | C20-C61 | σ* | 2.23 | 1.22 | 0.047 |
| C21-C24 | σ | C21-C22 | σ* | 3.01 | 1.21 | 0.054 |
| C21-C24 | σ | C21-C61 | σ* | 3.00 | 1.21 | 0.054 |
| C21-C24 | σ | C22-C23 | σ* | 2.23 | 1.22 | 0.047 |
| C21-C24 | σ | C24-C25 | σ* | 3.01 | 1.21 | 0.054 |
| C21-C24 | σ | C24-C30 | σ* | 3.00 | 1.21 | 0.054 |
| C21-C24 | σ | C25-C26 | σ* | 2.23 | 1.22 | 0.047 |
| C21-C24 | σ | C29-C30 | σ* | 2.23 | 1.22 | 0.047 |
| C21-C61 | σ | C20-H31 | σ* | 2.21 | 1.14 | 0.045 |
| C21-C61 | σ | C20-C61 | σ* | 3.43 | 1.27 | 0.059 |
| C21-C61 | σ | C21-C22 | σ* | 4.04 | 1.25 | 0.064 |
| C21-C61 | σ | C21-C24 | σ* | 3.29 | 1.16 | 0.055 |
| C21-C61 | σ | C22-H32 | σ* | 2.52 | 1.13 | 0.048 |
| C21-C61 | σ | C24-C30 | σ* | 1.99 | 1.25 | 0.045 |
| C21-C61 | σ | C61-H62 | σ* | 1.21 | 1.13 | 0.033 |
| C21-C61 | π | C19-C20 | π* | 22.09 | 0.28 | 0.070 |
| C21-C61 | π | C22-C23 | π* | 19.91 | 0.28 | 0.068 |
| C21-C61 | π | C24-C25 | σ* | 1.00 | 0.82 | 0.028 |
| C21-C61 | π | C24-C30 | σ* | 1.23 | 0.81 | 0.031 |
| C21-C61 | π | C24-C30 | π* | 9.89 | 0.28 | 0.047 |
| C22-C23 | σ | C19-C23 | σ* | 3.61 | 1.27 | 0.060 |
| C22-C23 | σ | C19-N58 | σ* | 4.26 | 1.11 | 0.062 |
| C22-C23 | σ | C21-C22 | σ* | 3.82 | 1.26 | 0.062 |
| C22-C23 | σ | C21-C24 | σ* | 3.48 | 1.17 | 0.057 |
| C22-C23 | σ | C22-H32 | σ* | 1.12 | 1.15 | 0.032 |
| C22-C23 | σ | C23-H33 | σ* | 1.25 | 1.15 | 0.034 |
| C22-C23 | π | C19-C20 | π* | 20.63 | 0.28 | 0.069 |
| C22-C23 | π | C21-C61 | π* | 19.91 | 0.29 | 0.068 |
| C22-H32 | σ | C19-C23 | σ* | 4.08 | 1.08 | 0.059 |
| C22-H32 | σ | C21-C22 | σ* | 0.80 | 1.08 | 0.026 |
| C22-H32 | σ | C21-C61 | σ* | 4.41 | 1.08 | 0.062 |
| C22-H32 | σ | C22-C23 | σ* | 0.79 | 1.10 | 0.026 |
| C22-H32 | σ | C23-H33 | σ* | 0.69 | 0.96 | 0.023 |
| C23-H33 | σ | C19-C20 | σ* | 4.49 | 1.08 | 0.062 |
| C23-H33 | σ | C19-C23 | σ* | 0.74 | 1.08 | 0.025 |
| C23-H33 | σ | C19-N58 | σ* | 0.84 | 0.93 | 0.025 |
| C23-H33 | σ | C21-C22 | σ* | 4.14 | 1.08 | 0.060 |
| C23-H33 | σ | C22-C23 | σ* | 0.91 | 1.10 | 0.028 |
| C23-H33 | σ | C22-H32 | σ* | 0.71 | 0.96 | 0.023 |
| C24-C25 | σ | C21-C22 | σ* | 1.93 | 1.25 | 0.044 |
| C24-C25 | σ | C21-C24 | σ* | 3.29 | 1.16 | 0.055 |
| C24-C25 | σ | C24-C30 | σ* | 4.03 | 1.25 | 0.063 |
| C24-C25 | σ | C25-C26 | σ* | 3.44 | 1.27 | 0.059 |
| C24-C25 | σ | C25-H56 | σ* | 1.22 | 1.13 | 0.033 |
| C24-C25 | σ | C26-H27 | σ* | 2.21 | 1.14 | 0.045 |
| C24-C25 | σ | C30-H35 | σ* | 2.53 | 1.13 | 0.048 |
| C24-C30 | σ | C21-C24 | σ* | 3.29 | 1.16 | 0.055 |
| C24-C30 | σ | C21-C61 | σ* | 1.99 | 1.25 | 0.045 |
| C24-C30 | σ | C24-C25 | σ* | 4.05 | 1.25 | 0.064 |
| C24-C30 | σ | C25-H56 | σ* | 2.53 | 1.13 | 0.048 |
| C24-C30 | σ | C29-C30 | σ* | 3.44 | 1.27 | 0.059 |
| C24-C30 | σ | C29-H34 | σ* | 2.21 | 1.14 | 0.045 |
| C24-C30 | σ | C30-H35 | σ* | 1.22 | 1.13 | 0.033 |
| C24-C30 | π | C21-C22 | σ* | 0.99 | 0.81 | 0.028 |
| C24-C30 | π | C21-C61 | σ* | 1.22 | 0.81 | 0.031 |
| C24-C30 | π | C21-C61 | π* | 9.93 | 0.28 | 0.047 |
| C24-C30 | π | C25-C26 | π* | 19.89 | 0.28 | 0.068 |
| C24-C30 | π | C28-C29 | π* | 22.11 | 0.28 | 0.070 |
| C25-C26 | σ | C21-C24 | σ* | 3.48 | 1.17 | 0.057 |
| C25-C26 | σ | C24-C25 | σ* | 3.82 | 1.27 | 0.062 |
| C25-C26 | σ | C25-H56 | σ* | 1.12 | 1.15 | 0.032 |
| C25-C26 | σ | C26-H27 | σ* | 1.25 | 1.15 | 0.034 |
| C25-C26 | σ | C26-C28 | σ* | 3.61 | 1.27 | 0.060 |
| C25-C26 | σ | C28-N57 | σ* | 4.27 | 1.11 | 0.062 |
| C25-C26 | π | C24-C30 | π* | 19.99 | 0.29 | 0.068 |
| C25-C26 | π | C28-C29 | π* | 20.68 | 0.28 | 0.069 |
| C25-H56 | σ | C24-C25 | σ* | 0.81 | 1.08 | 0.026 |
| C25-H56 | σ | C24-C30 | σ* | 4.42 | 1.08 | 0.062 |
| C25-H56 | σ | C25-C26 | σ* | 0.78 | 1.10 | 0.026 |
| C25-H56 | σ | C26-H27 | σ* | 0.69 | 0.96 | 0.023 |
| C25-H56 | σ | C26-C28 | σ* | 4.06 | 1.08 | 0.059 |
| C26-H27 | σ | C24-C25 | σ* | 4.14 | 1.08 | 0.060 |
| C26-H27 | σ | C25-C26 | σ* | 0.90 | 1.10 | 0.028 |
| C26-H27 | σ | C25-H56 | σ* | 0.71 | 0.96 | 0.023 |
| C26-H27 | σ | C26-C28 | σ* | 0.75 | 1.08 | 0.025 |
| C26-H27 | σ | C28-C29 | σ* | 4.51 | 1.08 | 0.062 |
| C26-H27 | σ | C28-N57 | σ* | 0.84 | 0.93 | 0.025 |
| C26-C28 | σ | C25-C26 | σ* | 3.42 | 1.28 | 0.059 |
| C26-C28 | σ | C25-H56 | σ* | 2.21 | 1.15 | 0.045 |
| C26-C28 | σ | C26-H27 | σ* | 1.22 | 1.15 | 0.034 |
| C26-C28 | σ | C28-C29 | σ* | 4.51 | 1.27 | 0.067 |
| C26-C28 | σ | C28-N57 | σ* | 1.76 | 1.11 | 0.040 |
| C26-C28 | σ | C29-H34 | σ* | 2.22 | 1.15 | 0.045 |
| C26-C28 | σ | C39-N57 | σ* | 2.27 | 1.14 | 0.046 |
| C26-C28 | σ | C46-N57 | σ* | 0.57 | 1.14 | 0.023 |
| C28-C29 | σ | C26-H27 | σ* | 2.22 | 1.15 | 0.045 |
| C28-C29 | σ | C26-C28 | σ* | 4.53 | 1.27 | 0.068 |
| C28-C29 | σ | C28-N57 | σ* | 1.76 | 1.11 | 0.040 |
| C28-C29 | σ | C29-C30 | σ* | 3.42 | 1.28 | 0.059 |
| C28-C29 | σ | C29-H34 | σ* | 1.22 | 1.15 | 0.034 |
| C28-C29 | σ | C30-H35 | σ* | 2.21 | 1.15 | 0.045 |
| C28-C29 | σ | C39-N57 | σ* | 0.54 | 1.14 | 0.022 |
| C28-C29 | σ | C46-N57 | σ* | 2.32 | 1.14 | 0.046 |
| C28-C29 | π | C24-C30 | π* | 19.96 | 0.29 | 0.069 |
| C28-C29 | π | C25-C26 | π* | 19.95 | 0.29 | 0.068 |
| C28-C29 | π | C39-N57 | σ* | 1.80 | 0.70 | 0.035 |
| C28-C29 | π | C46-N57 | σ* | 2.06 | 0.70 | 0.037 |
| C28-N57 | σ | C25-C26 | σ* | 1.42 | 1.36 | 0.039 |
| C28-N57 | σ | C26-C28 | σ* | 1.58 | 1.34 | 0.041 |
| C28-N57 | σ | C28-C29 | σ* | 1.58 | 1.34 | 0.041 |
| C28-N57 | σ | C29-C30 | σ* | 1.42 | 1.36 | 0.039 |
| C28-N57 | σ | C39-C40 | σ* | 1.18 | 1.33 | 0.035 |
| C28-N57 | σ | C39-N57 | σ* | 2.56 | 1.22 | 0.050 |
| C28-N57 | σ | C46-C51 | σ* | 1.18 | 1.33 | 0.035 |
| C28-N57 | σ | C46-N57 | σ* | 2.55 | 1.22 | 0.050 |
| C29-C30 | σ | C21-C24 | σ* | 3.48 | 1.17 | 0.057 |
| C29-C30 | σ | C24-C30 | σ* | 3.81 | 1.26 | 0.062 |
| C29-C30 | σ | C28-C29 | σ* | 3.61 | 1.27 | 0.060 |
| C29-C30 | σ | C28-N57 | σ* | 4.27 | 1.11 | 0.062 |
| C29-C30 | σ | C29-H34 | σ* | 1.25 | 1.15 | 0.034 |
| C29-C30 | σ | C30-H35 | σ* | 1.12 | 1.15 | 0.032 |
| C29-H34 | σ | C24-C30 | σ* | 4.13 | 1.08 | 0.060 |
| C29-H34 | σ | C26-C28 | σ* | 4.51 | 1.08 | 0.062 |
| C29-H34 | σ | C28-C29 | σ* | 0.75 | 1.08 | 0.025 |
| C29-H34 | σ | C28-N57 | σ* | 0.84 | 0.93 | 0.025 |
| C29-H34 | σ | C29-C30 | σ* | 0.90 | 1.10 | 0.028 |
| C29-H34 | σ | C30-H35 | σ* | 0.71 | 0.96 | 0.023 |
| C30-H35 | σ | C24-C25 | σ* | 4.43 | 1.08 | 0.062 |
| C30-H35 | σ | C24-C30 | σ* | 0.81 | 1.08 | 0.026 |
| C30-H35 | σ | C28-C29 | σ* | 4.06 | 1.08 | 0.059 |
| C30-H35 | σ | C29-C30 | σ* | 0.78 | 1.10 | 0.026 |
| C30-H35 | σ | C29-H34 | σ* | 0.69 | 0.96 | 0.023 |
| C36-C37 | σ | C36-C41 | σ* | 3.02 | 1.27 | 0.055 |
| C36-C37 | σ | C36-H42 | σ* | 1.09 | 1.14 | 0.031 |
| C36-C37 | σ | C37-C38 | σ* | 2.98 | 1.27 | 0.055 |
| C36-C37 | σ | C37-H43 | σ* | 1.07 | 1.14 | 0.031 |
| C36-C37 | σ | C38-H44 | σ* | 2.48 | 1.13 | 0.047 |
| C36-C37 | σ | C41-H45 | σ* | 2.51 | 1.13 | 0.048 |
| C36-C41 | σ | C36-C37 | σ* | 2.95 | 1.26 | 0.055 |
| C36-C41 | σ | C36-H42 | σ* | 1.17 | 1.14 | 0.033 |
| C36-C41 | σ | C37-H43 | σ* | 2.20 | 1.14 | 0.045 |
| C36-C41 | σ | C40-C41 | σ* | 3.76 | 1.27 | 0.062 |
| C36-C41 | σ | C40-C51 | σ* | 4.97 | 1.22 | 0.070 |
| C36-C41 | σ | C41-H45 | σ* | 1.20 | 1.14 | 0.033 |
| C36-C41 | π | C37-C38 | π* | 21.10 | 0.28 | 0.069 |
| C36-C41 | π | C39-C40 | π* | 18.08 | 0.28 | 0.066 |
| C36-H42 | σ | C36-C37 | σ* | 0.59 | 1.08 | 0.023 |
| C36-H42 | σ | C36-C41 | σ* | 0.68 | 1.10 | 0.024 |
| C36-H42 | σ | C37-C38 | σ* | 3.97 | 1.09 | 0.059 |
| C36-H42 | σ | C37-H43 | σ* | 0.66 | 0.96 | 0.022 |
| C36-H42 | σ | C40-C41 | σ* | 4.09 | 1.09 | 0.060 |
| C36-H42 | σ | C41-H45 | σ* | 0.66 | 0.95 | 0.022 |
| C37-C38 | σ | C36-C37 | σ* | 2.93 | 1.27 | 0.054 |
| C37-C38 | σ | C36-H42 | σ* | 2.11 | 1.15 | 0.044 |
| C37-C38 | σ | C37-H43 | σ* | 1.03 | 1.14 | 0.031 |
| C37-C38 | σ | C38-C39 | σ* | 4.01 | 1.27 | 0.064 |
| C37-C38 | σ | C38-H44 | σ* | 1.38 | 1.14 | 0.036 |
| C37-C38 | σ | C39-N57 | σ* | 6.32 | 1.13 | 0.076 |
| C37-C38 | π | C36-C41 | π* | 17.44 | 0.29 | 0.064 |
| C37-C38 | π | C39-C40 | π* | 20.66 | 0.28 | 0.072 |
| C37-H43 | σ | C36-C37 | σ* | 0.55 | 1.08 | 0.022 |
| C37-H43 | σ | C36-C41 | σ* | 3.87 | 1.10 | 0.058 |
| C37-H43 | σ | C36-H42 | σ* | 0.67 | 0.96 | 0.023 |
| C37-H43 | σ | C37-C38 | σ* | 0.61 | 1.10 | 0.023 |
| C37-H43 | σ | C38-C39 | σ* | 4.18 | 1.08 | 0.060 |
| C37-H43 | σ | C38-H44 | σ* | 0.65 | 0.96 | 0.022 |
| C38-C39 | σ | C37-C38 | σ* | 3.39 | 1.29 | 0.059 |
| C38-C39 | σ | C37-H43 | σ* | 2.22 | 1.16 | 0.045 |
| C38-C39 | σ | C38-H44 | σ* | 1.41 | 1.15 | 0.036 |
| C38-C39 | σ | C39-C40 | σ* | 5.07 | 1.25 | 0.071 |
| C38-C39 | σ | C39-N57 | σ* | 2.48 | 1.14 | 0.048 |
| C38-C39 | σ | C40-C51 | σ* | 1.69 | 1.23 | 0.041 |
| C38-C39 | σ | C46-N57 | σ* | 2.15 | 1.14 | 0.044 |
| C38-H44 | σ | C36-C37 | σ* | 3.76 | 1.09 | 0.057 |
| C38-H44 | σ | C37-C38 | σ* | 1.04 | 1.10 | 0.030 |
| C38-H44 | σ | C37-H43 | σ* | 0.65 | 0.97 | 0.022 |
| C38-H44 | σ | C38-C39 | σ* | 0.78 | 1.09 | 0.026 |
| C38-H44 | σ | C39-C40 | σ* | 4.55 | 1.06 | 0.062 |
| C39-C40 | σ | C28-N57 | σ* | 4.91 | 1.06 | 0.064 |
| C39-C40 | σ | C38-C39 | σ* | 4.72 | 1.23 | 0.068 |
| C39-C40 | σ | C38-H44 | σ* | 2.55 | 1.10 | 0.048 |
| C39-C40 | σ | C39-N57 | σ* | 1.22 | 1.09 | 0.033 |
| C39-C40 | σ | C40-C41 | σ* | 3.89 | 1.24 | 0.062 |
| C39-C40 | σ | C40-C51 | σ* | 2.70 | 1.18 | 0.051 |
| C39-C40 | σ | C41-H45 | σ* | 2.53 | 1.10 | 0.047 |
| C39-C40 | σ | C50-C51 | σ* | 5.06 | 1.24 | 0.071 |
| C39-C40 | π | C36-C41 | π* | 20.82 | 0.28 | 0.070 |
| C39-C40 | π | C37-C38 | π* | 18.63 | 0.28 | 0.065 |
| C39-C40 | π | C39-C40 | π* | 0.72 | 0.28 | 0.013 |
| C39-C40 | π | C46-C51 | π* | 18.57 | 0.28 | 0.065 |
| C39-N57 | σ | C26-C28 | σ* | 1.13 | 1.33 | 0.035 |
| C39-N57 | σ | C28-C29 | π* | 0.98 | 0.79 | 0.027 |
| C39-N57 | σ | C28-N57 | σ* | 2.62 | 1.18 | 0.050 |
| C39-N57 | σ | C37-C38 | σ* | 0.90 | 1.36 | 0.031 |
| C39-N57 | σ | C38-C39 | σ* | 2.16 | 1.35 | 0.048 |
| C39-N57 | σ | C39-C40 | σ* | 1.36 | 1.32 | 0.038 |
| C39-N57 | σ | C40-C41 | σ* | 2.40 | 1.36 | 0.051 |
| C39-N57 | σ | C46-C47 | σ* | 3.90 | 1.35 | 0.065 |
| C39-N57 | σ | C46-N57 | σ* | 2.30 | 1.21 | 0.047 |
| C40-C41 | σ | C36-C41 | σ* | 3.29 | 1.28 | 0.058 |
| C40-C41 | σ | C36-H42 | σ* | 2.30 | 1.14 | 0.046 |
| C40-C41 | σ | C39-C40 | σ* | 4.58 | 1.23 | 0.067 |
| C40-C41 | σ | C39-N57 | σ* | 2.07 | 1.12 | 0.043 |
| C40-C41 | σ | C40-C51 | σ* | 5.21 | 1.21 | 0.071 |
| C40-C41 | σ | C41-H45 | σ* | 1.20 | 1.13 | 0.033 |
| C40-C41 | σ | C46-C51 | σ* | 0.95 | 1.23 | 0.030 |
| C40-C51 | σ | C36-C41 | σ* | 1.46 | 1.23 | 0.038 |
| C40-C51 | σ | C38-C39 | σ* | 3.99 | 1.22 | 0.062 |
| C40-C51 | σ | C39-C40 | σ* | 2.61 | 1.19 | 0.050 |
| C40-C51 | σ | C39-N57 | σ* | 0.76 | 1.08 | 0.025 |
| C40-C51 | σ | C40-C41 | σ* | 4.61 | 1.22 | 0.067 |
| C40-C51 | σ | C46-C47 | σ* | 3.99 | 1.22 | 0.062 |
| C40-C51 | σ | C46-C51 | σ* | 2.61 | 1.19 | 0.050 |
| C40-C51 | σ | C46-N57 | σ* | 0.76 | 1.08 | 0.025 |
| C40-C51 | σ | C49-C50 | σ* | 1.46 | 1.23 | 0.038 |
| C40-C51 | σ | C50-C51 | σ* | 4.61 | 1.22 | 0.067 |
| C41-H45 | σ | C36-C37 | σ* | 3.82 | 1.08 | 0.058 |
| C41-H45 | σ | C36-C41 | σ* | 0.78 | 1.10 | 0.026 |
| C41-H45 | σ | C36-H42 | σ* | 0.66 | 0.97 | 0.023 |
| C41-H45 | σ | C39-C40 | σ* | 4.79 | 1.05 | 0.064 |
| C41-H45 | σ | C40-C41 | σ* | 0.81 | 1.09 | 0.027 |
| C46-C47 | σ | C39-N57 | σ* | 2.15 | 1.14 | 0.044 |
| C46-C47 | σ | C40-C51 | σ* | 1.69 | 1.23 | 0.041 |
| C46-C47 | σ | C46-C51 | σ* | 5.07 | 1.25 | 0.071 |
| C46-C47 | σ | C46-N57 | σ* | 2.48 | 1.14 | 0.048 |
| C46-C47 | σ | C47-C48 | σ* | 3.39 | 1.29 | 0.059 |
| C46-C47 | σ | C47-H52 | σ* | 1.41 | 1.15 | 0.036 |
| C46-C47 | σ | C48-H53 | σ* | 2.22 | 1.16 | 0.045 |
| C46-C51 | σ | C28-N57 | σ* | 4.91 | 1.06 | 0.064 |
| C46-C51 | σ | C40-C41 | σ* | 5.06 | 1.24 | 0.071 |
| C46-C51 | σ | C40-C51 | σ* | 2.70 | 1.18 | 0.051 |
| C46-C51 | σ | C46-C47 | σ* | 4.72 | 1.23 | 0.068 |
| C46-C51 | σ | C46-N57 | σ* | 1.22 | 1.09 | 0.033 |
| C46-C51 | σ | C47-H52 | σ* | 2.55 | 1.10 | 0.048 |
| C46-C51 | σ | C50-C51 | σ* | 3.89 | 1.24 | 0.062 |
| C46-C51 | σ | C50-H55 | σ* | 2.53 | 1.10 | 0.047 |
| C46-C51 | π | C39-C40 | π* | 18.57 | 0.28 | 0.065 |
| C46-C51 | π | C46-C51 | π* | 0.72 | 0.28 | 0.013 |
| C46-C51 | π | C47-C48 | π* | 18.63 | 0.28 | 0.065 |
| C46-C51 | π | C49-C50 | π* | 20.82 | 0.28 | 0.070 |
| C46-N57 | σ | C28-C29 | σ* | 1.15 | 1.33 | 0.035 |
| C46-N57 | σ | C28-C29 | π* | 0.89 | 0.79 | 0.026 |
| C46-N57 | σ | C28-N57 | σ* | 2.63 | 1.18 | 0.050 |
| C46-N57 | σ | C38-C39 | σ* | 3.90 | 1.35 | 0.065 |
| C46-N57 | σ | C39-N57 | σ* | 2.30 | 1.21 | 0.047 |
| C46-N57 | σ | C46-C47 | σ* | 2.16 | 1.35 | 0.048 |
| C46-N57 | σ | C46-C51 | σ* | 1.36 | 1.32 | 0.038 |
| C46-N57 | σ | C47-C48 | σ* | 0.90 | 1.36 | 0.031 |
| C46-N57 | σ | C50-C51 | σ* | 2.40 | 1.36 | 0.051 |
| C47-C48 | σ | C46-C47 | σ* | 4.01 | 1.27 | 0.064 |
| C47-C48 | σ | C46-N57 | σ* | 6.32 | 1.13 | 0.076 |
| C47-C48 | σ | C47-H52 | σ* | 1.38 | 1.14 | 0.036 |
| C47-C48 | σ | C48-C49 | σ* | 2.93 | 1.27 | 0.054 |
| C47-C48 | σ | C48-H53 | σ* | 1.03 | 1.14 | 0.031 |
| C47-C48 | σ | C49-H54 | σ* | 2.11 | 1.15 | 0.044 |
| C47-C48 | π | C46-C51 | π* | 20.66 | 0.28 | 0.072 |
| C47-C48 | π | C49-C50 | π* | 17.44 | 0.29 | 0.064 |
| C47-H52 | σ | C46-C47 | σ* | 0.78 | 1.09 | 0.026 |
| C47-H52 | σ | C46-C51 | σ* | 4.55 | 1.06 | 0.062 |
| C47-H52 | σ | C47-C48 | σ* | 1.04 | 1.10 | 0.030 |
| C47-H52 | σ | C48-C49 | σ* | 3.76 | 1.09 | 0.057 |
| C47-H52 | σ | C48-H53 | σ* | 0.65 | 0.97 | 0.022 |
| C48-C49 | σ | C47-C48 | σ* | 2.98 | 1.27 | 0.055 |
| C48-C49 | σ | C47-H52 | σ* | 2.48 | 1.13 | 0.047 |
| C48-C49 | σ | C48-H53 | σ* | 1.07 | 1.14 | 0.031 |
| C48-C49 | σ | C49-C50 | σ* | 3.02 | 1.27 | 0.055 |
| C48-C49 | σ | C49-H54 | σ* | 1.09 | 1.14 | 0.031 |
| C48-C49 | σ | C50-H55 | σ* | 2.51 | 1.13 | 0.048 |
| C48-H53 | σ | C46-C47 | σ* | 4.18 | 1.08 | 0.060 |
| C48-H53 | σ | C47-C48 | σ* | 0.61 | 1.10 | 0.023 |
| C48-H53 | σ | C47-H52 | σ* | 0.65 | 0.96 | 0.022 |
| C48-H53 | σ | C48-C49 | σ* | 0.55 | 1.08 | 0.022 |
| C48-H53 | σ | C49-C50 | σ* | 3.87 | 1.10 | 0.058 |
| C48-H53 | σ | C49-H54 | σ* | 0.67 | 0.96 | 0.023 |
| C49-C50 | σ | C40-C51 | σ* | 4.97 | 1.22 | 0.070 |
| C49-C50 | σ | C48-C49 | σ* | 2.95 | 1.26 | 0.055 |
| C49-C50 | σ | C48-H53 | σ* | 2.20 | 1.14 | 0.045 |
| C49-C50 | σ | C49-H54 | σ* | 1.17 | 1.14 | 0.033 |
| C49-C50 | σ | C50-C51 | σ* | 3.76 | 1.27 | 0.062 |
| C49-C50 | σ | C50-H55 | σ* | 1.20 | 1.14 | 0.033 |
| C49-C50 | π | C46-C51 | π* | 18.09 | 0.28 | 0.066 |
| C49-C50 | π | C47-C48 | π* | 21.10 | 0.28 | 0.069 |
| C49-H54 | σ | C47-C48 | σ* | 3.97 | 1.09 | 0.059 |
| C49-H54 | σ | C48-C49 | σ* | 0.59 | 1.08 | 0.023 |
| C49-H54 | σ | C48-H53 | σ* | 0.66 | 0.96 | 0.022 |
| C49-H54 | σ | C49-C50 | σ* | 0.68 | 1.10 | 0.024 |
| C49-H54 | σ | C50-C51 | σ* | 4.09 | 1.09 | 0.060 |
| C49-H54 | σ | C50-H55 | σ* | 0.66 | 0.95 | 0.022 |
| C50-C51 | σ | C39-C40 | σ* | 0.95 | 1.23 | 0.030 |
| C50-C51 | σ | C40-C51 | σ* | 5.21 | 1.21 | 0.071 |
| C50-C51 | σ | C46-C51 | σ* | 4.58 | 1.23 | 0.067 |
| C50-C51 | σ | C46-N57 | σ* | 2.07 | 1.12 | 0.043 |
| C50-C51 | σ | C49-C50 | σ* | 3.29 | 1.28 | 0.058 |
| C50-C51 | σ | C49-H54 | σ* | 2.30 | 1.14 | 0.046 |
| C50-C51 | σ | C50-H55 | σ* | 1.20 | 1.13 | 0.033 |
| C50-H55 | σ | C46-C51 | σ* | 4.79 | 1.05 | 0.064 |
| C50-H55 | σ | C48-C49 | σ* | 3.82 | 1.08 | 0.058 |
| C50-H55 | σ | C49-C50 | σ* | 0.78 | 1.10 | 0.026 |
| C50-H55 | σ | C49-H54 | σ* | 0.66 | 0.97 | 0.023 |
| C50-H55 | σ | C50-C51 | σ* | 0.81 | 1.09 | 0.027 |
| C59-H60 | σ | C11-C15 | σ* | 4.80 | 1.05 | 0.064 |
| C59-H60 | σ | C13-C14 | σ* | 3.82 | 1.08 | 0.057 |
| C59-H60 | σ | C14-H18 | σ* | 0.66 | 0.97 | 0.023 |
| C59-H60 | σ | C14-C59 | σ* | 0.78 | 1.10 | 0.026 |
| C59-H60 | σ | C15-C59 | σ* | 0.81 | 1.09 | 0.027 |
| C61-H62 | σ | C19-C20 | σ* | 4.08 | 1.08 | 0.059 |
| C61-H62 | σ | C20-H31 | σ* | 0.69 | 0.96 | 0.023 |
| C61-H62 | σ | C20-C61 | σ* | 0.79 | 1.10 | 0.026 |
| C61-H62 | σ | C21-C22 | σ* | 4.42 | 1.08 | 0.062 |
| C61-H62 | σ | C21-C61 | σ* | 0.80 | 1.08 | 0.026 |
| N57 | LP(1) | C26-C28 | σ* | 4.54 | 0.81 | 0.059 |
| N57 | LP(1) | C28-C29 | σ* | 4.46 | 0.81 | 0.059 |
| N57 | LP(1) | C28-C29 | π* | 9.93 | 0.27 | 0.047 |
| N57 | LP(1) | C39-C40 | π* | 33.70 | 0.29 | 0.091 |
| N57 | LP(1) | C46-C51 | π* | 33.70 | 0.29 | 0.091 |
| N58 | LP(1) | C4-C5 | π* | 33.66 | 0.29 | 0.091 |
| N58 | LP(1) | C11-C15 | π* | 33.67 | 0.29 | 0.091 |
| N58 | LP(1) | C19-C20 | σ* | 4.36 | 0.81 | 0.058 |
| N58 | LP(1) | C19-C20 | π* | 10.58 | 0.27 | 0.048 |
| N58 | LP(1) | C19-C23 | σ* | 4.46 | 0.81 | 0.059 |

Table S5: First-order EOPE hyperpolarizability (βEOPE), average second-order EOKE hyperpolarizability  (γEOKE), total second-order (χEOPE) and third order (χEOKE) EOPE susceptibilities evaluated using M06-2X and ωB97XD functionals.

| λ = 1550 nm |  |  |
| --- | --- | --- |
| Parameters\Functionals | M06-2X | ωB97XD |
| βEOPE(-ω;ω,0)( ×10-30 esu) | 2.43 | 2.05 |
| γEOKE(-ω;ω,0,0) ( ×10-36 esu) | 145.72 | 106.22 |
| χEOPE(ω)(pmV-1) | 2.31 | 1.75 |
| χEOKE(ω)(×10-22 m2V-2) | 15.41 | 10.08 |
| λ = 1907 nm |  |  |
| βEOPE(-ω;ω,0)( ×10-30 esu) | 2.37 | 2.02 |
| γEOKE(-ω;ω,0,0) ( ×10-36 esu) | 141.61 | 103.65 |
| χEOPE(ω)(pmV-1) | 2.26 | 1.73 |
| χEOKE(ω)(×10-22 m2V-2) | 14.97 | 9.84 |

Table S6: First-order hyperpolarizabilities β-2ω;ω,0, second-order hyperpolarizabilities γ(-2ω ; ω, 0, 0), and second (χSHG) and third order (χTHG) susceptibilities evaluated using M06-2X and ωB97XD functionals.

| λ = 1550 nm |  |  |
| --- | --- | --- |
| Parameters\Functionals | M06-2X | ωB97XD |
| β-2ω;ω,0( ×10-30 esu) | 2.84 | 2.24 |
| γ-2ω;ω,0,0 ( ×10-36 esu) | 174.26 | 123.61 |
| χSHG-2ω;ω,0 (pm.V-1) | 2.70 | 1.91 |
| χTHG-2ω;ω,0,0 (×10-22 m2V-2) | 18.43 | 11.74 |
| λ = 1907 nm |  |  |
| β-2ω;ω,0( ×10-30 esu) | 2.62 | 2.14 |
| γ-2ω;ω,0,0 ( ×10-36 esu) | 158.74 | 114.23 |
| χSHG-2ω;ω,0 (pm.V-1) | 2.49 | 1.83 |
| χTHG-2ω;ω,0,0 (×10-22 m2V-2) | 16.79 | 10.85 |

Table S7: First-order hyperpolarizabilities HRS (βHRS), second-order DFMW (γωDFWM), depolarization ratio (DR), DFMW susceptibility (χωDFMW) and refractive index n2ω  evaluated using the M06-2X and ωB97XD functionals.

| λ = 1550 nm |  |  |
| --- | --- | --- |
| Parameters\Functionals | M06-2X | ωB97XD |
| βHRS( ×10-30 esu) | 1.95 | 1.95 |
| DR | 1.57 | 1.56 |
| γωDFWM ( ×10-36 esu) | 159.11 | 114.44 |
| χωDFMW (×10-22 m2V-2) | 16.82 | 10.87 |
| n2ω( ×10-20 m2W-1) | 10.15 | 7.19 |
| λ = 1907 nm |  |  |
| βHRS( ×10-30 esu) | 1.87 | 1.88 |
| DR | 1.58 | 1.56 |
| γωDFWM ( ×10-36 esu) | 149.82 | 108.75 |
| χωDFMW (×10-22 m2V-2) | 15.84 | 10.33 |
| n2ω( ×10-20 m2W-1) | 9.57 | 6.85 |

References

[1]	P. J. Low et al., Towards an understanding of structure–property relationships in hole-transport materials: The influence of molecular conformation on oxidation potential in poly(aryl)amines, J. Mater. Chem., 15 (2005) 2304, doi: 10.1039/b417962e.