# Biochar as adsorbent in purification of clear-cut forest runoff water: adsorption rate and adsorption capacity

Taija Saarela1, Elham Kakaei Lafdani2, Ari Laurén2, Jukka Pumpanen1, and Marjo Palviainen3

1 Department of Environmental and Biological Sciences, University of Eastern Finland, Yliopistonranta 1 E, FI-70210 Kuopio, Finland

2 School of Forest Sciences, University of Eastern Finland, Yliopistokatu 7, FI-80101 Joensuu, Finland

3 Department of Forest Sciences, University of Helsinki, Latokartanonkaari 7, FI-00014 Helsinki, Finland

Corresponding Author:

Taija Saarela

Email address: taija.saarela@uef.fi

Supplementary Table 1. The structure and Akaike Information Criterion (AIC) of nonlinear mixed-effect models for TN and NO3-N in different treatments

|  |  | AIC |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | TN |  |  |  | NO3-N |  |  |  |
| Model | Structure | 12g high | 12g low | 3g high | 3g low | 12g high | 12g low | 3g high | 3g low |
| 0-model |  | -429 | -603 | -279 | -374 | -712 | -844 | n.a. | -485 |
| 1-model |  | -433 | -618 | -265 | -378 | -789 | n.a. | n.a. | -484 |
| 2-model |  | -434 | -622 | n.a. | -376 | -798 | -853 | -399 | -483 |
| 3-model |  | -432 | -625 | -309 | -377 | -802 | -856 | -499 | -484 |

replicate k, biochar type b (spruce, birch), particle size p (coarse, fine)

Supplementary Figure 1. The effect of a) 12 g of birch biochar, b) 12 g of spruce biochar, c) 3 g of birch biochar and d) 3 g of spruce biochar on pH of runoff water during the experiment. Values are mean ± SD.  Blue dots represent coarse particle size (4-6 mm), red dots represent fine particle size (<4 mm), and black dots are blank water samples without biochar

Supplementary Figure 2. The effect of a) 12 g of birch biochar, b) 12 g of spruce biochar, c) 3 g of birch biochar and d) 3 g of spruce biochar on electrical conductivity (µS cm-1) during the experiment. Values are mean ± SD. Blue dots represent coarse particle size (4-6 mm), red dots represent fine particle size (<4 mm), and black dots are blank water samples without biochar

Supplementary Figure 3. The effect of biochar on TOC concentrations in different treatments: a) 12 g of birch biochar and b) 12 g of spruce biochar (initial concentration 28 mg l-1), c) 12 g of birch biochar and d) 12 g of spruce biochar (initial concentration 25 mg l-1), e) 3 g of birch biochar and f) 3 g of spruce biochar (initial concentration 28 mg l-1), and g) 3 g of birch biochar and h) 3 g of spruce biochar (initial concentration 25 mg l-1). Values are mean± SD. Blue dots represent coarse particle size (4-6 mm), red dots represent fine particle size (<4 mm), and black dots are blank water samples without biochar