Supplementary Information

Magnetic Fe2O3/biochar composite prepared in a molten salt medium for antibiotic removal in Water

Huagen Liang1,3, Chenxi Zhu1,3, Shan Ji2*, Palanisamy Kannan2, Fu Chen,1,4**

1 Jiangsu Key Laboratory of Coal-based Greenhouse Gas Control and Utilization, China University of Mining and Technology, Low Carbon Energy Institute, China University of Mining and Technology, Xuzhou, 221008, China

2 College of Biological, Chemical Science and Engineering, Jiaxing University, Jiaxing, 314001, China

3 School of Materials Science and Engineering, China University of Mining and Technology, Xuzhou, 221008, China

4 School of Environment Science and Spatial Informatics, China University of Mining and Technology, Xuzhou, 221008, China

Corresponding authors:

Shan Ji (*): jishan@zjxu.edu.cn, Tel./fax: +86 (0)573 83643264

Fu Chen (**): chenfu@cumt.edu.cn, Tel./fax: +86(0)516 83883501

Table S1  Physical and chemical properties of CPW-700 and PWC-700.

| Samples | Yield | pH | BET surface area (m2 g-1) | Average pore size (nm) | Pore volume (cm3 g-1) | saturation magnetization (emu g-1) |
| --- | --- | --- | --- | --- | --- | --- |
| CPW-700 | 51.3% | 6.72 | 431.59 | 2.12 | 0.23 | 47.0 |
| PWC-700 | 34.1% | 7.18 | 422.06 | 3.17 | 0.33 | 0 |

Fig. S1 High-resolution XPS spectrum of C 1s (a) and O 1s (b) of CPW-700 and PWC-700.

Fig. S2 The elemental mapping results of CPW-700 (a) and PWC-700 (b).

| Samples | Pseudo-first-order |  | Pseudo-second-order |  |  | Intra-particle diffusion model |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | k1(×102) （min-1） | R2 | k2 （g/mg.min） | qe （mg/g） | R2 | ki （mg/g.min1/2） | R2 |
| CPW-700 | 0.004 | 0.9936 | 0.015 | 80.97 | 0.9991 | 0.39 | 0.6136 |
| PWC-700 | 0.002 | 0.9041 | 0.012 | 33.28 | 0.9977 | 0.37 | 0.5863 |

Table S2. Kinetic parameters for NOR adsorption on CPW-700 and PWC-700

Table S3. Parameters of Langmuir and Freundlich models for NOR adsorption.

| Samples | Freundlich isotherm model |  |  | Langmuir isotherm model |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 1/n | Kf （mg(n+1)/g/Ln） | R2 | Qm （mg/g） | KL (mg/L) | R2 |
| CPW-700 | 0.67 | 4.86 | 0.9953 | 379.85 | 0.005 | 0.9997 |
| PWC-700 | 0.88 | 1.73 | 0.9804 | 275.69 | 0.002 | 0.9858 |

Table S4. Adsorption thermodynamic parameters of CPW-700 and PWC-700.

| Samples | ΔH (kJ/mol) | ΔS (kJ/mol/K) | ΔG(kJ/mol) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | 288.15 K | 298.15 K | 308.15 K |
| CPW-700 | 8.0001 | 0.0567 | -8.2521 | -9.0619 | -9.3859 |
| PWC-700 | 5.1192 | 0.0198 | -0.6983 | -0.7131 | -1.0246 |

Fig. S3 FTIR spectra of CPW-700 and PWC-700 before and after adsorption.

Fig. S4 N2 adsorption/desorption isotherms and corresponding pore size distribution (inset) of CPW-700 and PWC-700 after adsorption.

Table S5  Physical and chemical properties of CPW-700 and PWC-700.

| Samples | BET surface area (m2 g-1) | Average pore size (nm) | Pore volume (cm3 g-1) |
| --- | --- | --- | --- |
| CPW-700 | 431.59 | 2.12 | 0.23 |
| PWC-700 | 422.06 | 3.17 | 0.33 |
| CPW-700+NOR | 327.28 | 1.56 | 0.13 |
| PWC-700+NOR | 375.22 | 2.15 | 0.20 |