# Supplementary Material

# Analysis of the simultaneous adsorption mechanism of ammonium and phosphate on magnesium-modified biochar and the slow release effect of fertiliser

Qingshan He a, b, c, Xiufen Li a, b, c *, Yueping Ren a, b, c

a Laboratory of Environmental Biotechnology, School of Environmental and Civil Engineering, Jiangnan University, Wuxi, Jiangsu 214122, PR China

b Jiangsu Key Laboratory of Anaerobic Biotechnology, Wuxi 214122, PR China

c Jiangsu Cooperative Innovation Center of Technology and Material of Water Treatment, Suzhou 215009, PR China

* Corresponding Author

School of Environment and Civil Engineering, Jiangnan University, Wuxi, 214122, China

E-mail address: xfli@jiangnan.edu.cn

# Text. S1

NH4+-N and PO43- adsorption capacity is calculated as follow.

Qe=C0-CeVm                               (1)

where Qe (mg/g) is the adsorption amount; C0 (mg/L) is the initial concentration of solution; Ce (mg/L) is the solution concentration after adsorption; V (L) is the solution volume; m (g) is the mass of biochar.

# Text. S2

Adsorption isotherm equations are as follows.

Langmuir model,

Qe=KqtCe1+KCe                                (2)

Freundlich model,

Qe=KfCen                                (3)

Langmuir-Freundlich model,

Qe=KlfqtCne1+KlfCne                               (4)

Separation factor(RL),

RL=11+C0K                                 (5)

where Qe (mg/g) is the saturation adsorption of N and P by biochar; qt (mg/g)is the maximum adsorption of biochar at time t; Ce (mg/L) is the equilibrium concentration of the solution after adsorption; C0 (mg/L) is the initial concentration of solution; K,Kf,Klf and n are the adsorption equilibrium constants.

# Text. S3

Adsorption kinetics equations are as follows.

Pseudo-first-order kinetic,

lnQe-qt=lnQe-k1t                     (6)

Pseudo-second-order kinetic,

tqt=1k2Qe2+tQe                      (7)

Intraparticle diffusion kinetic,

qt=kpt1/2+C                              (8)

Text. S4

The amount of leaching water was according to the average annual rainfall of Wuxi (Yao et al. 2010). The flow rate of water was set at 0.80±0.05 L/S·day-1. The L/S of approximately 4 corresponded to one year of average precipitation after fertilizer was applied to the soil according to Eq. S9. And the experiment ended until the cumulative L/S was reached 24 L/kg. Sampling was taken at cumulative L/S was 0.05, 0.1, 0.2, 0.3, 1.0, 2.0, 4.0, 8.0, 16 and 24 L/kg respectively. The specific calculation formula is as follows (Fang et al. 2017; Fang et al. 2018).

L/S=PD×H×t                                (9)

L/S: Ratio of liquid to solid, L/kg；

D: Soil bulk density, 1350 kg/m3；

P: Average annual rainfall in Wuxi;

H: Specimen height;

t: Time, Year.

References:

Fang W, Delapp RC, Kosson DS, van der Sloot HA, Liu J (2017) Release of heavy metals during long-term land application of sewage sludge compost: Percolation leaching tests with repeated additions of compost. Chemosphere 169:271-280. https://doi.org/10.1016/j.chemosphere.2016.11.086

Fang W, Qi G, Wei Y, Kosson DS, van der Sloot HA, Liu J (2018) Leaching characteristic of toxic trace elements in soils amended by sewage sludge compost: A comparison of field and laboratory investigations. Environ Pollut 237:244-252. https://doi.org/10.1016/j.envpol.2018.02.032

Yao Z, Zhou Z, Zheng X, Xie B, Mei B, Wang R, Butterbach-Bahl K (2010) Effects of organic matter incorporation on nitrous oxide emissions from rice-wheat rotation ecosystems in China. Plant Soil 327(1):315-330. 10.1007/s11104-009-0056-4

# Fig. S1 Diagram of soil leaching device

# Fig. S2 Characterizations of B, MgB and MgB-A. FTIR (a) and XRD (b)

# Fig. S3 XPS spectral analysis of Mg (A), Mg+B (B) and MgB (C) addition on NH4+-N and PO43- adsorption. Full spectrum (a), Mg 1s (b), N 1s (c) and (d) P 2p.

# Fig. S4 Effect of different treatments on Lolium perenne L. growth (a), cumulative seed germination (b), chlorophyll contents (c) and rhizome height or weight (d)

# Table S1 Physicochemical property of soil, MgB-A and CF

| Sample | pH | EC(mS/cm) | NH4+-N(mg/g) | PO43-(mg/g) | TN(mg/g) | TP(mg/g) | TK(mg/g) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Soil | 7.63 | 0.09 | 0.71 | 0.19 | 1.69 | 0.27 | 11.52 |
| MgB-A | 8.19 | 0.18 | 38.42 | 74.91 | 42.35 | 77.35 | 41.19 |
| CF | 6.72 | 5.74 | 104.16 | 54.28 | 135.34 | 69.23 | 127.65 |

# Table S2 Effect of pyrolysis temperature and Mg2+ content on the physicochemical properties of straw and MgB

| Temperature | Mg2+ | N | C | H | S | H/C | pH | Yield |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (℃) | (g/L) | (%) | (%) | (%) | (%) |  |  | (%) |
| corn stalks | 0 | 1.02 | 38.72 | 5.63 | 0.1 | 1.74 | 6.68 | - |
| 350 ℃ | CK | 1.01 | 59.71 | 4.92 | 0 | 0.99 | 8.14 | 54.75 |
|  | 0.6 | 0.81 | 58.61 | 4.85 | 0 | 0.99 | 8.76 | 53.88 |
|  | 1.2 | 1.02 | 57.34 | 4.82 | 0.09 | 1.01 | 8.88 | 54.52 |
|  | 1.8 | 0.98 | 56.21 | 4.76 | 0.12 | 1.02 | 9.05 | 55.11 |
|  | 2.4 | 0.84 | 56.4 | 4.84 | 0.08 | 1.03 | 9.11 | 55.23 |
|  | 3 | 0.79 | 55.31 | 4.83 | 0.04 | 1.05 | 9.19 | 55.33 |
|  | 3.6 | 0.72 | 55.21 | 4.84 | 0.05 | 1.05 | 9.22 | 56.04 |
| 450 ℃ | CK | 0.69 | 52.48 | 2.34 | 0 | 0.54 | 8.97 | 32.28 |
|  | 0.6 | 1.16 | 53.09 | 2.71 | 0 | 0.61 | 9.06 | 32.82 |
|  | 1.2 | 0.92 | 48.21 | 2.56 | 0 | 0.64 | 9.25 | 32.94 |
|  | 1.8 | 1.16 | 47.23 | 2.52 | 0 | 0.64 | 9.37 | 33.52 |
|  | 2.4 | 1.04 | 47.28 | 2.54 | 0 | 0.64 | 9.63 | 33.94 |
|  | 3 | 0.97 | 46.82 | 2.62 | 0 | 0.67 | 9.87 | 34.22 |
|  | 3.6 | 0.88 | 45.8 | 2.59 | 0 | 0.68 | 10.02 | 34.42 |
| 550 ℃ | CK | 0.77 | 52.11 | 2.17 | 0 | 0.50 | 9.03 | 30.35 |
|  | 0.6 | 1.02 | 50.92 | 2.22 | 0 | 0.52 | 9.24 | 30.64 |
|  | 1.2 | 0.75 | 51.34 | 2.19 | 0 | 0.51 | 9.32 | 30.72 |
|  | 1.8 | 1.37 | 48.93 | 2.16 | 0 | 0.53 | 9.56 | 30.81 |
|  | 2.4 | 1.02 | 47.92 | 2.38 | 0 | 0.60 | 9.85 | 29.91 |
|  | 3 | 0.91 | 48.92 | 2.33 | 0 | 0.57 | 10.06 | 30.21 |
|  | 3.6 | 0.82 | 45.38 | 2.29 | 0 | 0.61 | 10.12 | 29.71 |
| 650 ℃ | CK | 0.63 | 42.93 | 1.67 | 0 | 0.47 | 9.11 | 27.27 |
|  | 0.6 | 0.79 | 41.72 | 1.66 | 0 | 0.48 | 9.32 | 28.63 |
|  | 1.2 | 0.67 | 42.61 | 1.72 | 0 | 0.48 | 9.71 | 28.98 |
|  | 1.8 | 0.88 | 40.73 | 1.77 | 0 | 0.52 | 9.83 | 29.09 |
|  | 2.4 | 0.94 | 40.29 | 1.81 | 0 | 0.54 | 9.91 | 28.61 |
|  | 3 | 0.83 | 40.01 | 1.81 | 0 | 0.54 | 10.12 | 28.92 |
|  | 3.6 | 0.72 | 40.83 | 1.88 | 0 | 0.55 | 10.24 | 29.19 |

# Table S3 Parameters of adsorption kinetics and isotherms from MgB

| Model | Parameter |  | NH4+-N |  | PO43- |  |
| --- | --- | --- | --- | --- | --- | --- |
| Pseudo-first-order | k1(min-1) |  | 0.1818 |  | 0.2733 |  |
|  | Qe(mg/g) |  | 33.4635 |  | 74.6535 |  |
|  | R2 |  | 0.9881 |  | 0.9826 |  |
| Pseudo-second-order | k2(mg/g(min-1)) |  | 0.0099 |  | 0.0078 |  |
|  | Qe(mg/g) |  | 34.6110 |  | 76.6196 |  |
|  | R2 |  | 0.9973 |  | 0.9983 |  |
| Intraparticle diffusion | kp1 (mg/g·min0.5) |  | 15.1505 |  | 49.9030 |  |
|  | kp2 (mg/g·min0.5) |  | 31.7870 |  | 72.1666 |  |
|  | kp3 (mg/g·min0.5) |  | 34.6541 |  | 75.7959 |  |
|  | C1 |  | 3.3120 |  | 4.2957 |  |
|  | C2 |  | 0.1257 |  | 0.2430 |  |
|  | C3 |  | 0.0094 |  | 0.0546 |  |
|  | R2(kp1) |  | 0.9275 |  | 0.9829 |  |
|  | R2(kp2) |  | 0.8957 |  | 0.9742 |  |
|  | R2(kp3) |  | 1.0000 |  | 0.9998 |  |
| Langmuir model |  | K(L/mg) |  | 0.0334 |  | 0.0256 |
|  |  | Qe(mg/g) |  | 37.7118 |  | 73.2895 |
|  |  | R2(%) |  | 0.9912 |  | 0.9797 |
| Freundlich model |  | Kf(mg/g(L/mg)1/n) |  | 9.0742 |  | 14.8612 |
|  |  | n |  | 0.2178 |  | 0.2406 |
|  |  | R2(%) |  | 0.8552 |  | 0.8317 |
| Langmuir-Freundlich model |  | Qe(mg/g) |  | 36.0470 |  | 67.9238 |
|  |  | Klf(Ln/mgn) |  | 0.0143 |  | 0.0033 |
|  |  | n |  | 1.2812 |  | 1.5952 |
|  |  | R2(%) |  | 0.9974 |  | 0.9988 |
| Separation factor |  | RL |  | 0.0291-0.8569 |  | 0.0376-0.8866 |

# Table S4 Parameters of leaching kinetics from MgB

| Sample | Nutrient | First-order model |  |  | Second-order model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | K1 (year-1) | Qe(mg/g) | R2 | K2 [g·(mg·year)-1] | Qe(mg/g) | R2 |
| MgB-A | NH4+-N | 0.0635 | 35.2852 | 0.9943 | 0.0005 | 62.8899 | 0.9944 |
|  | PO43- | 0.1250 | 117.9680 | 0.9988 | 0.0003 | 201.7978 | 0.9989 |
| CF | NH4+-N | 11.9140 | 57.1893 | 0.9292 | 0.2357 | 61.6057 | 0.9703 |
|  | PO43- | 15.4612 | 135.709 | 0.9581 | 0.1386 | 144.3174 | 0.9776 |