Supplementary Material

Removal performance, mechanisms, and influencing factors of biochar for air pollutants: A critical review

Zhipeng Zhaoa, Bing Wanga,b*, Benny K. G. Thengc, Xinqing Leed, Xueyang Zhange, Miao Chena, Peng Xua

a College of Resource and Environmental Engineering, Guizhou University, Guiyang, 550025, China

b Key Laboratory of Karst Georesources and Environment, Ministry of Education, Guiyang, 550025, China

c Manaaki Whenua -Landcare Research, Palmerston North, New Zealand

d State Key Laboratory of Environmental Geochemistry, Institute of Geochemistry, Chinese Academy of Sciences, Guiyang, 550081, China

e Jiangsu Key Laboratory of Industrial Pollution Control and Resource Reuse, School of Environmental Engineering, Xuzhou University of Technology, Xuzhou, 221018, China

*Corresponding author: Bing Wang. E-mail: bwang6@gzu.edu.cn.

Table S1. The functional groups of various biochars involved in removing SO2

| Feedstocks | Preparation temperature (°C) | Modification conditions | Relative content (at%) | Functional groups | References |
| --- | --- | --- | --- | --- | --- |
| Corncobs | 600 | CO2 | 69.43/21.62/8.95/—/96.30/—/3.70/—/—/— | C-C (aromatic carbon)/C-OH/C-O/C=O/C-N/COOR/Pyrrolic and pyridonic N/Quaternary N/Pyridine-N-oxide/SO2/SO3/Sulfate | (Shao et al., 2018) |
| Corncobs | 600 | CO2+ Methyldiethanolamine-metalol | 34.56/9.77/46.63/9.04/21.81/21.59%/56.60/32.17/38.71/29.12 | C-C (aromatic carbon)/C-OH/C-O/C=O/C-N/COOR/Pyrrolic and pyridonic N/Quaternary N/Pyridine-N-oxide/SO2/SO3/Sulfate |  |
| Black spruce | 454 | / | 72.0/18.4/3.5/2.2 | Graphitic sp2 carbon/C‒OH/C= O or O‒C‒O/O = C‒O | (Braghiroli et al., 2019) |
| Black spruce | 454 | KOH | 65.4/8.1/7.9/6.4 | Graphitic sp2 carbon/C‒OH/C= O or O‒C‒O/O = C‒O |  |
| Black spruce | 454 | CO2 | 75.8/11.7/3.4/2.4 | Graphitic sp2 carbon/C‒OH/C= O or O‒C‒O/O = C‒O |  |
| Black spruce | 454 | Steam | 72.8/4.1/6.4/2.9 | Graphitic sp2 carbon/C‒OH/C= O or O‒C‒O/O = C‒O |  |
| Corncobs | 600 | CO2+ Methyldiethanolamine | 18.57/64.34/17.09/—/—/— | Pyrrolic-N/Quaternary-N/Oxidized N/SO2/SO42-/SO3 | (Zhang et al., 2020b) |
| Corncobs (used) | 600 | CO2+ Methyldiethanolamine | 21.82/21.58/56.60/32.17/38.71/29.12 | Pyrrolic-N/Quaternary-N/Oxidized N/SO2/SO42-/SO3 |  |

Note: “—” means that there is almost no content and it can be considered nil

Table S2. Physicochemical properties and removal performance of biochar as adsorbent for different air pollutants

| Feedstocks | Biochars | Synthetic methods | Ash (wt%) | pH | BET SSA (m2/g) | TPV (cm3/g) | Micropore volume (cm3/g) | Removal operating conditions | Adsorbate | Removal efficiency (%) | Removal capacity (mg/g) | References |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Corncobs | BAC-10% | Pyrolysis at 600 °C for 1 h. Modified with CO2 + 10% Methyldiethanolamine-metalol |  |  |  |  |  | Reaction temperature: 120 °C. SO2 flow rate: 20 mL/min | SO2 | / | 156.22 | (Shao et al., 2018) |
| Palm oil sludge | POSAB 442 °C | Pyrolysis at 442 °C. Modified with CO2 | 53.05 | 7.01 | 74.9 | 0.1654 | 0.0049 | SO2 concentration: 300 ppm. Flow rate: 300 mL/min. Biochar addition: 1 g. Room temperature and without humidity | SO2 | / | 16.65 | (Iberahim et al., 2019) |
| Palm oil mill sludge | POSB | Pyrolysis at 405 °C | 44.78 | 6.82 | 47.7 |  | 0.0066 | SO2 concentration: 300 ppm. Flow rate: 300 mL/min. Biochar addition: 1.0 g. Room temperature | SO2 | / | 9.75 | (Iberahim et al., 2018) |
| Dairy manure | DM-biochar | Pyrolysis at 500 °C for 4 h | 55.3 | 10.2 |  | 0.014 |  | SO2 concentration: 5000 ppm. Flow rate: 1500 mL/min. Biochar addition: 4.0 g. Room temperature | SO2 | / | 64.3 | (Xu et al., 2016) |
| Sewage sludge | SS-biochar | Pyrolysis at 500 °C for 4 h | 61.4 | 8.90 |  | 0.022 |  | SO2 concentration: 5000 ppm. Flow rate: 1500 mL/min. Biochar addition: 8.0 g. Room temperature | SO2 | / | 38.4 |  |
| Rice husk | RH-biochar | Pyrolysis at 500 °C for 4 h | 33.2 | 9.78 |  | 0.041 |  | SO2 concentration: 5000 ppm. Flow rate: 1500 mL/min. Biochar addition: 3.8 g. Room temperature | SO2 | / | 13.3 |  |
| Corncobs | CCAN850 | Pyrolysis at 600 °C for 1 h. Modified with CO2+ Methyldiethanolamine-metalol |  |  | 654 | 0.32 | 0.26 | SO2 concentration: 2000 ppm. Flow rate: 100 mL/min. Reaction temperature: 120 °C. NO concentration: 500 ppm. O2 concentration: 10% | SO2 | / | 216.19 | (Zhang et al., 2020b) |
| White birch | H2OBWB | Pyrolysis at 454 °C. Modified with steam |  | 8.6 | 590 | 0.34 | 0.23 | SO2 concentration: 50 ppm. Flow rate: 30 mL/min. Room temperature. | SO2 | / | 77 | (Braghiroli et al., 2019) |
| Camphor | S400P | Pyrolysis at 400 °C for 5 h |  | 9.74 | 17.1 |  |  | H2S concentration: 50 ppm. Flow rate: 40 mL/min. Biochar addition: 1.0 g. Room temperature | H2S | / | 109.3 | (Shang et al., 2016a) |
| Rice hull | S500R | Pyrolysis at 500 °C for 5 h |  | 10.56 | 115.49 |  |  | H2S concentration: 50 ppm. Flow rate: 40 mL/min. Biochar addition: 1.0 g. Room temperature | H2S |  | 382.7 |  |
| Bamboo | S500B | Pyrolysis at 500 °C for 5 h |  | 10.21 | 56.9 |  |  | H2S concentration: 50 ppm. Flow rate: 40 mL/min. Biochar addition: 1.0 g. Room temperature | H2S |  | 336.7 |  |
| Rice hull | SR500 | Pyrolysis at 500 °C for 5 h |  | 10.54 | 115.49 |  |  | H2S concentration: 50 µL/L. Flow rate: 40 mL/min. Room temperature | H2S |  | 382.7 | (Shang et al., 2016b) |
| Leaf waste biomass | LWB400 | Pyrolysis at 400 °C for 3 h |  | 10.23 | 13.59 | 0.0550 |  | Gas composition: 65% CH4, 35% CO2, <1% nitrogen, 4–5% moisture, trace amount of oxygen, and 500–1300 ppm H2S. Room temperature | H2S | 84.2% |  | (Sahota et al., 2018) |
| Anaerobically digested dairy fiber | T600x60 | Pyrolysis at 600 °C for 1 h. Modified with Na2CO3 |  |  | 142 (CO2) | 0.0350 |  | Synthetic gas containing 65.2 vol% CH4, 2045 ppm H2S, balance CO2. Biochar addition: 1.0 g. Flow rate: 5 mL/min | H2S |  | 542 | (Pelaez-Samaniego et al., 2018) |
| Pig manure | / | Pyrolysis at 500 °C for 4 h |  | 9.88 |  |  |  | H2S concentration: 1% (v/v). Flow rate: 500 mL/min. Biochar addition: 5.5 g. Room temperature. Moisture content: 25 wt% | H2S |  | 65.4 | (Xu et al., 2014) |
| Sewage sludge | / | Pyrolysis at 500 °C for 4 h |  | 8.33 |  |  |  | H2S concentration: 1% (v/v). Flow rate: 500 mL/min. Biochar addition: 10.0 g. Room temperature. Moisture content: 25 wt% | H2S |  | 47.5 |  |
| Wood pallets | ac.UWP | Pyrolysis at 700 °C for 0.5 h. Modified with steam |  | 9.0 | 625.4 |  |  | H2S concentration: 200 ppm. Flow rate: 180 mL/min. Room temperature. Syngas was composed: 30 v% of H2, 39.98 v% of CO, 15 v% of CH4, and 15 v% of CO2 | H2S |  | 12.92 | (Hervy et al., 2018) |
| Food Waste/Coagulation-flocculation sludge | ac.FW/CFS | Pyrolysis at 700 °C for 0.5 h. Modified with steam |  | 9.8 | 220.5 |  |  | H2S concentration: 200 ppm. Flow rate: 180 mL/min. Room temperature. Syngas was composed: 30 v% of H2, 39.98 v% of CO, 15 v% of CH4, and 15 v% of CO2 | H2S |  | 66.60 |  |
| Agricultural & forestry wastes | BC-4 | Pyrolysis at 500 °C for 0.5 h. Modified with urea |  |  | 987 | 0.534 |  | Simulated biogas containing 400 ± 10 mg/m3 of toluene, acetone, chlorobenzene, or hydrogen sulfide. Flow rate: 300 mL/min. Biochar addition: 10.0 g | H2S |  | 332 | (Qin et al., 2020) |
| Agricultural & forestry wastes | SBC-4 | Pyrolysis at 500 °C for 0.5 h. Modified with sludge |  |  | 931 | 0.516 |  | Simulated biogas containing 400 ± 10 mg/m3 of toluene, acetone, chlorobenzene, or hydrogen sulfide. Flow rate: 300 mL/min. Biochar addition: 10.0 g | H2S |  | 310 |  |
| Waste tire | T6 | Pyrolysis at 600 °C for 1 h |  |  | 85.4 | 0.311 |  | Reaction temperature (°C): 80. Hg0 concentration: 30 μg/m3. Flow rate: 850 mL/min. Carrier gas: 6 vol % O2 and N2. Biochar addition: 0.1 g | Hg0 | 88.3 | 407.0 (μg/g) | (Li et al., 2017) |
| Coconut pith | CP900 | Pyrolysis at 900 °C for 1 h |  |  | 393.46 | 0.2016 |  | Reaction temperature (°C): 50. Hg0 concentration: 200 μg/m3. Biochar addition: 0.05 g | Hg0 | / | 6067.49 (μg/g) | (Johari et al., 2016) |
| Municipal solid waste | C6WN5 | Pyrolysis at 600 °C for 2 h. Modified with NH4Cl |  |  | 12. | 0.040 |  | Reaction temperature (°C): 120. Hg0 concentration: 42 μg/m3. Flow rate: 850 mL/min. Flue gas: N2 and O2 (6 vol.%) | Hg0 | 65.9 | 157.7 (μg/g) | (Li et al., 2015) |
| Sorghum straw | SP-500-NO | Pyrolysis at 600 °C for 4 h |  |  | 6.4 | 0.014 |  | Hg0 concentration: 60.3 μg/m3. NO concentration: 4000ppm. Flow rate: 50 mL/min. Biochar addition: 0.03 g. Reaction temperature (°C): 30 | Hg0 | / | 2569.29 (ppm) | (Luo et al., 2019) |
| Rice straw | R6Cl | Pyrolysis at 600 °C for 1 h. Modified with Cl2 plasma |  |  | 33.5 |  |  | Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g. Reaction temperature (°C): 150 | Hg0 | 83.9 | 445.10 (μg/g) | (Wang et al., 2018b) |
| Tobacco straw | T6Cl | Pyrolysis at 600 °C for 1 h. Modified with Cl2 plasma |  |  | 6.2 |  |  | Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g. Reaction temperature (°C): 150 | Hg0 | 84.2 | 583.00 (μg/g) |  |
| Corn straw | C6Cl | Pyrolysis at 600 °C for 1 h. Modified with Cl2 plasma |  |  | 26.6 |  |  | Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g. Reaction temperature (°C): 150 | Hg0 | 42.7 | 150.80 (μg/g) |  |
| Wheat straw | W6Cl | Pyrolysis at 600 °C for 1 h. Modified with Cl2 plasma |  |  | 21.9 |  |  | Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g. Reaction temperature (°C): 150 | Hg0 | 52.7 | 217.60 (μg/g) |  |
| Millet straw | M6Cl | Pyrolysis at 600 °C for 1 h. Modified with Cl2 plasma |  |  | 31.9 |  |  | Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g. Reaction temperature (°C): 150 | Hg0 | 81.1 | 444.30 (μg/g) |  |
| Black bean straw | B6Cl | Pyrolysis at 600 °C for 1 h. Modified with Cl2 plasma |  |  | 6.1 |  |  | Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g. Reaction temperature (°C): 150 | Hg0 | 5.3 | 12.60 (μg/g) |  |
| Rice | RI-Cl | Pyrolysis at 600 °C for 1 h. Modified with HCl |  |  | 99.7 | 0.095 |  | Reaction temperature (°C): 150. Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g | Hg0 | 95 | 61.90 (μg/g) | (Wang et al., 2018c) |
| Tobacco | TO-Cl | Pyrolysis at 600 °C for 1 h. Modified with HCl |  |  | 353.4 | 0.245 |  | Reaction temperature (°C): 150. Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g | Hg0 | 100 | 81.30 (μg/g) |  |
| Corn | CO-Cl | Pyrolysis at 600 °C for 1 h. Modified with HCl |  |  | 93.3 | 0.163 |  | Reaction temperature (°C): 150. Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g | Hg0 | 94.3 | 65.00 (μg/g) |  |
| Wheat | WH-Cl | Pyrolysis at 600 °C for 1 h. Modified with HCl |  |  | 88.6 | 0.070 |  | Reaction temperature (°C): 150. Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g | Hg0 | 98.9 | 73.20 (μg/g) |  |
| Millet | MI-Cl | Pyrolysis at 600 °C for 1 h. Modified with HCl |  |  | 144.7 | 0.158 |  | Reaction temperature (°C): 150. Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g | Hg0 | 80 | 43.80 (μg/g) |  |
| Black bean straw | BB-Cl | Pyrolysis at 600 °C for 1 h. Modified with HCl |  |  | 60.7 | 0.064 |  | Reaction temperature (°C): 150. Hg0 concentration: 20 μg/m3. Flow rate: 2000 mL/min. Biochar addition: 0.05 g | Hg0 | 35.4 | 17.20 (μg/g) |  |
| Sawdust | Fe1.5MBC600 | One-step pyrolysis with FeCl3 at 600 °C for 1 h. |  |  | 120.82 | 0.20 |  | Reaction temperature (°C): 120. Hg0 concentration: 85 μg/m3. Flow rate: 1200 mL/min. Biochar addition: 0.05 g | Hg0 | >90 |  | (Yang et al., 2016) |
| Cotton straw | MnFe4%(3/10)/CSWU700 | Pyrolysis at 700 °C for 1 h. Modified with Microwave and Mn-Fe |  |  | 451.569 | 0.3011 |  | Reaction temperature (°C): 120. Flue gas consisted of 5% O2, 400 ppm NO, 600 ppm SO2, 5 vol% water vapor, 60 μg/m3 Hg0 vapor. Flow rate: 800 mL/min. Biochar addition: 0.1 g | Hg0 | 87.1 | 531.9 (μg/g) | (Shan et al., 2019) |
| Rice straw | B1C2 | Pyrolysis at 400 °C for 1 h. Modified with CaCO3 and CO2 |  |  | 742.5 | 0.70 |  | Carrier gas: N2, O2 (3.3 vol%), and Hg0 vapor (33.0 μg/m3). Flow rate: 1500 mL/min. Biochar addition: 0.03 g. Reaction temperature (°C): 80 | Hg0 | 90 |  | (Shi et al., 2020) |
| Bamboo | BB300 | Pyrolysis at 300 °C for 2 h. |  |  | 1.30 |  |  | Flow rate: 50 mL/min. Biochar addition: 0.05 g. Reaction temperature (°C): 20 | Acetone |  | 87.21 | (Zhang et al., 2017) |
| Sugarcane bagasse | BG300 | Pyrolysis at 300 °C for 2 h. |  |  | 5.20 |  |  | Flow rate: 50 mL/min. Biochar addition: 0.05 g. Reaction temperature (°C): 20 | Acetone |  | 91.84 |  |
| Hickory wood | HHP | Hydrothermal carbonization at 200 °C for 6 h. Modified with H3PO4 |  |  | 1436 | 0.028 |  | Flow rate: 50 mL/min. Biochar addition: 0.01 g. Reaction temperature (°C): 20 | Acetone/Cyclohexane |  | 148.05/159.67 | (Zhang et al., 2019b) |
| Peanut hull | PHP | Hydrothermal carbonization at 200 °C for 6 h. Modified with H3PO4 |  |  | 1091 | 0.079 |  | Flow rate: 50 mL/min. Biochar addition: 0.01 g. Reaction temperature (°C): 20 | Acetone/Cyclohexane |  | 113.72/100.68 |  |
| Hickory wood | HWBM450 | Pyrolysis at 450 °C for 2 h. Modified with ball milling |  |  | 284.74 | 0.304 |  | Flow rate: 50 mL/min. Biochar addition: 0.01 g. Reaction temperature (°C): 20 | Acetone/Ethanol/Chloroform/Cyclohexane/Toluene |  | 103.4/56.48/87.0/72.5/47.31 | (Xiang et al., 2020) |
| Rice husk | RH char-3 | Pyrolysis at 450 °C for 3 h. Modified with ball milling and KOH |  |  | 1818.45 | 0.90 |  | Toluene: 300 ppm, 30 mL/min. Phenol: 60ppm, 1.0 mL/min. Biochar addition: 0.1 g. Reaction temperature (°C): 20 | Toluene/Phenol |  | 263.6/6.53 | (Shen and Zhang, 2019) |
| Municipal solid waste | MSW-BC | Pyrolysis at 450 °C for 0.5 h |  |  |  |  |  | Toluene/M-xylene:50 μg/L. Biochar addition: 1 g/L. Reaction temperature (°C): 45 | Toluene/M-xylene |  | 850/612(μg/g) | (Jayawardhana et al., 2019) |
| Hickory wood chips | HH900 | Hydrothermal carbonization at 200 °C for 6 h. Modified with CO2 |  |  | 928 | 0.054 |  | Flow rate: 50 mL/min. Biochar addition: 0.01 g. Reaction temperature (°C): 20 | Acetone/Cyclohexane |  | 102.15/41.46/40.77/85.27/155.22/44.96 | (Zhang et al., 2020c) |
| Peanut shell | PH900 | Hydrothermal carbonization at 200 °C for 6 h. Modified with CO2 |  |  | 1308 | 0.114 |  | Flow rate: 50 mL/min. Biochar addition: 0.01 g. Reaction temperature (°C): 20 | Acetone/Cyclohexane |  | 122.43/47.14/32.78/99.37/65.52/59.53 |  |
| Agricultural & forestry wastes | BC-4 | Pyrolysis at 500 °C for 0.5 h. Modified with urea |  |  | 987 | 0.534 |  | Simulated biogas: 400 mg/m3 of toluene, acetone, chlorobenzene or hydrogen sulfide. Flow rate: 300 mL/min. Biochar addition: 10 g | Toluene/Acetone/Chlorobenzene |  | 519/236/516 | (Qin et al., 2020) |
| / | Biochar | / |  | 10.8 | 5.99 |  |  | 10% biochar+10% zeolite Running time of composting: 50d | NH3 | 63.4 |  | (Wang et al., 2017) |
| Tobacco stalk | Biochar | Pyrolyzed at 500-600 °C for 24 h |  | 10.80 |  |  |  | 10%biochar + 10% zeolite + 2.0%wood vinegar. Running time of composting: 50d | NH3 | 74.3 |  | (Wang et al., 2018a) |
| Paper sludge and wheat husks | P5000 | Pyrolyzed at 500 °C for 20 min |  | 9.3 in water |  |  |  | 6.67% biochar. [TAN]=6626 mg/kg. Running time of anaerobic digestion test: 63d | NH3 |  | 6.8 | (Mumme et al., 2014) |
| Wheat straw digestate | H5000 | 230 °C for 6 h |  | 4.8 in water |  |  |  | 6.67% biochar. [TAN]=6626 mg/kg. Running time of anaerobic digestion test: 63d | NH3 |  | 8.2 | (Mumme et al., 2014) |
| Rice husk | Biochar | / |  | 8.96 |  |  |  | 6% biochar. Running time of composting: 50d | NH3 | 75 |  | (Ravindran et al., 2022) |
| Charcoal | EG | Pyrolyzed at 400 °C |  |  | 35.48 |  |  | 10% biochar. Running time of composting:40d | NH3 | 20 |  | (Li et al., 2022) |
| Wheat straw | BC | Pyrolyzed at 500 °C |  | 10.1 | 79.6 |  |  | 0.5% biochar | NH3 | 26.5 |  | (Lan et al., 2022) |
| Tobacco stalk | R4 | Pyrolyzed at 450 °C for 2 h |  | 9.27 |  |  |  | 10% biochar. Running time of composting: 5d | NH3 | 58 |  | (Manu et al., 2021) |
| Wood materials | BC | Pyrolyzed at 600 °C |  |  |  |  |  | Experimental temperature: 25 °C. NH3 concentration: 50 ppm | NH3 |  | 50.8 | (Ramlogan et al., 2020) |
| Maple wood chips | py-ox wood NH3 + CO2 | Pyrolyzed at 500 °C |  |  |  |  |  | Exposed to CO2 for 1 h, flow rate of CO2 was 9 mL/min | NH3 |  | 40.57 | (Krounbi et al., 2020) |
| Switchgrass | Biochar | / |  |  | 16.73 |  |  | Fixed bed reactor. Biochar addition:1 g. gas residence time: 0.03−0.1 kg·m3/h. Space velocity:6.5 × 106 h−1. Reaction temperatures: 800 °C. Test time: 4 h | NH3 | Breakthrough time: 100 min |  | (Bhandari et al., 2014) |
| Agricultural & forestry wastes | BC-4 | Pyrolysis at 500 °C for 0.5 h. Modified with urea |  |  | 987 |  |  | Simulated biogas containing 400 ± 10 mg/m3 of toluene, acetone, chlorobenzene, or hydrogen sulfide. Flow rate: 300 mL/min. Biochar addition: 10.0 g | NH3 | 89.36 |  | (Qin et al., 2020) |

Note: “/” means “No”. SSA: specific surface area. TPV: Total pore volume.

Table S3. Functional groups of biochar involved in removing Hg0

| Feedstocks | Preparation temperature (°C) | Modification conditions | Before adsorption | After adsorption | Functional groups | References |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Content (%) | Content (%) |  |  |
| Municipal solid waste | 600 | NH4Cl+steam | 5.04/34.32/33.73/26.91 | 1.89/30.13/48.87/19.02 | Carbide/C–C/C–OH or C–O–C/C=O | (Li et al., 2015) |
| Wheat | 600 | / | 19.5/—/80.5/49.9/27.4/17.3/5.4 | / | Organic sulfide/Thiophenic sulfur/Sulfate sulfur/C-C/C-O/C=O/-O-C=O | (Zhang et al., 2019a) |
| Wheat | 600 | H2S plasma | 49.2/11.2/39.6/43.2/34.8/14.6/7.4 | 39.4/19.4/41.2/49.6/34.3/12.0/4.1 | Organic sulfide/Thiophenic sulfur/Sulfate sulfur/C-C/C-O/C=O/-O-C=O |  |
| Municipal solid waste | 600 | / | 79.5/17.5/3.0 | / | C-O/Chemisorbed O/Lattice O | (Li et al., 2017) |
| Municipal solid waste | 600 | NH4Cl | 89.4/10.6 | 47.4/52.6 | C-Cl/Cl- |  |
| BFR plastic computer shell/waste wood | One-step pyrolysis (500) | / | 0.25/1.478 | / | Br-/C-Br | (Xu et al., 2018) |
| BFR plastic computer shell/Waste wood | One-step pyrolysis (600) | / | 0.35/2.345 | / | Br-/C-Br |  |
| BFR plastic computer shell/Waste wood | One-step pyrolysis (700) | / | 0.16/0.613 | / | Br-/C-Br |  |
| FeCl3·6H2O/Sawdust | One-step pyrolysis (600) | / | 67.2/12.7/20.1/530.1-530.5/531.6-531.9/533.1-533.7 | 70.1/20.7/9.2/530.1-530.5/531.6-531.9/533.1-533.7 | C=C/C–O/C=O/Lattice oxygen/Chemisorbed oxygen/C-O | (Yang et al., 2016) |
| Rice straw | 600 | / | 83.8/11.4/1.9/2.9/28.6/43.9/27.5/60.9/34.1/5.0 | / | C–C/C-O/C=O/C(O)-O-C/Sulfide/Elemental (organic、sulfur)/Sulfate/Cl-/C-Cl2p2/3/C-Cl2p1/2 | (Wang et al., 2018b) |
| Rice straw | 600 | Cl2 plasma | 74.4/20.1/2.3/3.2/2.7/36.7/60.6/45.1/48.9/6.0 | —/—/—/—/—/—/—/57.9/35.5/6.6 | C–C/C-O/C=O/C(O)-O-C/Sulfide/Elemental (organic、sulfur)/Sulfate/Cl-/C-Cl2p2/3/C-Cl2p1/2 |  |
| Rice | 600 | / | 71.8/1.5/83.7/11.4/2.0/2.9/60.8/34.2/5.0 | / | C/Cl/C–C/C-O/C=O/C(O)-O-C/Cl-/C-Cl2p2/3/C-Cl2p1/2 | (Wang et al., 2018c) |
| Rice | 600 | HCl | 72.1/0.3/74.3/19.6/3.8/2.3/31.4/47.3/21.3 | / | C/Cl/C–C/C-O/C=O/C(O)-O-C/Cl-/C-Cl2p2/3/C-Cl2p1/2 |  |
| Rice straw | 600 | / | 55.6/44.4/7.8/49.3/42.9 | / | Cl-/C-Cl/C-NH2/Pyridone/NO3- | (Zhang et al., 2020a) |
| Rice straw | 600 | Cl2 plasma | 52.4/47.6/9.6/65.3/25.1 | / | Cl-/C-Cl/C-NH2/Pyridone/NO3- |  |

Note: “—” means “Not measured”

Fig. S1 Mechanisms involved in the removal of H2S by biochar, and the catalytic oxidation of COS/CS2

H2S(gas), H2S(ads) and H2S(ads–liq) denote H2S in gas phase, adsorption phase, and liquid phase, respectively. HS–(ads) denotes HS– adsorbed by biochar

Fig. S2 Mechanisms involved in the removal of Hg0 to modified biochar

References

Bhandari, P.N., Kumar, A., Huhnke, R.L., 2014. Simultaneous removal of toluene (Model Tar), NH3, and H2S, from biomass-generated producer gas using biochar-based and mixed-metal oxide catalysts. Energ Fuel 28, 1918-1925.

Braghiroli, F.L., Bouafif, H., Koubaa, A., 2019. Enhanced SO2 adsorption and desorption on chemically and physically activated biochar made from wood residues. Ind Crop Prod 138, 111456.

Hervy, M., Minh, P.D., Gérente, C., Weiss-Hortala, E., Nzihou, A., Villot, A., Coq, L.L., 2018. H2S removal from syngas using wastes pyrolysis chars. Chem Eng J 334, 2179-2189.

Iberahim, N., Sethupathi, S., Bashir, M.J.K., 2018. Optimization of palm oil mill sludge biochar preparation for sulfur dioxide removal. Environ. Sci. Pollut. Res. 25, 25702-25714.

Iberahim, N., Sethupathi, S., Goh, C.L., Bashir, M.J.K., Ahmad, W., 2019. Optimization of activated palm oil sludge biochar preparation for sulphur dioxide adsorption. J. Environ. Manage. 248, 109302.

Jayawardhana, Y., Gunatilake, S.R., Mahatantila, K., Ginige, M.P., Vithanage, M., 2019. Sorptive removal of toluene and m-xylene by municipal solid waste biochar: Simultaneous municipal solid waste management and remediation of volatile organic compounds. J. Environ. Manage. 238, 323-330.

Johari, K., Saman, N., Song, S.T., Cheu, S.C., Kong, H., Mat, H., 2016. Development of coconut pith chars towards high elemental mercury adsorption performance - Effect of pyrolysis temperatures. Chemosphere 156, 56-68.

Krounbi, L., Enders, A., Anderton, C.R., Engelhard, M.H., Hestrin, R., Torres-Rojas, D., Dynes, J.J., Lehmann, J., 2020. Sequential ammonia and carbon dioxide adsorption on pyrolyzed biomass to recover waste stream nutrients. ACS Sustain Chem Eng 8, 7121-7131.

Lan, T., Huang, Y., Song, X., Deng, O., Zhou, W., Luo, L., Tang, X., Zeng, J., Chen, G., Gao, X., 2022. Biological nitrification inhibitor co-application with urease inhibitor or biochar yield different synergistic interaction effects on NH3 volatilization, N leaching, and N use efficiency in a calcareous soil under rice cropping. Environ Pollut 293, 118499.

Li, G., Wang, S., Wang, F., Wu, Q., Tang, Y., Shen, B., 2017. Role of inherent active constituents on mercury adsorption capacity of chars from four solid wastes. Chem Eng J 307, 544-552.

Li, G.L., Shen, B.X., Li, F.K., Tian, L.H., Singh, S., Wang, F.M., 2015. Elemental mercury removal using biochar pyrolyzed from municipal solid waste. Fuel Process Technol 133, 43-50.

Li, Y., Ma, J., Yong, X., Luo, L., Wong, J.W.C., Zhang, Y., Wu, H., Zhou, J., 2022. Effect of biochar combined with a biotrickling filter on deodorization, nitrogen retention, and microbial community succession during chicken manure composting. Bioresour Technol 343, 126137.

Luo, J.J., Jin, M.C., Ye, L.R., Cao, Y.A., Yan, Y.G., Du, R.P., Yoshiie, R., Ueki, Y., Naruse, I., Lin, C.J., Lee, Y.Y., 2019. Removal of gaseous elemental mercury by hydrogen chloride non-thermal plasma modified biochar. J Hazard Mater 377, 132-141.

Manu, M.K., Wang, C., Li, D., Varjani, S., Xu, Y., Ladumor, N., Lui, M., Zhou, J., Wong, J.W.C., 2021. Biodegradation kinetics of ammonium enriched food waste digestate compost with biochar amendment. Bioresour Technol 341, 125871.

Mumme, J., Srocke, F., Heeg, K., Werner, M., 2014. Use of biochars in anaerobic digestion. Bioresour Technol 164, 189-197.

Pelaez-Samaniego, M.R., Smith, M.W., Zhao, Q.B., Garcia-Perez, T., Frear, C., Garcia-Perez, M., 2018. Charcoal from anaerobically digested dairy fiber for removal of hydrogen sulfide within biogas. Waste Manage 76, 374-382.

Qin, L.B., Huang, X.M., Xue, Q., Liu, L., Wan, Y., 2020. In-situ biodegradation of harmful pollutants in landfill by sludge modified biochar used as biocover. Environ Pollut 258, 113710.

Ramlogan, M.V., Rabinovich, A., Rouff, A.A., 2020. Thermochemical analysis of ammonia gas sorption by struvite from livestock wastes and comparison with biochar and metal-organic framework sorbents. Environ Sci Technol 54, 13264-13273.

Ravindran, B., Awasthi, M.K., Karmegam, N., Chang, S.W., Chaudhary, D.K., Selvam, A., Nguyen, D.D., Rahman Milon, A., Munuswamy-Ramanujam, G., 2022. Co-composting of food waste and swine manure augmenting biochar and salts: Nutrient dynamics, gaseous emissions and microbial activity. Bioresour Technol 344, 126300.

Sahota, S., Vijay, V.K., Subbarao, P.M.V., Chandra, R., Ghosh, P., Shah, G., Kapoor, R., Vijay, V., Koutu, V., Thakur, I.S., 2018. Characterization of leaf waste based biochar for cost effective hydrogen sulphide removal from biogas. Bioresour Technol 250, 635-641.

Shan, Y., Yang, W., Li, Y., Liu, Y.X., Pan, J.F., 2019. Preparation of microwave-activated magnetic bio-char adsorbent and study on removal of elemental mercury from flue gas. Sci Total Environ 697, 134049.

Shang, G.F., Li, Q.W., Liu, L., Chen, P., Huang, X.M., 2016a. Adsorption of hydrogen sulfide by biochars derived from pyrolysis of different agricultural/forestry wastes. J Air Waste Manage 66, 8-16.

Shang, G.F., Liu, L., Chen, P., Shen, G.Q., Li, Q.W., 2016b. Kinetics and the mass transfer mechanism of hydrogen sulfide removal by biochar derived from rice hull. J Air Waste Manage 66, 439-445.

Shao, J.G., Zhang, J.J., Zhang, X., Feng, Y., Zhang, H., Zhang, S.H., Chen, H.P., 2018. Enhance SO2 adsorption performance of biochar modified by CO2 activation and amine impregnation. Fuel 224, 138-146.

Shen, Y.F., Zhang, N.Y., 2019. Facile synthesis of porous carbons from silica-rich rice husk char for volatile organic compounds (VOCs) sorption. Bioresour Technol 282, 294-300.

Shi, Q.Q., Wang, Y.T., Zhang, X., Shen, B.X., Wang, F.M., Zhang, Y.F., 2020. Hierarchically porous biochar synthesized with CaCO3 template for efficient Hg0 adsorption from flue gas. Fuel Process Technol 199, 106247.

Wang, Q., Awasthi, M.K., Ren, X., Zhao, J., Li, R., Wang, Z., Chen, H., Wang, M., Zhang, Z., 2017. Comparison of biochar, zeolite and their mixture amendment for aiding organic matter transformation and nitrogen conservation during pig manure composting. Bioresour Technol 245, 300-308.

Wang, Q., Awasthi, M.K., Ren, X., Zhao, J., Li, R., Wang, Z., Wang, M., Chen, H., Zhang, Z., 2018a. Combining biochar, zeolite and wood vinegar for composting of pig manure: The effect on greenhouse gas emission and nitrogen conservation. Waste Manage 74, 221-230.

Wang, T., Liu, J., Zhang, Y.S., Zhang, H.C., Chen, W.Y., Norris, P., Pan, W.P., 2018b. Use of a non-thermal plasma technique to increase the number of chlorine active sites on biochar for improved mercury removal. Chem Eng J 331, 536-544.

Wang, T., Wu, J.W., Zhang, Y.S., Liu, J., Sui, Z.F., Zhang, H.C., Chen, W.Y., Norris, P., Pan, W.P., 2018c. Increasing the chlorine active sites in the micropores of biochar for improved mercury adsorption. Fuel 229, 60-67.

Xiang, W., Zhang, X.Y., Chen, K.Q., Fang, J., He, F., Hu, X., Tsang, D.C.W., Ok, Y.S., Gao, B., 2020. Enhanced adsorption performance and governing mechanisms of ball-milled biochar for the removal of volatile organic compounds (VOCs). Chem Eng J 385, 123842.

Xu, X.Y., Cao, X.D., Zhao, L., Sun, T.H., 2014. Comparison of sewage sludge- and pig manure-derived biochars for hydrogen sulfide removal. Chemosphere 111, 296-303.

Xu, X.Y., Huang, D.X., Zhao, L., Kan, Y., Cao, X.D., 2016. Role of inherent inorganic constituents in SO2 sorption ability of biochars derived from three biomass wastes. Environ Sci Technol 50, 12957-12965.

Xu, Y., Deng, F.F., Pang, Q.C., He, S.W., Xu, Y.Q., Luo, G.Q., Yao, H., 2018. Development of waste-derived sorbents from biomass and brominated flame retarded plastic for elemental mercury removal from coal-fired flue gas. Chem Eng J 350, 911-919.

Yang, J.P., Zhao, Y.C., Ma, S.M., Zhu, B.B., Zhang, J.Y., Zheng, C.G., 2016. Mercury removal by magnetic biochar derived from simultaneous activation and magnetization of sawdust. Environ Sci Technol 50, 12040-12047.

Zhang, H.C., Wang, T., Sui, Z.F., Zhang, Y.S., Sun, B.M., Pan, W.P., 2019a. Enhanced mercury removal by transplanting sulfur-containing functional groups to biochar through plasma. Fuel 253, 703-712.

Zhang, H.C., Wang, T., Zhang, Y.S., Sun, B.M., Pan, W.P., 2020a. Promotional effect of NH3 on mercury removal over biochar thorough chlorine functional group transformation. J Clean Prod, 120598.

Zhang, J.J., Shao, J.G., Huang, D.R., Feng, Y., Zhang, X., Zhang, S.H., Chen, H.P., 2020b. Influence of different precursors on the characteristic of nitrogen-enriched biochar and SO2 adsorption properties. Chem Eng J 385, 123932.

Zhang, X.Y., Gao, B., Fang, J., Zou, W.X., Dong, L., Cao, C.C., Zhang, J., Li, Y.C., Wang, H.L., 2019b. Chemically activated hydrochar as an effective adsorbent for volatile organic compounds (VOCs). Chemosphere 218, 680-686.

Zhang, X.Y., Gao, B., Zheng, Y.L., Hu, X., Creamer, A.E., Annable, M.D., Li, Y.C., 2017. Biochar for volatile organic compound (VOC) removal: Sorption performance and governing mechanisms. Bioresour Technol 245, 606-614.

Zhang, X.Y., Xiang, W., Wang, B., Fang, J., Zou, W.X., He, F., Li, Y.C., Tsang, D.C.W., Ok, Y.S., Gao, B., 2020c. Adsorption of acetone and cyclohexane onto CO2 activated hydrochars. Chemosphere 245, 125664.