Supporting Information (SI)

p-Arsanilic acid decontamination over a wide pH range using biochar-supported manganese ferrite material as an effective persulfate catalyst: Performances and mechanisms

Bin Yaoa, Xia Chena, Kun Zhoua, Zirui Luoa, Peipei Lia, Zihui Yangb, Yaoyu Zhoua*

a Hunan International Scientific and Technological Cooperation Base of Agricultural Typical Pollution Remediation and Wetland Protection, College of Resources and Environment, Hunan Agricultural University, Changsha 410128, China

b College of Veterinary Medicine, Hunan Agricultural University, Changsha 410128, China

The number of pages: 6

The number of tables: 1

The number of figures: 2

List of Supporting Information

Table:

Table S1. Porosity characteristic of BC and MFB. (Page S4).

Figures:

Fig. S1. Proposed degradation pathway of p-ASA in the MFB/PS system. (Page S5).

Fig. S2. Inorganic arsenic concentrations variations in the MFB/PS system. Reaction conditions: MFB = 1.0 g/L, PS = 2.1 mM, pH = 7.0, T = 298 K. (Page S6).
Table S1. Porosity characteristic of BC and MFB.

| Materials | BC | MFB |
| --- | --- | --- |
| SSABET (m2/g) | 9.82 | 97.83 |
| Total pore volume (cm3/g) | 0.016 | 0.16 |
| Average pore diameter (nm) | 7.72 | 8.53 |

BET: Brunauer-Emmett-Teller

Fig. S1. Proposed degradation pathway of p-ASA in the MFB/PS system.

Fig. S2. Inorganic arsenic concentrations variations in the MFB/PS system. Reaction conditions: MFB = 1.0 g/L, PS = 2.1 mM, pH = 7.0, T = 298 K.

* Corresponding author: zhouyy@hunau.edu.cn, (Y. Zhou)