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Table S1. Porosity characteristic of BC and MFB.
	Materials
	BC
	MFB

	SSABET (m2/g)
	[bookmark: OLE_LINK99][bookmark: OLE_LINK100]9.82
	97.83

	[bookmark: _GoBack]Total pore volume (cm3/g)
	0.016
	0.16

	Average pore diameter (nm)
	7.72
	8.53


BET: Brunauer-Emmett-Teller
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Fig. S1. Proposed degradation pathway of p-ASA in the MFB/PS system.
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Fig. S2. Inorganic arsenic concentrations variations in the MFB/PS system. Reaction conditions: MFB = 1.0 g/L, PS = 2.1 mM, pH = 7.0, T = 298 K.
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