Wood-derived biochar as thick electrodes for high-rate performance supercapacitors

Bing Yan1, Jiaojiao Zheng1, Li Feng1, Cheng Du2, 3, Shaoju Jian4, Weisen Yang4, Yimin A. Wu3,*, Shaohua Jiang1, Shuijian He1,*, Wei Chen 2, 5,*

1 International Innovation Center for Forest Chemicals and Materials, Co-Innovation Center of Efficient Processing and Utilization of Forest Resources, College of Materials Science and Engineering, Nanjing Forestry University, Nanjing, 210037, China.

2 State Key Laboratory of Electroanalytical Chemistry, Changchun Institute of Applied Chemistry, Chinese Academy of Sciences, Changchun 130022, Jilin, PR China.

3 Department of Mechanical and Mechatronics Engineering Waterloo Institute of Nanotechnology, University of Waterloo, Waterloo, ON, N2 L 3G1 Canada.

4 Fujian Key Laboratory of Eco-Industrial Green Technology, College of Ecology and Resources Engineering, Wuyi University, Wuyishan 354300, China.

5 University of Science and Technology of China, Hefei 230026, PR China.
* Corresponding authors

E-mail: yimin.wu@uwaterloo.ca (Yimin A. Wu), shuijianhe@njfu.edu.cn (Shuijian He), weichen@ciac.ac.cn (Wei Chen).

List of contents

S1. Material characterization and electrochemical measurements of samples

S2. Photographic images and SEM images of samples

S3. Analysis of heteroatom-containing functional groups

S4. Capacitive properties of electrodes

S5. Porosity and element characteristics of samples

S6. Specific parameters of capacitance performance

S7. Comparison of this work with other studies

## S1. Material characterization and electrochemical measurements of samples

## Material characterization

The average carbon crystallite lattice parameters: inter-layer spacing (d002) and crystallite height (Lc) were determined on basis of XRD results via the Bragg (equation (1)) and Scherrer equations (equation (2)) (Hadoun et al. 2013):

2d002sinθ = λ           (1)

Lc = 0.89λBccosθ             (2)

Where λ (nm), θ (°), and Bc (°) stands for X-ray wavelength (0.154056 nm for copper Kα radiation), peak position of (002) band, and full width at half maximum (FWHM) of the corresponding band, respectively.

## Electrochemical measurements

CV is a capable electrochemical analysis means for researching the reaction kinetics of different kinds of electrodes. Based on the Duun’s method (Augustyn et al. 2014), the voltage response of electroactive species at disparate scanning rates can be described in the following equations:

i = a × vb                      (3);                                                logi = b × logv + loga                         (4)

Where i is current response at a fixed potential, ν is the scan rate, the a and b present fitting parameters. The parameter b value determined from the slope of the log i with respect to log v, which can be used to estimate the type of charge storage. Usually, when b value is 0.5, it represents a diffusion-controlled faradaic behavior, and when b value of 1 indicate a non-faradaic capacitive process

By separating the total current response (i) at a given voltage, the contribution can be quantitatively separated into capacitive-controlled process and diffusion-controlled process according to the following equation:

i = k1v + k2v1/2          (5)

Where the k1ν and k2ν1/2 correspond to capacitive- and diffusion-controlled contribution, respectively.

The areal specific capacitances (Cs, mF cm-2), gravimetric specific capacitances (Cm, F g-1) and volumetric specific capacitances (Cv, F cm-3) were both calculated from discharge curves.

For three-electrode system, the Cs and Cm of a single electrode was obtained from GCD curves according to equations (6) and (7), respectively. The Cv of single electrode was calculated from Cs by the formula (8). Moreover, the SSA-normalized capacitance was calculated from Cm and SSA by formula (9).

Cs = IΔtsΔV                       (6);                      Cm = IΔtmΔV                (7);                      Cv = Csd                  (8)

SSA-normalized capacitance = CmSSA             (9)

Where I (A) is the discharge current, Δt (s) is the galvanostatic discharge time (s), s, d, m represent the area (cm2), thickness (cm) and mass (g) of carbon monolith in a single electrode, respectively. ΔV (V) is potential window of the discharge process. That is, I/s (mA cm-2) and I/m (A g-1) refer to the areal current density and gravimetric current density, respectively.

Two pieces of FA-OC2 slices were used to assemble a symmetric supercapacitor. The C’s, C’m and C’v of a single electrode under the two-electrode system can be calculated from GCD curves by the equations (10) to (12).

C's = 2×I×Δts×ΔV                 (10);              C'm = 2×I×Δtm×ΔV               (11);              C'v = C'sd                 (12)

Similarly, I (A) is the discharge current, Δt (s) is the galvanostatic discharge time (s), s, d, m represent the area (cm2), thickness (cm) and mass (g) of carbon monolith in a single electrode, respectively. ΔV (V) is potential window of the discharge process. That is, I/s (mA cm-2) and I/m (A g-1) refer to the areal current density and gravimetric current density, respectively.

The areal energy density (Es, mWh cm-2), areal power density (Ps, mW cm-2), gravimetric energy density (Em, Wh kg-1), gravimetric power density (Pm, W kg-1), volumetric energy density (Ev, mWh cm-3) and volumetric power density (Pv, mW cm-3) of electrodes was based on the calculated capacitance values and evaluated according to the following equation:

Es = C's×∆V27200                    (13);                                                    PS = 3600×ESΔt                            (14)

Em = C'm×∆V27.2                  (15);                                                   Pm = 3600×EmΔt                            (16)

Ev= Esd                               (17);                                                  Pv = Psd                                        (18)

## S2. Photographic images and SEM images of samples

Fig. S1 Photographic images of (a) the natural W, FA-W, FA-OC and the thickness of (b) W and (c) FA-OC

Fig. S2 SEM images of FA-OC2, (a) the top view of channels, (b) the cross-section view of vertical channels, (c) high magnification image of a channel

## S3. Analysis of heteroatom-containing functional groups

Fig. S3 High-resolution N 1s spectra of FA-OC

Fig. S4 Schematic diagram of the carbon matrix, indicating the locations of the various N/O-containing functional groups

## S4. Capacitive properties of electrodes

Fig. S5 (a) the CV curves of WC and OC at 100 mV s-1. (b) The GCD profiles of WC and OC at 10 mA cm-2

Fig. S6 (a-d) The capacitive contribution from CV curves of FA-OC electrodes at different scan rates. (e) The fitted EIS plots of FA-OC, the inset is the corresponding equivalent circuit diagram

Fig. S7 (a) The CV curves of FA-OC1 at different scan rates and (b-g) corresponding capacitive contribution. (h, i) The GCD profiles of FA-OC1 at various current densities

Fig. S8 (a-e) The capacitive contribution of FA-OC2 at different scan rates. (f) The GCD profiles of FA-OC2 at various current densities

Fig. S9 (a) The CV curves of FA-OC3 at different scan rates and (b-g) corresponding capacitive contribution. (h, i) The GCD profiles of FA-OC3 at various current densities

Fig. S10 The comparison profiles of rate performance of FA-OC, FA-OC1, FA-OC2 and FA-OC3: (a) Cs (b) Cm and Cv. (d) The fitted EIS plots of FA-OC1, FA-OC2 and FA-OC3, the inset is the corresponding equivalent circuit diagram

Fig. S11 The Ps, Pm, Pv and Es, Em, Ev of FA-OC2//FA-OC2 symmetric supercapacitor

## S5. Porosity and element characteristics of samples

Table S1 Porosity and element characteristics of the prepared WC, OC, FA-OC, FA-OC1, FA-OC2, and FA-OC3 samples

| Sample | SSA (m² g-1) | Vt (cm³ g-1) | C (atomic %) | O (atomic %) | N (atomic %) |
| --- | --- | --- | --- | --- | --- |
| WC | 110.7 | 0.15 | 92.7 | 7.3 | / |
| OC | 204.83 | 0.13 | 86.2 | 12.8 | / |
| FA-OC | 312.73 | 0.15 | 89.1 | 8.6 | 2.3 |
| FA-OC1 | 155.94 | 0.07 | 88.5 | 9.2 | 2.3 |
| FA-OC2 | 126.21 | 0.06 | 87.5 | 10.3 | 2.2 |
| FA-OC3 | 73.16 | 0.03 | 84.6 | 13.6 | 1.8 |

The SSA and Vt of WC was obtained from Ref. (Tang et al. 2018).

## S6. Specific parameters of capacitance performance

Table S2 The calculated Cs, Cm and Cv of the prepared OC electrodes at different current densities

| Current density (mA cm-2) | Current density (A g-1) | Cs (mF cm-2) | Cm (F g-1) | Cv (F cm-3) |
| --- | --- | --- | --- | --- |
| 5 | 0.09 | 3190.0 | 79.8 | 39.9 |
| 10 | 0.17 | 2640.0 | 66.0 | 33.0 |
| 30 | 0.56 | 2085.4 | 52.1 | 26.1 |
| 50 | 0.93 | 1802.3 | 45.1 | 22.5 |
| 100 | 1.85 | 1431.6 | 35.8 | 17.9 |

Table S3 The calculated Cs, Cm and Cv of the prepared FA-OC electrodes at different current densities

| Current density (mA cm-2) | Current density (A g-1) | Cs (mF cm-2) | Cm (F g-1) | Cv (F cm-3) |
| --- | --- | --- | --- | --- |
| 2 | 0.04 | 4346.1 | 120.7 | 54.3 |
| 5 | 0.10 | 3775.0 | 104.9 | 47.2 |
| 10 | 0.20 | 3506.3 | 97.4 | 43.8 |
| 30 | 0.58 | 3137.4 | 87.2 | 39.2 |
| 50 | 0.96 | 3005.0 | 83.5 | 37.6 |
| 100 | 1.92 | 2759.2 | 79.9 | 34.5 |
| 200 | 3.85 | 2333.3 | 66.9 | 29.2 |
| 300 | 5.77 | 1843.1 | 51.0 | 22.9 |
| 400 | 7.69 | 1208.4 | 33.4 | 15.1 |
| 500 | 9.62 | 821.8 | 23.1 | 10.3 |

Table S4 The fitted resistance value of OC and FA-OC, respectively

| Electrodes | Rs (ohm) | Rct (ohm) | Wo (ohm) |
| --- | --- | --- | --- |
| OC | 1.15 | 0.62 | 4.86 |
| FA-OC | 0.98 | 0.41 | 3.84 |

Table S5 The calculated Cs, Cm, Cv and SSA-normalized capacitance of the prepared FA-OC1 electrodes at different current densities

| Current density (mA cm-2) | Current density (A g-1) | Cs (mF cm-2) | Cm (F g-1) | Cv (F cm-3) | SSA-normalized capacitance (μF cm-2) |
| --- | --- | --- | --- | --- | --- |
| 2 | 0.05 | 4688.5 | 154.5 | 58.6 | 99.1 |
| 5 | 0.11 | 3955.6 | 130.1 | 49.4 | 83.4 |
| 10 | 0.23 | 3670.3 | 118.9 | 45.9 | 76.2 |
| 30 | 0.68 | 3309.8 | 108.6 | 41.4 | 69.6 |
| 50 | 0.14 | 3113.8 | 103.2 | 38.9 | 66.2 |
| 100 | 2.27 | 2973.1 | 97.8 | 37.2 | 62.7 |
| 200 | 4.55 | 2783.0 | 92.0 | 34.8 | 59.0 |
| 300 | 6.82 | 2681.7 | 89.2 | 33.5 | 57.2 |
| 400 | 9.09 | 2533.4 | 84.3 | 31.7 | 54.1 |
| 500 | 11.36 | 2367.0 | 78.7 | 29.6 | 50.5 |

Table S6 The calculated Cs, Cm, Cv and SSA-normalized capacitance of the prepared FA-OC2 electrodes at different current densities

| Current density (mA cm-2) | Current density (A g-1) | Cs (mF cm-2) | Cm (F g-1) | Cv (F cm-3) | SSA-normalized capacitance (μF cm-2) |
| --- | --- | --- | --- | --- | --- |
| 2 | 0.05 | 6538.5 | 223.9 | 81.7 | 177.4 |
| 5 | 0.13 | 5620.4 | 192.5 | 70.3 | 152.5 |
| 10 | 0.25 | 5183.6 | 177.5 | 64.8 | 140.6 |
| 30 | 0.75 | 4509.0 | 154.4 | 56.4 | 122.3 |
| 50 | 1.25 | 4386.0 | 150.2 | 54.8 | 119.1 |
| 100 | 2.50 | 4259.4 | 145.9 | 53.2 | 115.6 |
| 200 | 5.00 | 4152.4 | 142.2 | 51.9 | 112.7 |
| 300 | 7.50 | 4025.6 | 137.9 | 50.3 | 109.3 |
| 400 | 10.00 | 3948.8 | 135.2 | 49.4 | 107.1 |
| 500 | 12.50 | 3821.2 | 130.9 | 47.8 | 103.7 |

Table S7 The calculated Cs, Cm, Cv and SSA-normalized capacitance of the prepared FA-OC3 electrodes at different current densities

| Current density (mA cm-2) | Current density (A g-1) | Cs (mF cm-2) | Cm (F g-1) | Cv (F cm-3) | SSA-normalized capacitance (μF cm-2) |
| --- | --- | --- | --- | --- | --- |
| 2 | 0.05 | 6516.3 | 229.4 | 81.5 | 313.6 |
| 5 | 0.13 | 5128.4 | 180.6 | 64.1 | 246.9 |
| 10 | 0.26 | 4445.1 | 156.5 | 55.6 | 213.9 |
| 30 | 0.79 | 4048.6 | 142.6 | 50.6 | 194.9 |
| 50 | 1.32 | 3978.8 | 140.1 | 49.7 | 191.5 |
| 100 | 2.63 | 3763.4 | 133.2 | 47.0 | 182.1 |
| 200 | 5.26 | 3646.6 | 129.3 | 45.6 | 176.7 |
| 300 | 7.89 | 3557.4 | 124.9 | 44.5 | 170.7 |
| 400 | 10.53 | 3412.0 | 118.8 | 42.7 | 162.4 |
| 500 | 13.16 | 3309.5 | 114.8 | 41.4 | 156.9 |

Table S8 The fitted resistance value of FA-OC1, FA-OC2 and FA-OC3, respectively

| Electrodes | Rs (ohm) | Rct (ohm) | Wo (ohm) |
| --- | --- | --- | --- |
| FA-OC1 | 1.03 | 0.74 | 2.01 |
| FA-OC2 | 1.12 | 0.37 | 1.80 |
| FA-OC3 | 1.33 | 0.82 | 2.02 |

Table S9 The calculated C’s, C’m, C’v and SSA-normalized capacitance of the prepared FA-OC2//FA-OC2 symmetric supercapacitors at different current densities

| Current density (mA cm-2) | Current density (A g-1) | C’s (mF cm-2) | C’m (F g-1) | C’v (F cm-3) |
| --- | --- | --- | --- | --- |
| 2 | 0.05 | 5037.5 | 172.5 | 63.0 |
| 5 | 0.13 | 4924.9 | 168.7 | 61.6 |
| 10 | 0.25 | 4791.2 | 164.1 | 59.9 |
| 15 | 0.38 | 4551.7 | 155.9 | 56.9 |
| 20 | 0.50 | 4421.3 | 151.4 | 55.3 |
| 25 | 0.63 | 4250.0 | 145.5 | 53.1 |
| 30 | 0.75 | 4207.8 | 144.1 | 52.6 |
| 50 | 1.25 | 4006.2 | 137.2 | 50.1 |
| 100 | 2.50 | 3622.9 | 124.1 | 45.3 |

Table S10 The calculated Ps, Pm, Pv and Es, Em, Ev of FA-OC2//FA-OC2 symmetric supercapacitor

| Current density (mA cm-2) | Ps (mW cm-2) | Es (mWh cm-2) | Pm (W kg-1) | Em (Wh kg-1) | Pv (mW cm-3) | Ev (mWh cm-3) |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2 | 1.9 | 0.65 | 65.8 | 22.44 | 24.0 | 8.15 |
| 5 | 4.8 | 0.63 | 164.2 | 21.54 | 59.9 | 7.86 |
| 10 | 9.2 | 0.58 | 315.9 | 19.87 | 115.5 | 7.23 |
| 15 | 13.0 | 0.52 | 446.9 | 17.68 | 163.1 | 6.44 |
| 20 | 16.5 | 0.44 | 565.8 | 15.06 | 206.5 | 5.53 |
| 25 | 20.0 | 0.39 | 684.9 | 13.29 | 250.0 | 4.87 |
| 30 | 23.1 | 0.36 | 791.1 | 12.22 | 288.8 | 4.48 |
| 50 | 30.5 | 0.22 | 1045.6 | 7.56 | 381.6 | 2.76 |
| 100 | 58.0 | 0.16 | 1996.4 | 5.61 | 725.0 | 2.03 |

## S7. Comparison of this work with other studies

Table S9 The comparison of electrochemical performance between FA-OC2//FA-OC2 symmetric supercapacitor and the wood-based and other biomass-based symmetric/asymmetric supercapacitor reported in the literatures

| Precursor | Material functionalization | Initial capacitance | Rate performance | Cycle durability | Maximum energy density | Maximum power density | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Basswood | 10.3% for O, 2.2% for N. | 5037.5 mF cm-2, 172.5 F g-1, 63.0 F cm-3 at 2 mA cm-2 | 4207.8 mF cm-2, 144.1 F g-1, 52.6 F cm-3 at 30 mA cm-2 | 90.7% 10,000 100 mA cm-2 | 0.65 mWh cm-2, 22.44 Wh kg-1, 8.15 mWh cm-3 | 58.0 mW cm-2, 1996.4 W kg-1 725 mW cm-3 | This work |
| Chinese fir wood | N/O-doped NiCo-LDH | 4740 mF cm-2 at 5 mA cm-2 | 2460 mF cm-2 at 30 mA cm-2 | 93.2% 8,000 80 mA cm-2 | 1.48 mWh cm-2 | 22.4 mW cm-2 | (Li et al. 2021b) |
| Basswood | 19.86% for O 9.24% for P | 4700 mF cm-2, 206.5 F g-1, 29.3 F cm-3 at 1 mA cm-2 | 2900 mF cm-2 106 F g-1, 18.1 F cm-3 at 20 mA cm-2 | 90.5% 20,000 20 mA cm-2 | 0.94 mWh cm-2 | 14.4 mW cm-2 | (Wang et al. 2021a) |
| Basswood | 4.0% for O 5.2% for N 0.3% for S | 135 F g-1 at 0.2 A g-1 | 79 F g-1 at 4 A g-1 | 94% 5,000 2 A g-1 | 15.2 Wh kg-1 | 3234 W kg-1 | (Tang et al. 2018) |
| Chinese fir wood | Polyaniline/carbon nanotube | 90.9 F g-1, 25.1 F cm-3 at 5 mA cm-2 | 34.4 F g-1, 9.5 F cm-3 at 20 mA cm-2 | 93.7% 10,000 20 mA cm-2 | 40.5 Wh kg-1 | / | (Wu et al. 2020) |
| Basswood | Electrodeposition MnO2 | 3600 mF cm-2, 35.6 F g-1, at 1 mA cm-2 | 1300 mF cm-2 at 10 mA cm-2 | 93% 10,000 10 mA cm-2 | 16 Wh kg-1 | 107.7 W kg-1 | (Chen et al. 2017) |
| Poplar wood | Electrodeposition Co(OH)2 | 2200 mF cm-2, 34.8 F g-1, at 1 mA cm-2 | 1300 mF cm-2, 20.8 F g-1 at 20 mA cm-2 | 85% 10,000 50 mA cm-2 | 10.87 Wh kg-1 | 236.8 W kg-1 | (Wang et al. 2018) |
| Precursor | Material functionalization | Initial capacitance | Rate performance | Cycle durability | Maximum energy density | Maximum power density | Ref. |
| Poplar wood | Air-activated 9.09% for O | 1680 mF cm-2, 33.5 F g-1, 5.58 F cm-3 at 1 mA cm-2 | 1150 mF cm-2, 21 F g-1 at 20 mA cm-2 | 86% 10,000 10 mA cm-2 | 0.23 mWh cm-2, 4.59 Wh kg-1 | 200 mW kg-1 | (Zhang et al. 2020) |
| Basswood | Cellulase-treated | 1500 mF cm-2, 79 F g-1 at 1 mA cm-2 | 570 mF cm-2, 30 F g-1 at 50 mA cm-2 | 86.6% 15,000 20 mA cm-2 | 0.21 mWh cm-2, 10.97 Wh kg-1 | 15.0 mW cm-2 800 W kg-1 | (Wang et al. 2021b) |
| Balsa wood | 7.14% for O, 0.44% for N, 0.09 for P | 1363 mF cm-2, 44 F g-1, 2.8 F cm-3 at 1 mA cm-2 | 500 mF cm-2, at 20 mA cm-2 | 90% 10,000 20 mA cm-2 | 0.63 mWh cm-3 | 13.83 mW cm-3 | (Liu et al. 2020) |
| Balsa wood | Electrooxidation Ni-NiO | 4.59 F cm-3 at 10 mA cm-2 | 2.05 F cm-3 at 40 mA cm-2 | 97.8% 4,000 30 mA cm-2 | 4.36 Wh kg-1, 1.44 mWh cm-3 | 642.86 W kg-1 211.7 mW cm-3 | (Li et al. 2021a) |
| Cotton fiber wiper | MXene/CF | 76 F g-1, 1.54 F cm-3 at 0.5 A g-1 | 51 F g-1, 1.02 F cm-3 at 50 A g-1 | / | 10.6 Wh kg-1, 0.22 mWh cm-3 | 12780 W kg-1 250.2 mW cm-3 | (Sun et al. 2021b) |
| Cellulose nanofiber and corncob | MnO2/Bio-AC/rGO/CNF | 812.2 mF cm-2 at 1 mA cm-2 | 202 mF cm-2 at 20 mA cm-2 | 99% 5,000 | 0.365 mWh cm-2 | 15 mW cm-2 | (Chen et al. 2021) |
| Lignosulfonate | Lignosulfonate/polypyrrole/ carbon nanospheres | 522 mF cm-2 at 0.5 mA cm-2 | 228 mF cm-2 at 20 mA cm-2 | 79.8% 7,000 10 mA cm-2 | 72.5 μWh cm-2 | 250 μW cm-2 | (Peng et al. 2019) |
| Sodium alginate | ~10% for O | 419.3 F g-1 at 0.5 A g-1 | 244 F g-1 at 20 A g-1 | 90.2% 20,000 8 A g-1 | 58.24 Wh kg-1 | 61 kW kg-1 | (Xia et al. 2019) |
| Precursor | Material functionalization | Initial capacitance | Rate performance | Cycle durability | Maximum energy density | Maximum power density | Ref. |
| Flax | 5.56% for N | 1257.9 mF cm-2 at 1 mA cm-2 | 703.2 mF cm-2 at 1 mA cm-2 | 90% 5,000 1 A g-1 | 174.7 μWh cm-2 | 10 mW cm-2 | (He et al. 2020) |
| Cotton fabric | 7.39% for O 2.56 for N 0.61 for S 0.45 for P | 1804.6 mF cm-2, 30.1 F cm-3 at 2 mA cm-2 | 800 mF cm-2, 13 F cm-3 at 10 mA cm-2 | 91.1% 4.000 | 28.4 Wh kg-1 9.4 mWh cm-3 | ~800 W kg-1 | (Sun et al. 2021a) |
| Glucose | 2.1% for P 4.1% for N MnO2 | 96 F g-1 at 0.5 A g-1 | 32 F g-1 at 20 A g-1 | 93% 10,000 at 10 A g-1 | 41.5 Wh kg-1 | 7260 W kg-1 | (Liu et al. 2021) |
| Eucalyptus | 18.61% for O | 116 F g-1 at 1.5 A g-1 | 68 F g-1 at 5 A g-1 | / | 41 Wh kg-1 | 2396 W kg-1 | (Atika and Dutta 2021) |
| Tremella | N/O/S-doped | 138.9 F g-1 at 0.2 A g-1 | 50.1 F g-1 at 20 A g-1 | 93.5% 10,000 at 2 A g-1 | 19.29 Wh kg-1 | 1002 W kg-1, | (Zhang et al. 2019) |

References

Atika, Dutta RK (2021) Oxygen‐rich porous activated carbon from eucalyptus wood as an efficient supercapacitor electrode. Energy Technol 9(9):2100463. https://doi.org/10.1002/ente.202100463

Augustyn V, Simon P, Dunn B (2014) Pseudocapacitive oxide materials for high-rate electrochemical energy storage. Energy Environ Sci 7(5):1597. https://doi.org/10.1039/c3ee44164d

Chen CJ, Zhang Y, Li Y, Dai JQ, Song JW, Yao YG, Gong YH, Kierzewski I, Xie J, Hu LB (2017) All-wood, low tortuosity, aqueous, biodegradable supercapacitors with ultra-high capacitance. Energy Environ Sci 10(2):538-545. https://doi.org/10.1039/c6ee03716j

Chen R, Li X, Huang Q, Ling H, Yang Y, Wang X (2021) Self-assembled porous biomass carbon/RGO/nanocellulose hybrid aerogels for self-supporting supercapacitor electrodes. Chem Eng J 412:128755. https://doi.org/https://doi.org/10.1016/j.cej.2021.128755

Hadoun H, Sadaoui Z, Souami N, Sahel D, Toumert I (2013) Characterization of mesoporous carbon prepared from date stems by H3PO4 chemical activation. Appl Surf Sci 280:1-7. https://doi.org/10.1016/j.apsusc.2013.04.054

He D, Wu L, Yao Y, Zhang J, Huang Z-H, Wang M-X (2020) A facile route to high nitrogen-containing porous carbon fiber sheets from biomass-flax for high-performance flexible supercapacitors. Appl Surf Sci 507:145108. https://doi.org/10.1016/j.apsusc.2019.145108

Li L, Xiao R, Tao X, Wu Y, Jiang L, Zhang Z, Qing Y (2021a) Free-standing electrodes via coupling nanostructured Ni–NiO with hierarchical wood carbon for high-performance supercapacitors and Ni–Zn batteries. J Power Sources 491:229618. https://doi.org/10.1016/j.jpowsour.2021.229618

Li Z, Wang X, Wang Z, Wang L, Guo Y, Zhou C, Li X, Du K, Luo Y (2021b) Nickel-cobalt layered double hydroxide nanosheets anchored to the inner wall of wood carbon tracheids by nitrogen-doped atoms for high-performance supercapacitors. J Colloid Interface Sci 608:70-78. https://doi.org/10.1016/j.jcis.2021.09.127

Liu H, Fan W, Lv H, Zhang W, Shi J, Huang M, Liu S, Wang H (2021) N,P-doped carbon-based freestanding electrodes enabled by cellulose nanofibers for superior asymmetric Supercapacitors. ACS Appl Energy Mater 4(3):2327-2338. https://doi.org/10.1021/acsaem.0c02859

Liu K, Mo R, Dong W, Zhao W, Huang F (2020) Nature-derived, structure and function integrated ultra-thick carbon electrode for high-performance supercapacitors. J Mater Chem A 8(38):20072-20081. https://doi.org/10.1039/d0ta06108e

Peng Z, Wang C, Zhang Z, Zhong W (2019) Synthesis and enhancement of electroactive biomass/polypyrrole hydrogels for high performance flexible all‐solid‐state supercapacitors. Adv Mater Interfaces 6(23):1901393. https://doi.org/10.1002/admi.201901393

Sun C, Guo Z, Zhou M, Li X, Cai Z, Ge F (2021a) Heteroatoms-doped porous carbon electrodes with three-dimensional self-supporting structure derived from cotton fabric for high-performance wearable supercapacitors. J Power Sources 482:228934. https://doi.org/10.1016/j.jpowsour.2020.228934

Sun L, Fu Q, Pan C (2021b) Hierarchical porous “skin/skeleton”-like MXene/biomass derived carbon fibers heterostructure for self-supporting, flexible all solid-state supercapacitors. J Hazard Mater 410:124565. https://doi.org/https://doi.org/10.1016/j.jhazmat.2020.124565

Tang Z, Pei Z, Wang Z, Li H, Zeng J, Ruan Z, Huang Y, Zhu M, Xue Q, Yu J, Zhi C (2018) Highly anisotropic, multichannel wood carbon with optimized heteroatom doping for supercapacitor and oxygen reduction reaction. Carbon 130:532-543. https://doi.org/10.1016/j.carbon.2018.01.055

Wang F, Cheong JY, He Q, Duan G, He S, Zhang L, Zhao Y, Kim I-D, Jiang S (2021a) Phosphorus-doped thick carbon electrode for high-energy density and long-life supercapacitors. Chem Eng J 414:128767. https://doi.org/10.1016/j.cej.2021.128767

Wang F, Cheong JY, Lee J, Ahn J, Duan G, Chen H, Zhang Q, Kim ID, Jiang S (2021b) Pyrolysis of enzymolysis‐treated wood: Hierarchically assembled porous carbon electrode for advanced energy storage devices. Adv Funct Mater 31(31):2101077. https://doi.org/10.1002/adfm.202101077

Wang Y, Lin X, Liu T, Chen H, Chen S, Jiang Z, Liu J, Huang J, Liu M (2018) Wood-derived hierarchically porous electrodes for high-performance all-solid-state supercapacitors. Adv Funct Mater 28(52):1806207. https://doi.org/10.1002/adfm.201806207

Wu W, Wang X, Deng YY, Zhou C, Wang ZH, Zhang ML, Li XJ, Wu YQ, Luo YF, Chen DY (2020) In situ synthesis of polyaniline/carbon nanotube composites in a carbonized wood scaffold for high performance supercapacitors. Nanoscale 12(34):17738-17745. https://doi.org/10.1039/d0nr04617e

Xia L, Huang H, Fan Z, Hu D, Zhang D, Khan AS, Usman M, Pan L (2019) Hierarchical macro-/meso-/microporous oxygen-doped carbon derived from sodium alginate: A cost-effective biomass material for binder-free supercapacitors. Mater Des 182:108048. https://doi.org/10.1016/j.matdes.2019.108048

Zhang W, Liu T, Mou J, Huang J, Liu M (2020) Ultra-thick electrodes based on activated wood-carbon towards high-performance quasi-solid-state supercapacitors. Phys Chem Chem Phys 22(4):2073-2080. https://doi.org/10.1039/c9cp06181a

Zhang Y, Yang S, Wang S, Liu X, Li L (2019) Microwave/freeze casting assisted fabrication of carbon frameworks derived from embedded upholder in tremella for superior performance supercapacitors. Energy Storage Mater 18:447-455. https://doi.org/10.1016/j.ensm.2018.08.006