Carbon-negative cement-bonded biochar particleboards

Liang Chen1, Yuying Zhang1, Claudia Labianca1, Lei Wang 2, *‬, Shaoqin Ruan3, Chi Sun Poon1,4, Yong Sik Ok5, Daniel C.W. Tsang1,4,# ‬

1 Department of Civil and Environmental Engineering, The Hong Kong Polytechnic University, Hung Hom, Kowloon, Hong Kong, China

2 State Key Laboratory of Clean Energy Utilization, Institute for Thermal Power Engineering, Zhejiang University, Hangzhou, 310027, China.

3 College of Civil Engineering and Architecture, Zhejiang University, Hangzhou 310058, China

4 Research Centre for Resources Engineering towards Carbon Neutrality, The Hong Kong Polytechnic University, Hung Hom, Kowloon, Hong Kong, China

5 Korea Biochar Research Center, APRU Sustainable Waste Management Program & Division of Environmental Science and Ecological Engineering, Korea University, Seoul 02841, South Korea

* Corresponding author: wanglei.leo@zju.edu.cn

# Corresponding author: dan.tsang@polyu.edu.hk

F1 Supplementary Information

Figure S1 	Particle size distribution of raw materials.

Figure S2  Probability distributions of CO2 emission related to the production of 70BC-FA particleboard.

Figure S3  Water absorption of the MOSC biochar particleboards.

Figure S4 	Cost-benefit analysis of biochar particleboards based on the carbon prices in different countries.

Table S1 	Basic information of biochar.

Table S2   Chemical compositions of raw materials (wt.%).

Table S3 	Example of the cost-benefit analysis for biochar particleboards.

Fig. S1 Particle size distribution of raw materials.

Fig. S2 Probability distributions of CO2 emission related to the production of 70BC-FA particleboard.

Fig. S3 Water absorption of the MOSC biochar particleboards.

Fig. S4 Cost benefit analysis of biochar particleboards based on the carbon taxes in different countries: (a) 101.5 USD tonne-1 in Switzerland, (b) 52.4 USD tonne-1 in France, (c) 28.4 USD tonne-1 in England, and (d) 17.6 USD tonne-1 in Spain.

Table S1 Basic information of biochar.

|  | Biochar |
| --- | --- |
| Surface Area (m2 g-1) | 142 |
| Total Pore Volume (m3 g-1) | 0.08 |
| Average Pore Diameter (nm) | 2.01 |
| Water Adsorption Capacity (%) | 83.6 |

Table S2 Chemical compositions of raw materials (wt.%).

|  | Na2O | MgO | Al2O3 | SiO2 | P2O5 | SO3 | K2O | CaO | Fe2O3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OPC | 0.19 | 1.55 | 4.52 | 19.12 | 0.09 | 4.12 | 0.56 | 66.08 | 3.56 |
| MgO cement | 0 | 89.45 | 0.46 | 5.86 | 0.12 | 0.07 | 0.14 | 2.89 | 0.75 |
| GGBS | 0 | 6.55 | 15.78 | 35.82 | 0 | 2.31 | 0.82 | 38.14 | 0.24 |
| PFA | 1.06 | 2.86 | 25.58 | 51.15 | 0.69 | 0.76 | 1.56 | 7.75 | 8.53 |
| Biochar | 0 | 6.77 | 0.86 | 14.98 | 2.15 | 14.4 | 6.84 | 52.54 | 1.42 |

OPC: ordinary Portland cement; GGBS: ground granulated blast furnace slag; PFA: pulverized fly ash;

Table S3 Example of the cost-benefit analysis for biochar particleboards (50BC-MOSC particleboard).

| Assuming the production capacity of factory is 112 m3 per day and unit price is 119 USD per m3. |  |  |  |
| --- | --- | --- | --- |
| Capital costs (USD) | Unit Price (USD) | Price per m3 (USD) | Note |
| Land cost | 769 m-2 | 0.63 | Sub-urban land for non-living activities (1000 m2) |
| Building cost | 923,077 | 0.75 | 30-year service life |
| Production equipment | 3,077 | 2.51 | 30-year service life |
| Strength test equipment | 7,692 | 0.013 | 3-year service life |
| Total |  | 3.9 |  |
| Operational costs | Unit Price | Price per m3 |  |
| Materials cost |  | 55.59 | Including transportation fee |
| Energy cost | 0.15 kW·h-1 | 0.0275 | Including electricity, fuel |
| Maintenance cost | 15,384 y-1 | 0.38 | Machine maintenance |
| Labour cost | 30.8 d-1 | 1.37 | Five workers |
| Curing cost | 0 | 0 | Air curing, the curing room was included in land cost |
| Total |  | 57.37 |  |
| Comparative costs (Benefits) | Unit Price | Price per m3 |  |
| Landfill disposal fee saving (wood) | 25.6 t-1 | 30.40 | Wood waste |
| Total |  | 30.40 |  |
| Carbon tax/credit | 137.2 t-1 | 28.28 | Carbon price of Sweden |
| Product benefit per m3 = Price - Capital cost - Operational cost |  |  | 57.73 |
| Landfill disposal fee saving per m3 |  |  | 30.40 |
| Carbon tax/credit per m3 |  |  | 28.28 |
| Over benefit per m3 = Product benefit + Landfill disposal fee saving + Carbon tax/credit |  |  | 117.67 |