Additional Information

Three dimensional BC/rGA aerogel: Preparation, characterization, and adsorption of Cr(Ⅵ)

Naiju Che, Na Liu, Yinhui Li, Chao Li, Yanli Liu*, Chengliang Li*

(National Engineering Research Center for Efficient Utilization of Soil and Fertilizer Resources, College of Resources and Environment, Shandong Agricultural University, Tai’An 271018, China)

SI. 1 The preparation of reagent

SI. 2 Select the concentration of raw materials for preparing aerogel

SI. 3 Solid-liquid separation of different adsorbents after adsorption

SI. 4 Data analysis

SI. 5 Characterization of materials

SI. 6 Adsorption kinetic

SI. 7 Effect of pH and temperature on Cr(Ⅵ) adsorption and adsorption thermodynamics

SI. 8 Adsorption mechanism

References

# SI. 1 The preparation of reagent

GO solution or the BC/GO solution was prepared by dispersing GO in deionized water uniformly by ultrasonic (2 h) and stirring (1000 rpm, 8 h). The PVA solution was prepared by dispersing the PVA powder in deionized water and stirring with 90℃ water bath heating until the solution was uniformly. The glutaraldehyde mixed solution was prepared by mixing the 50% glutaraldehyde, methyl alcohol, acetic acid, sulfuric acid and deionized water with the volume ratio of 5:20:20:2:150.

# SI. 2 Preparation of rGA and BC/rGA

Firstly, 60 mL 2.5 g L-1, 5 g L-1, 10 g L-1, 15 g L-1 GO solution were prepared respectively, 3 mL 100 mg L-1 PVA solution and 10 mL glutaraldehyde mixed solution were putted into the GO solution under stirring. The mixture was poured into container and frozen-melt five times repeatedly. And then, the sample was immersed into 80 ℃ L-ascorbic acid solution for 12 h to reduce the GO and washed by 75% alcohol to removal the residual reagents. Finally, the samples were freezing dried for 48 h (-50℃), and the rGA was obtained which were named rGA(2.5), rGA(5), rGA(10) and rGA(15), respectively. Fig. S1 showed that the structure of rGA(10) and rGA(15) were unstable due to insufficient PVA connection with GO.

10 mg rGA(2.5), rGA(5), rGA(10), and rGA(15) were putted into 10 mL Cr(Ⅵ) solution with the initial concentration of 15 mg L-1, 35 mg L-1, 55 mg L-1, 75 mg L-1 and 100 mg L-1, respectively. The adsorption results showed that the rGA(5) had better adsorption capacity (Fig. S2). Therefore, the concentration of GO solution was determined as 5 mg L-1.

Fig. S1 rGA with different GO content

Fig. S2 The comparison of qe on different concentration Cr(Ⅵ) solution by rGA of different GO content

Fig. S3 rGA and BC/rGA with different ratio of BC and GO

Table S1 The preparation methods of aerogels

| Aerogel | Raw materials | Preparation methods and process | References |
| --- | --- | --- | --- |
| Graphene–carbon sphere hybridaerogel decorated with silver nanoparticles (G/AgCS) | Graphene oxide (GO) Carbon spheres Ailver nanoparticles (AgCS) | Graphene oxide (GO) and carbon spheres doped with silver nanoparticles (AgCS) were prepared separately. G/AgCS hydrogel was then synthesized by induced reduction and gelation of a mixture of GO and AgCS in an oil bath. The G/AgCS aerogel was obtained by freeze drying the hydrogel. | Dubey et al. 2014 |
| Metal salt templated carbon aerogels | Hexamethylomelamine | Formed hexamethylomelamine (MF) solution with metal salt, and adjust the solution pH to 4.5. Then, the solution was heated at 60 ℃ for 1 h to generate a MF resin/CaCl2 composite. The composite was dried and cured at 180 ℃ for 6 h and then carbonised at 700, 800 or 900 ℃ for 2 h under nitrogen. | Masika and Mokaya 2013 |
| Carbon Aerogel Monoliths (CAMs) | Linear phenolic resin Hexamethylenetetramine (HMTA) | CAMs was prepared through a sol-gel polymerization of linear phenolic resin and hexamethylenetetramine (HMTA) (16 h), followed by ambient pressure drying (24 h) and carbonization (900 ℃). | Jia et al. 2016 |
| 3D periodic graphene aerogel | Graphene oxide (GO) resorcinol–formaldehyde (R–F) | Fumed silica powders and catalyst (that is, (NH4)2CO3 or R–F solution) were added into as-prepared aqueous GO suspensions， and obtained GO ink. The GO ink was extruded through a micronozzle immersed in isooctane and supercritically dried to remove the liquid. Then, the structure was heated to 1,050 ℃ under N2 for carbonization. Finally, the silica filler was etched using HF acid | Zhu et al. 2015 |
| Graphene Aerogels | Graphene oxide (GO) | Graphene aerogels are developed by directionally freezing aqueous suspensions of polyamic acid salt and graphene oxide to form vertically aligned monoliths, followed by freeze-drying, imidization at 300 °C and graphitization at 2800 °C | Min et al. 2018 |
| CNT/graphene hybrid aerogel | Carbon nanotubes Graphene | The hydrothermal process was developed to prepare graphene aerogel by using GO as a precursor in Teflon-lined stainless steel autoclave at 120 ℃ for 12 h. The obtained aerogel was employed as a template for the in-situ growth of nanotubes, and the chemical vapor deposition (CVD) facility at 800℃ | Wang et al. 2017a |
| Graphene bonded carbon nanofiber aerogels | Electrospun polyacrylonitrile nanofibers Graphene oxide | The carbon aerogel was prepared using electrospun polyacrylonitrile nanofibers and graphene oxide as precursor. By freeze-shaping (liquid nitrogen) and subsequent carbonization (800 ℃), the aerogel obtained | Luo et al. 2018 |
| Arbitrary-shaped reduced graphene oxide aerogels | Graphene oxide (GO) | Arbitrary-shaped reduced graphene oxide (rGO) aerogels are prepared by freeze-drying process and followed unsaturated water vapor reduction method staring from GO aqueous suspensions | Shang et al. 2020 |
| Graphene oxide/biopolymer composite aerogels | Graphene oxide Biopolymer | GO suspension was added in GC blend and the composite hydrogel wad obtained after gelation. GC hydrogel was freeze-dried by a specific freeze-drying cycle, and was obtained after DHT treatment | Kovtun et al. 2020 |

# SI. 3 Solid-liquid separation of different adsorbents after adsorption

Fig. S4 Solid-liquid separation of different adsorbents after adsorption

# SI. 4 Data analysis

The adsorption capacity at time t (qt, mg g-1) and equilibrium (qe, mg g-1) were calculated by Eqs. (S1) and (S2), respectively:

qt=Ct-C0×Vm	(S1)

qe=Ce-C0×Vm	(S2)

where t (min) is the contact time, V (L) is the solution volume, and m (g) is the adsorbent mass. qe (mg g–1) and qt (mg g–1) are the amounts of contaminants adsorbed on the adsorbents at equilibrium and a given time t, respectively. C0 (mg L-1) is the initial concentration of Cr(Ⅵ), Ct (mg L-1) is the concentration of Cr(Ⅵ) after contacting t min and Ce (mg L-1) is the concentration of Cr(Ⅵ) when the adsorption has reached equilibrium.

The adsorption kinetics of Cr(Ⅵ) was studied with a pseudo-first order model, pseudo-second-order model, intra-particle diffusion model and Boyd model. The model equations were expressed in the Eqs (S3-S6) (Boyd et al. 1947; Ho et al, 1998; Liang et al. 2017a; Singh et al. 2017):

Pseudo-first-order model: qt=qe(1-e-k1t)	(S3)

Pseudo-second-order model: qt=t1k2qe2+tqe	(S4)

Intraparticle diffusion model: qt=Kit12+L	(S5)

Boyd model: Bt=-0.4977-ln⁡(1-qtqe)	(S6)

where L (mg g–1) is the intercept of the vertical axis; B is π2Di·r–2 (Di is the effective diffusion coefficient of the adsorbate and r is the radius of adsorbent particles hypothesized to be spherical). k1 (min–1) and k2 (g mg–1 min–1) are the adsorption rate constants of the pseudo-first-order model and the pseudo-second-order model, and Ki (mg g–1 min–1/2) is the overall diffusion constant for the sorption.

Adsorption isotherm data of Cr(Ⅵ) onto tested adsorbents were analyzed by Langmuir and Freundlich models, and the two models are expressed as Eqs. (S7, S8) (Liang et al. 2017b).

Langmuir: qe=qmaxKLCe1+KLCe	(S7)

Freundlich: qe=KFCe1n	(S8)

where qm (mg g-1) is the maximum adsorption capacity, KL is Langmuir constant, KF (mg(1–1/n) L1/n g–1) and n are the Freundlich adsorption constants.

The thermodynamic behavior of the adsorption was investigated using Gibbs free energy change (ΔG, KJ mol-1), adsorption heat (ΔH, KJ mol-1) and adsorption entropy change (ΔS, kJ (K·mol)-1). The thermodynamic parameters were calculated by the equation as Eqs. (S9-S12) (Hu et al. 2011; Saleh et al. 2018):

ΔG=-RTlnka	(S9)

ka=qeCe	(S10)

ΔG=ΔH-TΔS	(S11)

lnka=ΔSR-ΔHRT	(S12)

where R (8.314 J·(mol·K)-1) is the universal gas constant, T (K) is the temperature, ka represents the Langmuir constant (b), qe (mg g–1) and Ce (mg L–1) are the amounts of contaminants adsorbed on the adsorbents and concentration of the Cr(Ⅵ) at equilibrium, respectively; ΔG (kJ·mol-1) is the Gibbs free energy change, ΔH (kJ·mol-1) is the adsorption heat, ΔS (kJ·(K·mol)-1) is the adsorption entropy change.

SI. 5 Characterization of materials

Fig. S5 Nitrogen adsorption–desorption isotherm Linear absolute plot (a) and BJH desorption cumulative pore volume of rGA and BC/rGA (b)

Table S2 Textural properties of rGA and BC/rGA

| Adsorbent | BET surface area (m2 g-1) | Average pore diameter (nm) | t-Plot Micropore area (m2 g-1) | t-Plot external surface area (m2 g-1) |
| --- | --- | --- | --- | --- |
| rGA | 13.74 | 8.26 | 1.31 | 12.43 |
| BC/rGA | 17.65 | 6.96 | 5.73 | 11.92 |

Fig. S6 The FTIR spectra of BC/rGA with the ratio of BC to GO was 1:10, 1:4 and 1:2, respectively

Calculation of layer spacing by XRD

The layer spacing was calculated according to Bragg's law.

2dsinθ=nλ	(1)

Where d was layer spacing, n is X-ray wavelength (n=1). XRD measurements were employed with a X-ray diffractometer equipped with Cu-Ka tuber, λ=0.1542 nm (Bao et al. 2011).

Fig. S7 Raman spectra of rGA and BC/rGA

Fig. S8 The C 1s and O 1s of rGA and BC/rGA

Fig. S9 FTIR spectra (a) and SEM images of biochar (b) and ball milled biochar (c)

Put the same amount of biochar and BC into the same volume of water solution, and then shook for 30 min. And then started the timer after the shock stops. Fig. S10 showed the dispersion state of biochar and BC in aqueous solution after stopping shock for 0 min, 5 min, 30 min, 6 h and 24 h, respectively. It was obvious from the figure that biochar precipitated at the bottom of the container soon after stopping the oscillation, while BC could still be evenly dispersed in the aqueous solution after stopping the oscillation for 24 h. Good dispersity of BC could make BC uniformly distributed in BC/rGA. Therefore, BC was selected as one of the raw materials for preparing BC/rGA in this work.

Fig. S10 Comparison of the dispersion of biochar (left) and ball milled biochar in aqueous solution (right)

Fig. S11 SEM images of graphite (a) and GO (b)

Fig. S12 Comparison of the dispersion of graphite (left) and GO (right) in aqueous solution

Fig. S11 showed the SEM images of graphite and GO. Massive graphite (Fig. S9 a) reacted with strong oxidants such as KMnO4 and H2SO4, and then oxygen-containing functional groups were introduced into the layers to complete strong interactions (Marcano et al. 2010). The layers were removed from each other to form lamellar GO (Fig. S11 b).

Compared the dispersion of graphite and GO in aqueous solution, and the treatment was similar with the Comparison of the dispersion of biochar (left) and ball milled biochar in aqueous solution (right). It could be seen from the Fig. 12 that graphite almost precipitated at the bottom of the container after 30 min of shock, while GO could still be evenly dispersed in aqueous solution after 24 h. This was because graphite was hydrophobic, while GO was hydrophilic (Xu et al. 2011), which was also useful for the preparation of GAs.

Fig. S13 The density of rGA and BC/rGA

The density of prepared aerogels was tested by simply diving the weight by the volume, and the measured densities of rGA and BC/rGA were ranged from 0.0109 g cm-3 to 0.0175 g cm-3.

# SI. 6 Adsorption kinetic

Table S3 Internal diffusion equation parameters of Cr(Ⅵ) adsorption on GO and aerogels

| Adsorbents | The first stage |  |  | The second stage |  |  | The third stage |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C1 (mg g-1) | Kid 1 (mg g-1 min-0.5) | R12 | C2 (mg g-1) | Kid 2 (mg g-1 min-0.5) | R22 | C3 (mg g-1) | Kid 3 (mg g-1 min-0.5) | R32 |
| GO | 0.14 | 0.58 | 0.985 | 1.28 | 0.35 | 0.992 | 7.58 | 0.033 | 0.440 |
| rGA | 3.14 | 2.46 | 0.869 | 19.09 | 0.34 | 0.996 | 26.12 | 0.073 | 0.581 |
| BC/rGA(1:10) | 1.56 | 1.63 | 0.912 | 11.89 | 0.27 | 0.954 | 19.10 | -0.033 | 0.109 |
| BC/rGA(1:4) | 0.47 | 1.34 | 0.977 | 5.37 | 0.63 | 0.987 | 14.78 | 0.16 | 0.899 |

Fig. S14 The cycle adsorption capacity of rGA and BC/rGA (C Cr(Ⅵ)=50 mg L-1, pH=2, T= 298 K)

Table S4 The comparation of adsorption capacity with different adsorbents

| Adsorbent |  | qe (mg g-1) | Adsorption experimental condition | Separation method (from solution) | References |
| --- | --- | --- | --- | --- | --- |
| Mesoporous NiO |  | 4.74 | CCr(Ⅵ)=30 mg L-1, NiO = 6 g L-1, pH=4.7, T=30℃, 100 rpm | Centrifugation | Behnajady and Bimeghdar 2014 |
| Fe3O4@NiO |  | 6.50 | CCr(Ⅵ)=20 mg L-1, Fe3O4@NiO= 2 g L-1, T=25 ℃ | Centrifugation | Mahmoudi and Behnajady 2018 |
| Biochar particles from Onopordom Heteracanthom |  | 16.65 | CCr(Ⅵ)=20 mg L-1, biochar=1 g L-1, pH=2, T=15℃, 140 rpm | Filtration | Ghorbani-Khosrowshahi and Behnajady 2016 |
| Biochar prepared from raw corn |  | 1.63 | CCr(Ⅵ)=5 mg L-1, adsorbent=2 g L-1, T=25℃, 120 rpm | Filtration | Li et al. 2018 |
| Nano ZnO/ZnS modified biochar |  | 2.08 |  |  |  |
| Biochar prepared from the Artemisia argyi stem at 300, 450, 600°C | AS300 | 12.48 | CCr(Ⅵ)=50 mg L-1, adsorbent=2 g L-1, T=25℃, 120 rpm | Filtration | Song et al. 2019 |
|  | AS450 | 9.17 |  |  |  |
|  | AS600 | 15.77 |  |  |  |
| Biochar-based iron oxide composite (FeYBC) |  | 10.28 | CCr(Ⅵ)=20 mg L-1, adsorbent=2 g L-1, pH=4.72, T=30℃, 150 rpm | Filtration | Dong et al. 2021 |
|  |  | 19.13 | CCr(Ⅵ)=40 mg L-1, adsorbent=2 g L-1, pH=4.72, T=30℃, 150 rpm |  |  |
|  |  | 24.65 | CCr(Ⅵ)=80 mg L-1, adsorbent=2 g L-1, pH=4.72, T=30℃, 150 rpm |  |  |
|  |  | 25.08 | CCr(Ⅵ)=120 mg L-1, adsorbent=2 g L-1, pH=4.72, T=30℃, 150 rpm |  |  |
| Graphene–carbon sphere hybridaerogel decorated with silver nanoparticles (G/AgCS) |  | 12.69 | CCr(Ⅵ)=20 mg L-1, adsorbent= 0.5 g L-1, T=25℃, 200 rpm | Using tweezers | Dubey et al. 2014 |
| Reduced graphene oxide aerogel (rGA) |  | 26.95 | CCr(Ⅵ)=50 mg L-1, adsorbent=1 g L-1, T=25℃, 150 rpm | Using tweezers | This work |
| Ball-milled biochar/reduced graphene oxide aerogel (BC/rGA) |  | 19.43 |  |  |  |

# SI. 7 Effect of pH and temperature on Cr(Ⅵ) adsorption and adsorption thermodynamics

Fig. S15 Zeta potential of rGA and BC/rGA, and Cr(Ⅵ) ion species under different pH value

solution

Table S5 Adsorption isotherm parameters of of Cr(Ⅵ) adsorption on GO and carbon aerogel at different temperatures

| Adsorbents | Temperature K | Freundlich |  |  | Langmuir |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | N | KF (mg g-1) | R2 | Qm (mg g-1) | KL (L mg-1) | R2 |
| rGA | 288 | 2.50 | 7.51 | 0.906 | 48.76 | 0.017 | 0.990 |
|  | 298 | 2.31 | 5.98 | 0.982 | 61.92 | 0.041 | 0.999 |
|  | 303 | 2.42 | 6.85 | 0.946 | 52.37 | 0.030 | 0.986 |
| BC/rGA(1:4) | 288 | 2.91 | 6.39 | 0.911 | 34.82 | 0.039 | 0.949 |
|  | 298 | 2.69 | 6.36 | 0.949 | 41.03 | 0.040 | 0.982 |
|  | 303 | 2.64 | 6.13 | 0.959 | 46.41 | 0.051 | 0.977 |

Table S6 Thermodynamic parameters for the adsorption of rGA and BC/rGA

| Adsorbents | Temperature (K) | ΔG (kJ mol-1) | ΔH (kJ mol-1) | ΔS (J·(K·mol)-1) |
| --- | --- | --- | --- | --- |
| rGA | 288 | -10.75 | 0.28 | 1.01 |
|  | 298 | -17.04 |  |  |
|  | 303 | -27.01 |  |  |
| BC-rGA(1:4) | 288 | -13.37 | 0.22 | 0.80 |
|  | 298 | -16.30 |  |  |
|  | 303 | -26.81 |  |  |

# SI. 8 Adsorption mechanism

Fig. S16 The O 1s of rGA and BC/rGA after adsorption (rGA-Cr, BC/rGA-Cr)

# References

Bao CL, Guo YQ, Song L, Hu Y (2011) Poly (vinyl alcohol) nanocomposites based on graphene and graphite oxide: a comparative investigation of property and mechanism. J Mater Chem 21(36):13942-13950. http://dx.doi.org/10.1039/c1jm11662b

Behnajady MA, Bimeghdar S (2014) Synthesis of mesoporous NiO nanoparticles and their application in the adsorption of Cr(VI). Chem Eng J 239:105-113. http://dx.doi.org/10.1016/j.cej.2013.10.102

Boyd GE, Adamson AW, Myers Jr LS (1947) The Exchange Adsorption of Ions from Aqueous Solutions by Organic Zeolites. II. Kinetics. J Am Chem Soc 69(11):2800-2812. https://doi.org/10.1021/ja01203a066

Dong FX, Yan L, Zhou XH, Huang ST, Liang JY, Zhang WX, Guo ZW, Guo PR, Qian W, Kong LJ, Chu W, Diao ZH (2021) Simultaneous adsorption of Cr(VI) and phenol by biochar-based iron oxide composites in water: Performance, kinetics and mechanism. J Hazard Mater 416:125930. https://doi.org/10.1016/j.jhazmat.2021.125930

Dubey SP, Dwivedi AD, Kim IC, Sillanpaa M, Kwon YN, Lee C (2014) Synthesis of graphene–carbon sphere hybrid aerogel with silver nanoparticles and its catalytic and adsorption applications. Chem Eng J 244:160-167. https://doi.org/10.1016/j.cej.2014.01.042

Ghorbani-Khosrowshahi S, Behnajady MA (2016) Chromium(VI) adsorption from aqueous solution by prepared biochar from Onopordom Heteracanthom. Int J Environ Sci Technol 13:1803-1814. https://doi.org/10.1007/s13762-016-0978-3

Ho YS, McKay G (1998) A Comparison of Chemisorption Kinetic Models Applied to Pollutant Removal on Various Sorbents. Process Saf Environ 76(4):332-340. https://doi.org/10.1205/095758298529696

Hu XJ, Wang JS, Liu YG, Li X, Zeng GM, Bao ZL, Zeng XX, Chen AW, Long F (2011) Adsorption of chromium (VI) by ethylenediamine-modified cross-linked magnetic chitosan resin: Isotherms, kinetics and thermodynamics. J Hazard Mater 185:306-314. http://10.1016/j.jhazmat.2010.09.034

Jia XF, Dai B, Zhu ZX, Wang JT, Qiao WM, Long DH, Ling LC (2016) Strong and machinable carbon aerogel monoliths with low thermal conductivity prepared via ambient pressure drying. Carbon 108:551-560. https://doi.org/10.1016/j.carbon.2016.07.060

Kovtun A, Campodoni E, Favaretto L, Zambianchi M, Salatino A, Amalfitano S, Navacchia ML, Casentini B, Palermo V, Sandri M, Melucci M (2020) Multifunctional graphene oxide/biopolymer composite aerogels for microcontaminants removal from drinking water. Chemosphere 259:127501. https://doi.org/10.1016/j.chemosphere.2020.127501

Li CJ, Zhang L, Gao Y, Li AM (2018) Facile synthesis of nano ZnO/ZnS modified biochar by directly pyrolyzing of zinc contaminated corn stover for Pb(II), Cu(II) and Cr(VI) removals. Waste Manage 79:625-637. https://doi.org/10.1016/j.wasman.2018.08.035

Liang QW, Geng JJ, Luo HJ, Fang W, Yin YW (2017a) Fast and selective removal of Cr(Ⅵ) from aqueous solutions by a novel magnetic Cr(Ⅵ) ion-imprinted polymer. J Mol Liq 248:767-774. https://doi.org/10.1016/j.molliq.2017.10.114

Liang QW, Luo HJ, Geng JJ, Chen JD (2017b) Facile one-pot preparation of nitrogen-doped ultra-light graphene oxide aerogel and its prominent adsorption performance of Cr (VI). Chem Eng J 338:62-71. https://doi.org/10.1016/j.cej.2017.12.145

Liang QW, Luo HJ, Geng JJ, Chen JD (2018) Facile one-pot preparation of nitrogen-doped ultra-light graphene oxide aerogel and its prominent adsorption performance of Cr(Ⅵ). Chem Eng J 338:62-71. https://doi.org/10.1016/j.cej.2017.12.145

Luo GM, Wang YZ, Gao LX, Zhang DQ, Lin T (2018) Graphene bonded carbon nanofiber aerogels with high capacitive deionization capability. Electrochim Acta 260:656-663. https://doi.org/10.1016/j.electacta.2017.12.012

Mahmoudi E, Behnajady MA (2018) Synthesis of Fe3O4@NiO core-shell nanocomposite by the precipitation method and investigation of Cr(VI) adsorption efficiency. Colloid Surface A 538:287-296. https://doi.org/10.1016/j.colsurfa.2017.11.020

Marcano DC, Kosynkin DV, Berlin JM, Sinitskii A, Sun ZZ, Slesarev A, Alemany LB, Lu W, Tour JM (2010) Improved synthesis of graphene oxide. Amercan Chem Soc ACS Nano 4(8):4806-4814. https://doi.org/10.1021/nn1006368

Masika E, Mokaya R (2013) High surface area metal salt templated carbon aerogels via a simple subcritical drying route: preparation and CO2 uptake properties. Rsc Adv 3(39):17677-17681. https://doi.org/10.1039/c3ra43420f

Min P, Liu J, Li XF, An F, Liu PF, Shen YX, Koratkar N, Yu ZZ (2018) Thermally Conductive Phase Change Composites Featuring Anisotropic Graphene Aerogels for Real-Time and Fast-Charging Solar-Thermal Energy Conversion. Adv Funct Mater 28:1805365. https://doi.org/ 10.1002/adfm.201805365

Saleh TA, Tuzen M, Sarı A (2018) Polyamide magnetic palygorskite for the simultaneous removal of Hg (II) and methyl mercury; with factorial design analysis. J Environ Manage 211:323-333. https://doi.org/10.1016/j.jenvman.2018.01.050

Shang YX, Yang HQ, Qin Z, Yin SY, Yang LX, Xu MW, Li ZY, Jin ZQ, Sun H (2020) Arbitrary-shaped reduced graphene oxide aerogels via an unsaturated water vapor reduction. Carbon 168:169-179. https://doi.org/10.1016/j.carbon.2020.06.080

Singh DK, Kumar V, Mohan S, Hasan SH (2017) Polylysine functionalized graphene aerogel for the enhanced removal of Cr(Ⅵ) through adsorption: kinetic isotherm, and thermodynamic modeling of the process. J Chem Eng Data 62:1732–1742. http://10.1021/acs.jced.7b00188

Song JY, He QL, Hu XL, Zhang W, Wang CY, Chen RF, Wang HY, Mosa A (2019) Highly efficient removal of Cr(VI) and Cu(II) by biochar derived from Artemisia argyi stem. Environ Sci Pollut Res 26(13):13221-13234. https://doi.org/10.1007/s11356-019-04863-2

Wang CC, Yang SD, Ma Q, Jia X, Ma PC (2017a) Preparation of carbon nanotubes/graphene hybrid aerogel and its application for the adsorption of organic compounds. Carbon 118:765-771. http://dx.doi.org/10.1016/j.carbon.2017.04.001

Xu B, Yue SF, Sui ZY, Zhang XT, Hou SS, Cao GP, Yang YS (2011) What is the choice for supercapacitors: graphene or graphene oxide? Energy Environ Sci 4:2826-2830. http://10.1039/c1ee01198g

Zhu C, T. Han TYJ, Duoss EB, Golobic AM, Kuntz JD, Spadaccini CM, Worsley MA (2015) Highly compressible 3D periodic graphene aerogel microlattices. Nat Commun 22(6):6962. https://doi.org/10.1038/ncomms7962