Additional Information for

Synthesis, characterization, safety design, and application of NPs@BC for contaminated soil remediation and sustainable agriculture

Tong Zheng a # Shaohu Ouyang a # Qixing Zhou a *

a Key Laboratory of Pollution Processes and Environmental Criteria (Ministry of Education)/Tianjin Key Laboratory of Environmental

# These authors contributed equally to this work and should be considered co-first authors

* Corresponding author, E-mail: Qixing Zhou, zhouqx523@126.com; zhouqx@nankai.edu.cn

# Fig. S1 Scientific production on NPs@BC composites in the Web of Science database. Note: keywords used for the search “biochar-supported nanoparticles.” Note: NPs@BC, nanoparticles decorated biochar.

# Table S1 Recent researches on synthesis and characterization of NPs@BC composites

| Nanoparticles | Biomass | Method | Synthesis Conditions | Surface Area (m2∙g-1) | Pore Size (nm) | Pore volume (cm3∙g-1) | Characterization method | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| nZVI | Algae | The oxygen-limited heating and NaBH4 reduction | Algae: NaOH=2:1, maintained at 400 ℃ for 90 min, 800 ℃ activated 2 h, under nitrogen protected Fe2+: BC=1:1, 0.2 M NaBH4 is dropwise added into mixture of BC, Fe2+ and stirring for 30 min | 120.90 | 5.76 | 0.174 | BET, XPS, XRD, SEM, EDS | (Zhang et al. 2022b) |
| nZVI | Corn stalks | The oxygen-limited heating and NaBH4 reduction | Corn stalks pyrolyzed for 2 h at 450 °C Fe2+: BC=1:1, 0.108 M NaBH4 is dropwise added to mixture of BC and Fe2+, under N2 at 25 ℃ stirring 4 h | 68.08 | < 4 | 0.043 | SEM, TEM, FT-IR, BET | (Jiang et al. 2020) |
| Zr | Biosolid biomass | Pyrolysis and Co-precipitation | Pyrolysis is employed at 300 °C for 30 min Zr4+: BC=1: 11, 0.1 M NaOH is added to mixture of BC and ZrCl4 aging for 12 h at room temperature | 75.90 | 3.37 | 0.060 | BET, Element Analysis, FT-IR, XRD, SEM, EDS, HRTEM, XPS | (Rahman et al. 2021) |
| Cu | Rice straw | Pyrolysis and NaBH4 reduction | Rice straw is pyrolyzed for 2 h at 500 °C under N2 and treated with 0.1 M HCl for 6 h Cu2+: BC=1:5, biochar is dissolved in CuCl2·H2O solution with a N2 steam for 1 h and 0.054 M NaBH4 is added stirring for 30 min under N2 | 135.35 | - | 0.101 | XRD, FT-IR, BET, SEM, EDS, XPS, HRTEM, Element Analysis | (Fu et al. 2017) |
| Cu | Coconut shell | Pyrolysis and Impregnation | Coconut shell is pyrolyzed for 90 min at 900 °C under N2 and washing with 1.0 M HCl Cu2+: BC=0.06, BC is added into the CuSO4 solution standing still for 24 h and it is pretreated at 900 °C under N2 for 30-120 min | 916.20 | 1.7-3.7 | 0.100 | XRF, Element Analysis, XRD, SEM-EDX, BET, XPS | (Zhang et al. 2020b) |
| CuFeO2 | Pepper stalks | Pyrolysis and Hydrothermal | Pepper stalks are pyrolyzed at 450 °C at N2 for 2 h BC and NaOH are mixed with Cu2+/Fe3+ stirring for 1 h The precipitation is hydrothermally treated at 180 °C for 24 h | 37 | 7.95 | 0.074 | XRD, SEM-EDX, FT-IR, XPS, HRTEM, BET | (Xin et al. 2021) |
| CuFe2O4 | Bamboo powder | Pyrolysis and Sol-gel | Bamboo is pyrolyzed at 800 °C for 1 h BC mixed with solution of Cu2+/Fe3+/ citric acid is stirred at 80 °C for 4 h The solid is dried at 105 °C and calcined at 700 °C for 4 h in N2 | - | - | - | XRD, SEM, TEM, XPS, FT-IR, EPR | (Zhao et al. 2020) |
| nFe3O4 | Pine needles | Pyrolysis and Impregnation | Pine needle is pyrolyzed at 300/400/500/700 °C for 2 h Biochar is dispersed into NH3·H2O and placed in an ultrasound bath at 65 °C. The mixed solution of Fe2+/Fe3+ is added into the above solution | - | - | - | SEM, XRD, XPS, FT-IR | (Ouyang et al. 2017) |
| γFe2O3 | Banana peel | Pyrolysis and Hydrothermal | The banana peel and FeSO4·7H2O are mixed and stirred for 2 h The mixture is treated at 180 °C for 6 h, and product is dried and calcined at 600 °C for 2 h in N2 | 407-50 | - | 0.393-0.522 | XRD, HRTEM, Raman, FE-SEM-EDS, BET, XPS, VSM | (Rong et al. 2019) |
| Co3O4 | Wheat straw | Pyrolysis and Co-precipitation | Co2+: BC=1: 50, the Co2+ solution is mixed with BC reacting for 12 h The precipitate is calcined in air at 450 °C for 4 h | 76 | - | - | SEM-EDS, TEM, XRD, XPS, FT-IR | (Xu et al. 2020) |
| MnFe2O4 | Pine needles | Pyrolysis and Co-precipitation | The raw materials are pyrolyzed at 500 ℃ for 2 h BC is mixed with solution of Mn2+ and Fe3+ with ultrasound for 30 min NH3·H2O is mixed with the suspensions stirring for 1 h at 80 °C and composite is dried at 60 °C for 24 h | 121 | 3.17 | 0.218 | XRD, SEM-EDS, BET, FT-IR, XPS | (Lai et al. 2019) |
| ZnO | Water hyacinth | Plant enrichment and Pyrolysis | ZnO suspensions (Zn concentration is 160 mg·L-1) and water hyacinth are transferred to flowerpots for 20 days Roots and stems-leaves are pyrolyzed under N2 at 400 °C for 2 h | 140 | 2.70 | 0.095 | TEM, FE-SEM-EDS, FT-IR, XRD, BET, EXAFS | (Xu et al. 2022) |
| MnO2 | Rice husk | Pyrolysis and Hydrothermal | Rice husk is heated at 600 °C for 1 h under N2 Mn: BC=1:3, HCl is mixed with solution of MnO42- Thereafter, biochar is placed in the mixture solution stirred for 1 h and heated at 100 °C for 6-12 h | 112/173 | - | - | XRD, SEM-EDX, TEM, BET, XPS | (Jung et al. 2019) |
| MgO | Sugarcane crop Harvest residue | Impregnation and Pyrolysis | The mixed solution of Mg2+ and sugarcane crop harvest residue are heated at 80 °C and dried at 105 °C for 6 h The mixture is calcined under N2 for 30 min and pyrolyzed at 550 °C for 1 h under N2 | 41-219 | 2.35-22.38 | 0.061-0.372 | Elemental Analysis, BET, FEG-SEM-EDX, TEM, FT-IR, XPS, XANES | (Li et al. 2017b) |
| MnOx | Rape straw | Impregnation and Pyrolysis | Rape straw is mixed with MnO4- solution, stirred at 80 °C for 3 h and dried at 105 °C The biochar precursors are heated to 600 °C under N2, for 1 h and washed with NaHCO3 solution | 111 | 3.14 | 0.087 | BET, FT-IR, SEM | (Li et al. 2017a) |
| TiO2 | Rice husk | Pyrolysis and Sol-gel | Rice husks are carbonized at 600 °C under N2 for 30 min The biochar and KOH solution are activated at a solid-liquid ratio of 1:10 at 20 °C for 2.5 h The preliminary activated biochar with KOH powder in a ratio of 1:4 is activated again at 900 °C | 780 | 2.32 | 0.560 | SEM-EDS, HRTEM, XRD, BET, XPS, Raman | (Guo et al. 2022) |
| AlxOy | Distillers’ grains | Impregnation and Pyrolysis | Distillers’ grains and Al3+ solution is mixed stirring at 180 rpm for 24 h at 25 °C The mixture is dried at 80 °C and pyrolyzed at 600 °C for 2 h in N2 atmosphere | 51 | - | 0.081 | Elemental Analysis, ICP-OES, SEM-EDX, XRD, FT-IR | (Cheng et al. 2021) |
| CuO | Corn stalks | Pyrolysis and Co-precipitation | Corn stalks is pyrolyzed at 500 ℃ for 2 h 1 M NaOH is added in the mixture solution of BC, Cu (CH3COO)2 and 1-thioglycerol (Cu: BC=1.6) stirring for 1.5 h and the solid is dried and calcined in the N2 atmosphere at 550 °C for 2 h | 180 | 2-50 | - | XRD, BET, FT-IR, SEM, XPS | (Li et al. 2020) |
| P | Maize straw | Pyrolysis and Ball milling | Maize straw is pyrolyzed in N2 at 300/500/700 ℃ for 4 h Red phosphorus powder is mixed with biochar and the mixture is milled at 300 rpm for 6-24 h | 147 | - | - | Elemental Analysis, BET, XPS | (Zhang et al. 2022a) |
| P | Wood Bamboo Cornstalk Rice husk | Impregnation | Feedstock is treated in the pyrolysis system for 2 h at 350, 550, and 750 °C The biomass is impregnated in K3PO4 solution with a mass ratio of 1:2 (biomass to K3PO4) Mixture is heated for 6 h at 80 °C and pyrolyzed under N2 at 550 °C | 288.84-333.96 | - | 0.340-0.550 | Elemental Analysis; XRF, FT-IR, XRD, XPS, BET | (Zhang et al. 2020a) |
| N | Rice straw | Impregnation and Pyrolysis | Pyrolysis is conducted under N2 for 4 h at 400-1000 °C Urea is dissolved into water, in which biochar is thoroughly impregnated at 105 °C and mixture is carbonized at 1000 °C for 4 h under N2 | 158 | - | 0.196 | XRD, Raman, XPS | (Ding et al. 2020) |
| N | Corncob | Impregnation and Pyrolysis | Corncob is added to the urea solution in the weight ratio of 1:X (X=0, 1, 2, 3, 4) stirred for 12 h and dried at 80 °C The obtained mixture is heated to 700 °C and maintained under nitrogen flow for 2 h | 2-5 | - | - | XRD, EDS, XPS, BET, FT-IR | (Wang et al. 2019) |
| S | Rice straw | Impregnation and Pyrolysis | Pyrolysis is conducted under N2 for 4 h at 400-1000 °C Diphenyl disulfide is dissolved into water, in which biochar is impregnated at 105 °C and mixture is carbonized at 1000 °C for 4 h under N2 | 106 | - | 0.166 | XRD, Raman, XPS | (Ding et al. 2020) |
| S | Bamboo | Hydrothermal and Pyrolysis | Biomass is added into mixed solution with FeCl3 and Na2S2O8 stirring for 12 h Precipitation is aged for 2 h at 220 °C and are pyrolyzed in N2 for 2 h | 216.24 | 1.37 | 0.1029 | BET, FT-IR, Elemental Analysis, SEM, TGA, XPS, XRD | (Zhang et al. 2022c) |
| N-S | Rice straw | Impregnation and Pyrolysis | Pyrolysis is conducted under N2 for 4 h at 400-1000 °C Thiourea is completely dissolved into water, in which biochar is impregnated at 105 °C Mixture is carbonized at 1000 °C for 4 h under N2 | 109 | - | 0.188 | XRD, Raman, XPS | (Ding et al. 2020) |
| N-S | Bamboo | Hydrothermal and Pyrolysis | Biomass is added into mixed solution with FeCl3 and Na2S2O8, stirring for 12 h Precipitation is aged for 2 h at 220 °C and are pyrolyzed in N2 for 2 h | 103.87 | 1.79 | 0.0513 | BET, FT-IR, Elemental Analysis, SEM, TGA, XPS, XRD | (Zhang et al. 2022c) |
| N-P | Corn stalk | Pyrolysis | The biomass powders and ammonium phosphate are mixed at a mass ratio: 2.0: 1.1 The mixtures are pyrolyzed in N2 at 350/650 °C for 1 h | 43.9/81.6 | 6.8/ 28.8 | 0.139/ 0.316 | Elemental Analysis, FT-IR, XPS, SEM, BET | (Tang et al. 2021) |
| N-B | Wheat straw | Pyrolysis | Wheat straw and urea are mixed in water stirring at 70 °C and pyrolyzed at 700 °C under N2 for 1 h Mixture of the N-doped biochar and boric acid are pyrolyzed at 700 °C for 1 h The final products are rinsed with boiling water | 72.01-103.47 | - | - | SEM, EDS, FT-IR, XPS | (Dou et al. 2022) |

# Table S2 Data of CED and GHG for NPs@BC composites

| Nanoparticles | Cumulative energy demand CED/ (kJ/kg) | Greenhouse gas emission (CO2 equivalent) GHG/ kg CO2 eq tonne-1 | References |
| --- | --- | --- | --- |
| TiO2 | 19-40 | 4-30 | (Meyer et al. 2009) |
| nNi | 14.976-150 | 8.85-18.07 | (Guohua et al. 2021, Meyer et al. 2009) |
| nZVI | 0.281-324 | 1068-250506 | (Nduagu et al. 2022, Visentin et al. 2019, Visentin et al. 2021) |
| Fe3O4 | 92-30000 | 6110-37900 | (Marimon Bolivar and Gonzalez 2018, Rahman et al. 2022) |
| biochar | 2.925-581.65 | 0.351-262 | (Azzi et al. 2019, 2022, Brassard et al. 2018, Ibarrola et al. 2012, Meyer et al. 2011, Peters et al. 2015, Roberts et al. 2010) |

Table S3 Summary of reports about the adsorption kinetic and isotherm models of contaminants onto the NPs@BC composites

| Nanoparticles | Contaminants | Isotherm | Parameters | Kinetic model | Parameters | References |
| --- | --- | --- | --- | --- | --- | --- |
| Fe | Cr, As, Pb | Bandu | qm0: 1582/97.37/7.53 mg·L-1 b0: 0.002/0.03/4.38 L·mg-1 x: -0.31/-0.86/0.08 y: -0.4/0.25/0.16 R2: 0.995/0.979/0.974 | Pseudo-second-order | qe: 3.84/3.84/3.77 mg·g-1 K2: 0.002/0.003/0.005 g·mg-1·min-1 R2: 0.975/0.988/0.986 | (Neeli et al. 2020) |
| Fe | Cu | Bandu | qm0: 5.15mg·L-1 b0: 0.960 L·mg-1 x: -1 y: 0.38 R2: 0.991 | Pseudo-first-order | qe: 3.84/3.84/3.77 mg·g-1 K1: 0.002/0.003/0.005 h-1 R2: 0.975/0.988/0.986 | (Neeli et al. 2020) |
| nZVI | Cd, As | Redlich-Peterson | α: 0.0019/1.606 β: 1.2982/0.8592 R2: 0.983/0.940 | Pseudo-second-order | qe: 6.51/13.15 mg·L-1 K2: 0.41/4.26 g·mg-1·h-1 R2: 0.992/0.994 | (Yang et al. 2020) |
| Fe3O4 | Methylene blue | Langmuir | Qm: 163.93 mg·g-1 KL: 0.2155 L·mg-1 RL: 0.009-0.083 R2: 0.999 | Pseudo-second-order | qe: 151.5152 mg·g-1 h: 7.2833 mg·g-1·min-1 K2: 0.000317 g·mg-1·min-1 R2: 0.999 | (Ma et al. 2015) |
| MgO | Pb, Cd | Hill | n: 0.7879/1.1469 C: 21.42/48.26 R2: 0.987/0.989 | Pseudo-second-order | qe: 338.98/187.97 mg·L-1 K2: 3.8×10-5/7.8×10-5 g·mg-1·min-1 R2: 0.998/0.999 | (Cheng et al. 2022) |
| N | Norfloxacin | Freundlich | Kf: 5.90 mg1-n·L-n·g-1 n: 0.19 R2: 0.978 | Elovich | α: 2.10 mg·g-1·min-1 β: 1.12×108 g·mg-1 R2: 0.999 | (Wu et al. 2022) |
| N-P | Sulfapyridine | Freundlich | Kf: 6.29 mg1-n·L-n·g-1 n: 0.37 R2: 0.984 | Elovich | α: 0.36mg·g-1·min-1 β: 4805.6 g·mg-1 R2: 0.998 | (Tang et al. 2021) |

# Refences

Azzi, ES, Karltun, E and Sundberg, C (2019) Prospective life cycle assessment of large-scale biochar production and use for negative emissions in Stockholm. Environmental Science and Technology 53(14), 8466-8476. http://doi.org/10.1021/acs.est.9b01615

Azzi, ES, Karltun, E and Sundberg, C (2022) Life cycle assessment of urban uses of biochar and case study in Uppsala, Sweden. Biochar 4(1), 18. http://doi.org/10.1007/s42773-022-00144-3

Brassard, P, Godbout, S, Pelletier, F, et al. (2018) Pyrolysis of switchgrass in an auger reactor for biochar production: A greenhouse gas and energy impacts assessment. Biomass and Bioenergy 116, 99-105. http://doi.org/10.1016/j.biombioe.2018.06.007

Cheng, J, Li, X, Xiao, X, et al. (2021) Metal oxide loaded biochars derived from Chinese bai jiu distillers' grains used for the adsorption and controlled release of phosphate. Industrial Crops and Products 173, 114080. http://doi.org/10.1016/j.indcrop.2021.114080

Cheng, S, Zhao, S, Guo, H, et al. (2022) High-efficiency removal of lead/cadmium from wastewater by MgO modified biochar derived from crofton weed. Bioresource Technology 343, 126081. http://doi.org/10.1016/j.biortech.2021.126081

Ding, D, Yang, S, Qian, X, et al. (2020) Nitrogen-doping positively whilst sulfur-doping negatively affect the catalytic activity of biochar for the degradation of organic contaminant. Applied Catalysis B: Environmental 263, 118348. http://doi.org/10.1016/j.apcatb.2019.118348

Dou, J, Cheng, J, Lu, Z, et al. (2022) Biochar co-doped with nitrogen and boron switching the free radical based peroxydisulfate activation into the electron-transfer dominated nonradical process. Applied Catalysis B: Environmental 301, 120832. http://doi.org/10.1016/j.apcatb.2021.120832

Fu, D, Chen, Z, Xia, D, et al. (2017) A novel solid digestate-derived biochar-Cu NP composite activating H2O2 system for simultaneous adsorption and degradation of tetracycline. Environmental Pollution 221, 301-310. http://doi.org/10.1016/j.envpol.2016.11.078

Guo, D, Wei, Feng, D, Dong, Zhang, Y, Long, et al. (2022) Synergistic mechanism of biochar-nano TiO2 adsorption-photocatalytic oxidation of toluene. Fuel Processing Technology 229, 107200. http://doi.org/10.1016/j.fuproc.2022.107200

Guohua, Y, Elshkaki, A and Xiao, X (2021) Dynamic analysis of future nickel demand, supply, and associated materials, energy, water, and carbon emissions in China. Resources Policy 74, 102432. http://doi.org/10.1016/j.resourpol.2021.102432

Ibarrola, R, Shackley, S and Hammond, J (2012) Pyrolysis biochar systems for recovering biodegradable materials: A life cycle carbon assessment. Waste Management 32(5), 859-868. http://doi.org/10.1016/j.wasman.2011.10.005

Jiang, Z, Li, J, Jiang, D, et al. (2020) Removal of atrazine by biochar-supported zero-valent iron catalyzed persulfate oxidation: Reactivity, radical production and transformation pathway. Environmental Research 184, 109260. http://doi.org/10.1016/j.envres.2020.109260

Jung, KW, Lee, SY, Lee, YJ, et al. (2019) Ultrasound-assisted heterogeneous Fenton-like process for bisphenol A removal at neutral pH using hierarchically structured manganese dioxide/biochar nanocomposites as catalysts. Ultrasonics Sonochemistry 57, 22-28. http://doi.org/10.1016/j.ultsonch.2019.04.039

Lai, C, Huang, F, Zeng, G, et al. (2019) Fabrication of novel magnetic MnFe2O4/bio-char composite and heterogeneous photo-Fenton degradation of tetracycline in near neutral pH. Chemosphere 224, 910-921. http://doi.org/10.1016/j.chemosphere.2019.02.193

Li, B, Yang, L, Wang, C, quan, et al. (2017a) Adsorption of Cd(II) from aqueous solutions by rape straw biochar derived from different modification processes. Chemosphere 175, 332-340. http://doi.org/10.1016/j.chemosphere.2017.02.061

Li, R, Wang, JJ, Zhou, B, et al. (2017b) Simultaneous capture removal of phosphate, ammonium and organic substances by MgO impregnated biochar and its potential use in swine wastewater treatment. Journal of Cleaner Production 147, 96-107. http://doi.org/10.1016/j.jclepro.2017.01.069

Li, Z, Liu, D, Huang, W, et al. (2020) Biochar supported CuO composites used as an efficient peroxymonosulfate activator for highly saline organic wastewater treatment. Science of the Total Environment 721, 137764. http://doi.org/10.1016/j.scitotenv.2020.137764

Ma, H, Li, J-B, Liu, W-W, et al. (2015) Novel synthesis of a versatile magnetic adsorbent derived from corncob for dye removal. Bioresource Technology 190, 13-20. http://doi.org/https://doi.org/10.1016/j.biortech.2015.04.048

Marimon Bolivar, W and Gonzalez, EE (2018) Green synthesis with enhanced magnetization and life cycle assessment of Fe3O4 nanoparticles. Environmental Nanotechnology, Monitoring and Management 9, 58-66. http://doi.org/10.1016/j.enmm.2017.12.003

Meyer, DE, Curran, MA and Gonzalez, MA (2009) An examination of existing data for the industrial manufacture and use of nanocomponents and their role in the life cycle impact of nanoproducts. Environmental Science and Technology 43(5), 1256-1263. http://doi.org/10.1021/es8023258

Meyer, S, Glaser, B and Quicker, P (2011) Technical, economical, and climate-related aspects of biochar production technologies: A literature review. Environmental Science and Technology 45(22), 9473-9483. http://doi.org/10.1021/es201792c

Nduagu, EI, Yadav, D, Bhardwaj, N, et al. (2022) Comparative life cycle assessment of natural gas and coal-based directly reduced iron (DRI) production: A case study for India. Journal of Cleaner Production 347, 131196. http://doi.org/10.1016/j.jclepro.2022.131196

Neeli, ST, Ramsurn, H, Ng, CY, et al. (2020) Removal of Cr (VI), As (V), Cu (II), and Pb (II) using cellulose biochar supported iron nanoparticles: A kinetic and mechanistic study. Journal of Environmental Chemical Engineering 8(5), 103886. http://doi.org/https://doi.org/10.1016/j.jece.2020.103886

Ouyang, D, Yan, J, Qian, L, et al. (2017) Degradation of 1,4-dioxane by biochar supported nano magnetite particles activating persulfate. Chemosphere 184, 609-617. http://doi.org/10.1016/j.chemosphere.2017.05.156

Peters, JF, Iribarren, D and Dufour, J (2015) Biomass pyrolysis for biochar or energy applications? A life cycle assessment. Environmental Science and Technology 49(8), 5195-5202. http://doi.org/10.1021/es5060786

Rahman, A, Kang, S, McGinnis, S, et al. (2022) Life cycle impact assessment of iron oxide (Fe3O4/γ-Fe2O3) nanoparticle synthesis routes. ACS Sustainable Chemistry & Engineering 10(10), 3155-3165. http://doi.org/10.1021/acssuschemeng.1c05763

Rahman, MA, Lamb, D, Rahman, MM, et al. (2021) Removal of arsenate from contaminated waters by novel zirconium and zirconium-iron modified biochar. Journal of Hazardous materials 409, 124488. http://doi.org/10.1016/j.jhazmat.2020.124488

Roberts, KG, Gloy, BA, Joseph, S, et al. (2010) Life cycle assessment of biochar systems: Estimating the energetic, economic, and climate change potential. Environmental Science and Technology 44(2), 827-833. http://doi.org/10.1021/es902266r

Rong, X, Xie, M, Kong, L, et al. (2019) The magnetic biochar derived from banana peels as a persulfate activator for organic contaminants degradation. Chemical Engineering Journal 372, 294-303. http://doi.org/10.1016/j.cej.2019.04.135

Tang, W, Zanli, BLGL and Chen, J (2021) O/N/P-doped biochar induced to enhance adsorption of sulfonamide with coexisting Cu2+/ Cr (VI) by air pre-oxidation. Bioresource Technology 341, 125794. http://doi.org/10.1016/j.biortech.2021.125794

Visentin, C, Trentin, AWD, Braun, AB, et al. (2019) Lifecycle assessment of environmental and economic impacts of nano-iron synthesis process for application in contaminated site remediation. Journal of Cleaner Production 231, 307-319. http://doi.org/10.1016/j.jclepro.2019.05.236

Visentin, C, Trentin, AWdS, Braun, AB, et al. (2021) Life cycle sustainability assessment of the nanoscale zero-valent iron synthesis process for application in contaminated site remediation. Environmental Pollution 268, 115915. http://doi.org/10.1016/j.envpol.2020.115915

Wang, H, Guo, W, Liu, B, et al. (2019) Edge-nitrogenated biochar for efficient peroxydisulfate activation: An electron transfer mechanism. Water Research 160, 405-414. http://doi.org/10.1016/j.watres.2019.05.059

Wu, J, Wang, T, Liu, Y, et al. (2022) Norfloxacin adsorption and subsequent degradation on ball-milling tailored N-doped biochar. Chemosphere 303, 135264. http://doi.org/https://doi.org/10.1016/j.chemosphere.2022.135264

Xin, S, Liu, G, Ma, X, et al. (2021) High efficiency heterogeneous Fenton-like catalyst biochar modified CuFeO2 for the degradation of tetracycline: Economical synthesis, catalytic performance and mechanism. Applied Catalysis B: Environmental 280, 119386. http://doi.org/10.1016/j.apcatb.2020.119386

Xu, H, Zhang, Y, Li, J, et al. (2020) Heterogeneous activation of peroxymonosulfate by a biochar-supported Co3O4 composite for efficient degradation of chloramphenicols. Environmental Pollution 257, 113610. http://doi.org/10.1016/j.envpol.2019.113610

Xu, R, Li, M and Zhang, Q (2022) Collaborative optimization for the performance of ZnO/biochar composites on persulfate activation through plant enrichment-pyrolysis method. Chemical Engineering Journal 429, 132294. http://doi.org/10.1016/j.cej.2021.132294

Yang, D, Wang, L, Li, Z, et al. (2020) Simultaneous adsorption of Cd(II)andAs(III)by a novel biochar-supported nanoscale zero-valent iron in aqueous systems. Science of the Total Environment 708, 134823. http://doi.org/https://doi.org/10.1016/j.scitotenv.2019.134823

Zhang, H, Shao, J, Zhang, S, et al. (2020a) Effect of phosphorus-modified biochars on immobilization of Cu (II), Cd (II), and As (V) in paddy soil. Journal of Hazardous materials 390, 121349. http://doi.org/10.1016/j.jhazmat.2019.121349

Zhang, P, Xue, B, Jiao, L, et al. (2022a) Preparation of ball-milled phosphorus-loaded biochar and its highly effective remediation for Cd- and Pb-contaminated alkaline soil. Science of the Total Environment 813, 152648. http://doi.org/10.1016/j.scitotenv.2021.152648

Zhang, S, Kong, Z, Wang, H, et al. (2022b) Enhanced nitrate removal by biochar supported nano zero-valent iron (nZVI) at biocathode in bioelectrochemical system (BES). Chemical Engineering Journal 433, 133535. http://doi.org/10.1016/j.cej.2021.133535

Zhang, W, Li, Y, Li, B, et al. (2020b) Simultaneous NO/CO2 removal by Cu-modified biochar/CaO in carbonation step of calcium looping process. Chemical Engineering Journal 392, 123659. http://doi.org/10.1016/j.cej.2019.123659

Zhang, Y, Xu, M, He, R, et al. (2022c) Effect of pyrolysis temperature on the activated permonosulfate degradation of antibiotics in nitrogen and sulfur-doping biochar: Key role of environmentally persistent free radicals. Chemosphere 294, 133737. http://doi.org/10.1016/j.chemosphere.2022.133737

Zhao, Y, Song, M, Cao, Q, et al. (2020) The superoxide radicals’ production via persulfate activated with CuFe2O4@Biochar composites to promote the redox pairs cycling for efficient degradation of o-nitrochlorobenzene in soil. Journal of Hazardous materials 400, 122887. http://doi.org/10.1016/j.jhazmat.2020.122887