Additional information

Figure S1 A preliminary batch E.coli inactivation experiment to compare the efficacy of BC, Ag-BC, and ZVI. Each 125 mL borosilicate glass reactor contained 100 mL of 10 mM bicarbonate solution adjusted to pH 7.1. The initial E. coli concentration, [E. coli]o, was 3.6E6 CFU/mL in all reactors.

# Table S1. Physical and chemical properties of Soil Reef Biochar (BC)

|  | Value | Unit | Method |
| --- | --- | --- | --- |
| Porosity | 0.57a | — | mercury intrusion porosimetry |
| Skeletal Density | 1.816b | g/cm3 | mercury intrusion porosimetry |
| BET Surface Area | 164.5c | m2/g | N2 adsorption (23-point fit) |
| Cation Exchange Capacity | 0.241±0.005c | mmol/g | NH4+ saturation |
| Electron Storage Capacity | 4.0c,d | mmol/g | chemical reduction w/ dithionite |
| pH | 7.23±0.02c | — | 1:20 w/v in DI water, 24 h |

a Value from Yi (2018).

b Value from Saquing et al. (2016).

c Value from Xin et al. (2020).

d Value from Xin et al. (2019).

Table S2 Environmental parameters of wastewater effluents measured on-site in 2019

| Environmental Parameters | Exp. 1 | Exp. 2 | Exp. 3 | Exp. 4 | Exp. 5 | Exp. 6 |
| --- | --- | --- | --- | --- | --- | --- |
| Water Temperature (°C) | 4.9 | 10.0 | 19.9 | 20.6 | 22.1 | 22.4 |
| mmHg | 740.6 | 743.8 | 738 | 735.1 | 730.1 | 728.9 |
| Dissovled oxygen (DO%) | 128.2 | 118 | 69.7 | 21.7 | 22.6 | 21.1 |
| Conductivity (SPC uS/cm) | 464.0 | 704.7 | 1623.3 | 1064.5 | 1638.7 | 1620.3 |
| pH | 9.9 | 8.2 | 7.4 | 7.3 | 7.5 | 7.2 |
| Oxidation reduction potential (ORP mV) | 62.9 | 219.1 | 148.8 | 195.0 | 137.1 | 229.2 |
| Turbidity (FNU) | 2.6 | 6.5 | 24.4 | 21.9 | 16.9 | 14.1 |
| Nitrate nitrogen (mg/L) | 2.4 | 9.1 | - | - | - | - |
| Chloride (mg/L) | 131.3 | 72.8 | 59.3 | 35.8 | 30 | 1.9 |

*All the environmental parameters were measured triplicates

Reference

Guan, P., Prasher, S.O., Afzal, M.T., George, S., Ronholm, J., Dhiman, J., Patel, R.M., 2020. Removal of Escherichia coli from lake water in a biochar-amended biosand filtering system. Ecol. Eng. 150, 105819. https://doi.org/https://doi.org/10.1016/j.ecoleng.2020.105819

Mohanty, S.K., Cantrell, K.B., Nelson, K.L., Boehm, A.B., 2014. Efficacy of biochar to remove Escherichia coli from stormwater under steady and intermittent flow. Water Res. 61, 288–296. https://doi.org/https://doi.org/10.1016/j.watres.2014.05.026

Panthi, S., Sapkota, A.R., Raspanti, G., Allard, S.M., Bui, A., Craddock, H.A., Murray, R., Zhu, L., East, C., Handy, E., Callahan, M.T., Haymaker, J., Kulkarni, P., Anderson, B., Craighead, S., Gartley, S., Vanore, A., Betancourt, W.Q., Duncan, R., Foust, D., Sharma, M., Micallef, S.A., Gerba, C., Parveen, S., Hashem, F., May, E., Kniel, K., Pop, M., Ravishankar, S., Sapkota, A., 2019. Pharmaceuticals, herbicides, and disinfectants in agricultural water sources. Environ. Res. 174, 1–8. https://doi.org/10.1016/J.ENVRES.2019.04.011

Saquing, J.M., Yu, Y.-H., Chiu, P.C., 2016. Wood-Derived Black Carbon (Biochar) as a Microbial Electron Donor and Acceptor. Environ. Sci. Technol. Lett. 3, 62–66. https://doi.org/10.1021/acs.estlett.5b00354

Xin, D., Barkley, T., Chiu, P.C., 2020. Visualizing electron storage capacity distribution in biochar through silver tagging. Chemosphere 248, 125952. https://doi.org/10.1016/j.chemosphere.2020.125952

Xin, D., Xian, M., Chiu, P.C., 2019. New methods for assessing electron storage capacity and redox reversibility of biochar. Chemosphere 215, 827–834. https://doi.org/10.1016/j.chemosphere.2018.10.080

Yi, S.C., 2018. The impact of biochar surface properties on sand and on sandy loam regarding water repellency, water retention, and gas transmissivity. University of Delaware.