Supplementary Information

Application of Magnesium and Biosurfactant Functionalized Biochar Composite in Treating Cyanobacteria in Phosphorus and Crude Oil Contaminated Water

Zhuo Wei1, 2, Yaxi Xu1, Yi Wei1, Yang Liu1, Shuai Niu1, Jim J. Wang2*

1 Faculty of Environmental Science & Engineering, Kunming University of Science & Technology, Kunming, 650500, Yunnan, China

2 School of Plant, Environment and Soil Sciences, Louisiana State University AgCenter, Baton Rouge, LA 70803, USA

*Corresponding author:

- mail addresses: jjwang@agcenter.lsu.edu (Jim J. Wang)

Contents: 1 table and 5 figures

Table S1. Parameters of Freundlich and Langmuir adsorption isotherms models. (a) PO43− and (b) total petroleum hydrocarbons (TPH).

(a)

| PO43- adsorption | Freundlich model |  |  |  | Langmuir model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | KF | n | R2 |  | Qmax | KL | R2 |
|  | (mg g-1) / (mg L-1)n) |  |  |  | (mg g-1) | (L mg-1) |  |
| Biochar | 0.25 | 0.614 | 0.987 |  | 12.87 | 0.021 | 0.982 |
| Mg-biochar | 12.59 | 0.414 | 0.976 |  | 118.31 | 0.035 | 0.960 |
| RL-biochar | __ | __ | __ |  | __ | __ | __ |
| Mg-RL-biochar | 10.83 | 0.437 | 0.979 |  | 112.12 | 0.031 | 0.979 |

(b)

| TPH adsorption | Freundlich model |  |  |  | Langmuir model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | KF | n | R2 |  | Qmax | KL | R2 |
|  | (mg g-1) / (mg L-1)n) |  |  |  | (mg g-1) | (L mg-1) |  |
| Biochar | 0.03 | 0.733 | 0.994 |  | 2.34 | 0.022 | 0.968 |
| Mg-biochar | __ | __ | __ |  | __ | __ | __ |
| RL-biochar | 0.23 | 0.903 | 0.986 |  | 44.42 | 0.011 | 0.977 |
| Mg-RL-biochar | 0.15 | 0.956 | 0.985 |  | 40.21 | 0.007 | 0.983 |

Fig. S1. Oxygen volume change curve in 30 mins.(The space of furnace:10 L, the flow rate of N2: 400 mL min-1, time: 30 min. VO2=V0−vN2∙t)

Fig. S2. Phosphorous adsorption by biochar modified with different level of magnesium.

Fig. S3. Percentage total petroleum hydrocarbon (TPH) adsorbed by MgO-biochar composite modified with different levels of rhamnolipids (RL).

(a)										(b)

(c)										(d)

Fig. S4. Scanning electron microscopy (SEM) images and the corresponding energy dispersive X-ray spectroscope (EDX) of Mg-biochar before (a), (b) and after (c), (d) phosphorous adsorption.

2 weeks

Fig. S5. The effect of RL-Biochar with a series of levels on growth of algae (The cultivation time of algae was two weeks).