Additional file 1

Preparation of carbon-based material with high water absorption capacity and its effect on the water retention characteristics of sandy soil

Youming Yanga, b, Mingyang Zhonga, b, Xiuqi Biana, b,Yongjun Youa, b, Fayong Lia, b*

a College of Water Resources and Architectural Engineering, Tarim University, Alaer 843300, China

b Key Laboratory of Tarim Oasis Agriculture (Tarim University), Ministry of Education, Alaer 843300, China

*Corresponding author: Fayong Li.

E-mail address: lisen8279@163.com

Table S1: The water absorption of the carbon-based material in this paper is comparable to other paper

Fig. S1: Schematic of soil water infiltration test

Fig. S2: Effect of control (CK), biochar (BC), starch-carbon-based material (SB), sodium alginate-carbon-based material (SAB) and chitosan-carbon-based material (CB) on the particle size distribution of aggregates in different soil layers at 0.5% application rate

Fig. S3: Effect of control (CK), biochar (BC), starch-carbon-based material (SB), sodium alginate-carbon-based material (SAB) and chitosan-carbon-based material (CB) on the particle size distribution of aggregates in different soil layers at 1.0% application rate

Table S1 The water absorption of the carbon-based material in this paper is comparable to other paper

| Materials | Substrate | Water absorbency (g g-1) (In distilled water) | Refs |
| --- | --- | --- | --- |
| Starch-carbon-based material | Starch, biochar | 155 | In this study |
| Sodium alginate-carbon-based material | Sodium alginate, biochar | 188 | In this study |
| Chitosan-carbon-based material | Chitosan, biochar | 172 | In this study |
| Waxy starch | Starch | 78 | (Duquette and Dumont 2018) |
| Nano-ZnO coated cellulose/starch/activated carbon hydrogel | Starch, activated carbon | 15 | (Zhang et al. 2022) |
| Biochar (800 °C) | Biochar | 8 | (Li and Tan 2021) |
| The crosslinked gelatin/chitosan/poly (vinyl alcohol)/hydroxyapatite | Chitosan, hydroxyapatite | 44 | (Vo et al. 2021) |
| Based on sodium methacrylate alginate and carboxymethyl chitosan, double network hydrogels | Sodium methacrylate Alginate, carboxymethyl chitosan | 38 | (Wu et al. 2023) |
| Scaffold-chitosan hydrogel with activated carbon | Chitosan, activated carbon | 112 | (Gonçalves et al. 2019) |

Fig. S1 Schematic of soil water infiltration test

Fig. S2 Effect of control (CK), biochar (BC), starch-carbon-based material (SB), sodium alginate-carbon-based material (SAB) and chitosan-carbon-based material (CB) on the particle size distribution of aggregates in different soil layers at 0.5% application rate. Error bars indicate standard deviation; different lowercase letters indicate significant differences between different carbon-based materials at the same particle size (p<0.05, LSD test)

Fig. S3 Effect of control (CK), biochar (BC), starch-carbon-based material (SB), sodium alginate-carbon-based material (SAB) and chitosan-carbon-based material (CB) on the particle size distribution of aggregates in different soil layers at 1.0% application rate. Error bars indicate standard deviation; different lowercase letters indicate significant differences between different carbon-based materials at the same particle size (p<0.05, LSD test)

# References

Duquette D, Dumont MJ (2018) Influence of chain structures of starch on water absorption and copper binding of starch‐graft‐itaconic acid hydrogels. Starch 70:1700271

Gonçalves JO, Da Silva KA, Rios EC, Crispim MM, Dotto GL, Almeida Pinto LA (2019) Single and binary adsorption of food dyes on chitosan/activated carbon hydrogels. Chem Eng Technol 42:454-464

Li H, Tan Z (2021) Preparation of high water-retaining biochar and its mechanism of alleviating drought stress in the soil and plant system. Biochar 3:579–590

Vo TS, Vo TTBC, Nguyen TS, Pham ND (2021) Incorporation of hydroxyapatite in crosslinked gelatin/chitosan/poly (vinyl alcohol) hybrids utilizing as reinforced composite sponges, and their water absorption ability. Progress in Natural Science: Materials International 31:664-671

Wu P, Fang Y, Chen K, Wu M, Zhang W, Liu D, Gao J, Li H, Lv J, Zhao Y (2023) Study of double network hydrogels based on sodium methacrylate alginate and carboxymethyl chitosan. Eur Polym J 194:112137

Zhang X, Liu Q, Zhu S, Yu M (2022) Green and facile fabrication of nano-zno coated cellulose/starch/activated carbon hydrogel for enhanced dyes adsorption and antibacterial activity. Mater Today Commun 33:104355