Lignin-impregnated biochar assisted with microwave irradiation for CO2 capture: adsorption performance and mechanism

Xueyang Zhanga, Haoliang Xua, Wei Xianga, Xinxiu Youa, Huantao Daia, Bin Gaob

a School of Environmental Engineering, Xuzhou University of Technology, Xuzhou 221018, China

b Department of Civil and Environmental Engineering, Rensselaer Polytechnic Institute, Troy, NY 12180, USA

* Corresponding author, E-mail: zhaxuy@xzit.edu.cn

Part I

Adsorptive kinetics models

The adsorption kinetics could be described by the pseudo-first order model:

qt=qe(1-e-k1t)

pseudo-second order model:

qt=t∙k2∙qe21+qe∙t∙k2

and Avrami model:

qt=qe(1-e-(kAt)n)

Where qt (mg g-1) and qe (mg g-1) are the adsorption amount of CO2 at time t (min) and equilibrium, respectively; k1 (1 min-1), k2 (g (mg min)-1) and kA (1 min-1) are adsorption rate constants.

Adsorptive isotherms models

The adsorption isotherms could be described by the Langmuir model:

qt=(qeKlpe)/(1+Klpe)

And Freundlich model:

qt=Kfpe1/n

Where qt (mg g-1) is the amount of CO2 adsorbed at equilibrium, qe (mg g-1) is the saturated amount of adsorbed gas, pe (kPa) is the partial pressure of CO2, Kl (1 kPa-1) is the Langmuir constant related to adsorption capacity, Kf (mg (g kPa1/n)-1) is the Freundlich constant related to adsorption capacity and n is the adsorption intensity.

Activation energy calculation

The activation energy was calculated by Arrhenius equation:

Where K is the reaction rate constant, A is the pre-exponential factor (1 s-1), Ea is the activation energy (kJ mol-1), and R is the universal gas constant (8.3145 J (mol K)-1). By taking logarithm of both sides, the equation could be transformed to another form:

By fitting a line between ln K and 1000 T-1, the slope of line was used to obtain activation energy:

Where Kline is the slope of fitting line.

Part II

Table S1. Adsorption kinetic parameters of CO2 on biochar at 35 - 65 oC.

| Biochar | Pseudo-first order model |  |  | Pseudo-second order model |  |  | Avrami model |  |  |  | qe, exp (mg g-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | qt=qe(1-e-k1t) |  |  | qt=t∙k2∙qe21+qe∙t∙k2 |  |  | qt=qe(1-e-(kAt)n) |  |  |  |  |
|  | qe (mg g-1) | k1 (1 min-1) | R2 | qe (mg g-1) | k2 (g (mg min)-1) | R2 | qe (mg g-1) | kA (1 min-1) | n | R2 |  |
| Adsorption at 35 oC |  |  |  |  |  |  |  |  |  |  |  |
| BB | 42.14 | 1.416 | 0.912 | 43.60 | 0.060 | 0.815 | 41.95 | 1.445 | 2.822 | 0.986 | 42.54 |
| LBB3 | 39.43 | 1.086 | 0.943 | 41.15 | 0.046 | 0.896 | 39.23 | 1.123 | 1.606 | 0.959 | 40.16 |
| LBB5 | 39.66 | 1.284 | 0.931 | 41.08 | 0.058 | 0.829 | 39.47 | 1.298 | 2.324 | 0.987 | 39.73 |
| LBB10 | 44.52 | 1.262 | 0.931 | 46.17 | 0.050 | 0.836 | 44.29 | 1.285 | 2.305 | 0.985 | 44.75 |
| LBB15 | 48.51 | 1.341 | 0.925 | 50.18 | 0.049 | 0.824 | 48.28 | 1.362 | 2.486 | 0.987 | 48.61 |
| LBB20 | 48.81 | 1.320 | 0.927 | 50.51 | 0.049 | 0.824 | 48.58 | 1.336 | 2.429 | 0.988 | 48.97 |
| Adsorption at 45 oC |  |  |  |  |  |  |  |  |  |  |  |
| BB | 35.85 | 1.458 | 0.902 | 37.05 | 0.072 | 0.806 | 35.68 | 1.488 | 3.051 | 0.986 | 36.29 |
| LBB3 | 32.71 | 1.154 | 0.935 | 34.06 | 0.059 | 0.878 | 32.52 | 1.206 | 1.894 | 0.963 | 33.23 |
| LBB5 | 32.74 | 1.372 | 0.916 | 33.85 | 0.076 | 0.803 | 32.59 | 1.375 | 2.683 | 0.991 | 32.77 |
| LBB10 | 37.53 | 1.343 | 0.919 | 38.83 | 0.064 | 0.814 | 37.35 | 1.360 | 2.617 | 0.989 | 37.64 |
| LBB15 | 40.39 | 1.408 | 0.914 | 41.75 | 0.063 | 0.806 | 40.21 | 1.423 | 2.763 | 0.989 | 40.45 |
| LBB20 | 40.74 | 1.398 | 0.914 | 42.11 | 0.062 | 0.803 | 40.56 | 1.406 | 2.732 | 0.991 | 40.81 |
| Adsorption at 55 oC |  |  |  |  |  |  |  |  |  |  |  |
| BB | 32.61 | 1.413 | 0.909 | 33.77 | 0.075 | 0.837 | 32.45 | 1.476 | 2.697 | 0.972 | 33.25 |
| LBB3 | 29.49 | 1.180 | 0.936 | 30.70 | 0.068 | 0.880 | 29.33 | 1.229 | 1.810 | 0.960 | 30.02 |
| LBB5 | 29.10 | 1.411 | 0.918 | 30.07 | 0.088 | 0.811 | 28.98 | 1.419 | 2.629 | 0.989 | 29.29 |
| LBB10 | 33.51 | 1.382 | 0.921 | 34.66 | 0.074 | 0.819 | 33.36 | 1.401 | 2.568 | 0.988 | 33.69 |
| LBB15 | 36.04 | 1.439 | 0.918 | 37.23 | 0.072 | 0.816 | 35.88 | 1.459 | 2.655 | 0.988 | 36.24 |
| LBB20 | 36.58 | 1.428 | 0.918 | 37.79 | 0.071 | 0.814 | 36.42 | 1.443 | 2.643 | 0.989 | 36.79 |
| Adsorption at 65 oC |  |  |  |  |  |  |  |  |  |  |  |
| BB | 27.97 | 1.357 | 0.909 | 29.03 | 0.082 | 0.858 | 27.91 | 1.499 | 2.786 | 0.982 | 28.53 |
| LBB3 | 24.84 | 1.186 | 0.935 | 25.85 | 0.081 | 0.886 | 24.71 | 1.246 | 1.796 | 0.957 | 25.34 |
| LBB5 | 24.29 | 1.436 | 0.916 | 25.09 | 0.107 | 0.813 | 24.17 | 1.462 | 2.744 | 0.988 | 24.44 |
| LBB10 | 28.10 | 1.402 | 0.919 | 29.06 | 0.089 | 0.822 | 27.97 | 1.437 | 2.637 | 0.985 | 28.32 |
| LBB15 | 30.44 | 1.457 | 0.917 | 31.44 | 0.086 | 0.819 | 30.30 | 1.495 | 2.729 | 0.985 | 30.63 |
| LBB20 | 31.09 | 1.455 | 0.917 | 32.11 | 0.085 | 0.816 | 30.95 | 1.484 | 2.710 | 0.987 | 31.23 |

Table S2. Multicomponent adsorption experiment on impregnated biochar at 25 oC.

| Experiment | Gas | Flow rate (mL min-1) | Purity | Volume Concentration | Adsorption capacity (mg g-1) | Breaking point (s) | Dry point (s) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | CO2 | 3 | 100% | 12.0% | 28.50 | 68.6 | 161.6 |
|  | N2 | 22 | 100% | 88.00% |  |  |  |
| 2 | SO2 | 10 | 1% | 0.4% | 51.10 | 3999.0 | 6372.8 |
|  | N2 | 15 | 100% | 99.6% |  |  |  |
| 3 | NO | 10 | 1% | 0.4% | 0.24 | 14.4 | 110.4 |
|  | N2 | 15 | 100% | 99.6% |  |  |  |
| 4 | CO2 | 3 | 100% | 12.0% | 23.70 | 70.1 | 133.4 |
|  | NO | 10 | 1% | 0.4% | 0.14 | 17.3 | 35.8 |
|  | SO2 | 10 | 1% | 0.4% | 45.06 | 3572.0 | 6160.8 |
|  | N2 | 2 | 100% | 87.2% |  |  |  |

Breaking point and dry point are recorded when the ratio of outlet concentration to inlet concentration reached 0.05 and 0.95. Adsorption capacity was calculated when the ratio of outlet concentration to inlet concentration reached 1 for the first time.