Supplementary Materials

Xu Zhao a,, Qingliang Wang b,d, Yige Sun c, Haoshuai Lib, Zhiwu Lei b, Boyuan Zheng b, Hongyang Xia b, Yucheng Su b, Khan Muhammad Yaruq Ali b, Hongqiang Wangb,c, Fang Hu b,*

a School of Nuclear Science and Technology, University of South China, Hengyang 421001, Hunan, China

b School of Resource Environment and Safety Engineering, University of South China, Hengyang 421001, Hunan, China

c College of Chinese Language and Literature, Luoyang Normal University, Luoyang 471934, Henan, China

d School of Chemistry and Chemical Engineering, University of South China, Hengyang 421001, China

* Corresponding author: Fang Hu;

Tel: (+86)13787340058; E-mail address: csuhufang@163.com

Number of pages: 7

2 Tables and 1 Figure

Table of Contents

Equations	3

1.1 Beryllium Analysis Method	3

1.2 Adsorption Kinetics	3

1.3 Adsorption Isotherm	3

1.4 Adsorption Thermodynamics	4

1.5 Be Removal Rate	4

1.6 pH Analysis	4

Figure	5

Fig. S1	5

Tables	6

Table S1	6

Table S2	6

References	7

# Equations

## 1.1 Beryllium Analysis Method

The concentration of beryllium (Be) was determined by UV-Vis spectrophotometer (UV-2550, Shimadzu) with ellirocyanine R as the colorant. The wavelength of beryllium is 590 nm. The adsorption capacity qe of Be is formulated as follows[1]:

(S1)

## 1.2 Adsorption Kinetics

The pseudo-first-order kinetic model is formulated as follows [2]:

(S2)

In the formula, qe (g/kg) is the equilibrium adsorption capacity; qt (g/kg) is the adsorption capacity of the adsorbent at time t; and k1 (min-1) is the primary rate coefficient.

The pseudo-second-order kinetic model is formulated as follows [3]:

(S3)

Where, k2 (min·g/mg) is a pseudo-second-order rate coefficient.

The in-particle diffusion model is formulated as follows [4]:

(S4)

Where, Ks [mg/(g·min1/2)] is the coefficient of internal diffusion rate; and C (g/kg) is the coefficient related to the thickness of the adhesive layer on the adsorbent surface .

## 1.3 Adsorption Isotherm

Langmuir model formula is as follows [5].

(S5)

Where, Ce (mg/L) is the equilibrium concentration; qm is the saturated adsorption capacity (g/kg) of the adsorbent at a certain temperature. kL (L/mg) is the Langmuir coefficient.

Freundlich model is as follows [6]:

(S6)

Where kF is the Freundlich constant and 1/ nF is the heterogeneity factor.

The expression of Temkin model is as follows [3]:

(S7)

Where, at is Temkin constant (L/mg); B (J/mol) is Temkin adsorption heat correlation coefficient, B = RT /bt; R is 8.314 J/(mol·K); T is the adsorption process temperature (K); The constant bt is related to the heat of adsorption.

## 1.4 Adsorption Thermodynamics

Adsorption thermodynamics is helpful to understand the adsorption mechanism, and the distribution coefficient Kd of beryllium on MLLB is calculated using equation (8).

(S8)

In formula (8), the unit of Ce is mg/L and the unit of qe is g/kg.

The entropy change (ΔS0) and enthalpy change (ΔH0) are derived from the Van Hove equation [2]. The relevant equation is as follows:

(S9)

(S10)

(S11)

## 1.5 Be Removal Rate

The formula for calculating the beryllium removal rate is as follows:

(S12)

Among them, C0 (mg/L) is the Initial concentration. Ce (mg/L) is the adsorption equilibrium concentration.

## 1.6 pH Analysis

This experiment used a pH meter (SevenExcellence S400-Basic) to measure the pH. The initial pH is measured before solid-liquid contact. The final pH was measured after solid-liquid contact.

# Figures

Fig. S1 Adsorption effect of the five adsorption materials at different times (a), pH of the five materials after stirring in deionized water for 5 h (b),

# Tables

Table S1 Comparison of different adsorbent

| Sample | chlorella vulgaris Immobilized | chitosan modified zeolite | modified chitosan resin | polystyrene-based chelating | aerobic granule | CC-LBC | H-AC | Fe-AC | Al-AC | MWBI | MLLB |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| pH | 6.5 | 7-9 | 1.0 | 8.0 | 7.5-8 | 6.0 | 5.0 | 6.0 | 6.0 | 6.0 | 6.0 |
| qm (g/kg) | -- | 0.252 | 44.96 | 22.5 | 14 | 55 | 30.63 | 45.68 | 32.86 | 1.45 | 40.38 |
| Removal rate % | 80 | 90.1 | -- | 98 | 82 | 99 | 99 | 99 | 99 | 80 | 99.9 |
| Reference | [7] | [8] | [9] | [10] | [4] | [2] | [11] | [12] | [1] | [13] | This study |

Table S2 Thermodynamic parameters for the adsorption of breyllium by MLLB.

| T (℃) | ln Kc | ΔG0 (kJ/mol) | ΔH0 (kJ/mol) | ΔS0 [J/(mol·K)] |
| --- | --- | --- | --- | --- |
| 15 | 9.69 | -23.23 | 1.84 | 36.49 |
| 25 | 10.82 | -26.84 | 2.29 | 35.95 |
| 35 | 12.53 | -32.11 | 2.85 | 34.46 |

References

[1] Zhao, X., Su, Y., Wang, H., Lei, Z., Hu, E., Hu, F., ... & Hao, X. (2023). Modification of activated carbon from agricultural waste lotus leaf and its adsorption mechanism of beryllium. Korean Journal of Chemical Engineering, 40(1), 255-266.

[2] Zhao Xu, Shuai Dong, Hongqiang Wang, Eming Hu, Fang Hu, Zhiwu Lei, Qingliang Wang, Chunze Zhou, Shiyao Fan, Xinwei Liu, Xuanzhang Hao, Yucheng Su, (2023). Preparation of Porous Calcium Carbonate Biochar and its Beryllium Adsorption Performance, Journal of Environmental Chemical Engineering, 110102.

[3] Zhao, X., Su, Y., Hao, X. et al (2023). Effect of mechanical−chemical modification on adsorption of beryllium by calcite. Environ Sci Pollut Res.

[4] Sun, F (Sun, Fang) , Sun, WL (Sun, Wei-Ling),et al (2011). Biosorption behavior and mechanism of beryllium from aqueous solution by aerobic granule(J).Chemical Engineering Journal,172(2-3):783-791.

[5] Vetrivel S A, Diptanghu M, Ebhin M R, et al. Green algae of the genus Spirogyra: A potential absorbent for heavy metal from coal mine water[J]. Remediation Journal, 2017, 27(3): 81-90.

[6] Xin, Q., Wang, Q., Gan, J., Lei, Z., Hu, E., Wang, H., & Wang, H. (2023). Enhanced performance in uranium extraction by the synergistic effect of functional groups on chitosan-based adsorbent. Carbohydrate Polymers, 300, 120270.

[7] Gatewood, P.L. , J. Sneddon. Removal and recovery of beryllium in waters by chlorella vulgaris (J). Journal of Environmental Science and Health Part A,1990. 25(1):21-28.

[8] Ren Gang, Yu Yan, et al (2016). Adsorption of Beryllium (Be) from wastewater by chitosan modified zeolite [J] . Journal of Safety and Environment,16(06) : 208-213.

[9] Mahmoud O. Abd El-Magied, Asmaa Mansour, Fathi A. Al Ghani Alsayed, Samia Abd Eldayem (2018). Biosorption of beryllium from aqueous solutions onto modified chitosan resin: Equilibrium, kinetic and thermodynamic study. Journal of Dispersion Science and Technology(11).

[10] N. N. Basargin,O. V. Miroshnichenko (2012). Beryllium(II) sorption from aqueous solutions by polystyrene-based chelating polymer sorbents[J]. Russian Journal of Inorganic Chemistry, 57(5): 759-762.

[11] Zhao X, Xia H, Su Y, et al. Study on removal of beryllium from uranium beryllium ore wastewater by acid leaching activated carbon and its mechanism[J]. Journal of Radioanalytical and Nuclear Chemistry, 2023: 1-12.

[12] Zhao X, Su Y, Lei Z, et al. Adsorptive removal of beryllium by Fe-modified activated carbon prepared from lotus leaf[J]. Environmental Science and Pollution Research, 2023, 30(7): 18340-18353.

[13] Tokarčíková M, Motyka O, Peikertová P, et al. Magnetically modified biosorbent for rapid beryllium elimination from the aqueous environment[J]. Materials, 2021, 14(21): 6610.

* Corresponding author.

Tel:13787340058

E-mail address: csuhufang@163.com (Fang Hu)