Supporting Information

Preparation of nano Cu-Mo2C interface supported on ordered mesoporous biochar of ultrahigh surface area for reverse water gas shift reaction

Xueyuan Pana, Hao Suna*, Mingzhe Maa, Haiquan Liaoa, Guowu Zhanb*, Kui Wanga,c*, Mengmeng Fanc, Jingcheng Xuc, Linfei Dingc, Kang Suna, Jianchun Jianga

a Key Lab. of Biomass Energy and Material, Jiangsu Province, Key and Open Lab. of Forest Chemical Engineering, SFA, National Engineering Lab. for Biomass Chemical Utilization, Institute of Chemical Industry of Forest Products, Chinese Academy of Forestry, Nanjing 210042, China

b Academy of Advanced Carbon Conversion Technology, College of Chemical Engineering, Huaqiao University, Xiamen, Fujian, 361021, China

c Co-Innovation Center of Efficient Processing and Utilization of Forest Resources, Nanjing Forestry University, Nanjing 210042, China

* Corresponding author at: Institute of Chemical Industry of Forest Products, Chinese Academy of Forestry, Nanjing 210042, China.

E-mail address: sunhao@icifp.cn (H. Sun); gwzhan@hqu.edu.cn (G. Zhan); wangkui@caf.ac.cn (K. Wang)

Fig. S1. (a) The N2 adsorption-desorption isotherms patterns of MB and 0.8wt.%Cu-20wt.%Mo2C/MB catalysts at different carburizing temperatures, and XRD patterns of Cu-Mo2C/MB catalysts with (b) different Cu loading and (c) different Cu-Mo2C loading.

Fig. S2. (a) The Raman patterns of 0.8wt%Cu-20wt%Mo2C/MB catalysts at different carburizing temperatures, and the SEM images of 0.8wt%Cu-20wt%Mo2C/MB catalysts at carburizing temperatures of (b) 750 ℃, (c) 800 ℃ and (d) 850 ℃.

Raman spectroscopy was conducted to further determine the surface structures of the catalysts and reveal their phase composition. As shown in Fig. S2(a), the typical bands of carbon materials at 1330 cm-1 (D band) and 1590 cm-1 (G band), where the ordering of the carbon is shown by the intensity ratio of the D to G bands (ID/IG) (Baklanova et al. 2017). It is clear that the disorder structures of the catalysts exhibit similarities at different carburizing temperatures.

Fig. S3. The XPS spectra of (a) C 1s, and (b) O 1s of BC-1, BC-2, and MB.

Fig. S4. (a) Stability evolution over 1.4wt.%Cu-35wt.%Mo2C/MB-800 catalyst, (b) XRD and (c) Raman patterns of catalysts before and after reaction.

Fig. S5. The XPS spectra of (a) Mo 3d, (b) C 1s, (c) Cu 2p, and (d) Cu AES spectra of catalysts before and after reaction.

Fig. S6. (a) TEM images of the used 1.4wt.%Cu-35wt.%Mo2C/MB-800 catalyst at 50 nm (The inset is distributions and mean diameters (<d>) of nanoparticles), (b) HRTEM image of the used 1.4wt.%Cu-35wt.%Mo2C/MB-800 catalyst, (c) EDS spectra of the used 1.4wt.%Cu-35wt.%Mo2C/MB-800 catalyst.
Table S1. Characteristics of specific surface area and pore structure of MB and Cu-Mo2C/MB catalysts.

| Sample | SBET (m2/g)a | Vtotal (cm3/g)b | Vmeso (cm3/g)c | Mo (wt.%)d |
| --- | --- | --- | --- | --- |
| MB | 2693 | 1.56 | 0.81 | - |
| 0.8wt.%Cu-20wt.%Mo2C/MB-750 | 1361 | 0.76 | 0.36 | 15.32 |
| 0.8wt.%Cu-20wt.%Mo2C/MB-800 | 1281 | 0.73 | 0.38 | 16.02 |
| 0.8wt.%Cu-20wt.%Mo2C/MB-850 | 1356 | 0.76 | 0.38 | 17.32 |

a Total surface area (SBET) obtained according to BET method with a 3 m2/g standard deviation.

b Total pore volume (Vtotal) obtained according to volume absorbed at P/P0 = 0.99.

c Mesopore volume (Vmeso) derived from the NLDFT model.

d Mo Loading obtained according to XPS.

Table S2. Compositions and positions of Mo 3d5/2, Cu 2p1/2 for all samples.

| Catalyst | Mo 3d5/2 binding energy/eV |  |  |  | Cu 2p1/2 binding energy/eV |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Mo2+ | Mo4+ | Mo6+ |  | Cu0 | Cu+ |
| 0.8wt.%Cu-20wt.%Mo2C/MB-750 | 5.06 | 3.92 | 91.02 |  | 62.58 | 37.42 |
| 0.8wt.%Cu-20wt.%Mo2C/MB-800 | 13.74 | 5.51 | 80.75 |  | 56.09 | 43.91 |
| 0.8wt.%Cu-20wt.%Mo2C/MB-850 | 14.11 | 5.78 | 80.11 |  | 41.39 | 58.61 |

Table S3. Comparison of CO2 conversion rate and CO selectivity for the as-prepared and reported catalysts.

| Catalyst | CO2/H2 | GHSV （ml/g/h） | P (Mpa) | T (°C) | Rate (×10-5molCO2/gcat/s) | SCO (%) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cu/Mo2C-C | 1:2 | 300000 | 0.1 | 500 | 27.74 | 99.1 | This work |
| α-Mo2C/C | 1:3 | 100000 | 0.1 | 500 | 14.50 | 100 | (Ahmadi Khoshooei et al. 2024) |
| Cs-Mo2C | 1:2 | 12000 | 0.1 | 500 | 1.19 | ~95 | (Zhang et al. 2019) |
|  | 1:4 | 12000 | 0.1 | 500 | 1.25 | ~98 |  |
| Cu-Mo2C | 1:4 | 12000 | 0.1 | 500 | 1.55 | ~96 |  |
| MoN/NC | 1:3 | 8000 | 0.1 | 500 | 1.01 | 100 | (Jiang et al. 2022) |
| Mo2C@N-C | 1:3 | 24000 | 0.1 | 400 | 1.56 | 99.5 | (Ma et al. 2020) |
| 1K-Cu/Mo2C | 1:2.5 | 84000 | 0.1 | 500 | 12.20 | 100 | (Xu et al. 2021) |
| Mo2C/SBA-15 | 1:1 | 60000 | 0.1 | 500 | 4.09 | 98 | (Marquart et al. 2021) |
| Mo2C/SiO2 |  |  |  |  | 6.32 | 98 |  |
| Cu-Mo2C-C | 1:4 | 60000 | 0.1 | 400 | 0.85 | 100 | (Xiong et al. 2018) |
| Cu–Mo2C–NC |  |  |  |  | 1.72 | 100 |  |
| MoxC | 1:3 | 3000a | 0.1 | 400 | - | 98 | (Liu et al. 2020) |
| MoC/γ-Al2O3 | 1:3 | 60000 | 0.3 | 500 | 1.34 | 100 | (Sun et al. 2021) |
| Pt/CeO2 | 1:3 | 72000 | 0.1 | 450 | 2.12 | 99 | (Zhao et al. 2021) |
| Co−Fe@(N)G | 1:3 | 6000 | 0.1 | 500 | 1.04 | 98 | (Peng et al. 2021) |
| K-Mo2C/γ-Al2O3 | 1:3 | 13320 | 2.1 | 450 | 1.74 | 99.3 | (Juneau et al. 2020) |
| NiCu-Saponite | 1:4 | 15000 | 0.1 | 500 | 1.97 | 89 | (Nityashree et al. 2020) |
| NiCo-Saponite |  |  |  |  | 1.82 | 37 |  |
| Ni-Saponite |  |  |  |  | 2.12 | 16 |  |

References

Ahmadi Khoshooei M, Wang X, Vitale G, Formalik F, Kirlikovali KO, Snurr RQ, Pereira-Almao P, Farha OK （2024） An active, stable cubic molybdenum carbide catalyst for the high-temperature reverse water-gas shift reaction. Science 384: 540-546. http://doi.org/10.1126/science.adl1260

Baklanova ON, Vasilevich AV, Lavrenov AV, Drozdov VA, Muromtsev IV, Arbuzov AB, Trenikhin MV, Sigaeva SS, Temerev VL, Gorbunova OV, Likholobov VA, Nizovskii AI, Kalinkin AV （2017） Molybdenum carbide synthesized by mechanical activation an inert medium. J Alloy Compd 698: 1018-1027. http://doi.org/10.1016/j.jallcom.2016.12.186

Jiang Y, Sung Y, Choi C, Bang GJ, Hong S, Tan X, Wu T-S, Soo Y-L, Xiong P, Li MM-J, Hao L, Jung Y, Sun Z （2022） Single-Atom Molybdenum-N3 Sites for Selective Hydrogenation of CO2 to CO. AngewChem Int Ed 61: e202203836. http://doi.org/10.1002/anie.202203836

Juneau M, Vonglis M, Hartvigsen J, Frost L, Bayerl D, Dixit M, Mpourmpakis G, Morse JR, Baldwin JW, Willauer HD, Porosoff MD （2020） Assessing the viability of K-Mo2C for reverse water-gas shift scale-up: molecular to laboratory to pilot scale. Energy Environ Sci 13: 2524-2539. http://doi.org/10.1039/d0ee01457e

Liu X, Pajares A, Calinao Matienzo DJD, Ramirez de la Piscina P, Homs N （2020） Preparation and characterization of bulk MoXC catalysts and their use in the reverse water-gas shift reaction. Catal Today 356: 384-389. http://doi.org/10.1016/j.cattod.2019.11.011

Ma Y, Guo Z, Jiang Q, Wu K-H, Gong H, Liu Y （2020） Molybdenum carbide clusters for thermal conversion of CO2 to CO via reverse water-gas shift reaction. J Energy Chem 50: 37-43. http://doi.org/10.1016/j.jechem.2020.03.012

Marquart W, Raseale S, Prieto G, Zimina A, Sarma BB, Grunwaldt J-D, Claeys M, Fischer N （2021） CO2 reduction over Mo2C-based catalysts. ACS Catal 11: 1624-1639. http://doi.org/10.1021/acscatal.0c05019

Nityashree N, Price CAH, Pastor-Perez L, Manohara GV, Garcia S, Maroto-Valer MM, Reina TR （2020） Carbon stabilised saponite supported transition metal-alloy catalysts for chemical CO2 utilisation via reverse water-gas shift reaction. Appl Catal B Environ 261: 118241. http://doi.org/10.1016/j.apcatb.2019.118241

Peng L, Jurca B, Primo A, Gordillo A, Parvulescu VI, Garcia H （2021） Co-Fe clusters supported on N-doped graphitic carbon as highly selective catalysts for reverse water gas shift reaction. ACS Sustain Chem Eng 9: 9264-9272. http://doi.org/10.1021/acssuschemeng.1c01401

Sun G, Mottaghi-Tabar S, Ricardez-Sandoval L, Simakov DSA （2021） Highly active, selective and stable reverse water gas shift catalyst based on high surface area MoC/gamma-Al2O3 synthesized by reverse microemulsion. Top Catal 64: 414-430. http://doi.org/10.1007/s11244-020-01411-y

Xiong K, Zhou G, Zhang H, Shen Y, Zhang X, Zhang Y, Li J （2018） Bridging Mo2C–C and highly dispersed copper by incorporating N-functional groups to greatly enhance the catalytic activity and durability for carbon dioxide hydrogenation. J Mater Chem A 6: 15510-15516. http://doi.org/10.1039/c8ta04096f

Xu J, Gong X, Hu R, Liu Z-w, Liu Z-t （2021） Highly active K-promoted Cu/β-Mo2C catalysts for reverse water gas shift reaction: effect of potassium. Mol Catal 516: 111954. http://doi.org/10.1016/j.mcat.2021.111954

Zhang Q, Pastor-Perez L, Jin W, Gu S, Reina TR （2019） Understanding the promoter effect of Cu and Cs over highly effective beta-Mo2C catalysts for the reverse water-gas shift reaction. Appl Catal B Environ 244: 889-898. http://doi.org/10.1016/j.apcatb.2018.12.023

Zhao Z, Wang M, Ma P, Zheng Y, Chen J, Li H, Zhang X, Zheng K, Kuang Q, Xie Z-X （2021） Atomically dispersed Pt/CeO2 catalyst with superior CO selectivity in reverse water gas shift reaction. Appl Catal B Environ 291: 120101. http://doi.org/10.1016/j.apcatb.2021.120101