Developing an activated biochar-mineral supplement for reducing methane formation in anaerobic fermentation

Sara Tahery1*, Mariano C. Parra2, Paul Munroe1, David R.G Mitchell3, Sarah J. Meale2, Stephen Joseph1

- School of Materials Science and Engineering, University of New South Wales (UNSW), Sydney, NSW 2052, Australia

- School of Agriculture and Food Sciences, The University of Queensland, Gatton, QLD, Australia

- Electron Microscopy Centre, AIIM Building, Innovation Campus, University of Wollongong, Squires Way, Fairy Meadow, NSW 2517, Australia

*Corresponding author. Tel.: +61 422120095

E-mail address: s.taherymoosavi@unsw.edu.au

This document includes:

Pages 6

Tables 7

Table S1. Composition and post-treatment of the biochar-mineral supplement.

| Constituents of the biochar-mineral supplement | (wt%) |
| --- | --- |
| Wheat straw | 52.7 |
| Wheat straw ash | 10.3 |
| Zeolite | 10.3 |
| Bentonite | 10.3 |
| Red kaolinite | 4.1 |
| Diatomite | 4.1 |
| FeSO4 | 4.1 |
| ZnO | 4.1 |
| Post-treatment |  |
| Peracetic acid | 22.2 |
| Propionic acid | 11.2 |
| KNO3 | 22.2 |

Adjusted in vitro dry matter digestibility (IVDMD) calculation:

- Soluble fraction (%DM) = percentage of remaining in the bags at time 0h after bags being washed continuously until water ran clear under the tap

- Amount of soluble fraction (in g) = Soluble fraction (%DM) × proportion of additives added

- Corrected residues (g) = [(Bags + residues after 48h incubation) – bags weight] + Amount of soluble fraction (in g)

- Digestible DM (g) = (Substrate + additives; DM basis) - corrected residues

- IVDMD = Digestible DM (g) / (Substrate + additives; DM basis) × 100

Table S2. Ultimate and elemental analyses of the biochar-mineral supplement.

| Ultimate and elemental analyses | Biochar-mineral supplement |
| --- | --- |
| Ultimate analysis (wt%) |  |
| C | 14.30 |
| H | 0.81 |
| N | 5.44 |
| Elemental analysis (mg kg-1) |  |
| Na | 4.36 × 103 |
| Mg | 1.9 × 103 |
| Al | 7.2 × 103 |
| Si | 35.6 × 103 |
| S | 21.7 × 103 |
| K | 205.1 × 103 |
| Ca | 2.2 × 103 |
| Fe | 18.2 × 103 |
| Zn | 16.1 × 103 |
| P | 5.95 × 102 |
| Cl | 2.8 × 102 |
| Cu | 4.85 × 102 |
| Mn | 1.28 × 102 |
| Ti | 1.10 × 102 |
| Cr | 21.6 |
| Ni | 10.7 |
| Sr | 58.4 |
| Ba | 38.2 |
| Cd | 0.6 |
| Pb | 5.1 |
| B | 13.3 |
| As | 2.1 |
| Co | 2.3 |
| Zr | 11.2 |

Table S3. Specific capacitances of the biochar-mineral supplement at scan rates of 20 and 50 mV s-1.

| Specific capacitance | Biochar-mineral supplement (F g-1) |
| --- | --- |
| Scan rate 20 (mV s-1) | 2.0 |
| Scan rate 50 (mV s-1) | 0.77 |

Table S4. Concentration of free radicals in the biochar-mineral supplement and g factor compared to standard DPPH, measured by ESR.

|  | DPPH* | Biochar-mineral supplement |
| --- | --- | --- |
| Concentration of free radicals/mg | 1.40 x 108 | 1.05 x 1011 |
| G factor | 2.00387 | 2.0049 |

*2,2-diphenyl-1-picrylhydrazyl

Table S5. Concentration of inorganic functional groups on the surface of the biochar-mineral supplement, measured by XPS.

| Name | Functional groups | Peak BE | Concentration (at.%) |
| --- | --- | --- | --- |
| K2p3 |  | 293.38 | 3.97 |
| Si2p |  | 103.17 | 2.22 |
| S2p3 |  | 169.39 | 2.69 |
| Mg1s |  | 1304.92 | 1.41 |
| Cl2p3 |  | 198.86 | 1.84 |
| Na1s |  | 1071.92 | 0.97 |
| Zn2p3 |  | 1022.39 | 1.91 |
| Ca2p3 |  | 348.42 | 2.18 |
| Al2s |  | 119.59 | 0.84 |
| Cu2p3 |  | 934.96 | 0.51 |

Table S6. The type and concentration of DOC fractions in the biochar-mineral supplement, measured by LC-OCD (n=3).

| DOC* and its fractions | Concentration (mg L-1) | Concentration (%) |
| --- | --- | --- |
| DOC | 68.37 | 100 |
| Hydrophobic DOC | 22.76 | 33.3 |
| Hydrophilic DOC | 45.60 | 66.7 |
| Biopolymers | 10.68 | 15.6 |
| Humic-like substances | 6.82 | 10.0 |
| Building blocks | 5.28 | 7.7 |
| LMW neutrals | 18.18 | 26.6 |
| LMW acids | 4.64 | 6.8 |

*Dissolved organic carbon

Table S7. The type and concentration of hydrophilic DOC fractions in the rumen media (n=3).

| DOC fractions (Mg L-1) | Control | Biochar-mineral supplement |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 1.5% (DM) | 4.0% (DM) | 6.0% (DM) | SEM1 | P-value |
| Hydrophilic DOC | 3666.2 | 3632.3 | 3489.3 | 2913.1* | 107.77 | 0.013 |
| Biopolymers | 49.35 | 27.4* | 29.6* | 48.8 | 4.03 | 0.050 |
| Humic-like substances | 143.6 | 171.7 | 179.3 | 121.3 | 13.09 | 0.422 |
| Building blocks | 226.9 | 112.0* | 145.8* | 170.5 | 14.88 | 0.013 |
| LMW neutrals | 206.3 | 214.3 | 217.7 | 201.6 | 4.89 | 0.704 |
| LMW acids | 3040.0 | 3106.9 | 2917.3 | 2370.8* | 100.20 | <0.01 |

1Standard error of means; *Means differ (P<0.05) compared to the control.