Adsorptive-photocatalytic removal of tetracycline from wastewater by Fe3O4- and SnO2-containing biochar nanocomposites

Chuchen Zhang1#, Shuwen Zhao1#, Qilan Huang1, Jianqiao Liu2, *, Qianru Zhang1, *

1. State Key Laboratory of Efficient Utilization of Arid and Semi-arid Arable Land in Northern China, Institute of Agricultural Resources and Regional Planning, Chinese Academy of Agricultural Sciences, Beijing 100081, China

2. College of Information Science and Technology, Dalian Maritime University, Dalian 116026, China.

* Corresponding author, Qianru Zhang, E−mail: zhangqianru@caas.cn

* Corresponding author, Jianqiao Liu, E−mail: jqliu@dlmu.edu.cn

#Chuchen Zhang and Shuwen Zhao are co-first authors of the article.

Address: No. 12 Zhongguancun South Street, Beijing 100081, China.

Fig. S1. The photolysis of TC.

Fig. S2. UV-vis absorption spectra of (a) BC, (b) BC@Fe3O4@SnO2-1:1:1 and (c) BC@Fe3O4@SnO2-1:2:1.

Fig. S3. The EPR results about the generation of (a) ·OH, (b) ·O2, (c) h+ of BC, (d) ·OH, (e) ·O2 and (f) h+ of BC@Fe3O4@SnO2-1:1:2.

Fig. S4. Electrostatic Potential Surfaces of TC.

Fig. S5. Charge populations of carbon structures containing multiple functional groups.

Table S1. NPA charges and condensed Fukui functions of TC

| Atom | q(N) | q(N+1) | q(N-1) | f - | f + | f 0 |
| --- | --- | --- | --- | --- | --- | --- |
| C1 | 0.36347 | 0.34579 | 0.39604 | 0.03257 | 0.01768 | 0.025125 |
| C2 | -0.31799 | -0.33362 | -0.29272 | 0.02527 | 0.01563 | 0.02045 |
| C3 | -0.20306 | -0.24681 | -0.16986 | 0.0332 | 0.04375 | 0.038475 |
| C4 | -0.26228 | -0.26633 | -0.20781 | 0.05447 | 0.00405 | 0.02926 |
| C5 | -0.00959 | -0.02124 | -0.00604 | 0.00355 | 0.01165 | 0.0076 |
| C6 | -0.17795 | -0.17093 | -0.16209 | 0.01586 | -0.00702 | 0.00442 |
| C7 | 0.2484 | 0.24721 | 0.25408 | 0.00568 | 0.00119 | 0.003435 |
| C8 | -0.2791 | -0.27252 | -0.29123 | -0.01213 | -0.00658 | -0.009355 |
| C9 | -0.24236 | -0.25846 | -0.14594 | 0.09642 | 0.0161 | 0.05626 |
| C10 | 0.51548 | 0.47306 | 0.50989 | -0.00559 | 0.04242 | 0.018415 |
| C11 | -0.46908 | -0.46642 | -0.47463 | -0.00555 | -0.00266 | -0.004105 |
| C12 | -0.2867 | -0.28301 | -0.28817 | -0.00147 | -0.00369 | -0.00258 |
| C13 | 0.14781 | 0.14567 | 0.14921 | 0.0014 | 0.00214 | 0.00177 |
| C14 | 0.42755 | 0.42283 | 0.47257 | 0.04502 | 0.00472 | 0.02487 |
| C15 | -0.10194 | -0.10006 | -0.10562 | -0.00368 | -0.00188 | -0.00278 |
| C16 | 0.43236 | 0.27852 | 0.45287 | 0.02051 | 0.15384 | 0.087175 |
| C17 | -0.29544 | -0.32282 | -0.29573 | -0.00029 | 0.02738 | 0.013545 |
| C18 | 0.54701 | 0.4447 | 0.54511 | -0.0019 | 0.10231 | 0.050205 |
| C19 | 0.6644 | 0.66868 | 0.66296 | -0.00144 | -0.00428 | -0.00286 |
| O20 | -0.64427 | -0.69483 | -0.62809 | 0.01618 | 0.05056 | 0.03337 |
| O21 | -0.67145 | -0.67759 | -0.63705 | 0.0344 | 0.00614 | 0.02027 |
| N22 | -0.86614 | -0.88702 | -0.84293 | 0.02321 | 0.02088 | 0.022045 |
| O23 | -0.62228 | -0.66736 | -0.53912 | 0.08316 | 0.04508 | 0.06412 |
| O24 | -0.52673 | -0.58366 | -0.3834 | 0.14333 | 0.05693 | 0.10013 |
| O25 | -0.6473 | -0.65961 | -0.59291 | 0.05439 | 0.01231 | 0.03335 |
| O26 | -0.57317 | -0.68127 | -0.54539 | 0.02778 | 0.1081 | 0.06794 |
| C27 | -0.69926 | -0.69507 | -0.70577 | -0.00651 | -0.00419 | -0.00535 |
| N28 | -0.56878 | -0.58129 | -0.56851 | 0.00027 | 0.01251 | 0.00639 |
| C29 | -0.48392 | -0.47977 | -0.48867 | -0.00475 | -0.00415 | -0.00445 |
| C30 | -0.49605 | -0.48739 | -0.50117 | -0.00512 | -0.00866 | -0.00689 |
| O31 | -0.79773 | -0.8231 | -0.77458 | 0.02315 | 0.02537 | 0.02426 |
| O32 | -0.7747 | -0.78148 | -0.74682 | 0.02788 | 0.00678 | 0.01733 |
| H33 | 0.23775 | 0.22124 | 0.26186 | 0.02411 | 0.01651 | 0.02031 |
| H34 | 0.24864 | 0.23197 | 0.2731 | 0.02446 | 0.01667 | 0.020565 |
| H35 | 0.24635 | 0.23597 | 0.26556 | 0.01921 | 0.01038 | 0.014795 |
| H36 | 0.26105 | 0.24719 | 0.28596 | 0.02491 | 0.01386 | 0.019385 |
| H37 | 0.26322 | 0.27107 | 0.26919 | 0.00597 | -0.00785 | -0.00094 |
| H38 | 0.25235 | 0.23509 | 0.27022 | 0.01787 | 0.01726 | 0.017565 |
| H39 | 0.26875 | 0.24806 | 0.27821 | 0.00946 | 0.02069 | 0.015075 |
| H40 | 0.23375 | 0.20724 | 0.24616 | 0.01241 | 0.02651 | 0.01946 |
| H41 | 0.5137 | 0.49254 | 0.52325 | 0.00955 | 0.02116 | 0.015355 |
| H42 H43 | 0.50518 0.43005 | 0.49295 | 0.52649 | 0.02131 | 0.01223 | 0.01677 |
|  |  | 0.40708 | 0.4451 | 0.01505 | 0.02297 | 0.01901 |
| H44 | 0.44962 | 0.45146 | 0.45157 | 0.00195 | -0.00184 | 5.5E-05 |
| H45 | 0.53498 | 0.52966 | 0.55529 | 0.02031 | 0.00532 | 0.012815 |
| H46 | 0.24428 | 0.23668 | 0.25345 | 0.00917 | 0.0076 | 0.008385 |
| H47 | 0.25463 | 0.24236 | 0.26693 | 0.0123 | 0.01227 | 0.012285 |
| H48 | 0.24999 | 0.25153 | 0.2612 | 0.01121 | -0.00154 | 0.004835 |
| H49 | 0.25335 | 0.23544 | 0.2651 | 0.01175 | 0.01791 | 0.01483 |
| H50 | 0.24347 | 0.23987 | 0.2392 | -0.00427 | 0.0036 | -0.000335 |
| H51 | 0.21331 | 0.19861 | 0.2242 | 0.01089 | 0.0147 | 0.012795 |
| H52 | 0.25291 | 0.23148 | 0.26518 | 0.01227 | 0.02143 | 0.01685 |
| H53 | 0.26842 | 0.27643 | 0.26539 | -0.00303 | -0.00801 | -0.00552 |
| H54 | 0.20624 | 0.19397 | 0.21651 | 0.01027 | 0.01227 | 0.01127 |
| H55 | 0.5276 | 0.52187 | 0.53632 | 0.00872 | 0.00573 | 0.007225 |
| H56 | 0.51121 | 0.51545 | 0.50604 | -0.00517 | -0.00424 | -0.004705 |