Table S1. Physicochemical properties of the vermiculite before and after pyrolysis

|  | Origin vermiculite | V300 | V500 | V700 |
| --- | --- | --- | --- | --- |
| pH | 7.04 | 7.38 | 7.08 | 7.05 |
| EC (μS cm-1) | 127.53 | 67.07 | 87.67 | 22.30 |
| Pyrolysis loss rate (%) | NA | 10.38 | 14.85 | 14.33 |
| SSA (m2 g-1) | 8.42 | 7.94 | 4.70 | 3.61 |
| PV (cm3 g-1) | 0.22 | 0.019 | 0.017 | 0.014 |
| APD (nm) | 10.43 | 9.70 | 14.36 | 15.16 |

V300: vermiculite after pyrolysis at 300℃; V500: vermiculite after pyrolysis at 500℃; V700: vermiculite after pyrolysis at 700℃; EC: electrical conductivity; SSA: specific surface area; PV: pore volume; APD: average pore diameter; NA: not applicable.

Table S2. Results of multi-way analysis of variance of the cumulative CO2 emissions from SOC and the priming effect on 105 days among different biochar treatments with three influencing factors

|  | Cumulative CO2 emissions from SOC on 105 days |  |  |  |  | Priming effect on 105 days |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Type III Sum of Squares | Degrees of Freedom | Mean Square | F - value | Significance | Type III Sum of Squares | Degrees of Freedom | Mean Square | F - value | Significance |
| Corrected model | 53491.597 a | 13 | 4114.738 | 46.362 | 0.000 | 8354.801 b | 13 | 642.677 | 73.959 | 0.000 |
| Intercept | 3060677.195 | 1 | 3060677.195 | 34485.512 | 0.000 | 4821.467 | 1 | 4821.467 | 554.850 | 0.000 |
| A | 1902.544 | 1 | 1902.544 | 21.437 | 0.000 | 205.755 | 1 | 205.755 | 23.678 | 0.000 |
| B | 14743.175 | 2 | 7371.587 | 83.058 | 0.000 | 3096.405 | 1 | 3096.405 | 356.331 | 0.000 |
| C | 10320.534 | 1 | 10320.534 | 116.284 | 0.000 | 1416.536 | 2 | 708.268 | 81.507 | 0.000 |
| A*B | 1060.812 | 2 | 530.406 | 5.976 | 0.007 | 28.521 | 1 | 28.521 | 3.282 | 0.081 |
| A*C | 98.396 | 1 | 98.396 | 1.109 | 0.301 | 72.045 | 2 | 36.022 | 4.145 | 0.026 |
| B*C | 2007.368 | 2 | 1003.684 | 11.309 | 0.000 | 165.359 | 2 | 82.679 | 9.515 | 0.001 |
| A*B*C | 1937.100 | 2 | 968.55 | 10.913 | 0.000 | 158.135 | 2 | 79.067 | 9.099 | 0.001 |
| Error | 2485.071 | 28 | 88.753 |  |  | 243.311 | 28 | 8.690 |  |  |
| Total | 3266800.847 | 42 |  |  |  | 15485.922 | 42 |  |  |  |
| Revised total | 55976.669 | 41 |  |  |  | 8598.112 | 41 |  |  |  |

a: R2 = 0.956 (Adjusted R2 = 0.935); b: R2 = 0.972 (Adjusted R2 = 0.959); A, B, and C represent the influencing factor of vermiculite modification, pyrolysis temperature, and soil type, respectively.

Table S3. Priming effect intensity and topological features of soil bacterial community network

|  | Red soil |  |  |  | Paddy soil |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Nodes | Edges | Priming effect |  | Nodes | Edges | Priming effect |
| BC300 | 46 | 131 | 7.39 |  | 45 | 125 | -12.2 |
| BC500 | 45 | 137 | 1.08 |  | 47 | 82 | -32.2 |
| BC700 | 47 | 117 | -7.52 |  | 47 | 93 | -31.8 |
| VBC300 | 47 | 156 | 4.08 |  | 46 | 108 | -23.7 |
| VBC500 | 46 | 124 | -8.97 |  | 48 | 91 | -34.4 |
| VBC700 | 49 | 109 | -13.9 |  | 49 | 101 | -27.2 |
| CK | 50 | 87 | 0.00 |  | 48 | 94 | 0.00 |

BC: rice straw biochar; VBC: vermiculite-modified rice straw biochar; CK: control.