Supplementary Information

Synergistic multi-metal stabilization of contaminated lead-zinc smelting contaminated soil by Ochrobactrum EEELCW01-loaded iron-modified biochar: Performance and long-term efficacy

Yayuan Huanga, Yuxuan Luoa, Chuan Wua,b,*, Shengguo Xuea, Yahui Wua, Waichin Lib,*

aSchool of Metallurgy and Environment, Central South University, Changsha 410083, China

bDepartment of Science and Environmental Studies, the Education University of Hong Kong, Tai Po, Hong Kong Special Administrative Region, 999077, China

* Corresponding authors:

Prof, Chuan Wu.

Email: wuchuan@csu.edu.cn.

Name of the journal: Biochar
Date of the document prepared: November 1, 2024

Pages: 4
Figure: 2

Table: 3

1 Analysis of BET and XPS

  - BET analysis of Fe-BC and B-FeOB

We measured the specific surface area SBET of iron-modified biochar (Fe-BC) and Ochrobactrum EEELCW01-loaded iron-modified biochar (B-FeOB) using the N2-BET method. The specific surface area SBET of Fe-BC and B-FeOB were 183.64 m2/g and 158.26 m2/g, respectively. The decrease in specific surface area may be because the loading of Ochrobactrum EEELCW01 blocked some pores in Fe-BC, resulting in a decrease in SBET and further confirming the successful loading of Ochrobactrum EEELCW01 onto the surface of biochar.

  - XPS analysis of FeOB

We conducted XPS analysis on the mineral precipitation formed by Ochrobactrum EEELCW01 after incubation for 7 days (Fig. S1). Fig. S1 presents the XPS full spectrum (a) and Fe 2p (b) of iron oxide precipitates from Ochrobactrum EEELCW01 incubated in Fe-containing medium for 7 days. In Fig. S1b, the photoelectron peaks at 711, 719, 725, and 732 eV represent the binding energies of 2p3/2, shake-up satellite 2p3/2, 2p1/2, and shake-up satellite 2p1/2, respectively. By comparing with the XPS characteristic spectrum library of Fe, it is indicated that the iron in the collected precipitates mainly exists in the form of Fe(II) and Fe(III) compounds. The peak at 711.5 eV is from the Fe 2p3/2 orbital of Fe(III) compounds, accounting for 79.99% of the total Fe content, while the peak at 710.3 eV is from the Fe 2p3/2 orbital of Fe(II) compounds, with a relative proportion of 20.01%. This result shows that the iron oxide precipitates obtained from Ochrobactrum EEELCW01 incubated in Fe-containing medium for 7 days are Fe(II)-Fe(III) compounds with an Fe(II):Fe(III) ratio of approximately 1:4. In the mineral precipitates, Fe(III) is the predominant form, which aligns with the oxidizing action of Ochrobactrum EEELCW01. Therefore, Ochrobactrum EEELCW01 primarily manifests as the oxidation of trivalent iron and the potential reduction of divalent iron during biomineralization, demonstrating its potential functions in iron cycling and heavy metal remediation.

Fig. S1 XPS analysis of mineral precipitation after incubation of Ochrobactrum EEELCW01 for 7 days

2 Supplementary data

Table S1 Basic properties of iron-modified biochar (Fe-BC) and Ochrobactrum EEELCW01-loaded iron-modified biochar (B-FeOB)

|  | pH | C (%) | H (%) | O (%) | N (%) | P (%) | BET (m2/g) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Fe-BC | 9.16 | 58.60 | 5.23 | 19.52 | 1.36 | 1.27 | 183.64 |
| B-FeOB | 8.37 | 57.74 | 4.59 | 18.28 | 3.43 | 1.05 | 158.26 |

Table S2 The concentrations of heavy metals (Pb, Cd, As, and Zn) of soil (mg·kg-1)

| Total-Pb | Total-Cd | Total-As | Total-Zn | Available-Pb | Available-Cd | Available-As | Available-Zn |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 17175 | 177 | 4890 | 2481 | 0.316 | 0.312 | 3.901 | 5.525 |

Table S3 Fluorescence intensity of soil DOM components under different treatments

| Treatment | Fluorescence intensity / a.u. |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | total | component I | component II | component III | component IV |
| CK | 109224.372 | 9882.46124 | 20443.1368 | 20247.1861 | 58651.5883 |
| FeOB | 151877.031 | 14745.8583 | 26781.543 | 29089.6179 | 81260.012 |
| Biochar | 190930.8 | 17262.5012 | 39395.5804 | 30872.0974 | 103400.621 |
| B-FeOB | 196339.128 | 17228.2841 | 37385.6063 | 33204.8029 | 108520.435 |

Fig. S2 Plant growth in different treatment groups