Development of hazelnut shell-derived biochar to support a bifunctional MoCo electrocatalyst for HER/OER in alkaline medium

Jaime Ñanculeo a, Teresa Andreu b, Ignasi Sirés b, Andrés Ramírez c, Mara Cea d,e, Benjamín Nahuelcura a, Gerson Valenzuela d, Karla Garrido-Miranda e, María Eugenia González d,e,*

a Doctoral program in Engineering Sciences with Specialization in Bioprocesses, University of La Frontera, Av. Francisco Salazar 01145, Temuco-Chile.

b Departament de Ciència de Materials i Química Física, Secció de Química Física, Facultat de Química, Universitat de Barcelona, Martí i Franquès, 1-11, 08028 Barcelona, Spain.

c Department of Chemical Sciences and Natural Resources, Faculty of Engineering and Sciences, University of La Frontera, Av. Francisco Salazar 01145, Temuco 4780000, Chile.

d Department of Chemical Engineering, University of La Frontera, Av. Francisco Salazar 01145, Temuco 4780000, Chile

e Scientific and Technological Bioresource Nucleus (BIOREN-UFRO), Universidad de La Frontera, Av. Francisco Salazar 01145, Temuco 4780000, Chile

* Corresponding author, mariaeugenia.gonzalez@ufrontera.cl

Fig. S1 Pyrolysis system used for this study.

Table S1. Elemental composition HS.

| Element | Content (%) |
| --- | --- |
| C | 53.254 |
| O | 40.779 |
| H | 5.779 |
| N | 0.535 |
| Ash | 0.347 |

Fig. S2 Thermogravimetric analysis (TGA) and derivate thermogravimetric (DTG) of HS.

Fig. S3 Inorganic content of HS by Total reflection X-ray fluorescence (TXRF).

Fig. S4 FTIR spectrum of HS and electrocatalysts synthesized.

Fig. S5 X-ray diffraction (XRD) of biochar.

Fig. S6 High-resolution XPS spectra for C 1s in BC-Mo/Co.

Fig. S7 Circuit equivalent of BC-Mo/Co for HER and OER.

Fig. S8 HER performance: a) turnover frequency (TOF), and b) chronoamperometric at -0.257 V of BC-Mo/Co.

Fig. S9 OER performance: a) turnover frequency (TOF), and b) chronoamperometric at 1.6 V of BC-Mo/Co.

Fig. S10 Cyclic voltammetry for ECSA determination: a) BC, b) BC-Mo, c) BC-Co and d) BC-Mo/Co.

Fig. S11. Effect of BC-Mo/Co synthesis temperature on the overpotential of a) HER and b) OER.