Engineered mineral-doped biochar-infused paraffin for synergistic enthalpy storage and enhanced thermal management

Dimberu G. Atinafu, Jihee Nam, Sumin Kim*

a Department of Architecture and Architectural Engineering, Yonsei University, Seoul 03722, Republic of Korea

* Corresponding author, E-mail: kimsumin@yonsei.ac.kr

## Production and characteristics of biochar

The thermal, chemical and physical properties of biochar, obtained from spruce feedstock carbonization at 600 °C, is shown in Table S1.

Table S1 Proximate analysis of biochar sample.

| Parameters | Values |
| --- | --- |
| Fixed carbon (FC) | >90% |
| Bulk density | 200 kg m–3 |
| Conductivity | 21.5 mS m–1 |
| Moisture content | 30–50% |
| Ash content | 1.6–4% |
| pH | 10 |
| Total nitrogen | 0.6–0.8% |
| Heavy metals (mg (kg. d)–1) | Arsenic (<0.5), Cadmium (0.04), Chromium (13), Copper (4.7), Lead (4.2), Nickel, (13), Zink (56), Mercury (<0.02) |
| Total potassium | 3200 mg (kg. d)–1 |