Supplementary Information

Highly Porous Biochar from Spent Coffee Ground

for Fully Green Thermal Insulating Composites

with Thermal Conductivity of 0.04 W m−1 K−1

Sung Jin Kim a   Seong Yun Kim a *

a Department of Carbon Composites Convergence Materials Engineering, Jeonbuk National University, Jeonju 54896, Republic of Korea

* Corresponding author, E-mail: sykim82@jbnu.ac.kr

S1 Specific information of materials

- Spent coffee ground (NESCAFÉ Dolce Gusto Lungo, Nestlé, Vevey, Switzerland)

- Ethyl cellulose (EC; 48.0–49.5% (w/w) ethoxyl basis, Sigma-Aldrich, MO, USA)

- Ethanol (EtOH; Samchun Pure Chemical, Pyeongtaek, Korea)

- Propylene glycol (PG; Daejung Chemicals & Metals Co., Ltd., Siheung, Korea)

- Cellulase (C2370, Sigma-Aldrich, MO, USA)

- Expanded polystyrene (EPS, BEWI ASA, Trondheim, Norway)

S2 Characterization

Sample preparation and characterization were carried out using the instruments specified below:

- Tube furnace (LF-GT 630, LK Lab, Namyangju, Korea)

- Thinky mixer (ARE 310, Thinky Co., Tokyo, Japan)

- Heating press (D3P-20J, Dae Heung Science, Incheon, Korea)

- Fourier transform infrared spectroscopy (Frontier, PerkinElmer Ltd., Buckinghamshire, UK)

- X-ray photoelectron spectroscopy (K-Alpha+, Thermo Fisher Scientific Inc., Waltham, MA, USA)

- X-ray diffractometer (PANalytical X'Pert Pro, Malvern Panalytical Ltd., Royston, UK)

- Raman spectroscopy (RAMAN Touch, Nanophoton, Osaka, Japan)

- Field-emission scanning electron microscope (GeminiSEM 500, Carl Zeiss, Oberkochen, Germany)

- Sputter machine (Ion Sputter E-1030, Hitachi High Technologies, Tokyo, Japan)

- Cs-corrected transmission electron microscope (JEM-ARM200F, JEOL, Peabody, MA, USA)

- Mercury intrusion porosimeter (Autopore V9620, Micromeritics, Norcross, GA, USA)

- Gas adsorption instrument (BELSORP MINI X, MicrotracBEL Corp., Osaka, Japan)

- Gas pycnometer (Ultrapyc 5000 Foam, Anton Paar, Graz, Austria)

- Differential scanning calorimeter (DSC 204 F1 Phoenix, NETZSCH, Selb, Germany)

- TCI thermal conductivity analyzer (C-Therm Technologies Ltd., Fredericton, NB, Canada)

- Contact angle goniometer (L2004A1, Ossila Ltd., Sheffield, UK)

- Three-dimensional micro-computed tomography (Skyscan 1272, Bruker Co., MA, USA)

- Infrared camera (FLIR E54, Teledyne FLIR LLC, Wilsonville, OR, USA)

Fourier transform infrared spectroscopy (FT-IR) was utilized to identify the chemical functional groups of the SB in the range of 4000–500 cm−1. The chemical bonds of the SB were analyzed using X-ray photoelectron spectroscopy (XPS) with an Al X-ray source. The crystal structure of the SB was analyzed using an X-ray diffractometer (XRD) with a Cu-Kα radiation source (1.54 Å). SB was scanned over a 2θ range of 10–60° at a rate of 0.02°/s. The carbon structure of the SB was identified using Raman spectroscopy with a 532 nm laser source. The surface morphology of the SB and interior morphology of the composites were observed by a field-emission scanning electron microscope (FE-SEM). The samples were coated with platinum for 100 s using a sputter machine. The morphology of the SB was observed at high resolution with a Cs-corrected transmission electron microscope. The pore structure was analyzed using two different methods, with nitrogen adsorption for micro-/mesopores and mercury intrusion for macropores. The nitrogen adsorption-desorption isotherms were measured at −196 °C using a gas adsorption analyzer after degassing at 200 °C for 6 h. The specific surface area of SB was calculated using the Brunauer-Emmett-Teller (BET) method, and the micropore volume (Vmicro) was evaluated using the t-plot method. The mesopore volume (Vmeso) was determined by the Barrett-Joyner-Halenda method. The macropore volume (Vmacro) and macroporosity were obtained using a mercury intrusion porosimeter. The total pore volume (VTotal) was calculated as the sum of the micro-, meso-, and macropore volumes. The relative volume fraction of each pore type (micro-, meso-, and macropores) in SB was calculated using the following equation:

Relative Pore volume fraction (%)=VxVTotal×100    x=micro, meso, macro                     (S1)

The true density (ρtrue) of SB and EC was measured using a gas pycnometer. The apparent density (ρapp), which takes into account the internal pores of the material, was calculated by (Yao et al. 2022):

ρapp=ρtrue(1-ϕ/100)                                                                  (S2)

The specific heat capacity (Cp) of SB and EC was measured with a differential scanning calorimeter. The thermal effusivity (e) of the SB was measured with a TCI thermal conductivity analyzer. The thermal conductivity (K) of SB as derived from the measured thermal effusivity can be expressed as (Lei et al. 2019):

K=e2ρappCp                                                                                (S3)

The pore structure of the SB in the composites was confirmed using three-dimensional (3D) micro-computed tomography (micro-CT) with a charge-coupled device detector. The thermal conductivity of the composites was analyzed with a TCI thermal conductivity analyzer. The thermal insulation performance was evaluated by observing a sample placed on a hot plate at 45 °C using an infrared (IR) camera.

S3 Governing equations

The FEM simulation was performed under steady-state heat transfer, assuming that the heat flow was homogeneous with no heat generation. The governing equation for thermal conductivity was derived from Fourier’s law, expressed as follows (Comsol 2018; Alvarez-Guerrero et al. 2022; Ngo et al. 2018):

q=-k∇T                                                                                (S4)

where q, k, and ∇T are heat flux density, thermal conductivity, and temperature gradient, respectively. In the steady-state without a heat source, the rate of temperature change over time is zero (Comsol 2018). The law of energy conservation can be simplified as follows:

∇∙q=0                                                                                  (S5)

By applying Fourier’s law, this can be expressed as the Laplace equation (Comsol 2018; Alvarez-Guerrero et al. 2022; Ngo et al. 2018):

∇2T=0                                                                                  (S6)

Therefore, the governing equation of heat transfer in the composite can be described as follows (Comsol 2018; Alvarez-Guerrero et al. 2022; Ngo et al. 2018):

∂∂x∂Ti∂x+∂∂y∂Ti∂y+∂∂z∂Ti∂z=0         i=m, f                                                   (S7)

where the subscripts m and f indicate the matrix and filler, respectively.

S4 Solubility based on relative energy difference

The relative energy difference (RED) is an important indicator for determining the solubility between a solvent and a solute (Li et al. 2022). A solvent with RED<1.0 exhibits a high affinity for the solute, whereas a solvent with RED>1.0 indicates low solubility (Li et al. 2022). The R0 value of EC has been reported as 10.3 MPa1/2 (Archer 1992). The RED values of the solvents for EC are presented in Table S7. Water and PG exhibited RED values greater than 1, indicating a low affinity for EC. However, EtOH had an RED value of 0.98, suggesting excellent affinity and solubility with EC. Therefore, the RED values confirmed that EC was insoluble in water and PG but soluble in EtOH.

Table S1 Properties of EPS

| Property | Value |
| --- | --- |
| Thermal conductivity (W m−1 K−1) | 0.04 |
| Density (kg m−3) | 43 |
| Average pore size (μm) | 83 |
| Porosity (%) | 82 |
| biodegradability | Non-biodegradable |

Table S2 Carbonization conditions and pore characteristics of as-prepared SB

| Label | Temperature (°C) | Atmosphere | Time (hour) | SBETa (m2 g−1) | Vmicrob (cm3 g−1) | Vmesoc (cm3 g−1) | Vmacrod (cm3 g−1) | Yield (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SCG | – | – | – | – | – | – | 0.8654 | – |
| SB500 | 500 | Ambient air | 1 | 34.87 | 0.0145 | 0.0031 | 1.3066 | 36 |
| SB700 | 700 | Ambient air | 1 | 247.5 | 0.0905 | 0.0150 | 1.7830 | 23 |
| SB900 | 900 | Ambient air | 1 | 891.5 | 0.2790 | 0.1483 | 1.9517 | 19 |
| NSB700 | 700 | Nitrogen | 1 | – | – | – | 1.7730 | 25 |

a BET surface area

b Micropore pore volume

c Mesopore pore volume

d Macropore pore volume

Table S3 Label and composition of the fabricated composites

| Label | Filler type | EC (wt%) | SB (wt%) |  | PG (g g−1 of SB) |  |
| --- | --- | --- | --- | --- | --- | --- |
| EC/SCG/PG-05 | SCG | 95 |  | 5 |  | 2.0 |
| EC/SCG/PG-10 |  | 90 |  | 10 |  | 2.0 |
| EC/SCG/PG-15 |  | 85 |  | 15 |  | 2.0 |
| EC/SCG/PG-20 |  | 80 |  | 20 |  | 2.0 |
| EC/SCG/PG-25 |  | 75 |  | 25 |  | 2.0 |
| EC/SB500/PG-05 | SB500 | 95 |  | 5 |  | 2.0 |
| EC/SB500/PG-10 |  | 90 |  | 10 |  | 2.0 |
| EC/SB500/PG-15 |  | 85 |  | 15 |  | 2.0 |
| EC/SB500/PG-20 |  | 80 |  | 20 |  | 2.0 |
| EC/SB500/PG-25 |  | 75 |  | 25 |  | 2.0 |
| EC/SB700/PG-05 | SB700 | 95 |  | 5 |  | 2.0 |
| EC/SB700/PG-10 |  | 90 |  | 10 |  | 2.0 |
| EC/SB700/PG-15 |  | 85 |  | 15 |  | 2.0 |
| EC/SB700/PG-20 |  | 80 |  | 20 |  | 2.0 |
| EC/SB700/PG-25 |  | 75 |  | 25 |  | 2.0 |
| EC/SB900/PG-05 | SB900 | 95 |  | 5 |  | 2.0 |
| EC/SB900/PG-10 |  | 90 |  | 10 |  | 2.0 |
| EC/SB900/PG-15 |  | 85 |  | 15 |  | 2.0 |
| EC/SB900/PG-20 |  | 80 |  | 20 |  | 2.0 |
| EC/SB900/PG-25 |  | 75 |  | 25 |  | 2.0 |
| EC/NSB700/PG-25 | NSB700 | 75 |  | 25 |  | 2.0 |

Table S4 Label and composition of the control samples

| Label | Filler type | EC (wt%) | SB (wt%) |  | Solvent (g g−1 of SB) |  |
| --- | --- | --- | --- | --- | --- | --- |
| EC/SB700/none-25 | SB700 | 75 |  | 25 |  | – |
| EC/SB700/water-25 |  | 75 |  | 25 |  | 2.0 (water) |
| EC/SB700/EtOH-25 |  | 75 |  | 25 |  | 2.0 (EtOH) |

Table S5 Material properties used in FEM simulation

| Property | EC | SB700 | SB900 |
| --- | --- | --- | --- |
| Specific heat capacity (Cp, J kg−1 K−1) | 1532 | 1021 | 875 |
| True density (ρtrue, kg m−3) | 1234 | 1238 | 1339 |
| Apparent density (ρapp, kg m−3) | – | 414 | 431 |
| Thermal effusivity (e, W s1/2 m−2 K−1) | – | 130 | 154 |
| Thermal conductivity (K, W m−1 K−1) | 0.24 | 0.04 | 0.06 |

Table S6 Hansen solubility parameter of EC and solvents

| Material | Hansen solubility parameters (MPa1/2) |  |  | Reference |
| --- | --- | --- | --- | --- |
|  | δd | δp | δh |  |
| EC | 17.0 | 7.7 | 9.6 | (Shlush and Davidovich-Pinhas 2023) |
| Water | 15.6 | 16.0 | 42.3 | (Subrahmanyam et al. 2015) |
| EtOH | 15.8 | 8.8 | 19.4 |  |
| PG | 16.8 | 9.4 | 23.3 |  |

Table S7 RED values of solvents with EC

| Solvent | RED value |
| --- | --- |
| Water | 3.28 |
| EtOH | 0.98 |
| PG | 1.33 |

Fig. S1 Micro-CT image of EPS

Fig. S2 Macropore size distribution of (a) SCG, (b) SB500, (c) SB700, and (d) SB900

Fig. S3 Nitrogen adsorption-desorption isotherms of SB

Fig. S4 Relative pore volume fractions of SB

Fig. S5 FE-SEM fracture surface image of SB700-based composite (25 wt%) fabricated with 1.5 g of PG per 1.0 g of SB700

Fig. S6 Micro-CT image of EC/SB700/none-25

Fig. S7 PV cells integrated with thermal insulation material

Fig. S8 Ice state before and after the scaled-down BIPV system experiment

## References

Alvarez-Guerrero S, Ordonez-Miranda J, de Coss R, Alvarado-Gil JJ (2022) Determination of the effective thermal conductivity of particulate composites based on VO2 and SiO2. International Journal of Thermal Sciences 172:107278. https://doi.org/10.1016/j.ijthermalsci.2021.107278

Archer WL (1992) Hansen solubility parameters for selected cellulose ether derivatives and their use in the pharmaceutical industry. Drug development and industrial pharmacy 18(5):599-616.

Comsol A (2018) Heat transfer module user’s guide. COMSOL Multiphysics R, Stockholm, Sweden. 5

Lei H, Fu C, Zou Y, Guo S, Huo J (2019) A thermal energy storage composite with sensing function and its thermal conductivity and thermal effusivity enhancement. Journal of Materials Chemistry A 7(12):6720-6729. https://doi.org/10.1039/C8TA11753E

Li M, Ren T, Sun Y et al (2022) New parameter derived from the hansen solubility parameter used to evaluate the solubility of asphaltene in solvent. ACS omega 7(16):13801-13807. https://doi.org/10.1021/acsomega.2c00018

Ngo IL, Byon C, Lee BJ (2018) Analytical study on thermal conductivity enhancement of hybrid-filler polymer composites under high thermal contact resistance. International journal of heat and mass transfer 126:474-484. https://doi.org/10.1016/j.ijheatmasstransfer.2018.05.162

Shlush E, Davidovich-Pinhas M (2023) Fabrication of bioplastic material based on ethyl-cellulose using hot-melt extrusion. Food Packaging and Shelf Life 40:101206. https://doi.org/10.1016/j.fpsl.2023.101206

Subrahmanyam R, Gurikov P, Dieringer P, Sun M, Smirnova I (2015) On the road to biopolymer aerogels—Dealing with the solvent. Gels 1(2):291-313. https://doi.org/10.3390/gels1020291

Yao Y, Panahi A, Schiemann M, Levendis YA (2022) Determination of size and porosity of chars during combustion of biomass particles. Combustion and Flame 242:112182. https://doi.org/10.1016/j.combustflame.2022.112182