# Titanium Dioxide-Loaded Biochar Composite Simultaneously Reduces Arsenic Mobilization and Methane Emissions in Flooded Paddy Soils

Song Wu1, Zhiyuan Zhu1, 2, Dunfeng Si3, Chuang Zhao4, Hai Feng1, Qian Zhang1, 5, Juan Wang5, Dongmei Zhou3, and Yujun Wang1, *

1State Key Laboratory of Soil and Sustainable Agriculture, Institute of Soil Science, Chinese Academy of Sciences, Nanjing 210008, China.

2School of Environmental Science and Engineering, Suzhou University of Science and Technology, Suzhou, China.

3State Key Laboratory of Pollution Control and Resource Reuse, School of Environment, Nanjing University, Nanjing 210023, China.

4Shandong Institute of Geophysical and Geochemical Exploration, Jinan 250013, China

5School of Environmental and Municipal Engineering, North China University of Water Resources and Electric Power, Zhengzhou 450046, PR China.

*Corresponding author: yjwang@issas.ac.cn (Y. Wang)

Text S1

Biochar modification generally involves pore activation, heteroatom doping, and metal loading. In Tables S1 and S2 below, we summarize research and review articles published in the Biochar journal in 2025 that utilized pore activators to prepare modified biochar. In most cases, heteroatom doping and metal loading are widely discussed, however, these modifications are typically built upon the foundation of pore activation, a process that is often overlooked. In fact, such pore-activated biochars can also be classified as activated carbons.

From a soil biogeochemistry perspective, unmodified biochar has a limited capacity to significantly influence the fate of arsenic during the flooding of paddy soil. Therefore, we evaluated the modification of biochar via pore activation and TiO2 loading to tune the behavior of arsenic and mitigate methane emissions. For the convenience of synthesizing TiO2-loaded biochar with a high specific surface area, the material was not directly derived from agricultural biomass and an activator. Instead, it was prepared by direct pyrolysis of a mixture of commercially available activated carbon and a titanium salt. The activated carbon used in this study was prepared through the activation of charcoal. We believe the findings of our study are applicable to guiding the remediation of soil arsenic contamination using pore- and metal-modified biochar.

Table S1 Recent published research articles that preparing modified biochar with pore-activator in Biochar journal.

| Research article No. | Title | Biomass | Name | Activator |
| --- | --- | --- | --- | --- |
| 1 (Wang et al., 2025) | P-modified biochar alters the microbial community in heavy metal-contaminated soils by regulating nutrient supply balance | Apple tree branches | Phosphorus-modified biochar | K3PO4 |
| 2 (Cong et al., 2025) | Improved adsorption capacity of ammonium from aqueous solution by modified biogas residue biochar | Distillery grains | NaOH-modified biochar | NaOH |
| 3 (Xu et al., 2025) | Composite adsorbent material for the effective removal of benzaldehyde from Chinese spirit: synergistic adsorption behavior of AC-SiO2 | Distillery grains | Silica removed activated carbon | Steam |
| 4 (Ñanculeo et al., 2025) | Development of hazelnut shell-derived biochar to support a bifunctional MoCo electrocatalyst for HER/OER in alkaline medium | Hazelnut shells | Molybdenum or cobalt supported biochar | KOH |
| 5 (Cheng et al., 2025) | Cobalt-based multicomponent embedded in biomass-derived porous biochar as a highly efficient oxygen reduction reaction electrocatalyst | Wood biomass | Cobalt embedded in N-doped biochar | Zn2(OH)2CO3 |
| 6 (Zhou et al., 2025) | Unraveling the synergistic mechanism of urea and sodium carbonate during biochar modification and peroxymonosulfate activation for wastewater decontamination | Corncobs | Modified biochar | Na2CO3 |
| 7 (Atinafu et al., 2025) | Sustainable thermal buffering of microencapsulated bio-phase change materials through an engineered biochar dopant | Food waste | Food-waste-derived engineered biochar | KOH |
| 8 (Zhao et al., 2025b) | Collaborative modification strategy to improve the formation of biochar-derived persistent free radicals for aniline removal via peroxymonosulfate activation | Corncob | Modified biochar | Na2CO3 |

Table S2 Recent published review articles that addressing the importance of preparing modified biochar with pore-activator in Biochar journal.

| Review article No. | Title | Description |
| --- | --- | --- |
| 1 (Sun et al., 2025) | Preparation of bio-carbon by polymerization of bio-tar: a critical review on mechanisms, processes, and applications | Adding chemical activators and heteroatom dopants is an effective method for improving the pore structure and functional group characteristics of bio-carbon. |
| 2 (Zhao et al., 2025a) | Unlocking the potential of element-doped biochar: from tailored synthesis to multifunctional applications in environment and energy | Pore size structure is a critical factor influencing biochar performance, and elemental doping serves as an effective modification method to significantly alter its pore characteristics, thereby enhancing its application potential. |
| 3 (Ye et al., 2025) | The state-of-the-art review on biochar as green additives in cementitious composites: performance, applications, machine learning predictions, and environmental and economic implications | In chemical activation, the activation of biomass is achieved using chemical reagents, including KOH, HNO3, Fe(NO3)3, CaCl2, Na2CO3, AlCl3, and FeCl3. Chemical activation introduces chemical precursors into biomass, which exhibits a higher specific surface area, a more porous structure, higher stability, and more functional groups after pyrolysis |
| 4 (Fakhar et al., 2025) | Advancing modified biochar for sustainable agriculture: a comprehensive review on characterization, analysis, and soil performance | The specific surface area (SSA) and pore structure of biochar play a significant role in adsorption and regulating the nature of biochar as hydrophilic or hydrophobic. The general purpose of modification in pristine biochar is to expand its surface area, which ultimately modifies its functional groups and enhances its magnetic performance and catalytic capacity |
| 5 (Li et al., 2025) | Review of modified biochar for removing humic acid from water: analysis of structure-activity relationship | Biochar is immersed in an acidic or alkaline solution, which increases its specific surface area, improves its pore structure, and introduces more surface functional groups while removing NOM. |
| 6 (Xiong et al., 2025) | Remediation of uranium-contaminated water and soil by biochar-based materials: a review. | The specific surface area was verified as the most vital parameter determining the adsorption efficacy of biochar, with an optimal range of 500-1200 m2 g-1. |

Figure S1 Scanning electron microscopy images of PABC (a), Ti-PABC-1 (b), and Ti-PABC-2 (c). Energy dispersive X-ray spectroscopy mapping spectrum of Ti-PABC-3 (d).

Figure S2 Suspension Fe(II) percentage (a) and filtrate dissolved arsenite (b) and ferrous ion (c and d) during Shewanella oneidensis MR-1 (d) or abiotic (a-c) reduction of arsenite-bearing ferrihydrite in the absence and presence of PABC, Ti-PABC-1, Ti-PABC-2, and Ti-PABC-3, respectively.

Figure S3 X-ray diffractograms of the solid phases collected at 774 h during abiotic reduction of arsenite/arsenate-bearing ferrihydrite in the absence and presence of PABC and Ti-PABC-2, respectively.

Figure S4 Morphology of vivianite precipitated by drop-wise adding 0.05 M KOH to the mixture solution of 0.035 M H3PO4 and 0.05 M FeSO4 to a final pH of 6.00 in a glovebox.

Figure S5 Energy dispersive X-ray spectroscopy spectra of elements composition at different sites as noted in Figure 5a.

Figure S6 Scanning electron microscopy-energy dispersive X-ray spectroscopy characterization of the morphology (a) and Fe (b), P (c), C (d), Ti (e), and As (f) elements distribution on the solid phase precipitates that generated during Shewanella oneidensis MR-1 reduction of arsenite-bearing ferrihydrite in the presence of Ti-PABC-2.

Figure S7 Energy dispersive X-ray spectroscopy spectra of elements composition at different sites as noted in Figure 6a.

References

Atinafu, D.G., Choi, J.Y., Nam, J., Yun, B.Y. and Kim, S.  2025.  Sustainable thermal buffering of microencapsulated bio-phase change materials through an engineered biochar dopant. Biochar 7(1), 27.

Cheng, Y., Ding, J., Pan, H., Li, Y., Zhu, N., Ma, L., Sun, H. and Wu, J.  2025.  Cobalt-based multicomponent embedded in biomass-derived porous biochar as a highly efficient oxygen reduction reaction electrocatalyst. Biochar 7(1), 40.

Cong, P., Song, S., Zhu, Y., Ji, X., Liu, S., Kuang, S., Xu, Y., Hou, Q., Zheng, X. and Song, W.  2025.  Improved adsorption capacity of ammonium from aqueous solution by modified biogas residue biochar. Biochar 7(1), 97.

Fakhar, A., Galgo, S.J.C., Canatoy, R.C., Rafique, M., Sarfraz, R., Farooque, A.A. and Khan, M.I.  2025.  Advancing modified biochar for sustainable agriculture: a comprehensive review on characterization, analysis, and soil performance. Biochar 7(1), 8.

Li, Y., Zhu, Y., Liu, J., Fan, W., Cao, Y., Huo, Y. and Wei, J.  2025.  Review of modified biochar for removing humic acid from water: analysis of structure-activity relationship. Biochar 7(1), 1.

Ñanculeo, J., Andreu, T., Sirés, I., Ramírez, A., Cea, M., Nahuelcura, B., Valenzuela, G., Garrido-Miranda, K. and González, M.E.  2025.  Development of hazelnut shell-derived biochar to support a bifunctional MoCo electrocatalyst for HER/OER in alkaline medium. Biochar 7(1), 72.

Sun, Y., Jia, J., Huo, L., Zhang, X., Zhao, L., Liu, Z., Zhao, Y. and Yao, Z.  2025.  Preparation of bio-carbon by polymerization of bio-tar: a critical review on mechanisms, processes, and applications. Biochar 7(1), 90.

Wang, Q., Xu, C., Pan, K., Wu, X., Pan, Y., Duan, C. and Geng, Z.  2025.  P-modified biochar alters the microbial community in heavy metal-contaminated soils by regulating nutrient supply balance. Biochar 7(1), 93.

Xiong, X., Liu, J., Xiao, T., Lin, K., Huang, Y., Deng, P., Hu, H. and Wang, J.  2025.  Remediation of uranium-contaminated water and soil by biochar-based materials: a review. Biochar 7(1), 41.

Xu, X., Jiang, Z., Xu, S. and Shi, B.  2025.  Composite adsorbent material for the effective removal of benzaldehyde from Chinese spirit: synergistic adsorption behavior of AC-SiO2. Biochar 7(1), 79.

Ye, P., Guo, B., Qin, H., Wang, C., Liu, Y., Chen, Y., Bian, P., Lu, D., Wang, L., Zhao, W., Yang, Y., Hong, L., Gao, P., Ma, P., Zhan, B. and Yu, Q.  2025.  The state-of-the-art review on biochar as green additives in cementitious composites: performance, applications, machine learning predictions, and environmental and economic implications. Biochar 7(1), 21.

Zhao, J., Jiang, Y., Chen, X., Wang, C. and Nan, H.  2025a.  Unlocking the potential of element-doped biochar: from tailored synthesis to multifunctional applications in environment and energy. Biochar 7(1), 77.

Zhao, Z., Zhu, S., Qi, S., Zhou, T., Yang, Y., Wang, F., Han, Q., Dong, W., Wang, H. and Sun, F.  2025b.  Collaborative modification strategy to improve the formation of biochar-derived persistent free radicals for aniline removal via peroxymonosulfate activation. Biochar 7(1), 24.

Zhou, T., Zhu, S., Li, X., Wang, X., Huang, R., Dong, W., Zhao, Z. and Wang, H.  2025.  Unraveling the synergistic mechanism of urea and sodium carbonate during biochar modification and peroxymonosulfate activation for wastewater decontamination. Biochar 7(1), 35.