Supplementary Materials

Conventional and Microwave-Assisted Pyrolysis Biochars: Comparative Mechanistic Insights, Structural Evolution, and Environmental Remediation Applications

Atta Rasool1,*, Kateřina Brožová1, Jitka Chromíková1, Eva Pertile1, Jan Halfar1, Petra Malíková1, Oldřich Motyka1, Silvie Drabinová1, Kristina Čabanová1, Silvie Heviánková1

1Faculty of Mining and Geology, VSB – Technical University of Ostrava, 17. listopadu 2172/15, Ostrava-Poruba, 708 00, Czech Republic

*Corresponding author

Name: Atta Rasool

Email: atta.rasool@vsb.cz

Fig. S1 shows a comparative schematic of the mechanisms of pore structure evolution and surface functional group synthesis during CP and MAP

# Table S1. Quantitative Benchmarking of CP vs. MAP Biochars (Typical Literature Ranges).

| Property |  | Conventional Pyrolysis (CP) Biochar | Microwave-Assisted Pyrolysis (MAP) Biochar | Notes & Interpretation | Representative References |
| --- | --- | --- | --- | --- | --- |
| BET Surface Area (m² g⁻¹) |  | 10–350 | 150–850 | MAP often produces higher SA due to rapid heating and better pore development | Shadi et al. 2023 |
| Pore Volume (cm³ g⁻¹) |  | 0.01–0.20 | 0.10–0.60 | Greater mesoporosity in MAP char improves the diffusion of larger molecules | Tomczyk et al., 2020 |
| Dominant Pore Type |  | Microporous | Mesoporous + microporous | MAP favors mesopore formation via internal dielectric heating | Meyer et al., 2024; Ellison et al. 2017 |
| pH |  | 6–9 (feedstock dependent) | 7–11 | Higher pH is often due to the concentration of basic functional groups in MAP chars | Dennison et al. 2025 |
| Elemental C (%) |  | 50–75 | 60–85 | MAP enhances carbonization and aromaticity | Nizamuddin et al. 2019 |
| Elemental H (%) |  | 2–4 | 1–3 | Lower H indicates greater aromatic condensation in MAP | Wijitkosum and Jiwnok 2019 |
| Elemental O (%) |  | 10–25 | 5–20 | Controlled MAP heating reduces oxygen loss, preserving OFGs at moderate temperatures | Yu et al. 2023 |
| C/O Ratio |  | 2–8 | 4–12 | Higher C/O ratio indicates stronger graphitization in MAP | Ahmad et al., 2014; Zuo et al. 2023 |
| Ash Content (%) |  | 5–20 | 1–10 | MAP typically generates lower ash because mineral migration is limited | Chen et al. 2023 |
| Surface Functional Groups |  | Moderate; decreases sharply at high T | Often higher abundance at equivalent T | MAP preserves OFGs due to rapid heat exposure | Chen et al. 2017 |
| Heating Rate (°C s⁻¹) |  | 5–50 | 50–500+ | Rapid MAP heating drives unique pore and carbon structures | Lei et al. 2023; Chaubey et al. 2024 |

Table S2. Comparative mechanistic matrix linking CP vs. MAP structural characteristics to adsorption mechanisms, thermodynamic signatures, kinetic behavior, and key findings.

| Structural Feature | CP Biochar Characteristics | MAP Biochar Characteristics | Effect on Adsorption Mechanisms | Thermodynamic Implications | Kinetic Implications | Key Findings / Conclusions | Supporting References |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Surface area & pore structure | Moderate SA; micropore-dominant; slower devolatilization | Higher SA; mesopore-rich due to rapid internal heating | MAP enhances pore filling, intraparticle diffusion, accessibility for bulky organics & emerging contaminants | Higher q_max; often endothermic due to increased surface accessibility | Faster intraparticle diffusion; pseudo-second-order best fit | MAP biochars provide faster sorption and higher capacities due to mesoporosity and improved accessibility | Tomczyk et al., 2020; Puteri et al. 2025 |
| Graphitization/aromaticity | Lower aromatic order | Higher graphitization, π-rich domains | Stronger π–π and hydrophobic interactions for aromatic organics | Spontaneous (ΔG < 0), endothermic for aromatic compounds | Enhanced film diffusion; rapid uptake | MAP graphitization significantly improves organic pollutant adsorption | Mohona et al. 2023 |
| Surface oxygen functional groups (OFGs) | Reduced at high CP temperature | Often higher OFGs due to controlled MAP heating | Enhanced H-bonding, electrostatic attraction, surface complexation | Exothermic chemisorption for metals; improved affinity | Faster initial sorption; chemisorption dominates (PSO kinetics) | MAP chars show stronger metal sorption due to abundant OFGs | Suliman et al. 2017; Ahmad et al., 2014 |
| Mineral/ash content | Higher ash (depending on feedstock) | Lower mineral residues | CP favors ion exchange, precipitation, and co-precipitation | Multi-step isotherms; increased heterogeneity | Slower overall kinetics; mineral-dependent reactions | CP biochars are more suitable for precipitation-driven metal immobilization | (Bedia et al. 2018 |
| Surface charge (pHₚzc) | Often lower; varies widely | Often higher due to lower ash and higher OFGs | MAP enhances anion adsorption; CP supports cation exchange | pH-sensitive ΔG; MAP improves anion affinity | Faster equilibrium for anions in MAP systems | MAP biochars outperform CP in removal of oxyanions (As(V), Cr(VI)) | Haider et al. 2022 |
| Chemical stability / recalcitrance | Moderate structural stability | Higher aromatic stability | Maintains active sites during reuse; improved catalytic performance | Higher entropy (ΔS) contributions | Improved regeneration kinetics | MAP chars exhibit superior regenerability and reusability | Priyanka et al. 2024; Portillo et al. 2024 |
| Surface defects / active sites | Fewer defect sites | Higher defect density due to rapid MAP heating | Improved redox reactions and catalysis | Higher ΔH in redox-mediated adsorptions | Faster electron transfer kinetics | MAP potentially superior for emerging contaminants requiring redox pathways | Bongosia et al. 2024; Zhang et al., 2024 |