Supplementary Material

Biochar-Regulated LDH-Derived Co-Mn Spinel for Non-Radical Peroxymonosulfate Activation: High-Efficiency Imidacloprid Degradation Dominated by High-Valent Metal−Oxo Species and Singlet Oxygen

Text Legends

Text S1 Reagents and materials

Text S2 Analytical method

Text S3 Electrochemical measurement

Text S4 Theoretical calculations based on DFT

Text S5 Toxicity assessment

Table Legends

Table S1 The HPLC methods and conditions for organic contaminants

Table S2 Pore structure parameters of BC, CoMn0.5/BC, CoMn0.75/BC, and CoMn1/BC

Table S3 The contents of functional groups and metal valence states in CoMn2O4 and CoMn0.75/BC fresh and used the reaction

Table S4 Comparison of removal of IMI by activated PS with different catalysts

Table S5 The proposed products of IMI degradation in the CoMn0.75/BC/PMS system

Figure Legends

Fig. S1 SEM images of BC

Fig. S2 SEM images of (a) CoMn0.5/BC and (b) CoMn1/BC

Fig. S3 XRD of CoMn-LDH and CoMn-LDH/BC

Fig. S4 BET of CoMnBC

Fig. S5 XPS C 1s spectra of (a) CoMn0.75/BC, (b) CoMn0.5/BC, (c) CoMn1/BC; (d) Analysis of the correlation between C=O groups and the conversion efficiency of PMSO to PMSO2

Fig. S6 Adsorption of IMI in various systems

Fig. S7 (a) Effects of catalyst dosage on the removal efficiency in the CoMn0.75/BC/PMS system; Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with different (b) catalyst dosage, (c) PMS concentration, and (d) pH

Fig. S8 Removal ability and Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with (a, b) Cl− and (c, d) SO42−

Fig. S9 Removal ability and Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with HCO3−

Fig. S10 Removal ability and Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with HA

Fig. S11 TOC removal in CoMn0.75/BC/PMS system

Fig. S12 Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with different NNIs and water matrices

Fig. S13. The UV-vis absorption spectrum of DPBF consumption (a) CoMn2O4 and (b) CoMn2O4/BC.

Fig. S14 CV curves of different catalysts

Fig. S15 CoMn0.75/BC XPS spectra (a) C 1s, (b) O 1s, (c) Mn 2p and (d) Co 2p fresh and used catalytic degradation

Fig. S16 The MS spectra of IMI degradation products in the CoMn0.75/BC/PMS system

Fig. S17 bioaccumulation of IMI and its intermediate degradation

Fig. S18 (a-d) TEM and HR-TEM of used CoMn0.75/BC; (e) The mapping spectrum of used CoMn0.75/BC

References

Text S1 Reagents and materials

(Co(NO3)2·6H2O), Mn(NO3)2·4H2O, dimethyl sulfoxide (DMSO), methyl phenyl sulfoxide (PMSO), methyl phenyl sulfone (PMSO2) and tert-butanol (TBA, C4H9OH) were purchased from Aladdin (Shanghai, China). Sodium hydroxide (NaOH) was purchased from Tianjin Cameo Chemical Reagent Co. Ltd. in China. L-histidine (L-his, C6H9N3O2), p-benzoquinone (p-BQ, C6H4O2), methanol (MeOH), peroxymonosulfate (PMS), dimethylpyridine nitrogen oxide (DMPO, C6H11NO), 2,2,6,6-tetramethylpiperidine (TEMP, C9H19ON), and potassium iodide (KI) were obtained from Maclean's (Shanghai, China). The five NNIs including Imidacloprid (IMI), Thiamethoxam (THM), Clothianidin (CLO), Dinotefuran (DIN), Nitenpyram (NIT) were procured from Alta Technology (Tianjin, China)

Text S2 Analytical method

The concentration in IMI solution was determined by HPLC system (Agilent 1260 Infinity). The mobile phase consisted of 50% Acetonitrile and 50% ultrapure water at a flow rate of 0.4 mL/min, and the injection volume of the solution to be measured was 20 μL. The temperature of the column chamber was maintained at 35 °C and the detection wavelength was 270 nm.

PMS concentration measurement: PMS concentration determination: based on Liu et al. (2024) research to improve. Firstly, a 0.5 mL liquid sample was added into a 10 mL mixed solution of KHCO3 and KI (1.25 g KHCO3 + 10 g KI dissolved in 250 mL deionized water). The subsequent solution was initially hand shaken and then analyzed by a UV-visible spectrometer (Evolution TM 201) at 352 nm.

The quantitative of 1O2

based on Chu et al. (2024) research to improve. Because the 1, 3-diphenylisobenzofuran (DPBF, 0.01 mM) can react with 1O2 in a molar ratio of 1: 1, it is employed to quantitatively reflect the production amount of 1O2. The DPBF concentrations were measured with a UV-vis at 411 nm (scanning range 300 to 500 nm).

The rate of degradation of IMI and the rate constant (kobs) were calculated by eqs. 1 and 2, respectively.

| ω=1-CtC0×100% | (1) |
| --- | --- |
| lnCtC0=-kobst | (2) |

where ω represents the degradation rate of IMI; Ct is the concentration of IMI in solution at t min (mg L−1); C0 is the initial concentration of IMI in solution (mg/L).

HPLC-MS operation: The degradation intermediates of IMI were detected by HPLC-MS (Waters XEVO G2-XS QToF). A BEH C18 column (50 mm × 2.1 mm i.d., 1.7 μm; Waters, Milford, USA) was used. The isocratic mobile phase was prepared by using 0.1% acetic acid and acetonitrile with the ratio of 50:50 (v/v) at a flow rate of 0.2 mL/min and a column temperature of 40 ℃. The injection volume was 10 μL, and the scan range was 50-1500 m/z.

DMPO/TEMP-EPR: Spin-trapping EPR signals were detected in different air-saturated methanol/aqueous dispersions of the corresponding samples at room temperature. Firstly, 1 mL catalyst methanol suspension (0.05 g/L) was added to 50 mL DMPO (100 mM) solution. After mixing, 5 mM PMS solution was added to above dispersion. The suspension shocked for 5 min and then drawn into a capillary for ·O2− detection. The 1O2 detection using the same procedure by replacing DMPO with TEMP.

Text S3 Electrochemical measurement

All electrochemical properties were measured in the electrochemical workstation (CHI 760E, CH Instruments, Inc.) using a normal three-electrode system with 50 mM Na2SO4 as electrolyte (Dong et al. 2025). A standard three-electrode electrochemical system was employed with Ag/AgCl (saturated KCl) as the reference electrode, platinum wire as the counter electrode, and a catalyst-modified glassy carbon (GC) electrode as the working electrode.

Preparation of the working electrode: A 50 mM Na2SO4 electrolyte was utilized. Initially, a homogeneous catalyst suspension was prepared through ultrasonication with catalyst powder, 0.1 mL of Nafion solution (5%, Sigma-Aldrich), and 1 mL of anhydrous ethanol. The resulting catalyst suspension was then deposited onto the surface of the GC electrode and air-dried at room temperature. This process was repeated twice to ensure uniformity. chronoamperometry (CA), linear sweep voltammetry (LSV), and cyclic voltammetry (CV) curves were acquired from the workstation.

Text S4 Theoretical calculations based on DFT

Theoretical Calculations: To analyze the adsorption energy, the density functional theory (DFT) calculations have been performed using the Vienna ab initio simulation package (VASP 6.1) and the visualization of VESTA software (Kresse and Furthmuller 1996). The electron exchange-correlation function was treated using a generalized gradient approximation (GGA) in the form proposed by Perdew, Burke, and Ernzerhof (PBE) (Perdew et al. 1996). The energy cutoff of the plane waves was set to 500 eV. All presented geometry optimizations are obtained until the maximum displacement below 0.005 Å, energy tolerance below 1×10−5 Ha, and the maximum forces lower than 0.01 eV Å−1. The lattice constants larger than 15 Å along the x- and y-directions and vacuum region of about 20 Å along the z-direction was adopted. The k-point grid of 3 × 3 × 1 was selected for geometry optimizations. The force convergence criterion in geometric optimization was set to 0.01 eV/Å. For the electron self-consistent field calculations, the convergence criterion was set to 1×10−5 Ha. The adsorption energy (Eads) between substrate and adsorbed molecule was defined by the following formula:

Eads=Etot–ECoMo2O4-BC–EPMS

Where Etot, ECoMo2O4-BC, and EPMS are the total energy of the CoMo2O4-BC and adsorbed PMS molecule, CoMo2O4-BC, and PMSmolecule, respectively. The isosurface values for the charge density difference is 0.005 eV Å−3. The green and yellow regions correspond to electron accumulation and depletion, respectively. The quantized charge transfer using Bader charge analysis.

Text S5 Toxicity assessment

The Toxicity Estimation Software Tool (T·E·S·T) was utilized to evaluate the comprehension toxicities of IMI and its reaction intermediates. Five essential parameters, Fathead minnow LC50 (96 h), daphnia magna LC50 (48 h), bioaccumulation factor, developmental toxicity and mutagenicity of IMI and the corresponding intermediates, were evaluated.

Table S1 The HPLC analysis conditions for different organic pollutants

| Compound | Detector wavelength | Mobile phase | Flow rate | Injection volume |
| --- | --- | --- | --- | --- |
| IMI | 270 nm | Acetonitrile:Water =50:50 (v : v) | 0.4 mL min−1 | 20 μL |
| THM | 270 nm | Acetonitrile:Water =50:50 (v : v) | 0.4 mL min−1 | 20 μL |
| CLO | 254 nm | Acetonitrile:Water =50:50 (v : v) | 0.4 mL min−1 | 20 μL |
| DIN | 254 nm | Acetonitrile:Water =70:30 (v : v) | 0.4 mL min−1 | 20 μL |
| NIT | 270 nm | Acetonitrile:Water =70:30 (v : v) | 0.4 mL min−1 | 20 μL |
| PMSO | 230 nm | Acetonitrile:Water =60:40 (v : v) | 1.0 mL min−1 | 20 μL |
| PMSO2 | 215 nm | Acetonitrile:Water =60:40 (v : v) | 1.0 mL min−1 | 20 μL |

Table S2 Pore structure parameters of BC, CoMn0.5/BC, CoMn0.75/BC, and CoMn1/BC

|  | SBET (m2 g−1) | Average pore size (nm) | Pore volume (cm3/g) |
| --- | --- | --- | --- |
| BC CoMn0.5/BC CoMn0.75/BC | 24.5 104.2 128.8 | 3.27 9.39 8.22 | 0.06 0.21 0.28 |
| CoMn1/BC | 91.6 | 7.10 | 0.13 |

Table S3 The contents of functional groups and metal valence states in CoMn2O4 and CoMn0.75/BC fresh and used the reaction

| Functional groups or metal valence states |  | CoMn2O4 | CoMn0.75/BC |  |
| --- | --- | --- | --- | --- |
|  |  |  | Fresh | Used |
| C 1s | C=O | / | 16.5% | 14.7% |
|  | C−O | / | 41.9% | 49.1% |
|  | C−C | / | 41.6% | 36.2% |
| O 1s | OA | 35.6% | 4.1% | 7.2% |
|  | OV | 11.3% | 22.3% | 19.8% |
|  | OL | 53.1% | 73.6% | 73.0% |
| Mn 2p | Mn4+ | / | 25.5% | 29.5% |
|  | Mn3+ | 55.5% | 26.7% | 44.1% |
|  | Mn2+ | 44.5% | 47.8% | 26.4% |
| Co 2p | Co3+ | 51.1% | 52.4% | 54.4% |
|  | Co2+ | 48.9% | 47.6% | 45.6% |

Table S4 Comparison of removal of NNIs by activated PS with different catalysts

(specific rate constant (Kvalue) = Kobs/(CPMS))

| Catalysts | NNIs concentration (mg L−1) | Catalyst dosage (g L−1) | PS dosage (mM) | Removal efficiency | Kobs (min-1) | Kvalue (min −1 M−1) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| FeS2-NP | 2.56 (IMI) | 0.15 | 1 mM/PDS | 80.3% (60 min) | 0.054 | 0.054 | (Liu et al. 2023) |
| CuFeS2 | 10 (IMI) | 0.9 | 0.6 mM/PDS | 45.5% (80 min) | 0.027 | 0.045 | (Chen et al. 2023) |
| AP0.5BWLDH0.3 | 50 (NIT) | 0.8 | 0.4 mM/PMS | 100% (90 min) | 0.075 | 0.188 | (Zheng et al. 2022a) |
| FeS/ZVI | 38.35 (IMI) | 0.1 | 2.5 mM/PDS | 99.8% (60 min) | 0.051 | 0.020 | (Du et al. 2021) |
| nAgFeO2 | 2.5 (IMI) | 0.001 | 1.2 mM/PMS | 44% (300 min) | 0.039 | 0.032 | (Kan et al. 2020) |
| CuO/BC | 30 (IMI) | 1 | 5 mM/PDS | 38% (300 min) | 0.045 | 0.009 | (Hayat et al. 2020) |
| FeS2 |  |  |  | 82.7% (300 min) | 0.032 | 0.064 |  |
| Fe@BC | 10 (IMI) | 0.67 | 5 mM/PDS | 90% (360 min) | 0.036 | 0.007 | (Wang et al. 2022) |
| Mn@BC |  |  |  | 38% (360 min) | 0.014 | 0.003 |  |
| FeMn-BC | 10 (THM) | 0.1 | 6 mM/PDS | 99.0% (90 min) | 0.064 | 0.010 | (Yang et al. 2023) |
| Fe@RTCOF-1Acb | 6.2 (THM) | 0.2 | 0.3 mM/PMS | 93.09% (40 min) | 0.0402 | 0.081 | (Hu et al. 2025) |
| nZVI | 2 (DIN) | 1 | 10 mM/PMS | 69% (15 min) | 0.07 | 0.007 | (Zou et al. 2022) |
| E/BASBC | 0.5 (CLO) | 0.1 | 1 mM/PMS | 82.6% (60 min) | 0.136 | 0.136 | (Ma et al. 2023) |
| MCN-PTFE | 1 (NIT) | 0.05 | 1 mM/PMS | 100% (30 min) | 0.199 | 0.199 | (Guo et al. 2023) |
| AACMO3.4 | 40 (NIT) | 0.8 | 2.4 mM/PMS | 100% (45 min) | 0.31 | 0.129 | (Zheng et al. 2022b) |
| CoMn0.75/BC | 5 (IMI) | 0.05 | 0.8 mM/PMS | 96.9% (40 min) | 0.209 | 0.261 | In this study |
|  | 5 (THM) |  |  | 98.7% (40 min) | 0.233 | 0.291 |  |
|  | 5 (CLO) |  |  | 98.3% (40 min) | 0.278 | 0.348 |  |
|  | 5 (DIN) |  |  | 83.5% (40 min) | 0.135 | 0.169 |  |
|  | 5 (NIT) |  |  | 81.9% (40 min) | 0.149 | 0.186 |  |

Table S5 The maximum leaching of Co in different catalyst systems

|  | Co (mg/L) | Refs. |
| --- | --- | --- |
| P-Fe-N-C/PMS Co-VOH/PMS KNbO3/ZIF-67(Co)/PMS Co2(V4O12)(bpy)2/PMS Co0.5Fe1.5/PMS 10%Co/CNH/PMS B5S5C8F2/PMS | 2.30 0.38 1.50 0.25 1.30 0.46 4.90 | (Yu et al. 2024) (Zhang et al. 2026) (Chen et al. 2025) (Lan et al. 2024) (Lin et al. 2025) (Mao et al. 2023) (Li et al. 2025) |
| CoMn0.75/BC | 0.16 | In this study |

Table S6 The proposed products of IMI degradation in the CoMn0.75/BC/PMS system

| Sample | Formula | Molecular | Mass-to-charge ratio |
| --- | --- | --- | --- |
| IMI | C9H10ClN5O2 |  | 256 |
| P1 | C9H13ClN4 |  | 213 |
| P2 | C9H12ClN3O |  | 214 |
| P3 | C9H11ClN3O2 |  | 230 |
| P4 | C9H10ClN3O2 |  | 228 |
| P5 | C9H11ClN4 |  | 211 |
| P6 | C6H5ClN2O |  | 157 |
| P7 | C6H4ClNO2 |  | 158 |
| P8 | C5H4ClNO |  | 129 |
| P9 | C9H8ClN5O2 |  | 254 |
| P10 | C7H8ClN5O2 |  | 231 |
| P11 | C5H4ClN |  | 114 |

Fig. S1 SEM images of BC

Fig. S2 SEM images of (a) CoMn0.5/BC and (b) CoMn1/BC

Fig. S3 XRD of CoMn-LDH and CoMn-LDH/BC

X-Ray Diffraction (XRD) analysis confirmed the successful synthesis of the CoMn-LDH/BC precursor, as evidenced by the characteristic diffraction peaks of LDH located at 11.6° (003), 23.4° (006), 31.3° (009), 34.2° (012), 38.7° (015), 45.3° (018), 59.6° (110), and 60.4° (113). The (003) diffraction peak corresponds to an interlayer spacing of approximately 0.71 nm, which is consistent with the intercalation of CO32− anions during LDH synthesis. After calcination, the characteristic peaks of LDH completely disappeared, and new diffraction peaks emerged at 18.5° (101), 28.9° (112), 34.1° (103), and 36.3° (211). These peaks match the standard pattern for CoMn2O4 spinel (PDF#77-0471), confirming that the CoMn-LDH underwent a topological transformation via thermal decomposition, whereby the layered structure collapsed and reorganized into a spinel lattice.

Fig. S4 BET of CoMnBC

Preparation of CoMnBC

Specifically, an aqueous ammonia solution (NH3·H2O) was added as an effective precipitant to a deionized water dispersion containing manganese nitrate tetrahydrate (Mn(NO3)2·4H2O, 2 mmol), followed by magnetic stirring for 1 h to facilitate the growth of the metal framework. After complete precipitation, an ethanol-deionized water solution of cobalt nitrate hexahydrate (Co(NO3)2·6H2O, 1 mmol) was added to induce coordination precipitation. The resulting precursor was subsequently annealed at 500 °C for 2 h under a nitrogen atmosphere to obtain the CoMn2O4 spinel. This material was then milled with 0.3 g BC for 20 min and designated as CoMnBC.

Fig. S5 XPS C 1s spectra of (a) CoMn0.75/BC, (b) CoMn0.5/BC, (c) CoMn1/BC; (d) Analysis of the correlation between C=O groups and the conversion efficiency of PMSO to PMSO2.

Fig. S6 Adsorption of IMI in various systems

Fig. S7 (a) Effects of catalyst dosage on the removal efficiency in the CoMn0.75/BC/PMS system; Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with different (b) catalyst dosage, (c) PMS concentration and (d) pH

Fig. S8 Removal ability and Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with (a, b) Cl− and (c, d) SO42−

Fig. S9 Removal ability and Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with HCO3−

Fig. S10 Removal ability and Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with HA

Fig S11 TOC removal in CoMn0.75/BC/PMS system.

Fig. S12 Kobs of IMI degradation efficiency in CoMn0.75/BC/PMS system with different NNIs

Fig. S13 The UV-vis absorption spectrum of DPBF consumption (a) CoMn2O4 and (b) CoMn0.75/BC.

Fig. S14 CV curves of different catalysts

Fig. S15 CoMn0.75/BC XPS spectra (a) C 1s, (b) O 1s, (c) Mn 2p and (d) Co 2p fresh and used catalytic degradation

Fig. S16 The MS spectra of IMI degradation products in the CoMn0.75/BC/PMS system

Fig. S17 bioaccumulation of IMI and its intermediate degradation

Fig. S18 (a-d) TEM and HR-TEM of used CoMn0.75/BC; (e) The mapping spectrum of used CoMn0.75/BC

References

Chen X, Zhang WX, Chen ZL, Yao XW, Chen ML, Tong LY, Qian W, Guo PR, Kong LJ, Diao ZH (2023) Efficient activation of persulfate by metallic sulfide mineral for the efficient removal of pesticides: Performance, radical generation and mechanism. J Clean Prod 421:138521. https://doi.org/10.1016/j.jclepro.2023.138521

Chen ZY, Zhao C, Ma RX, Yao ZN, Guo ZH, Zhao ZX, Zheng YF, Fu HF (2025) Interface and Polarization Engineering of ZIF-67(Co)-Based Heterojunctions for Selective Non-Radical PMS Activation: Simultaneous Generation of 1O2 and Co(IV)=O for Efficient and Safe Water Remediation. Adv Funct Mater: e16474. https://doi.org/10.1002/adfm.202516474

Chu Z, Han Z, Liu H, Chen T, Zou X, Wang H, Sun F, Wang H, Chen D (2024) Autocatalytic degradation of Cu-EDTA in the Calcite/PMS system: Singlet oxygen and Cu (III). J Hazard Mater 477: 135286. https://doi.org/10.1016/j.jhazmat.2024.135286

Dong X, Fu, Q, Liu G, Fan X, Zhang F, Li YF, Cui S (2025) Imidacloprid degradation activated by peroxydisulfate with NiCoAl layered metal oxide catalysts: The unique role of Al. Sep Purif Technol 356:129845. https://doi.org/10.1016/j.seppur.2024.129845

Du M, Kuang H, Zhang Y, Zeng X, Yi C, Hussain I, Huang S, Zhao S (2021) Enhancement of ball-milling on pyrite/zero-valent iron for persulfate activation on imidacloprid removal in aqueous solution: A mechanistic study. J Environ Chem Eng 9(4):105647. https://doi.org/10.1016/j.jece.2021.105647

Guo R, Guo C, Zhang H, Xi B, Lv N, Xu J (2023) Enhanced nitenpyram degradation by metallic carbon nitrogen composites catalyzed peroxymonosulfate: Synergistic effect of radical and nonradical pathways. Chem Eng J 476:146483. https://doi.org/10.1016/j.cej.2023.146483

Hayat W, Zhang Y, Hussain I, Huang S, Du X (2020) Comparison of radical and non-radical activated persulfate systems for the degradation of imidacloprid in water. Ecotoxicol Environ Saf 188:109891. https://doi.org/10.1016/j.ecoenv.2019.109891

Hu X, Yi Z, Zhou Y, Xiao X, Zhou Y, Qin P, Luo L, Liang Y, Yang Y, Gong X, Wu Z (2025) Metal single-atom coordination to manipulate photogenerated electron transfer pathway of imine-based COFs for highly efficient persulfate activation on thiamethoxam degradation. Chem Eng J 512:162623. https://doi.org/10.1016/j.cej.2025.162623

Kan Q, Lu K, Dong S, Shen D, Huang Q, Tong Y, Wu W, Gao S, Mao L (2020) Transformation and removal of imidacloprid mediated by silver ferrite nanoparticle facilitated peroxymonosulfate activation in water: Reaction rates, products, and pathways. Environ Pollut 267:115438. https://doi.org/10.1016/j.envpol.2020.115438

Kresse G, Furthmuller J (1996) Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set. Phys Rev B 54(16):11169. https://doi.org/10.1103/PhysRevB.54.11169

Lan MY, Li YH, Wang CC, Li XJ, Cao JZ, Meng LH, Gao S, Ma YH, Ji HD, Xing MY (2024) Multi-channel electron transfer induced by polyvanadate in metal-organic framework for boosted peroxymonosulfate activation. Nat Commun 15(1): 7208. https://doi.org/10.1038/s41467-024-51525-0

Li ZY, Zhang XY, Xue M, Wei MZ, Chen SW, Lu QF, Guo EY, Han XJ, Si CH (2025) Enhanced peroxymonosulfate activation in organic degradation by modulating cationic doping of BaxSr1-xCoyFe1-yO3-δ perovskites: DFT calculations and mechanism study. Appl Catal B Environ 377 125502. https://doi.org/10.1016/j.apcatb.2025.125502

Lin XL, Zhao YJ, Zhang L, Li YY, Zhai SR, Shan S, Guo H, Li XQ (2025) Mechanistic elucidation and catalyst design of Fe-doped ZnCo2O4 spinels for oxygen vacancy-mediated PMS activation. Chem Eng J 522 167740. https://doi.org/10.1016/j.cej.2025.167740

Liu SS, Fu H, Wang F, Wei Y, Meng B, Wang P, Zhao C, Liu W, Wang CC (2024) Insight into the extremely different catalytic behaviors of asymmetric and symmetric oxygen vacancies for peroxymonosulfate activation. Appl Catal B Environ 346:123753. https://doi.org/10.1016/j.apcatb.2024.123753

Liu Z, An Y, Li X (2023) Insight into mechanism of peroxydisulfate activation by natural pyrite: Participation of Fe(IV) and regulation of Fe(III)/Fe(II) cycle by sulfur species. Chemosphere 314:137657. https://doi.org/10.1016/j.chemosphere.2022.137657

Ma Y, Tang J, Chen S, Yang L, Shen S, Chen X, Zhang Z (2023) Ball milling and acetic acid co-modified sludge biochar enhanced by electrochemistry to activate peroxymonosulfate for sustainable degradation of environmental concentration neonicotinoids. J Hazard Mater 444:130336. https://doi.org/10.1016/j.jhazmat.2022.130336

Mao S, Zhao P, Wu Y, Liu C, Xia MZ, Wang FY (2023) Promoting charge migration of Co(OH)2/g-C3N4 by hydroxylation for improved PMS activation: Catalyst design, DFT calculation and mechanism analysis. Chem Eng J 451 138503. https://doi.org/10.1016/j.cej.2022.138503

Perdew, Burke and Ernzerhof (1996) Generalized Gradient Approximation Made Simple. Phys Rev Lett 77:3865. https://doi.org/10.1103/PhysRevLett.77.3865

Wang X, Zhang P, Wang C, Jia H, Shang X, Tang J, Sun H (2022) Metal-rich hyperaccumulator-derived biochar as an efficient persulfate activator: Role of intrinsic metals (Fe, Mn and Zn) in regulating characteristics, performance and reaction mechanisms. J Hazard Mater 424:127225. https://doi.org/10.1016/j.jhazmat.2021.127225

Yang X, Guo Z, Chen X, Xi S, Cui K, Li J, Dong D, Wu F, Wu Z (2023) Efficient degradation of thiamethoxam pesticide in water by iron and manganese oxide composite biochar activated persulfate. Chem Eng J 473:145051. https://doi.org/10.1016/j.cej.2023.145051

Yu FK, Xiao YR, Tao L (2024) The activation of PMS for PFOA degradation by adjustable metal stripping Fe/Co/N@BC catalysts: Degradation performance with single-line oxygen and high-valent metal oxides as the main active substances. Sep Purif Technol 351 127589. https://doi.org/10.1016/j.seppur.2024.127589

Zhang WF, Chen BC, Zhang XZ, Huang LY, Chen XD, Li HY, Wang CL, Pan FP, Li XH (2026) Engineering a Co-O-V tripod electron bridge to promote non-radical PMS activation via high-valent Co(IV)=O. J Hazard Mater 501 140768. https://doi.org/10.1016/j.jhazmat.2025.140768

Zheng J, Deng Y, Fan C, Li X, Gong D, Li C, Ye Z (2022a) Novel Zn-Al LDHs based S-scheme heterojunction with coral reef-like structure for photocatalytic activation of peroxymonosulfate towards nitenpyram decomposition. J Environ Chem Eng 10(4):108188. https://doi.org/10.1016/j.jece.2022.108188

Zheng J, Tang X, Fan C, Deng Y, Li X, Yang Q, Wang D, Duan A, Luo J, Chen Z, Zhang B (2022b) Facile synthesis of Ag@AgCl/ZnAl-LDH sesame balls nanocomposites with enhanced photocatalytic performance for the degradation of neonicotinoid pesticides. Chem Eng J 446:136485. https://doi.org/10.1016/j.cej.2022.136485

Zou Z, Zhao E, Yu P, Jing J, Li Y, Li B, Wu J (2022) Simultaneous remediation of three neonicotinoids in soil using nanoscale zero-valent iron-activated persulfate process: Performance, effect of process parameters, and mechanisms. Process Saf Environ 167:308-321. https://doi.org/10.1016/j.psep.2022.09.005