Candle Soot-Enhanced Pyroelectric Generator for 
Thermal Energy Harvesting and Self-Powered Sensing

1Premkumar Bhosale, 1*Sugato Hajra, 2Krystian Mistewicz, 1Mohamed Belal, 1Kushal Ruthvik Kaja, 3Basanta Kumar Panigrahi, 4Naratip Vittayakorn, 1*Hoe Joon Kim

1Department of Robotics and Mechatronics Engineering, Daegu Gyeongbuk Institute of Science and Technology, Daegu 42988, South Korea

2Institute of Physics – Centre for Science and Education, Silesian University of Technology, Krasińskiego 8, 40-019 Katowice, Poland

3Department of Electrical Engineering, Siksha O Anusandhan deemed to be University, Orissa, 751030, India

4Department of Chemistry, School of Science, King Mongkut's Institute of Technology, Ladkrabang, Bangkok, 10520, Thailand

*Corresponding Authors: Sugato Hajra (sugatohajra@dgist.ac.kr) and Hoe Joon Kim (joonkim@dgist.ac.kr)

Figure S1: The cycling temperature changes (a) and corresponding pyroelectric current response (b) of the bare PZT sample.

Figure S2: The cycling temperature changes (a) and corresponding pyroelectric current response (b) of the PZT sample coated with candle soot.

Table T1: A comparison of the pyroelectric coefficient determined for examined samples with literature data reported for PZT. The values in the round brackets represent the measurement uncertainties.

| Sample | Sample dimensions | p, µC/(m2K) | Reference |
| --- | --- | --- | --- |
| PZT-5H slice | 14 mm diameter, 2 mm thickness | 416 | [1] |
| thick PZT film | - | 352 | [2] |
| PZT epitaxial film | 150 nm thickness | 200 | [3] |
| sol-gel derived PZT thin film | - | 250 | [4] |
| PZT porous layer | 20 μm thickness | 120 | [5] |
| PZT ceramic | - | 380 | [5] |
| PZT dense thick film | - | 200 | [5] |
| hot-pressed PZT ceramic | 22 mm × 22 mm, 30-80 μm thickness | 450 | [6] |
| Sr-doped PZT | - | 625 | [7] |
| sol-gel derived PZT 53/47 film | - | 770 | [8] |
| Bare PZT disk | 25 mm diameter | 447(79) | This work |
| PZT disk coated with candle soot | 25 mm diameter | 436(51) |  |

References

1. E. Tang, Y. Wang, R. Wang, Y. Han, M. Chang, C. Chen, K. Guo, and L. He, Electrical output performance of PZT-5H under the superposition of temperature, temperature change rate and pulse stress, Mater. Chem. Phys. 307, 128109 (2023).

2. M. Es-Souni, M. Kuhnke, A. Piorra, and C. H. Solterbeck, Pyroelectric and piezoelectric properties of thick PZT films produced by a new sol-gel route, J. Eur. Ceram. Soc. 25, 2499-2503 (2005).

3. B. Bhatia, J. Karthik, T. Tong, D. G. Cahill, L. W. Martin, and W. P. King, Pyroelectric current measurements on PbZr0.2Ti0.8O3 epitaxial layers, J. Appl. Phys. 22, 431-438 (2006).

4. G. Teowee, F. S. McCarthy, K. C. McCarthy, B. H. Dietz, and D. R. Uhlmann, Pyroelectric properties of sol-gel derived PZT thin films with various Zr/Ti ratios, Integrated Ferroelectrics 22, 431 (1998).

5. G. De Cicco, B. Morten, D. Dalmonego, and M. Prudenziati, Pyroelectricity of PZT-Based Thick-Films, Sens. Actuators A: Phys. 76, 409-415 (1999).

6. Y. Guo, S. Guo, C. Yao, Z. Pan, and G. Wang, A Large Voltage Responsivity Pyroelectric Sensor Based on Hot-Pressed Lead Zirconate Titanate Ceramic, Sensors 25, 2025 (2025).

7. M. A. Aleem, H. Nawaz, M. Shuaib, S. Qaisar, and M. S. Akbar, Piezoelectric and Pyroelectric Properties of Sr-Doped PZT (PSZT) with Minor Manganese Additions, J. Phys.: Conf. Ser. 439, 012021 (2013).

8. K. C. McCarthy, F. S. McCarthy, G. Teowee, T. J. Bukowski, T. P. Alexander, and D. R. Uhlmann, Pyroelectric properties of various sol-gel derived PLZT thin films, Integrated Ferroelectrics. 17, 377-385 (2006).