Table S1. The full list of 3DCP database for ML modeling

| No. | Cement kg/m3 | Water kg/m3 | Fine Agg kg/m3 | Fly Ash kg/m3 | Silica Fume kg/m3 | SP kg/m3 | Slag kg/m3 | Admixture kg/m3 | Fibers kg/m3 | P-S mm/s | CS MPa | CF tCo2/m3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 579 | 261 | 1167 | 165 | 83 | 5.75 | 0 | 0 | 0 | 60 | 70 | 1682.15 |
| 2 | 430 | 180 | 1240 | 170 | 180 | 10 | 0 | 0 | 0 | 75 | 73.4 | 1256.35 |
| 3 | 290 | 285 | 1211 | 278 | 145 | 0 | 0 | 7 | 0 | 150 | 52 | 868.60 |
| 4 | 289 | 284 | 1209 | 277 | 145 | 0 | 0 | 9 | 13.5 | 150 | 51 | 901.62 |
| 5 | 682.75 | 236.25 | 850 | 0 | 0 | 1.76 | 0 | 0 | 0 |  | 88 | 1971.72 |
| 6 | 675 | 236.25 | 800 | 0 | 0 | 1.76 | 0 | 0 | 0 |  | 79 | 1948.89 |
| 7 | 828 | 248 | 1242 | 0 | 0 | 17 | 0 | 2 | 0 | 0.25 | 13 | 2402.43 |
| 8 | 497 | 248 | 1242 | 331 | 0 | 17 | 0 | 2 | 0 | 0.25 | 33 | 1458.77 |
| 9 | 497 | 248 | 1242 | 331 | 0 | 17 | 0 | 2 | 0 | 0.25 | 40 | 1458.77 |
| 10 | 497 | 248 | 1242 | 331 | 0 | 17 | 0 | 2 | 0 | 0.25 | 47 | 1458.77 |
| 11 | 483 | 182 | 1074 | 0 | 268 | 10.7 | 322 | 6.44 | 0 | 130 | 90 | 1426.81 |
| 12 | 483 | 182 | 1074 | 0 | 268 | 10.7 | 322 | 6.44 | 19.6 | 130 | 110 | 1472.61 |
| 13 | 483 | 182 | 1074 | 0 | 268 | 10.7 | 322 | 6.44 | 39.3 | 130 | 110 | 1518.65 |
| 14 | 483 | 182 | 1074 | 0 | 268 | 10.7 | 322 | 6.44 | 58.9 | 130 | 109 | 1564.46 |
| 15 | 483 | 182 | 1074 | 0 | 268 | 10.7 | 322 | 6.44 | 78.5 | 130 | 96 | 1610.26 |
| 16 | 376 | 150 | 1612 | 107 | 54 | 0 | 0 | 0 | 0 |  | 100 | 1100.98 |
| 17 | 446 | 178 | 1485 | 127 | 64 | 0 | 0 | 0 | 0 |  | 100 | 1301.08 |
| 18 | 513 | 205 | 1362 | 147 | 73 | 0 | 0 | 0 | 0 |  | 100 | 1492.62 |
| 19 | 579 | 232 | 1241 | 165 | 83 | 8.27 | 0 | 4.135 | 1.2 |  | 100 | 1695.63 |
| 20 | 643 | 257 | 1123 | 184 | 92 | 0 | 0 | 0 | 0 |  | 100 | 1864.20 |
| 21 | 600 | 259 | 1379 | 0 | 0 | 0 | 0 | 0.96 | 0 | 60 | 44.7 | 1741.61 |
| 22 | 540 | 259 | 1357 | 0 | 60 | 0 | 0 | 0.96 | 0 | 60 | 49.9 | 1569.04 |
| 23 | 600 | 259 | 1379 | 0 | 0 | 0 | 0 | 0.96 | 1.8 | 60 | 45.1 | 1745.82 |
| 24 | 600 | 259 | 1379 | 0 | 0 | 0 | 0 | 0.96 | 0 | 60 | 45.9 | 1741.61 |
| 25 | 573.6 | 262.2 | 1229.1 | 164 | 81.9 | 1.39 | 0 | 0 | 1.8 | 44 | 70.9 | 1670.22 |
| 26 | 663 | 265.2 | 1243 | 165.7 | 0 | 1.49 | 0 | 0.82 | 1.8 | 44 | 67.4 | 1929.02 |
| 27 | 546 | 219 | 1171 | 156 | 78 | 0 | 0 | 8.2 | 0 | 50 | 80 | 1603.47 |
| 28 | 812 | 324.8 | 1218 | 0 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 75 | 2354.41 |
| 29 | 771.4 | 324.8 | 1218 | 40.6 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 73 | 2238.66 |
| 30 | 751.1 | 324.8 | 1218 | 60.9 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 72 | 2180.79 |
| 31 | 730.8 | 324.8 | 1218 | 8.2 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 64 | 2121.32 |
| 32 | 690.2 | 324.8 | 1218 | 121.8 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 50 | 2007.17 |
| 33 | 771.4 | 324.8 | 1218 | 40.6 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 69 | 2238.66 |
| 34 | 751.8 | 324.8 | 1218 | 60.9 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 68 | 2182.80 |
| 35 | 730.8 | 324.8 | 1218 | 81.2 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 63 | 2122.91 |
| 36 | 690.2 | 324.8 | 1218 | 121.8 | 0 | 16.24 | 0 | 0 | 0 | 0.0833 | 59 | 2007.17 |
| 37 | 574 | 262 | 1230 | 164 | 82 | 1.35 | 0 | 0 | 1.8 | 44 | 62 | 1671.37 |
| 38 | 663 | 265 | 1243 | 166 | 0 | 1.41 | 0 | 0.83 | 1.8 | 44 | 58 | 1929.03 |
| 39 | 1000 | 360 | 0 | 0 | 0 | 10.4 | 0 | 12 | 0 | 40.74 | 100 | 2902.46 |
| 40 | 1000 | 300 | 500 | 0 | 0 | 10.4 | 0 | 12 | 0 | 40.74 | 101 | 2908.13 |
| 41 | 500 | 150 | 500 | 0 | 0 | 5.2 | 0 | 8 | 0 | 40.74 | 102 | 1461.31 |
| 42 | 750 | 292.5 | 750 | 0 | 0 | 5.5 | 0 | 8 | 0 | 40.74 | 103 | 2182.51 |
| 43 | 750 | 250 | 750 | 0 | 0 | 5 | 0 | 9 | 0 | 40.74 | 104 | 2184.54 |
| 44 | 1500 | 550 | 1500 | 0 | 0 | 11 | 0 | 18 | 0 | 40.74 | 105 | 4369.39 |
| 45 | 1000 | 361.6 | 1000 | 0 | 0 | 6.67 | 0 | 12 | 0 | 40.74 | 106 | 2912.73 |
| 46 | 1000 | 343 | 1000 | 0 | 0 | 6.67 | 0 | 12 | 0 | 40.74 | 107 | 2912.72 |
| 47 | 1000 | 350 | 1000 | 0 | 0 | 6.5 | 0 | 12 | 0 | 40.74 | 108 | 2912.67 |
| 48 | 1000 | 375 | 1250 | 0 | 0 | 5 | 0 | 14 | 0 | 40.74 | 109 | 2919.48 |
| 49 | 750 | 300 | 1000 | 0 | 0 | 5 | 0 | 9 | 0 | 40.74 | 110 | 2187.41 |
| 50 | 750 | 250 | 1000 | 0 | 0 | 5 | 0 | 9 | 0 | 40.74 | 110 | 2187.38 |
| 51 | 625 | 218.8 | 937.5 | 0 | 0 | 0 | 0 | 0 | 0 | 20 | 60 | 1806.28 |
| 52 | 625 | 218.8 | 937.5 | 0 | 0 | 0 | 0 | 0 | 0 | 20 | 61 | 1806.28 |
| 53 | 625 | 218.8 | 937.5 | 0 | 0 | 0 | 0 | 0 | 0 | 20 | 58 | 1806.28 |
| 54 | 625 | 218.8 | 937.5 | 0 | 0 | 0 | 0 | 0 | 0 | 20 | 48 | 1806.28 |
| 55 | 625 | 218.8 | 937.5 | 0 | 0 | 0 | 0 | 0 | 0 | 20 | 47 | 1806.28 |
| 56 | 625 | 218.8 | 937.5 | 0 | 0 | 0 | 0 | 0 | 0 | 20 | 46 | 1806.28 |
| 57 | 625 | 218.8 | 937.5 | 0 | 0 | 6.3 | 0 | 0 | 0 | 20 | 46 | 1808.17 |
| 58 | 625 | 218.8 | 937.5 | 0 | 0 | 12.5 | 0 | 0 | 0 | 20 | 46 | 1810.03 |
| 59 | 625 | 218.8 | 937.5 | 0 | 0 | 18.8 | 0 | 0 | 0 | 20 | 48 | 1811.92 |
| 60 | 562.5 | 218.8 | 937.5 | 62.5 | 0 | 0 | 0 | 0 | 0 | 20 | 49 | 1628.09 |
| 61 | 562.5 | 218.8 | 937.5 | 62.5 | 0 | 0 | 0 | 0 | 0 | 20 | 50 | 1628.09 |
| 62 | 437.5 | 218.8 | 937.5 | 187.5 | 0 | 0 | 0 | 0 | 0 | 20 | 50 | 1271.73 |
| 63 | 437.5 | 218.8 | 937.5 | 187.5 | 0 | 6.3 | 0 | 0 | 0 | 20 | 51 | 1273.62 |
| 64 | 437.5 | 218.8 | 937.5 | 187.5 | 0 | 12.5 | 0 | 0 | 0 | 20 | 50 | 1275.48 |
| 65 | 437.5 | 218.8 | 937.5 | 187.5 | 0 | 18.8 | 0 | 0 | 0 | 20 | 52 | 1277.37 |
| 66 | 437.5 | 218.8 | 937.5 | 125 | 62.5 | 6.3 | 0 | 0 | 0 | 20 | 62 | 1272.29 |
| 67 | 437.5 | 218.8 | 937.5 | 125 | 62.5 | 12.5 | 0 | 0 | 0 | 20 | 62 | 1274.15 |
| 68 | 437.5 | 218.8 | 937.5 | 125 | 62.5 | 18.8 | 0 | 0 | 0 | 20 | 63 | 1276.04 |
| 69 | 437.5 | 234.4 | 937.5 | 125 | 62.5 | 12.5 | 0 | 0 | 0 | 20 | 64 | 1274.16 |
| 70 | 437.5 | 250 | 937.5 | 125 | 62.5 | 12.5 | 0 | 0 | 0 | 20 | 55 | 1274.17 |
| 71 | 700 | 160 | 1000 | 0 | 300 | 10 | 0 | 3 | 43.5 | 30 | 48 | 2133.88 |
| 72 | 579 | 232 | 1241 | 165 | 83 | 8.27 | 0 | 0 | 1.2 | 200 | 82 | 1686.54 |
| 73 | 579 | 232 | 1005.57 | 165 | 83 | 8.27 | 0 | 0 | 1.2 | 200 | 72 | 1683.86 |
| 74 | 579 | 232 | 770.15 | 165 | 83 | 8.27 | 0 | 0 | 1.2 | 200 | 53 | 1681.18 |
| 75 | 579 | 232 | 534.72 | 165 | 83 | 8.27 | 0 | 0 | 1.2 | 200 | 47 | 1678.50 |
| 76 | 579 | 232 | 299.29 | 165 | 83 | 8.27 | 0 | 0 | 1.2 | 200 | 47 | 1675.82 |
| 77 | 579 | 232 | 63.86 | 165 | 83 | 8.27 | 0 | 0 | 1.2 | 200 | 42 | 1673.14 |
| 78 | 628.6 | 235.7 | 1115.6 | 78.6 | 78.6 | 2 | 0 | 6.4 | 0 | 30 | 38.5 | 1835.09 |
| 79 | 430 | 280 | 400 | 570 | 0 | 1.2 | 0 | 1 | 2 | 100 | 47 | 1259.69 |
| 80 | 430 | 280 | 400 | 570 | 0 | 1.2 | 0 | 1 | 2 | 100 | 47 | 1259.69 |
| 81 | 430 | 280 | 400 | 570 | 0 | 1.2 | 0 | 1 | 1.5 | 100 | 51 | 1258.52 |
| 82 | 430 | 280 | 400 | 570 | 0 | 1.2 | 0 | 1 | 1 | 100 | 49 | 1257.35 |
| 83 | 675 | 246 | 1350 | 0 | 0 | 0 | 0 | 1.0125 | 0 | 70 | 62 | 1956.85 |
| 84 | 580 | 232 | 1146 | 166 | 83 | 0 | 0 | 8.29 | 0 | 75 | 66 | 1689.20 |
| 85 | 325 | 123.5 | 675 | 0 | 0 | 9.75 | 0 | 1.625 | 0 | 25 | 35 | 947.90 |
| 86 | 325 | 126.75 | 675 | 0 | 0 | 9.75 | 0 | 1.625 | 0 | 25 | 35 | 947.90 |
| 87 | 325 | 130 | 675 | 0 | 0 | 9.75 | 0 | 1.625 | 0 | 25 | 35 | 947.90 |
| 88 | 325 | 136.5 | 675 | 0 | 0 | 9.75 | 0 | 1.625 | 0 | 25 | 35 | 947.91 |
| 89 | 325 | 142.025 | 675 | 0 | 0 | 9.75 | 0 | 1.625 | 0 | 25 | 35 | 947.91 |
| 90 | 325 | 149.5 | 675 | 0 | 0 | 9.75 | 0 | 1.625 | 0 | 25 | 35 | 947.91 |
| 91 | 325 | 126.75 | 675 | 0 | 0 | 9.75 | 0 | 3.25 | 0 | 25 | 35 | 951.47 |
| 92 | 325 | 130 | 675 | 0 | 0 | 9.75 | 0 | 3.25 | 0 | 25 | 35 | 951.47 |
| 93 | 325 | 133.25 | 675 | 0 | 0 | 9.75 | 0 | 3.25 | 0 | 25 | 35 | 951.48 |
| 94 | 325 | 136.5 | 675 | 0 | 0 | 9.75 | 0 | 3.25 | 0 | 25 | 35 | 951.48 |
| 95 | 325 | 142.025 | 675 | 0 | 0 | 9.75 | 0 | 3.25 | 0 | 25 | 35 | 951.48 |
| 96 | 325 | 149.5 | 675 | 0 | 0 | 9.75 | 0 | 3.25 | 0 | 25 | 35 | 951.48 |
| 97 | 325 | 126.75 | 675 | 0 | 0 | 9.75 | 0 | 4.875 | 0 | 25 | 35 | 955.04 |
| 98 | 325 | 130 | 675 | 0 | 0 | 9.75 | 0 | 4.875 | 0 | 25 | 35 | 955.05 |
| 99 | 325 | 133.25 | 675 | 0 | 0 | 9.75 | 0 | 4.875 | 0 | 25 | 35 | 955.05 |
| 100 | 325 | 136.5 | 675 | 0 | 0 | 9.75 | 0 | 4.875 | 0 | 25 | 35 | 955.05 |
| 101 | 325 | 142.025 | 675 | 0 | 0 | 9.75 | 0 | 4.875 | 0 | 25 | 35 | 955.05 |
| 102 | 325 | 149.5 | 675 | 0 | 0 | 9.75 | 0 | 4.875 | 0 | 25 | 35 | 955.05 |
| 103 | 400 | 373.996 | 669.972 | 0 | 0 | 2 | 0 | 0.2 | 0 | 50 | 60.1 | 1157.96 |
| 104 | 323.456 | 303.24 | 817.304 | 0 | 0 | 2 | 0 | 0.2 | 0 | 50 | 63.1 | 939.71 |
| 105 | 301.796 | 225.264 | 970.368 | 0 | 0 | 2 | 0 | 0.2 | 0 | 50 | 67.6 | 879.19 |
| 106 | 1000 | 460 | 1500 | 0 | 0 | 0 | 0 | 25 | 0 | 50 | 43.5 | 2945.04 |
| 107 | 627 | 263.34 | 1391 | 0 | 0 | 4.7025 | 0 | 0 | 0 | 75 | 78 | 1818.62 |
| 108 | 391 | 343.14 | 1260 | 213 | 213 | 16.34 | 0 | 0 | 0 | 75 | 102.7 | 1147.48 |
| 109 | 1000 | 300 | 500 | 1000 | 100 | 1.3 | 0 | 0 | 0 | 66.67 | 42 | 2900.96 |
| 110 | 1000 | 300 | 500 | 1000 | 100 | 1.3 | 0 | 0 | 0 | 66.67 | 49.7 | 2900.96 |
| 111 | 1000 | 300 | 500 | 1000 | 100 | 1.3 | 0 | 0 | 0 | 66.67 | 50.5 | 2900.96 |
| 112 | 1000 | 300 | 500 | 1000 | 100 | 1.3 | 0 | 0 | 0 | 66.67 | 60 | 2900.96 |
| 113 | 376.3 | 263.4 | 1279.3 | 0 | 0 | 5.27 | 376.3 | 0.75 | 0 | 100 | 58 | 1109.92 |
| 114 | 374.2 | 261.9 | 1272.3 | 0 | 0 | 5.24 | 374.2 | 0.75 | 0 | 100 | 54 | 1103.74 |
| 115 | 370.8 | 259.6 | 1260.9 | 0 | 0 | 5.19 | 370.8 | 0.74 | 0 | 100 | 52 | 1093.71 |
| 116 | 614.47 | 245.788 | 850 | 0 | 68.28 | 0 | 0 | 0 | 0 |  | 77.4 | 1775.09 |
| 117 | 614.47 | 245.788 | 850 | 0 | 68.28 | 0 | 0 | 0 | 0 |  | 72.5 | 1775.09 |
| 118 | 614.47 | 245.788 | 850 | 0 | 68.28 | 0 | 0 | 0 | 0 |  | 71.9 | 1775.09 |
| 119 | 614.47 | 245.788 | 850 | 0 | 68.28 | 0 | 0 | 0 | 0 |  | 56.5 | 1775.09 |
| 120 | 350 | 179 | 1489 | 140 | 105 | 5 | 0 | 0 | 0 | 150 | 57.7 | 1027.15 |
| 121 | 1000 | 360 | 1500 | 0 | 0 | 0 | 0 | 0 | 0 | 12 | 43.5 | 2890.05 |
| 122 | 800 | 310 | 1000 | 100 | 100 | 8 | 0 | 2 | 0 | 30 | 59 | 2318.82 |
| 123 | 700 | 460 | 1200 | 200 | 100 | 0 | 0 | 0 | 0 | 100 | 30 | 2029.28 |
| 124 | 780 | 455 | 1300 | 390 | 130 | 4.55 | 0 | 13 | 0 | 80 | 50 | 2294.35 |
| 125 | 780 | 390 | 1300 | 390 | 130 | 4.55 | 0 | 13 | 0 | 80 | 60 | 2294.32 |
| 126 | 581 | 212 | 1244 | 166 | 83 | 4.2 | 0 | 8.3 | 1.2 |  | 102 | 1709.35 |

Table S2. The full list of references for the 3DCP database

| No. | Ref |
| --- | --- |
| 1 | Kruger et al., 2021 |
| 2 | Nerella and Mechtcherine, 2016 |
| 3 | Paul et al., 2018 |
| 4 | Paul et al., 2018 |
| 5 | Khalil et al., 2017 |
| 6 | Khalil et al., 2017 |
| 7 | Chen et al., 2019 |
| 8 | Chen et al., 2019 |
| 9 | Chen et al., 2019 |
| 10 | Chen et al., 2019 |
| 11 | Pham et al., 2020 |
| 12 | Pham et al., 2020 |
| 13 | Pham et al., 2020 |
| 14 | Pham et al., 2020 |
| 15 | Pham et al., 2020 |
| 16 | Le et al., 2012 |
| 17 | Le et al., 2012 |
| 18 | Le et al., 2012 |
| 19 | Le et al., 2012 |
| 20 | Le et al., 2012 |
| 21 | Kazemian et al., 2017 |
| 22 | Kazemian et al., 2017 |
| 23 | Kazemian et al., 2017 |
| 24 | Kazemian et al., 2017 |
| 25 | Rahul et al., 2019 |
| 26 | Rahul et al., 2019 |
| 27 | Murcia et al., 2020 |
| 28 | Rehman et al., 2020 |
| 29 | Rehman et al., 2020 |
| 30 | Rehman et al., 2020 |
| 31 | Rehman et al., 2020 |
| 32 | Rehman et al., 2020 |
| 33 | Rehman et al., 2020 |
| 34 | Rehman et al., 2020 |
| 35 | Rehman et al., 2020 |
| 36 | Rehman et al., 2020 |
| 37 | Rahul et al., 2019 |
| 38 | Rahul et al., 2019 |
| 39 | Shakor et al., 2017 |
| 40 | Shakor et al., 2017 |
| 41 | Shakor et al., 2017 |
| 42 | Shakor et al., 2017 |
| 43 | Shakor et al., 2017 |
| 44 | Shakor et al., 2017 |
| 45 | Shakor et al., 2017 |
| 46 | Shakor et al., 2017 |
| 47 | Shakor et al., 2017 |
| 48 | Shakor et al., 2017 |
| 49 | Shakor et al., 2017 |
| 50 | Shakor et al., 2017 |
| 51 | Bos et al., 2020 |
| 52 | Bos et al., 2020 |
| 53 | Bos et al., 2020 |
| 54 | Bos et al., 2020 |
| 55 | Bos et al., 2020 |
| 56 | Bos et al., 2020 |
| 57 | Bos et al., 2020 |
| 58 | Bos et al., 2020 |
| 59 | Bos et al., 2020 |
| 60 | Bos et al., 2020 |
| 61 | Bos et al., 2020 |
| 62 | Bos et al., 2020 |
| 63 | Bos et al., 2020 |
| 64 | Bos et al., 2020 |
| 65 | Bos et al., 2020 |
| 66 | Bos et al., 2020 |
| 67 | Bos et al., 2020 |
| 68 | Bos et al., 2020 |
| 69 | Bos et al., 2020 |
| 70 | Bos et al., 2020 |
| 71 | Bos et al., 2020 |
| 72 | Bos et al., 2020 |
| 73 | Bos et al., 2020 |
| 74 | Bos et al., 2020 |
| 75 | Bos et al., 2020 |
| 76 | Bos et al., 2020 |
| 77 | Bos et al., 2020 |
| 78 | Bos et al., 2020 |
| 79 | Zhu et al., 2019 |
| 80 | Zhu et al., 2019 |
| 81 | Zhu et al., 2019 |
| 82 | Zhu et al., 2019 |
| 83 | Van Der Putten et al., 2019 |
| 84 | Lee et al., 2019 |
| 85 | Mazhoud et al., 2019 |
| 86 | Mazhoud et al., 2019 |
| 87 | Mazhoud et al., 2019 |
| 88 | Mazhoud et al., 2019 |
| 89 | Mazhoud et al., 2019 |
| 90 | Mazhoud et al., 2019 |
| 91 | Mazhoud et al., 2019 |
| 92 | Mazhoud et al., 2019 |
| 93 | Mazhoud et al., 2019 |
| 94 | Mazhoud et al., 2019 |
| 95 | Mazhoud et al., 2019 |
| 96 | Mazhoud et al., 2019 |
| 97 | Mazhoud et al., 2019 |
| 98 | Mazhoud et al., 2019 |
| 99 | Mazhoud et al., 2019 |
| 100 | Mazhoud et al., 2019 |
| 101 | Mazhoud et al., 2019 |
| 102 | Mazhoud et al., 2019 |
| 103 | Chen et al., 2021 |
| 104 | Chen et al., 2021 |
| 105 | Chen et al., 2021 |
| 106 | Marchment et al., 2019 |
| 107 | Nerella et al., 2019 |
| 108 | Nerella et al., 2019 |
| 109 | Weng et al., 2018 |
| 110 | Weng et al., 2018 |
| 111 | Weng et al., 2018 |
| 112 | Weng et al., 2018 |
| 113 | Rahul et al., 2022 |
| 114 | Rahul et al., 2022 |
| 115 | Rahul et al., 2022 |
| 116 | Baz et al., 2020 |
| 117 | Baz et al., 2020 |
| 118 | Baz et al., 2020 |
| 119 | Baz et al., 2020 |
| 120 | Mechtcherinea et al., 2019 |
| 121 | Mechtcherinea et al., 2019 |
| 122 | Yu et al., 2021 |
| 123 | Ting et al., 2019 |
| 124 | Long et al., 2019 |
| 125 | Long et al., 2019 |
| 126 | Wang et al., 2020 |

Machine learning models

1.1 Boosting models

Extreme Gradient Boosting (XGBoost), introduced by Chen and Guestrin in 2016 [92], is a supervised learning technique that enhances gradient boosting machines by combining weak learners to construct strong learners through sequential training. It minimizes the loss function using gradient descent and leverages both first- and second-order gradient statistics for optimization. Known for its efficiency in handling large datasets and delivering precise predictions, XGBoost supports parallel and distributed training, making it widely utilized in various applications [93,94]. In 2017, Microsoft introduced LightGBR, another advanced model based on Gradient Boosting Decision Trees (GBDT), designed to overcome the limitations of conventional GBDT in terms of memory usage and computational efficiency. LightGBR uses a leaf-wise growth strategy and an enhanced histogram method to improve training speed and space utilization [95,96]. The AdaBoost algorithm, developed by Freund and Schapire in 1997 [97], sequentially combines weak classifiers, adjusting instance weights based on classification accuracy to form a strong classifier. It is known for its ability to correct misclassifications and improve model accuracy by focusing on challenging instances [98].

1.2 Tree based models

Random forests, introduced by Leo Breiman in 2001, are an advanced ensemble learning technique that combines multiple decision trees to enhance classification accuracy and robustness [83]. These algorithms develop many classification or regression trees and integrate bootstrap and aggregation methods [83,84]. Each tree is generated from a randomly chosen subset of the training data, with splits determined by a random subset of input variables [84]. This randomness improves the diversity of the trees, all of which are fully developed binary trees. There are two key descriptors for random forests: one describes them as an ensemble of tree predictors where each tree depends on a random vector independently sampled with the same distribution across all trees [85], and the other discusses the generalization error for decision trees within the forest [85]. For regression, the predicted value is the average of the decision trees' predictions. Decision trees are constructed by splitting a dataset into segments, forming an inverted tree structure with a root node at the top [86]. The model's predictions are explained by tracing the decision path, where each decision node contributes additively to the final prediction [86]. Decision trees are powerful tools for data classification, and their performance can be improved by forming ensembles, which reduce overfitting and generalization errors [87-89].

1.3 Multi-layer perceptron

Deep learning involves training multi-layer artificial neural networks, also known as deep neural networks. The concept originated with Rosenblatt's introduction of the perceptron model in the 1950s, which was a variation designed to perform non-linear transformations [90]. The perceptron represents a non-linear mathematical function constrained by specific value limitations [91]. A multi-layer perceptron (MLP) is a type of feed-forward artificial neural network (ANN) that consists of sequentially connected layers: input, hidden, and output layers. MLPs operate under the supervised learning paradigm and use backpropagation as the training method.

The MLP regressor, a variant of the MLP, employs backpropagation—a gradient-descent algorithm that computes the error function by comparing the network's output to the target values. This algorithm then adjusts the weights of neurons in each layer by propagating the error values backward through the network. These weight adjustments fine-tune the network's performance.

The output of a neuron in an MLP is determined by a weighted sum of its inputs, as expressed by the Equation (S1).

youtput=(weights*inputs)+bias 		(S1)

The prediction produced by the neuron, youtput​, is obtained by applying an activation function, pact​, to the weighted sum of inputs along with the bias term. In practice, an MLP model can be used to predict relationships between input features and outputs, such as predicting the compressive strength and pump speed of 3DCP materials based on nine input elements. Figure S1 illustrates the proposed MLP model for this application.

Figure S1 Multilayer perceptron proposed model.

References

Alajmi, M. S., & Almeshal, A. M. (2020). Predicting the tool wear of a drilling process using novel machine learning XGBoost-SDA. Materials, 13(21), 1–16. https://doi.org/10.3390/ma13214952

Breiman, L. (2001). Random forests. Lecture Notes in Computer Science (Including Subseries Lecture Notes in Artificial Intelligence and Lecture Notes in Bioinformatics, 12343 LNCS, 503–515. https://doi.org/10.1007/978-3-030-62008-0_35

Chen, T., & Guestrin, C. (2016). XGBoost: A scalable tree boosting system. In Proceedings of the 22nd ACM SIGKDD International Conference on Knowledge Discovery and Data Mining (pp. 785–794). ACM. https://doi.org/10.1145/2939672.2939785

Dai, B., Gu, C., Zhao, E., & Qin, X. (2018). Statistical model optimized random forest regression model for concrete dam deformation monitoring. Structural Control and Health Monitoring, 25(4), e2170. https://doi.org/10.1002/stc.2170

Freund, Y., & Schapire, R. E. (1997). A decision-theoretic generalization of on-line learning and an application to boosting. Journal of Computer and System Sciences, 55(1), 119–139.

Grömping, U. (2009). Variable importance assessment in regression: Linear regression versus random forest. The American Statistician, 63(4), 308–319. https://doi.org/10.1198/tast.2009.08199

Ju, Y., Sun, G., Chen, Q., Zhang, M., Zhu, H., & Rehman, M. U. (2019). A model combining convolutional neural network and LightGBM algorithm for ultra-short-term wind power forecasting. IEEE Access, 7, 28309–28318. https://doi.org/10.1109/ACCESS.2019.2901920

Ke, G., Meng, Q., Finley, T., Wang, T., Chen, W., Ma, W., Ye, Q., & Liu, T. Y. (2017). LightGBM: A highly efficient gradient boosting decision tree. In Advances in Neural Information Processing Systems (pp. 3147–3155).

Liaw, A., & Wiener, M. (2002). Classification and regression by randomForest. R News, 2(3), 18–22.

Mangalathu, S., Hwang, S. H., & Jeon, J. S. (2020). Failure mode and effects analysis of RC members based on machine-learning-based SHapley Additive exPlanations (SHAP) approach. Engineering Structures, 219, 110927. https://doi.org/10.1016/j.engstruct.2020.110927

Mohan, M. K., Rahul, A. V., Van Tittelboom, K., & De Schutter, G. (2021). Rheological and pumping behaviour of 3D printable cementitious materials with varying aggregate content. Cement and Concrete Research, 139, 106258. https://doi.org/10.1016/j.cemconres.2020.106258

Panda, B., & Tan, M. J. (2018). Experimental study on mix proportion and fresh properties of fly ash-based geopolymer for 3D concrete printing. Ceramics International, 44(10), 10258–10265. https://doi.org/10.1016/j.ceramint.2018.03.031

Pavan, R., Nara, M., Gopinath, S., & Patil, N. (2021). Bayesian optimization and gradient boosting to detect phishing websites. In 2021 55th Annual Conference on Information Sciences and Systems (CISS) (pp. 1–5). IEEE. https://doi.org/10.1109/CISS50987.2021.9400317

Pirizadeh, M., Alemohammad, N., Manthouri, M., & Pirizadeh, M. (2021). A new machine learning ensemble model for class imbalance problem of screening enhanced oil recovery methods. Journal of Petroleum Science and Engineering, 198, 108214. https://doi.org/10.1016/j.petrol.2020.108214

Ruppert, D. (2010). The elements of statistical learning: Data mining, inference, and prediction. Journal of the American Statistical Association, 99(467), 567–567. https://doi.org/10.1198/jasa.2004.s339

Villarin, M. C., & Rodriguez-Galiano, V. F. (2019). Machine learning for modeling water demand. Journal of Water Resources Planning and Management, 145(5), 04019017. https://doi.org/10.1061/(asce)wr.1943-5452.0001067.