Supplemental Table. 1 Comprehensive Comparison of Mycelium-Based Composites and Global Conventional Construction Materials

| Material | Compressive Strength (MPa) | Density (kg/m³) | Recyclability | Manufacturing Method | Average cost | Credit/Modification from website/scientific paper |
| --- | --- | --- | --- | --- | --- | --- |
| Mycelium-Based Composites (MBCs) | 0.015–20.0 | 25–954 | Fully biodegradable and compostable | Fungal colonization on organic substrates, followed by molding and heat treatment | The average cost of MBCs products varies depending on factors such as material composition, processing methods, and intended application. | https://www.sciencedirect.com/science/article/pii/S0264127519308354?via%3Dihub/accessed on February 14, 2025 |
| Concrete (Global Standard) | 20–50 | 2,300–2,500 | Limited (can be crushed and reused as aggregate) | Mixing cement, water, and aggregates; casting and curing | 200-300 USD/m3 | https://www.ultratechcement.com/for-homebuilders/home-building-explained-single/descriptive-articles/what-is-density-of-concrete/accessed on February 14, 2025; https://www.hy-tec.com.au/concrete/accessed on February 14, 2025; https://www.researchgate.net/publication/325750161_Designing_Cost_Production_of_Concrete/accessed on February 14, 2025 |
| Reinforced Concrete (RC) | 17–70 | 2,400–2,600 | Limited (recyclable as crushed aggregate) | Concrete mixed with steel reinforcement bars for added strength | N/A | https://www.bigdreadymix.com/what-is-the-standard-strength-of-concrete/accessed on February 14, 2025; https://www.ultratechcement.com/for-homebuilders/home-building-explained-single/descriptive-articles/what-is-density-of-concrete/accessed on February 14, 2025 |
| Clay Bricks (Global) | 7–24 (Class 1: 11 – 24), Class 2: 7- 13, and Class 3: 5 -8) | 1,700–2,000 | Partially recyclable (can be crushed for reuse) | Clay molding, drying, and firing at high temperatures | N/A | https://www.mdpi.com/2075-5309/14/12/3882/accessed on February 14, 2025; https://www.modularclayproducts.co.uk/news/clay-bricks-vs-hollow-clay-bricks/accessed on February 14, 2025 |
| Cement Concrete Blocks (Global) | 7–34 | 1,800–2,200 | Partially recyclable (can be reused as crushed material) | Concrete mixture poured into molds and cured | The cost of a cubic meter of cement blocks in India ranges from $24 to $48 USD, depending on market conditions. | https://housing.com/news/an-essential-guide-to-cement-block-prices/accessed on February 14, 2025; https://www.indiamart.com/proddetail/aac-concrete-block-21938684297.html/ accessed on February 14, 2025; https://lignacite.co.uk/introduction-to-dense-concrete-blocks-properties-benefits-uses/accessed on February 14, 2025 |
| Steel (Structural) | 250–400 | 7,850–8,000 | Fully recyclable (melted and reused) | Smelting, casting, and rolling | Steel prices in the U.S. averaged $704 per metric ton in 2024 | https://www.amardeepsteel.com/blog/density-of-steel.html/accessed on February 14, 2025; https://www.tevema.com/is-concrete-stronger-in-compression-than-steel/ accessed on February 14, 2025 |
| Aluminum (Framing, Roofing) | Pure aluminum (≥99% purity): $30 per metric ton Aluminum alloys: $80–$700 per metric ton (varies by composition and other factors) | 2,600–3,730 | Fully recyclable (melted and reused) | Smelting and extrusion | Aluminum roofing costs range from $3,800 for smaller roofs to $50,000 for large or complex structures. | https://www.tevema.com/is-aluminium-stronger-in-compression/accessed on February 14, 2025; https://www.omnicalculator.com/construction/aluminum-weight/accessed on February 14, 2025 |
| Glass (Facade, Windows) | 35–120 | 2,200–2,700 | Partially recyclable (requires energy-intensive recycling) | Melting silica and molding | $200 to $2,900 per linear foot. Glass walls cost an average of $5,000 to install, but these prices can range from $1,300 to $18,000 | https://www.homeadvisor.com/cost/doors-and-windows/install-a-glass-wall/ accessed on February 14, 2025; https://www.angi.com/articles/how-much-glass-walls-cost.htm/accessed on February 14, 2025; https://www.researchgate.net/publication/44087629_The_Strength_and_testing_of_window_glass/ accessed on February 14, 2025; https://www.omnicalculator.com/construction/glass-weight/accessed on February 14, 2025; |
| Wood (Plywood, Oriented strand board, Timber) | Pine (Eastern White, Jack, Loblolly, Lodgepole, Longleaf, Pitch): 33.1–49.2 | Depending on the wood type, softwood plywood ranges from 400–600, hardwood plywood from 500 to 800, and OSB panels from 400–850. | Partially recyclable (can be chipped for reuse) | Sawmilling, gluing, and pressing wood layers | N/A | https://www.engineeringtoolbox.com/wood-density-d_40.html/ accessed on February 14, 2025; https://www.researchgate.net/publication/237639918_Localized_density_effects_on_fastener_holding_capacities_in_wood-based_panels/figures?lo=1/ accessed on February 14, 2025; https://www.engineeringtoolbox.com/timber-mechanical-properties-d_1789.html/accessed on February 14, 2025 |
| Plastic-Based Composites | 0.1–158 | 50–2100 | Limited (recyclable depending on polymer type) | Polymer molding or extrusion with fillers | N/A | https://omnexus.specialchem.com/polymer-property/density/accessed on February 14, 2025; https://www.sciencedirect.com/science/article/abs/pii/S0950061822017482/ accessed on February 14, 2025 |
| Bamboo Composites (Asia, Tropics) | 30–76 | 600–800 | Biodegradable and recyclable | Bamboo fiber processing, gluing, and pressing | N/A | https://iopscience.iop.org/article/10.1088/1757-899X/1007/1/012095/pdf/accessed on February 14, 2025; https://www.sciencedirect.com/science/article/abs/pii/S0950061822013563/ accessed on February 14, 2025 |
| Rammed Earth (Africa, Asia) | 0.2–10 | 1,800–2,200 | Fully recyclable (natural material) | Compacting layers of moist earth within temporary frames | A rammed earth home costs $4,000 to $4,500 per m² for a complete build, while rammed earth walls range from $450 to $750 per face m². | https://www.researchgate.net/publication/245308516_Structural_Capacity_of_Rammed_Earth_in_Compression/accessed on February 14, 2025; https://www.sciencedirect.com/science/article/pii/S2214509514000084/ accessed on February 14, 2025; https://www.sciencedirect.com/science/article/abs/pii/S0950061803001375/ accessed on February 14, 2025; https://www.ecosustainablehomes.com.au/how-much-does-a-rammed-earth-house-cost/accessed on February 14, 2025 |
| Cob (Earthen Material, Global) | 0.1–3 | 1,200–1,700 | Fully recyclable (natural material) | Mixing clay, sand, straw, and water, then hand-molding walls | A cob house ($18 to $42 USD per square foot. Outside India, the cost ranges from $150 to $500 USD per square foot | https://www.sciencedirect.com/science/article/pii/S2352710224005278/accessed on February 14, 2025; https://chateigner.ensicaen.fr/pdf/Affan_Buildings_13_932_2023_Earth-Based%20Building%20Incorporating%20Sargassum%20muticum%20Seaweed-%20Mechanical%20and%20Hygrothermal%20Performances.pdf/ accessed on February 14, 2025; https://www.tinyfarmlab.com/post/what-is-the-cost-of-building-a-cob-house/ accessed on February 14, 2025 |
| Cork Composites (Europe) | 1–3 | 200–300 | Fully recyclable and biodegradable | Harvesting cork bark, grinding, and compressing into panels | N/A | https://www.researchgate.net/publication/387130325_A_comparative_study_of_expanded_and_raw_cork_waste_composite_materials/ accessed on February 14, 2025; https://www.mdpi.com/1996-1944/2/3/776/accessed on February 14, 2025 |
| Gypsum Board (Global) | 1.5–2.5 | 600–1,000 | Partially recyclable (limited reuse potential) | Heating gypsum, pressing into sheets, and drying | Sheetrock and drywall prices are $10 to $20 per sheet or $0.30 to $0.50 per square foot on average, depending on size, thickness, and type. Gypsum plasterboard costs $12 to $16 per sheet. | https://www.british-gypsum.com/accessed on February 14, 2025/ https://www.sciencedirect.com/topics/engineering/gypsum-concrete/ accessed on February 14, 2025/ https://homeguide.com/costs/sheetrock-drywall-prices/accessed on February 14, 2025/ |
| Basalt Fiber (China, India) | 20–35 | 2,610–2,800 | Partially recyclable (difficult to recycle) | Melting basalt rock and spinning fibers into composites | 2- US$ 5 per 1 kilogram | https://www.mdpi.com/2071-1050/14/19/12517/accessed on February 14, 2025/ https://pmc.ncbi.nlm.nih.gov/articles/PMC9865098/accessed on February 14, 2025/ https://www.mdpi.com/2076-3417/11/18/8729/accessed on February 14, 2025/ https://www.made-in-china.com/products-search/hot-china-products/Basalt_Fiber_Price.html/ accessed on February 14, 2025/ |
| Straw Bale (Rural) | 0.16–0.48 | 90–190 | Fully biodegradable (compostable) | Baling straw and stacking within frames | N/A | https://www.sciencedirect.com/topics/engineering/straw-bale/accessed on February 14, 2025 |