Supplementary Table S1. Database-specific search strategies and search-term framework used to identify expanded-perlite and bio-based cementitious-material studies.

| Database / source | Search field / role | Search strategy | Limits / handling | Search timing |
| --- | --- | --- | --- | --- |
| Scopus | TITLE-ABS-KEY | “expanded perlite” OR “perlite aggregate” OR “perlite powder” OR “waste perlite” OR “ground perlite” OR “hempcrete” OR “hemp fiber” OR “hemp fibre” OR “rice husk ash” OR “rice husk concrete” OR “date palm fiber” OR “date palm fibre” OR “date palm ash” OR “kenaf fiber” OR “kenaf fibre” OR “bamboo fiber” OR “bamboo fibre” OR “bamboo ash” OR “corn stalk ash” OR “corn stalk fiber” OR “wheat straw ash” OR “wheat straw fiber” OR “palm oil fuel ash” AND “mortar” OR “concrete” OR “cementitious composite” OR “cement mortar” OR “geopolymer” AND “thermal conductivity” OR “compressive strength” OR “water absorption” OR “sound absorption” OR “hygrothermal” OR “embodied carbon” OR “carbon footprint” OR “life cycle assessment” OR “LCA”. | English; publication years 2010-2026; document types: Article, Review, and Conference Paper. | 13 April 2026 |
| Web of Science | Title (TI), Abstract (AB), and Author Keywords (AK) | (TI=("expanded perlite" OR "perlite aggregate" OR "perlite powder" OR "waste perlite" OR hempcrete OR "hemp fiber" OR "hemp fibre" OR "rice husk ash" OR "date palm fiber" OR "date palm fibre" OR "date palm ash" OR "kenaf fiber" OR "kenaf fibre" OR "bamboo fiber" OR "bamboo fibre" OR "corn stalk ash" OR "wheat straw ash" OR "palm oil fuel ash") OR AB=("expanded perlite" OR "perlite aggregate" OR "perlite powder" OR "waste perlite" OR hempcrete OR "hemp fiber" OR "hemp fibre" OR "rice husk ash" OR "date palm fiber" OR "date palm fibre" OR "date palm ash" OR "kenaf fiber" OR "kenaf fibre" OR "bamboo fiber" OR "bamboo fibre" OR "corn stalk ash" OR "wheat straw ash" OR "palm oil fuel ash") OR AK=("expanded perlite" OR "perlite aggregate" OR "perlite powder" OR "waste perlite" OR hempcrete OR "hemp fiber" OR "hemp fibre" OR "rice husk ash" OR "date palm fiber" OR "date palm fibre" OR "date palm ash" OR "kenaf fiber" OR "kenaf fibre" OR "bamboo fiber" OR "bamboo fibre" OR "corn stalk ash" OR "wheat straw ash" OR "palm oil fuel ash")) AND (TI=(mortar OR concrete OR cementitious OR geopolymer) OR AB=(mortar OR concrete OR cementitious OR geopolymer) OR AK=(mortar OR concrete OR cementitious OR geopolymer)) AND (TI=("thermal conductivity" OR "compressive strength" OR "water absorption") OR AB=("thermal conductivity" OR "compressive strength" OR "water absorption") OR AK=("thermal conductivity" OR "compressive strength" OR "water absorption")) | English; publication years 2010-2026; document types: Article, Review, and Proceedings Paper. | 13 April 2026 |
| ScienceDirect | Title, abstract or author-specified keywords | (“perlite” OR “hemp” OR “rice husk” OR “date palm fiber” OR “bamboo”) AND (“mortar” OR “concrete”) AND (“thermal conductivity” OR “compressive strength”) | English; publication years 2010-2026. Article and Review. | 13 April 2026 |

Supplementary Table S2. Study-level methodological appraisal of selected studies within the review corpus.

| Ref. | Material composition and dosage/replacement basis | Test method/standard | Control/reference comparison | Replicates/ sample size | Moisture/ conditioning | Curing procedure/test age | Uncertainty/variability reporting | Methodological rigor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 20 | High | High | Moderate | High | Low | N/A | High | Moderate |
| 21 | Moderate | Moderate | High | Low | High | N/A | Moderate | Low |
| 22 | Moderate | High | High | Low | High | N/A | Low | Low |
| 23 | Moderate | High | Moderate | Low | Moderate | Low | Low | Low |
| 24 | High | High | High | High | Moderate | High | Low | Moderate |
| 25 | High | Moderate | High | Low | High | High | High | Moderate |
| 26 | High | Moderate | High | Low | High | High | Low | Low |
| 27 | High | High | High | High | High | Moderate | Moderate | Moderate |
| 28 | High | Moderate | High | Moderate | Moderate | High | Moderate | Moderate |
| 29 | High | High | High | High | High | High | Moderate | High |
| 30 | Low | High | High | N/A | N/A | N/A | High | Moderate |
| 31 | High | High | High | High | High | High | High | High |
| 32 | Low | High | Low | High | High | High | High | Low |
| 33 | High | High | High | High | High | High | High | High |
| 35 | High | High | High | Moderate | High | High | Moderate | Moderate |
| 36 | High | High | High | Moderate | High | High | Low | Moderate |
| 37 | High | High | High | High | High | High | High | High |
| 45 | Low | Moderate | High | High | High | N/A | Low | Low |
| 46 | High | Moderate | High | Moderate | High | High | Moderate | Moderate |
| 47 | High | High | High | Moderate | Moderate | Moderate | High | Moderate |
| 48 | High | High | High | High | High | High | Moderate | High |
| 49 | High | High | High | High | High | High | High | High |
| 50 | High | High | High | High | High | High | Moderate | High |
| 51 | High | Moderate | High | High | N/A | N/A | High | High |
| 52 | High | Moderate | High | Moderate | Moderate | High | Moderate | Moderate |
| 53 | High | Moderate | High | High | High | High | High | High |
| 54 | High | High | High | Moderate | Moderate | High | Moderate | Moderate |
| 56 | High | High | High | Moderate | Moderate | Moderate | Moderate | Moderate |
| 57 | High | High | High | Moderate | High | High | Low | Moderate |
| 58 | High | High | High | High | High | High | Moderate | High |
| 59 | High | High | High | High | High | High | Low | Moderate |
| 60 | High | High | High | Moderate | High | High | Low | Moderate |
| 61 | High | High | High | Moderate | Low | High | Moderate | Moderate |
| 62 | High | High | High | High | High | High | Moderate | High |
| 63 | High | High | High | High | High | High | Moderate | High |
| 64 | High | High | High | High | High | N/A | High | High |
| 65 | High | High | High | High | High | Moderate | Moderate | Moderate |
| 66 | High | High | High | High | Moderate | N/A | High | High |
| 67 | High | Moderate | High | Moderate | Moderate | Moderate | High | Moderate |
| 68 | High | High | High | High | High | High | High | High |
| 69 | High | High | High | High | High | High | High | High |
| 70 | High | High | High | Moderate | Moderate | High | Low | Moderate |
| 71 | High | High | High | High | High | Moderate | High | High |
| 72 | High | High | High | Moderate | High | Moderate | Moderate | Moderate |
| 73 | High | High | High | Moderate | Moderate | Moderate | Moderate | Moderate |
| 74 | High | High | High | High | High | Moderate | Moderate | Moderate |
| 75 | High | High | High | High | Moderate | High | Moderate | Moderate |
| 76 | High | High | High | High | High | High | High | High |
| 77 | High | High | High | High | High | Moderate | Moderate | Moderate |
| 78 | High | High | High | High | Moderate | High | High | High |
| 79 | High | High | High | High | High | High | High | High |
| 80 | High | High | High | High | High | High | High | High |
| 81 | High | Moderate | High | High | Moderate | High | Low | Moderate |
| 82 | High | High | High | High | High | High | Moderate | High |
| 83 | High | High | High | High | High | High | High | High |
| 84 | High | Moderate | High | High | High | High | Low | Moderate |
| 85 | High | High | High | High | Moderate | High | Low | Moderate |
| 86 | High | Moderate | High | Moderate | Moderate | High | Low | Moderate |
| 87 | High | High | High | High | High | High | High | High |
| 88 | High | High | Moderate | High | High | High | High | High |
| 89 | High | High | High | High | High | High | High | High |
| 90 | High | High | High | High | High | High | Moderate | High |
| 92 | High | High | High | High | High | Moderate | Moderate | Moderate |
| 93 | High | Moderate | High | High | Moderate | High | High | Moderate |
| 95 | High | High | High | Moderate | Low | High | High | Moderate |
| 96 | High | Moderate | High | High | Moderate | High | Moderate | Moderate |
| 97 | High | High | High | High | Low | Moderate | Low | Low |
| 98 | High | Moderate | High | Low | High | High | Low | Low |
| 99 | High | High | High | High | High | High | High | High |
| 100 | High | High | High | High | Moderate | High | High | High |
| 101 | High | High | High | High | High | High | High | High |
| 102 | High | Moderate | High | Low | Moderate | High | Low | Low |
| 103 | High | High | High | High | High | High | High | High |
| 104 | High | High | High | High | Low | High | Moderate | Moderate |
| 105 | High | High | High | High | Low | High | High | Moderate |
| 106 | High | High | High | High | High | High | Moderate | High |
| 108 | High | High | High | High | Moderate | High | High | High |
| 109 | High | High | High | High | Moderate | High | High | High |
| 112 | High | High | High | High | High | High | High | High |
| 113 | High | High | High | High | High | High | High | High |
| 114 | High | High | High | High | High | N/A | Moderate | High |
| 120 | High | High | High | High | Moderate | High | High | High |
| 124 | High | High | High | Moderate | High | High | High | High |
| 125 | High | High | High | Moderate | High | High | Low | Moderate |
| 126 | High | High | High | Moderate | High | Moderate | Low | Moderate |
| 127 | Moderate | High | High | High | High | Moderate | High | Moderate |
| 128 | High | High | High | High | High | High | Moderate | High |
| 130 | High | High | High | Moderate | Moderate | High | High | Moderate |
| 131 | High | High | High | High | High | High | High | High |
| 132 | High | High | High | High | High | N/A | High | High |
| 133 | High | High | High | Moderate | High | High | High | High |
| 134 | High | High | High | High | Moderate | High | High | High |
| 135 | High | Moderate | High | Moderate | Moderate | Moderate | High | Moderate |
| 136 | High | High | High | Moderate | High | Moderate | High | Moderate |
| 138 | Moderate | High | High | High | High | Low | Moderate | Moderate |
| 139 | High | High | High | Low | Low | Low | Low | Low |
| 140 | High | High | High | High | High | High | High | High |
| 141 | High | High | High | High | High | High | High | High |
| 142 | High | High | High | High | High | High | High | High |

Supplementary Table S3. Traceability dataset for the Ashby-style comparative performance map.

| Source | Material class | Mixture details | Curing / test age | Moisture / conditioning | Test method(s) | Density used for CS plot (kg/m³) | Compressive strength (MPa) | Density used for λ plot (kg/m³) | Thermal conductivity, λ (W/m·K) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 5% nominal large corn stalk (LCS), 11.8 mm; W/B=0.100 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 1656.983 | 20.816 | 1656.983 | 0.643 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 10% nominal large corn stalk (LCS), 11.8 mm; W/B=0.100 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 1395.329 | 11.796 | 1395.329 | 0.467 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 15% nominal large corn stalk (LCS), 11.8 mm; W/B=0.156 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 1185.195 | 9.686 | 1185.195 | 0.318 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 20% nominal large corn stalk (LCS), 11.8 mm; W/B=0.218 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 1083.401 | 6.980 | 1083.401 | 0.192 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 25% nominal large corn stalk (LCS), 11.8 mm; W/B=0.224 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 684.507 | 5.084 | 684.507 | 0.167 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 30% nominal large corn stalk (LCS), 11.8 mm; W/B=0.333 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 556.674 | 1.749 | 556.674 | 0.051 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 5% nominal small corn stalk (SCS), 7.0 mm; W/B=0.124 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 1853.601 | 28.367 | 1853.601 | 0.998 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 10% nominal small corn stalk (SCS), 7.0 mm; W/B=0.100 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 1665.071 | 24.490 | 1665.071 | 0.654 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 15% nominal small corn stalk (SCS), 7.0 mm; W/B=0.130 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 1335.198 | 12.473 | 1335.198 | 0.443 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 20% nominal small corn stalk (SCS), 7.0 mm; W/B=0.159 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 1048.218 | 9.441 | 1048.218 | 0.213 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 25% nominal small corn stalk (SCS), 7.0 mm; W/B=0.259 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 816.937 | 6.269 | 816.937 | 0.180 |
| (Ahmad et al., 2018) | Bio-based lightweight aggregate (corn-stalk/MPC) | MPC–fly-ash matrix + 30% nominal small corn stalk (SCS), 7.0 mm; W/B=0.374 | CS: tested from 1 h to 28 d; plotted CS value: 28 d; λ: 28 d | λ specimens oven-dried at 50 °C to constant mass, then conditioned to 25 °C before testing; CS specimen moisture state: NR | CS method: Instron 8501, hydraulic servo-controlled; λ method: TC3000E thermal conductivity meter | 709.267 | 2.598 | 709.267 | 0.099 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | A: 80/12/8 vol% hemp/lime/water; air-dried hurd | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 309 ± 11 | 0.318 ± 0.013 | 309 ± 11 | 0.047 ± 0.007 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | A: 80/12/8 vol%; hurd pre-treated 120 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 312 ± 14 | 0.331 ± 0.019 | 312 ± 14 | 0.057 ± 0.009 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | A: 80/12/8 vol%; hurd pre-treated 160 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 298 ± 9 | 0.325 ± 0.028 | 298 ± 9 | 0.063 ± 0.004 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | A: 80/12/8 vol%; hurd pre-treated 200 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 281 ± 11 | 0.383 ± 0.016 | 281 ± 11 | 0.072 ± 0.002 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | A: 80/12/8 vol%; hurd pre-treated 240 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 240 ± 15 | 0.466 ± 0.022 | 240 ± 15 | 0.080 ± 0.001 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | A: 80/12/8 vol%; hurd pre-treated 280 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 225 ± 20 | 0.515 ± 0.031 | 225 ± 20 | 0.081 ± 0.002 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | B: 75/15/10 vol% hemp/lime/water; air-dried hurd | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 382 ± 17 | 0.334 ± 0.022 | 382 ± 17 | 0.088 ± 0.007 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | B: 75/15/10 vol%; hurd pre-treated 120 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 400 ± 5 | 0.452 ± 0.042 | 400 ± 5 | 0.089 ± 0.011 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | B: 75/15/10 vol%; hurd pre-treated 160 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 379 ± 13 | 0.375 ± 0.032 | 379 ± 13 | 0.096 ± 0.007 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | B: 75/15/10 vol%; hurd pre-treated 200 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 362 ± 16 | 0.498 ± 0.032 | 362 ± 16 | 0.118 ± 0.007 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | B: 75/15/10 vol%; hurd pre-treated 240 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 321 ± 18 | 0.511 ± 0.011 | 321 ± 18 | 0.134 ± 0.006 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | B: 75/15/10 vol%; hurd pre-treated 280 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 298 ± 22 | 0.540 ± 0.026 | 298 ± 22 | 0.142 ± 0.008 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | C: 65/20/15 vol% hemp/lime/water; air-dried hurd | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 469 ± 10 | 0.512 ± 0.018 | 469 ± 10 | 0.121 ± 0.005 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | C: 65/20/15 vol%; hurd pre-treated 120 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 451 ± 26 | 0.513 ± 0.019 | 451 ± 26 | 0.128 ± 0.007 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | C: 65/20/15 vol%; hurd pre-treated 160 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 443 ± 16 | 0.532 ± 0.018 | 443 ± 16 | 0.137 ± 0.002 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | C: 65/20/15 vol%; hurd pre-treated 200 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 438 ± 11 | 0.677 ± 0.012 | 438 ± 11 | 0.149 ± 0.007 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | C: 65/20/15 vol%; hurd pre-treated 240 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 432 ± 17 | 0.777 ± 0.022 | 432 ± 17 | 0.156 ± 0.005 |
| (D’Eusanio et al., 2024) | Bio-based lightweight aggregate (hempcrete) | C: 65/20/15 vol%; hurd pre-treated 280 °C for 6 h | CS: 28 d; λ: 28 d | Specimen pre-test moisture state for CS/λ not separately specified; density based on mass after 28 d curing | CS: Tecnotest compression test machine; λ: KD2 Pro, ASTM D5334-08, transient-line heat-source method | 418 ± 17 | 0.829 ± 0.026 | 418 ± 17 | 0.166 ± 0.003 |
| (Sengul et al., 2011) | Reference concrete | NC; 0% EP; cement 317; water 175; sand 1517; EP 0; SP 4.8; AEA 1.0 kg/m³; effective w/c=0.55; EP 2–4 mm | 24 h in mold; lime-saturated water at 20 °C to 28 d; then 20 °C/50% RH; tests at 35 d | CS/mechanical tests: air-dry; λ test: oven-dry | CS: EN 206 / EN 12390; three 70-mm cubes. λ: EN 12667 | 1937 | 28.80 | 1833 | 0.60 |
| (Sengul et al., 2011) | Expanded-perlite aggregate concrete | EPC20; 20 vol% sand replacement by EP; cement 337; water 185; pre-absorption water 37; sand 1288; EP 17; SP 5.1; AEA 1.0 kg/m³; effective w/c=0.55; EP 2–4 mm | 24 h in mold; lime-saturated water at 20 °C to 28 d; then 20 °C/50% RH; tests at 35 d | CS/mechanical tests: air-dry; λ test: oven-dry | CS: EN 206 / EN 12390; three 70-mm cubes. λ: EN 12667 | 1775 | 17.30 | 1677 | 0.57 |
| (Sengul et al., 2011) | Expanded-perlite aggregate concrete | EPC40; 40 vol% replacement; cement 326; water 179; pre-absorption water 71; sand 937; EP 33; SP 1.5; AEA 1.0 kg/m³; effective w/c=0.55; EP 2–4 mm | 24 h in mold; lime-saturated water at 20 °C to 28 d; then 20 °C/50% RH; tests at 35 d | CS/mechanical tests: air-dry; λ test: oven-dry | CS: EN 206 / EN 12390; three 70-mm cubes. λ: EN 12667 | 1402 | 10.90 | 1316 | 0.53 |
| (Sengul et al., 2011) | Expanded-perlite aggregate concrete | EPC60; 60 vol% replacement; cement 301; water 166; pre-absorption water 100; sand 581; EP 47; SP 0; AEA 0.9 kg/m³; effective w/c=0.55; EP 2–4 mm | 24 h in mold; lime-saturated water at 20 °C to 28 d; then 20 °C/50% RH; tests at 35 d | CS/mechanical tests: air-dry; λ test: oven-dry | CS: EN 206 / EN 12390; three 70-mm cubes. λ: EN 12667 | 980 | 4.60 | 909 | 0.35 |
| (Sengul et al., 2011) | Expanded-perlite aggregate concrete | EPC80; 80 vol% replacement; cement 297; water 163; pre-absorption water 131; sand 286; EP 61; SP 0; AEA 0.9 kg/m³; effective w/c=0.55; EP 2–4 mm | 24 h in mold; lime-saturated water at 20 °C to 28 d; then 20 °C/50% RH; tests at 35 d | CS/mechanical tests: air-dry; λ test: oven-dry | CS: EN 206 / EN 12390; three 70-mm cubes. λ: EN 12667 | 673 | 1.10 | 613 | 0.21 |
| (Sengul et al., 2011) | Expanded-perlite aggregate concrete | EPC100; 100 vol% replacement; cement 295; water 162; pre-absorption water 162; sand 0; EP 76; SP 0; AEA 0.9 kg/m³; effective w/c=0.55; EP 2–4 mm | 24 h in mold; lime-saturated water at 20 °C to 28 d; then 20 °C/50% RH; tests at 35 d | CS/mechanical tests: air-dry; λ test: oven-dry | CS: EN 206 / EN 12390; three 70-mm cubes. λ: EN 12667 | 392 | 0.10 | 354 | 0.13 |
| (Leyton-Vergara et al., 2019) | Expanded-perlite aggregate mortar | F-SG; Fine EP; FM 2.20; max nominal size 2.36 mm; cement 170 kg/m³; water 228 L/m³; W/C 1.34; EP 81 kg/m³; no additives; no EP pre-absorption | 24 h in mold; 28 d humid chamber at 20 °C/96% RH; then laboratory conditions (~20 °C/50% RH) | Density used with CS is the reported humid-state density immediately after curing; exact CS specimen moisture at testing: NR. λ specimens: dried 24 h at 60 °C | CS: NCh 158 Of:1969 (partial adaptation ASTM C109/C109M-16a), 40-mm cubes. λ: guard-ring, NCh 850.Of 2008 (partial adaptation ASTM C177-19) | 1008.8 | 0.42 | 660.8 | 0.184 |
| (Leyton-Vergara et al., 2019) | Expanded-perlite aggregate mortar | M-SG; Medium EP; FM 2.85; max nominal size 2.36 mm; cement 170 kg/m³; water 228 L/m³; W/C 1.34; EP 81 kg/m³; no additives; no EP pre-absorption | 24 h in mold; 28 d humid chamber at 20 °C/96% RH; then laboratory conditions (~20 °C/50% RH) | Density used with CS is the reported humid-state density immediately after curing; exact CS specimen moisture at testing: NR. λ specimens: dried 24 h at 60 °C | CS: NCh 158 Of:1969 (partial adaptation ASTM C109/C109M-16a), 40-mm cubes. λ: guard-ring, NCh 850.Of 2008 (partial adaptation ASTM C177-19) | 720.0 | 0.21 | 403.5 | 0.163 |
| (Leyton-Vergara et al., 2019) | Expanded-perlite aggregate mortar | C-SG; Coarse EP; FM 3.50; max nominal size 4.75 mm; cement 170 kg/m³; water 228 L/m³; W/C 1.34; EP 81 kg/m³; no additives; no EP pre-absorption | 24 h in mold; 28 d humid chamber at 20 °C/96% RH; then laboratory conditions (~20 °C/50% RH) | Density used with CS is the reported humid-state density immediately after curing; exact CS specimen moisture at testing: NR. λ specimens: dried 24 h at 60 °C | CS: NCh 158 Of:1969 (partial adaptation ASTM C109/C109M-16a), 40-mm cubes. λ: guard-ring, NCh 850.Of 2008 (partial adaptation ASTM C177-19) | 540.1 | 0.13 | 375.4 | 0.100 |

Abbreviations and notations used in Supplementary Table S3

| Notations | Full name |
| --- | --- |
| CS | compressive strength |
| λ | thermal conductivity |
| MPC | magnesium phosphate cement |
| LCS | large corn stalk |
| SCS | small corn stalk |
| EP | expanded perlite |
| SP | superplasticizer |
| AEA | air-entraining admixture |
| FM | fineness modulus |
| NR | not reported |