Appendix 1: Variations in particle sizes (in µm) of the different phases and their sedimentation rates (in cm/s)

| D | SE |  | Vs | SE |
| --- | --- | --- | --- | --- |
| Phosphate sludge waste (N=9) |  |  |  |  |
| 44.5 | 0.17 |  | 0.23 | 0.00166 |
| 32 | 0.38 |  | 0.12 | 0.00268 |
| 20 | 0.31 |  | 0.05 | 0.00134 |
| 14 | 0.24 |  | 0.02 | 0.00073 |
| 10 | 0.14 |  | 0.01 | 0.00034 |
| 7 | 0.10 |  | 0.01 | 0.00018 |
| 5 | 0.07 |  | 0.003 | 0.00008 |
| 3 | 0.03 |  | 0.001 | 0.00002 |
| 2 | 0.01 |  | 0.0003 | 8.70×10-7 |
| 1 | 0.003 |  | 0.0002 | 1.09×10-6 |
| Apatite-rich phases (N=9) |  |  |  |  |
| 43.52 | 0.61 |  | 0.26 | 0.0072 |
| 31 | 0.49 |  | 0.13 | 0.0041 |
| 20 | 0.31 |  | 0.05 | 0.0016 |
| 14 | 0.22 |  | 0.03 | 0.0008 |
| 10 | 0.15 |  | 0.01 | 0.0004 |
| 7 | 0.11 |  | 0.01 | 0.0002 |
| 5 | 0.08 |  | 0.003 | 0.0001 |
| 3 | 0.04 |  | 0.001 | 0.00003 |
| 1.4 | 0.02 |  | 0.0003 | 0.000008 |
| 1 | 0.02 |  | 0.0002 | 0.000006 |
| Clay-rich phases (N=9) |  |  |  |  |
| 3 | 0.01 |  | 0.001 | 5,670×10-6 |
| 2 | 0.001 |  | 0.0003 | 3.544×10-7 |
| 1 | 0.01 |  | 0.0002 | 5.665×10-6 |

SE: standard errors

D: Equivalent particle size

Vs: Sedimentation or particle fall rates

Appendix 2: pH, electrical conductivity, redox potential, bulk density and effective cation exchange capacity values in phosphate sludge waste and different phases (pH unitless, EC in mS/cm, Eh in mV, ρs in g/cm3 and ECEC in meq/100g)

|  | pHH2O | pHKCl | EC | Eh | ρs | ECEC |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Phosphate sludge waste |  |  |  |
| B1 | 6.33 | 6.27 | 14.30 | 69.00 | 1.23 | 27.10 |
| B2 | 6.29 | 6.11 | 15.14 | 71.00 | 1.26 | 31.28 |
| B3 | 6.56 | 6.22 | 8.64 | 70.00 | 1.24 | 28.56 |
| B4 | 6.62 | 6.22 | 7.56 | 65.00 | 1.17 | 26.87 |
| B5 | 6.50 | 6.14 | 17.38 | 59.00 | 1.21 | 27.16 |
| B6 | 6.42 | 6.10 | 15.21 | 65.00 | 1.21 | 25.84 |
| B7 | 6.44 | 6.04 | 12.15 | 68.00 | 1.27 | 25.53 |
| B8 | 6.43 | 5.95 | 12.31 | 74.00 | 1.23 | 28.29 |
| B9 | 6.19 | 5.85 | 22.40 | 79.00 | 1.19 | 34.75 |
| Min | 6.19 | 5.85 | 7.56 | 59.00 | 1.17 | 25.53 |
| Max | 6.62 | 6.27 | 22.40 | 79.00 | 1.27 | 34.75 |
| Mean | 6.42 | 6.10 | 13.90 | 68.89 | 1.22 | 28.38 |
| SE | 0.13 | 0.14 | 4.49 | 5.73 | 0.03 | 2.93 |
|  |  | Apatite-rich phases |  |  |  |
| B-A1 | 6.86 | 6.29 | 2.72 | 51.00 | 1.41 | 21.68 |
| B-A2 | 6.90 | 6.36 | 2.13 | 42.00 | 1.38 | 21.68 |
| B-A3 | 7.22 | 6.27 | 0.74 | 48.00 | 1.32 | 23.99 |
| B-A4 | 7.00 | 6.30 | 1.48 | 49.00 | 1.30 | 22.68 |
| B-A5 | 6.42 | 6.23 | 21.70 | 51.00 | 1.28 | 24.61 |
| B-A6 | 6.45 | 6.15 | 17.77 | 55.00 | 1.40 | 23.20 |
| B-A7 | 6.35 | 5.92 | 21.70 | 62.00 | 1.40 | 28.73 |
| B-A8 | 6.22 | 5.82 | 32.10 | 60.00 | 1.34 | 24.13 |
| B-A9 | 6.48 | 6.07 | 16.41 | 55.00 | 1.39 | 22.08 |
| Min | 6.22 | 5.82 | 0.74 | 42.00 | 1.28 | 21.68 |
| Max | 7.22 | 6.36 | 32.10 | 62.00 | 1.41 | 28.73 |
| Mean | 6.66 | 6.16 | 12.97 | 52.56 | 1.36 | 23.64 |
| SE | 0.34 | 0.19 | 11.50 | 6.19 | 0.05 | 2.19 |
|  |  | Clay-rich phases |  |  |  |
| B-D1 | 6.69 | 5.94 | 1.92 | 59.00 | 1.21 | 23.50 |
| B-D2 | 6.64 | 5.90 | 1.64 | 59.00 | 1.27 | 24.44 |
| B-D3 | 6.66 | 5.83 | 1.20 | 65.00 | 1.18 | 20.11 |
| B-D4 | 6.53 | 5.76 | 3.24 | 67.00 | 1.23 | 20.66 |
| B-D5 | 6.35 | 6.18 | 16.74 | 44.00 | 1.23 | 22.26 |
| B-D6 | 6.20 | 6.18 | 10.42 | 53.00 | 1.27 | 24.21 |
| B-D7 | 6.40 | 6.10 | 15.80 | 54.00 | 1.29 | 25.37 |
| B-D8 | 6.36 | 6.01 | 15.01 | 54.00 | 1.28 | 22.27 |
| B-D9 | 6.22 | 5.89 | 26.10 | 65.00 | 1.28 | 24.35 |
| Min | 6.20 | 5.76 | 1.20 | 44.00 | 1.18 | 20.11 |
| Max | 6.69 | 6.18 | 26.10 | 67.00 | 1.29 | 25.37 |
| Mean | 6.45 | 5.98 | 10.23 | 57.78 | 1.25 | 23.02 |
| SE | 0.19 | 0.15 | 8.81 | 7.36 | 0.04 | 1.81 |

SE: standard errors